Supporting Information (SI):

Similarities and differences between tannin- and resorcinol-based carbon aerogels: nitrogen-doping, electrical conductivity, and performance in a Zn-based electrochemical cell

Jessica Kröner1, Daniela Söllinger2, Ann-Kathrin Koopmann2, Christoph Thurner3, Simon Penner3, Michael S. Elsaesser2, and Marina Schwan1*

1	Institute for Frontier Materials on Earth and in Space, German Aerospace Center, 51147 Cologne, Germany

2	Chemistry and Physics of Materials, University of Salzburg, 5020 Salzburg, Austria

3	Institute of Physical Chemistry, University of Innsbruck, Innsbruck, Austria

*	Corresponding author: Marina.Schwan@dlr.de

Figure S1: TEM images of RF-CA, RF-CAa, TF-CA and TF-CAa. The figure shows that RF-based carbon aerogels have much smaller particles than TF-based carbon aerogels. Furthermore, activation leads to a denser structure.

| a) | b) |
| --- | --- |
| c) | d) |
| e) | f) |
| g) | h) |

Figure S2: a) RF-CA, b) RF-CAa, c) RF-CAa,NH3, d) RF-CAa,M, e) TF-CA, f) TF-CAa, g) TF-CAa,NH3 and h) TF-CAa,M cumulatively fitted by deconvolution into the bands D*, D, D**, G and D’ in accordance to Kaniyoor and Ramaprabhu [45]

Table S3: Elemental ratios of the samples obtained from XPS

| Sample | C [at.-%] | N [at.-%] | O [at.-%] |
| --- | --- | --- | --- |
| RF-CAa | 98 | 0 | 2 |
| RF-CAa,NH3 | 96 | 2 | 2 |
| RF-CAa,M | 94 | 5 | 1 |
| TF-CAa | 97 | 0 | 3 |
| TF-CAa, NH3 | 96 | 2 | 2 |
| TF-CAa,M | 94 | 4 | 2 |

Table S4: Energy densities of RF-CAa, RF-CAa,M, RF-CAa,NH3, TF-CAa, TF-CAa,M and

TF-CAa,NH3 calculated by the integration of the potential versus capacity curve after the initial cycle at 0.0 to 1.9 V vs. Zn/Zn2+ at a current density of 500 mA‧g-1.

| Sample | Energy density [Wh‧kg-1] |
| --- | --- |
| RF-CAa | 72.239 |
| RF-CAa,M | 48.704 |
| RF-CAa,NH3 | 48.343 |
| TF-CAa | 45.511 |
| TF-CAa,M | 42.254 |
| TF-CAa,NH3 | 44.699 |

Figure S5: GCD curves of RF- and TF-based carbon aerogels vs. Zn/Zn2+ in the potential range 0.0-1.9 V measured at a) 0.5 A·g-1, b) 1 A·g-1, c) 2 A·g-1, d) 5 A·g-1 and 10 A·g-1

Figure S6: The figure shows the galvanostatic discharge of RF-CAa and the area which was used for the calculation of the energy density as an example.

Figure S7: Ragone plot of RF- and TF-based carbon aerogels vs. Zn/Zn2+ in the potential range 0.0-1.9 V measured at 0.5, 1, 2, 5 and 10 A·g-1.