Exploring the Role of Rare Earth Elements Doped TiO₂ Based Photoanodes on the Performance of Dye-Sensitized Solar Cells

Berrak CALISKAN1*, Enes SAYAN1, Erdal IGMAN2

1 Atatürk University, Faculty of Engineering, Department of Chemical Engineering, (esayan@atauni.edu.tr), 25240, Erzurum, TURKEY

2 Bayburt University, Department of Material Science and Nanotechnology Engineering, (eigman@bayburt.edu.tr), 69100, Bayburt, TURKEY

* Corresponding author:

Dr. Berrak CALISKAN

Atatürk University, Faculty of Engineering,

Department of Chemical Engineering,

25240, Erzurum, TURKEY

e-mail: berrak.c@atauni.edu.tr

Supplementary Information

Figure S3: SEM images of pure and TiO2 working electrodes doped with different percentages (%0,5, %1,0 and %1,5) of REEs (Ho+3, La+3, Er+3, Yb+2) and the weight percentages and atomic weight percentages of the elements proven by EDS.

Figure S3 continued

Figure S3 continued

Figure S4: SEM image of the GO-PVP structure applied to the FTO base material with the ‘Doctor Blade’ technique.

Figure S5: SEM image of the rGO-PVP structure applied to the FTO base material with the ‘Doctor Blade’ technique.

Figure S6: Weight percentages and atomic weight percentages of elements proven by EDS of GO-PVP and rGO-PVP photocathode electrodes.

Figure S15: Raman spectra of GO-PVP and rGO-PVP CE used in DSSCs

Figure S16: XRD patterns of TiO2 and (0.5%, 1.0% and 1.5% M Ho+3) doped TiO2 films synthesized by the Sol-Gel method.

Figure S17: XRD patterns of TiO2 and TiO2 films (0.5%, 1.0% and 1.5% M Er+3) doped synthesized by the Sol-Gel method.

Figure S18: XRD patterns of TiO2 and 1.0 M La+3 doped TiO2 films synthesized by the Sol-Gel method.

Figure S19: XRD patterns of TiO2 and 1.0 M Yb+2 doped TiO2 films synthesized by the Sol-Gel method.

Figure S20: XRD patterns of FTO, GO-PVP/FTO and rGO-PVP/FTO films

Table S2: Determination of β, 2θ and Crystal Size Values ​​of Photo-Anode Electrodes

| Photo-anode electrodes | Β (Half Height Width (FWHM) (radians) | 2θ (Derece) | Crystal size (D) (nm) |
| --- | --- | --- | --- |
| TiO2 | 0.55 | 25.10 | 16.59 |
| %0,5 M Ho TiO2 | 0.58 | 25.04 | 15.57 |
| %1,0 M Ho TiO2 | 0.61 | 25.04 | 14.87 |
| %1,5 M Ho TiO2 | 0.67 | 25.05 | 13.62 |
| %1,0 M La TiO2 | 0.6 | 25.03 | 15.10 |
| %0,5 M Er TiO2 | 0.58 | 25.04 | 15.52 |
| %1,0 M Er TiO2 | 0.60 | 25.04 | 14.71 |
| %1,5 M Er TiO2 | 0.62 | 25.04 | 14.69 |
| %1,0 M Yb TiO2 | 0.6 | 25.06 | 15.14 |

Figure S26: Absorption (a) and optical band gap (b) graph of pure TiO2 photoanode film synthesized by sol-gel method.

Figure S27: Absorption (a) and optical band gap (b) graph of TiO2 photoanode film doped with (0.5%, 1.0% and 1.5% M Ho+3) synthesized by sol-gel method.

Figure S28: Absorption (a) and optical band gap (b) graph of TiO2 photoanode film doped with (0.5%, 1.0% and 1.5% M Er+3) synthesized by sol-gel method.

Figure S29: Absorption (a) and optical band gap (b) graph of 1.0 M La+3 doped TiO2 photoanode film synthesized by sol-gel method.

Figure S30: Absorption (a) and optical band gap (b) graph of 1.0% M Yb+2 doped TiO2 photoanode film synthesized by sol-gel method.

Table S4: Determination of Band Gap Values ​​of WEs

| Working Electrodes | Band Gap (eV) |
| --- | --- |
| TiO2 | 3.03 |
| %0,5 M Ho+3 TiO2 | 2.24 |
| %1,0 M Ho+3 TiO2 | 2.22 |
| %1,5 M Ho+3 TiO2 | 2.16 |
| %0,5 M Er+3 TiO2 | 2.55 |
| %1,0 M Er+3 TiO2 | 2.25 |
| %1,5 M Er+3 TiO2 | 2.18 |
| %1,0 M La+3 TiO2 | 2.29 |
| %1,0 M Yb+2 TiO2 | 2.45 |

Figure S31: Absorbance spectrum of dyes obtained from (a) N-719 and (b) hibiscus plant.

Figure S32: FTIR spectrum of dyes obtained from (a) N-719 (b) hibiscus plant