Controlling Grain Growth in Electrospun ZrO2 Nanofibers: The Role of Biphasic Precursor Systems

Jingyu Li 1, Danchi Zhou 1, Panpan Tian 2, Cewen He 1, Nana Xu 1*, Yuanbing Li 3

1 School of Materials Science and Engineering, Hunan University of Science and Technology, Xiangtan 411201, China

2 Beijing Advanced Innovation Center for Materials Genome Engineering, School of Advanced Materials Innovation, University of Science and Technology Beijing, Beijing 100083, China

3 State Key Laboratory of Advanced Refractories, Wuhan University of Science and Technology, Wuhan 430081, China

* Correspondence: nana616849790@163.com

Table S1 Regulation of spinning parameters

| Voltage (kV) | Distance (cm) | Flow rate (mL/h) | Phenomenon |
| --- | --- | --- | --- |
| 28.0 | 20 | 0.75 | solution pooling |
| 27.0 | 16 | 0.75 | jet breakdown |
| 26.0 | 14 | 0.75 | jet breakdown |
| 27.5 | 18 | 0.75 | continuous jetting |
| 27.5 | 18 | 0.8 | solution pooling |
| 27.5 | 18 | 0.7 | jet breakdown |
| 27.5 | 18 | 0.6 | jet breakdown |