










[bookmark: OLE_LINK27][bookmark: OLE_LINK4]Controlling Grain Growth in Electrospun ZrO2 Nanofibers: The Role of Biphasic Precursor Systems
[bookmark: OLE_LINK7]Jingyu Li 1, Danchi Zhou 1, Panpan Tian 2, Cewen He 1, Nana Xu 1*, Yuanbing Li 3
1 School of Materials Science and Engineering, Hunan University of Science and Technology, Xiangtan 411201, China
2 Beijing Advanced Innovation Center for Materials Genome Engineering, School of Advanced Materials Innovation, University of Science and Technology Beijing, Beijing 100083, China
3 State Key Laboratory of Advanced Refractories, Wuhan University of Science and Technology, Wuhan 430081, China
* Correspondence: nana616849790@163.com


Table S1 Regulation of spinning parameters
	Voltage (kV)
	Distance (cm)
	Flow rate (mL/h)
	Phenomenon

	[bookmark: _Hlk206693116]28.0
	20
	0.75
	[bookmark: OLE_LINK60]solution pooling

	27.0
	16
	0.75
	[bookmark: OLE_LINK62]jet breakdown

	26.0
	14
	0.75
	jet breakdown

	27.5
	18
	0.75
	continuous jetting

	[bookmark: OLE_LINK61]27.5
	18
	0.8
	solution pooling

	27.5
	18
	0.7
	jet breakdown

	27.5
	18
	0.6
	jet breakdown
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