Hydrothermal preparation and characterization of Cd-doped ZnS photocatalyst for efficient dye wastewater degradation

Chengrui Xiong a, Tao Xiong a, Yi Zhou b, Qi Feng b,c,∗, Chenglun Liu a,∗, Longjun Xu b,∗

a College of Chemistry and Chemical Engineering, Chongqing University, Chongqing, 400044, PR China

b State Key Laboratory of Coal Mine Disaster Dynamics and Control, Chongqing University, Chongqing, 400044, PR China

c Department of Civil and Environmental Engineering, University of Alberta, Edmonton, AB T6G 1H9, Canada

∗Corresponding author. qifeng868@cqu.edu.cn (Q. Feng); xlclj@cqu.edu.cn (C. Liu), xulj@cqu.edu.cn (L. Xu).

Fig. S1. Time-dependent dark adsorption behavior of (a) MB, (b) RhB, and (c) MG over Cd-doped ZnS before visible-light irradiation

Fig. S2. Cycling photocatalytic degradation performance of 7.5-CZS toward (a) MB and (b) MG over four consecutive runs.

Table S1. Surface elemental composition of 7.5-CZS obtained from XPS survey analysis.

| Element | Atomic % |
| --- | --- |
| Zn | 13.56 |
| Cd | 1.61 |
| S | 18.73 |
| C | 43.57 |
| O | 5.49 |