Hydrothermal preparation and characterization of Cd-doped ZnS photocatalyst for efficient dye wastewater degradation
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Fig. S1. Time-dependent dark adsorption behavior of (a) MB, (b) RhB, and (c) MG over Cd-doped ZnS before visible-light irradiation
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Fig. S2. Cycling photocatalytic degradation performance of 7.5-CZS toward (a) MB and (b) MG over four consecutive runs.


Table S1. Surface elemental composition of 7.5-CZS obtained from XPS survey analysis.
	Element 
	Atomic %

	Zn
	13.56

	Cd
	1.61

	S
	18.73

	C
	43.57

	O
	5.49
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