INFLUENCE OF STABILIZERS AND NITROGEN CONTENT ON THE THERMAL PROPERTIES OF NITROCELLULOSE GRANULES

Katarzyna Cieślak1, Katarzyna Gańczyk-Specjalska2,, Katarzyna Drożdżewska-Szymańska3, Michał Uszyński1

1 Warsaw University of Technology, Faculty of Chemistry, Division of High Energetic Materials, Noakowskiego 3, 00-664 Warsaw, Poland

2 Lukasiewicz Research Network – Institute of Industrial Organic Chemistry, Department of High Energetic Materials, Annopol 6, 03-236 Warsaw, Poland

3 Lukasiewicz Research Network – Institute of Industrial Organic Chemistry, Chemical Safety and Static Electricity Department, Annopol 6, 03-236 Warsaw, Poland

Supplementary Materials

Fig. S1 The dependences of cumulative heat on time with linear relations for granules containing triphenylamine and nitrocellulose with different nitrogen content

Fig. S2 The dependences of cumulative heat on time with linear relations for granules containing centralite I and nitrocellulose with different nitrogen content

Table S1 Apparent activation energy (aEa) and logarithm of pre-exponential factor (logA) for different conversion degree for G(TPA)3 decomposition reaction determined with DSC and TGA methods

| Conversion degree | aEa/kJ mol-1 | log(A/s-1) | aEa/kJ mol-1 | log(A/s-1) |
| --- | --- | --- | --- | --- |
|  | DSC method |  | TGA method |  |
| 0.05 | 188.52 ± 4.02 | 18.1 | 158.62 ± 13.68 | 14.8 |
| 0.10 | 172.47 ± 2.92 | 16.4 | 186.31 ± 6.03 | 18.1 |
| 0.15 | 169.03 ± 2.84 | 16.1 | 185.32 ± 4.18 | 18.0 |
| 0.20 | 170.21 ± 3.23 | 16.2 | 188.40 ± 3.25 | 18.4 |
| 0.25 | 173.64 ± 4.02 | 16.7 | 193.15 ± 2.84 | 18.9 |
| 0.30 | 177.65 ± 4.99 | 17.2 | 200.85 ± 4.13 | 19.8 |
| 0.35 | 181.61 ± 5.83 | 17.6 | 206.33 ± 4.88 | 20.5 |
| 0.40 | 185.30 ± 6.52 | 18.1 | 212.56 ± 5.65 | 21.2 |
| 0.45 | 188.70 ± 7.08 | 18.5 | 217.73 ± 6.36 | 21.8 |
| 0.50 | 191.87 ± 7.54 | 18.9 | 222.46 ± 6.87 | 22.3 |
| 0.55 | 194.95 ± 7.92 | 19.2 | 226.90 ± 7.15 | 22.8 |
| 0.60 | 198.12 ± 8.20 | 19.6 | 232.38 ± 7.53 | 23.4 |
| 0.65 | 201.46 ± 8.46 | 20.0 | 239.31 ± 8.01 | 24.2 |
| 0.70 | 205.30 ± 8.73 | 20.4 | 249.44 ± 8.51 | 25.2 |
| 0.75 | 210.02 ± 9.08 | 20.9 | 267.21 ± 9.78 | 27.1 |
| 0.80 | 216.36 ± 9.64 | 21.6 | 296.29 ± 13.85 | 30.2 |
| 0.85 | 225.19 ± 10.61 | 22.5 | 332.49 ± 22.29 | 33.9 |
| 0.90 | 234.48 ± 12.33 | 23.5 | 374.69 ± 37.97 | 38.0 |
| 0.95 | 231.58 ± 14.40 | 23.0 | 504.94 ± 104.85 | 50.6 |

Table S2 Apparent activation energy (aEa) and logarithm of pre-exponential factor (logA) for different conversion degree for G(TPA)2 decomposition reaction determined with DSC and TGA methods

| Conversion degree | aEa/kJ mol-1 | log(A/s-1) | aEa/kJ mol-1 | log(A/s-1) |
| --- | --- | --- | --- | --- |
|  | DSC method |  | TGA method |  |
| 0.05 | 180.79 ± 5.93 | 17.1 | 159.20 ± 5.76 | 14.8 |
| 0.10 | 173.56 ± 3.03 | 16.5 | 190.35 ± 2.75 | 18.5 |
| 0.15 | 170.90 ± 2.02 | 16.2 | 192.34 ± 2.39 | 18.7 |
| 0.20 | 170.82 ± 1.50 | 16.3 | 197.62 ± 2.60 | 19.4 |
| 0.25 | 171.77 ± 1.35 | 16.4 | 203.23 ± 3.20 | 20.0 |
| 0.30 | 173.19 ± 1.41 | 16.6 | 211.45 ± 3.32 | 21.0 |
| 0.35 | 175.04 ± 1.60 | 16.8 | 217.87 ± 3.42 | 21.7 |
| 0.40 | 177.48 ± 1.76 | 17.1 | 224.85 ± 3.97 | 22.5 |
| 0.45 | 180.39 ± 1.90 | 17.5 | 232.00 ± 4.37 | 23.4 |
| 0.50 | 183.94 ± 1.89 | 17.9 | 238.08 ± 5.06 | 24.0 |
| 0.55 | 188.15 ± 1.85 | 18.4 | 244.23 ± 5.46 | 24.7 |
| 0.60 | 192.99 ± 1.83 | 19.0 | 251.54 ± 6.45 | 25.5 |
| 0.65 | 198.65 ± 1.90 | 19.6 | 260.41 ± 7.49 | 26.5 |
| 0.70 | 205.32 ± 2.20 | 20.4 | 275.34 ± 8.73 | 28.0 |
| 0.75 | 213.33 ± 2.89 | 21.2 | 292.81 ± 10.95 | 29.9 |
| 0.80 | 222.77 ± 4.02 | 22.2 | 311.48 ± 13.71 | 31.7 |
| 0.85 | 231.97 ± 5.62 | 23.2 | 333.33 ± 16.65 | 33.9 |
| 0.90 | 235.19 ± 7.65 | 23.4 | 354.74 ± 19.99 | 35.7 |
| 0.95 | 222.59 ± 8.63 | 21.9 | 449.19 ± 83.00 | 44.6 |

Table S3 Apparent activation energy (aEa) and logarithm of pre-exponential factor (logA) for different conversion degree for G(TPA)1 decomposition reaction determined with DSC and TGA methods

| Conversion degree | aEa/kJ mol-1 | log(A/s-1) | aEa/kJ mol-1 | log(A/s-1) |
| --- | --- | --- | --- | --- |
|  | DSC method |  | TGA method |  |
| 0.05 | 171.42 ± 3.60 | 16.0 | 119.20 ± 25.65 | 10.2 |
| 0.10 | 161.90 ± 2.23 | 15.1 | 177.09 ± 6.55 | 17.0 |
| 0.15 | 161.64 ± 1.74 | 15.2 | 179.91 ± 4.09 | 17.3 |
| 0.20 | 163.30 ± 1.46 | 15.4 | 185.12 ± 3.14 | 17.9 |
| 0.25 | 165.62 ± 1.25 | 15.7 | 190.04 ± 2.27 | 18.5 |
| 0.30 | 168.05 ± 1.21 | 16.0 | 193.97 ± 1.74 | 19.0 |
| 0.35 | 170.81 ± 1.11 | 16.3 | 199.63 ± 2.07 | 19.6 |
| 0.40 | 173.75 ± 1.04 | 16.7 | 206.05 ± 2.71 | 20.4 |
| 0.45 | 176.86 ± 0.96 | 17.1 | 210.07 ± 2.82 | 20.8 |
| 0.50 | 180.13 ± 0.95 | 17.5 | 213.90 ± 2.75 | 21.2 |
| 0.55 | 183.52 ± 0.93 | 17.8 | 217.82 ± 2.56 | 21.7 |
| 0.60 | 187.13 ± 0.96 | 18.3 | 223.61 ± 2.78 | 22.3 |
| 0.65 | 191.11 ± 1.07 | 18.7 | 232.64 ± 3.18 | 23.3 |
| 0.70 | 195.66 ± 1.24 | 19.2 | 242.11 ± 2.62 | 24.2 |
| 0.75 | 201.01 ± 1.46 | 19.8 | 254.63 ± 3.00 | 25.5 |
| 0.80 | 207.03 ± 1.71 | 20.4 | 266.73 ± 4.15 | 26.7 |
| 0.85 | 212.36 ± 2.23 | 20.9 | 276.89 ± 6.05 | 27.5 |
| 0.90 | 212.76 ± 3.67 | 20.9 | 301.91 ± 8.94 | 29.8 |
| 0.95 | 202.18 ± 5.09 | 19.6 | 435.75 ± 25.96 | 42.8 |

Table S4 Apparent activation energy (aEa) and logarithm of pre-exponential factor (logA) for different conversion degree for G(CI)1 decomposition reaction determined with DSC and TGA methods

| Conversion degree | aEa/kJ mol-1 | log(A/s-1) | aEa/kJ mol-1 | log(A/s-1) |
| --- | --- | --- | --- | --- |
|  | DSC method |  | TGA method |  |
| 0.05 | 176.68 ± 12.76 | 16.7 | 151.15 ± 6.19 | 13.9 |
| 0.10 | 168.64 ± 6.95 | 15.9 | 183.40 ± 3.58 | 17.7 |
| 0.15 | 167.23 ± 4.94 | 15.8 | 184.46 ± 2.61 | 17.8 |
| 0.20 | 168.32 ± 3.89 | 16.0 | 189.51 ± 2.70 | 18.4 |
| 0.25 | 170.37 ± 3.24 | 16.2 | 194.74 ± 2.83 | 19.0 |
| 0.30 | 172.68 ± 2.93 | 16.5 | 201.67 ± 3.39 | 19.8 |
| 0.35 | 175.27 ± 2.81 | 16.8 | 208.44 ± 4.32 | 20.6 |
| 0.40 | 178.16 ± 2.78 | 17.2 | 213.89 ± 4.70 | 21.2 |
| 0.45 | 181.30 ± 2.76 | 17.6 | 218.80 ± 5.22 | 21.8 |
| 0.50 | 184.67 ± 2.76 | 18.0 | 223.93 ± 5.42 | 22.4 |
| 0.55 | 188.33 ± 2.76 | 18.4 | 229.96 ± 6.49 | 23.0 |
| 0.60 | 192.37 ± 2.77 | 18.8 | 235.94 ± 6.43 | 23.6 |
| 0.65 | 196.93 ± 2.82 | 19.3 | 244.32 ± 8.04 | 24.5 |
| 0.70 | 202.11 ± 2.97 | 19.9 | 255.56 ± 7.70 | 25.7 |
| 0.75 | 208.08 ± 3.30 | 20.6 | 270.62 ± 8.85 | 27.2 |
| 0.80 | 214.86 ± 3.84 | 21.3 | 289.74 ± 11.71 | 29.1 |
| 0.85 | 221.13 ± 4.63 | 21.9 | 301.11 ± 15.83 | 30.1 |
| 0.90 | 221.84 ± 5.77 | 21.9 | 317.45 ± 25.45 | 31.4 |
| 0.95 | 208.12 ± 6.51 | 20.2 | 384.43 ± 71.73 | 37.4 |

Author for correspondence: specjalska@ipo.waw.pl