Physicochemical properties and thermal behavior of nitrocellulose granules with eutectic mixtures of stabilizers

Katarzyna Cieślak1, Katarzyna Gańczyk-Specjalska2,, Katarzyna Drożdżewska-Szymańska3, Marta Królikowska4, Marcin Jakubczak1

1 Warsaw University of Technology, Faculty of Chemistry, Division of High Energetic Materials, Noakowskiego 3, 00-664 Warsaw, Poland

2 Lukasiewicz Research Network – Institute of Industrial Organic Chemistry, Department of High Energetic Materials, Annopol 6, 03-236 Warsaw, Poland

3 Lukasiewicz Research Network – Institute of Industrial Organic Chemistry, Chemical Safety and Static Electricity Department, Annopol 6, 03-236 Warsaw, Poland

4 Warsaw University of Technology, Faculty of Chemistry, Department of Physical Chemistry, Noakowskiego 3, 00-664 Warsaw, Poland

Supplementary Materials

Fig. S1 DSC curves for binary system TPA+CI

Fig. S2 DSC curves for binary system TPA+AkaII

Table S1 Apparent activation energy (aEa) and logarithm of pre-exponential factor (logA) for different conversion degree for G(TPA+AkaII)1 decomposition reaction

| Conversion degree | aEa/kJ mol-1 | log(A/s-1) |
| --- | --- | --- |
| 0.05 | 162.70 ± 8.53 | 15.0 |
| 0.10 | 161.17 ± 4.56 | 15.0 |
| 0.15 | 163.57 ± 3.38 | 15.3 |
| 0.20 | 166.46 ± 2.86 | 15.7 |
| 0.25 | 169.44 ± 2.71 | 16.1 |
| 0.30 | 172.53 ± 2.82 | 16.5 |
| 0.35 | 175.74 ± 2.99 | 16.9 |
| 0.40 | 179.15 ± 3.19 | 17.3 |
| 0.45 | 182.57 ± 3.50 | 17.7 |
| 0.50 | 185.83 ± 4.03 | 18.1 |
| 0.55 | 188.79 ± 4.79 | 18.4 |
| 0.60 | 191.29 ± 5.91 | 18.7 |
| 0.65 | 193.19 ± 7.50 | 18.9 |
| 0.70 | 194.26 ± 9.66 | 19.0 |
| 0.75 | 194.20 ± 12.51 | 19.0 |
| 0.80 | 192.19 ± 15.99 | 18.7 |
| 0.85 | 187.05 ± 19.42 | 18.1 |
| 0.90 | 178.48 ± 21.19 | 17.1 |
| 0.95 | 167.57 ± 19.59 | 15.8 |

Table S2 Apparent activation energy (aEa) and logarithm of pre-exponential factor (logA) for different conversion degree for G(TPA+CI)1 decomposition reaction

| Conversion degree | aEa/kJ mol-1 | log(A/s-1) |
| --- | --- | --- |
| 0.05 | 159.82 ± 5.53 | 14.7 |
| 0.10 | 157.48 ± 2.59 | 14.6 |
| 0.15 | 160.67 ± 1.81 | 15.0 |
| 0.20 | 163.87 ± 1.47 | 15.4 |
| 0.25 | 167.04 ± 1.25 | 15.8 |
| 0.30 | 170.26 ± 1.16 | 16.2 |
| 0.35 | 173.73 ± 1.09 | 16.7 |
| 0.40 | 177.20 ± 1.11 | 17.1 |
| 0.45 | 180.64 ± 1.23 | 17.5 |
| 0.50 | 184.11 ± 1.42 | 17.9 |
| 0.55 | 187.57 ± 1.67 | 18.3 |
| 0.60 | 191.11 ± 1.93 | 18.7 |
| 0.65 | 194.76 ± 2.27 | 19.1 |
| 0.70 | 198.69 ± 2.67 | 19.5 |
| 0.75 | 203.11 ± 3.19 | 20.0 |
| 0.80 | 207.89 ± 3.87 | 20.5 |
| 0.85 | 211.19 ± 4.89 | 20.8 |
| 0.90 | 208.22 ± 6.25 | 20.4 |
| 0.95 | 193.56 ± 6.95 | 18.6 |

Corresponding author: katarzyna.ganczyk-specjalska@ipo.lukasiewicz.gov.pl

ORCID	Katarzyna Cieślak 			0000-0002-5418-5763

Katarzyna Gańczyk-Specjalska		0000-0002-8394-1513

Katarzyna Drożdżewska-Szymańska	0000-0002-1397-4635

Marta Królikowska			0000-0001-6534-4427