The Influence of Phosphorus- and Nitrogen- Containing Groups on the Thermal Stability and Combustion Characteristics of Styrenic Polymers

Aloshy Babya, Svetlana Tretsiakova-McNallya, *, Paul Josephb, Malavika Arunb, Jianping Zhanga, Doris Pospiechc

a Belfast School of Architecture and the Built Environment, Ulster University, Newtownabbey BT37 0QB, UK,  b Institute for Sustainable Industries and Liveable Cities, Victoria University, PO Box 14428, Melbourne 8001, Victoria, Australia, c Leibniz-Institute of Polymer Research Dresden, Hohe Straβe 6, 01069 Dresden, Germany

* Correspondence: baby-a1@ulster.ac.uk; Tel.: +44 7568669161

Supplementary Information

SI. 1 1H NMR spectra of PS and styrenic co-polymer, poly(S-co-DEAMP), poly(S-co-DEpVBP) and poly(S-co-ADEPMAE)

SI. 2 FT-IR (ATR) spectra of PS and styrene-based co- and ter-polymers

SI. 3 DSC curves obtained at 10℃ min-1 for PS, styrenic co- (a) and ter- (b) polymers under nitrogen atmosphere

SI. 4 Heat of Pyrolysis (∆Hpyro) of PS and modified styrenic polymers obtained at 10 ℃ min-1 under nitrogen atmosphere

| Sample | ∆Hpyro (J/g) |
| --- | --- |
| PS | 717 |
| Poly(S-co-DEAMP) | 393 |
| Poly(S-co-DEpVBP) | 674 |
| Poly(S-co-ADEPMAE) | 701 |
| Poly(S-co-MI) | 660 |
| Poly(S-ter-DEAMP-ter-MI) | 191 |
| Poly(S-ter-DEpVBP-ter-MI) | 217 |

SI. 5 TGA obtained at 60℃ min-1 for PS, styrenic co- polymer, poly(S-co-ADEPMAE) and ter-polymers poly(S-ter-DEAMP-ter-MI) and poly(S-ter-DEpVBP-ter-MI) under nitrogen atmosphere