Supplementary File

Table S1

Structural parameters of Na2MnF5(s) obtained by Rietveld refinement

| Atoms | Sites | x* | y* | z* | Uiso (Å)2# | occ@ |
| --- | --- | --- | --- | --- | --- | --- |
| Mn1 Mn2 | 2a 2b | 0.0000 0.5000 | 0.0000 0.0000 | 0.0000 0.0000 | 0.016(1) 0.022(1) | 1 1 |
| Na1 | 4e | 0.1527(5) | -0.0064(1) | 0.3659(4) | 0.017(1) | 1 |
| Na2 | 4e | 0.3446(2) | 0.4521(11) | 0.1825(4) | 0.022(2) | 1 |
| F1 | 4e | 0.0470(10) | 0.1436(12) | 0.1651(6) | 0.021(2) | 1 |
| F2 | 4e | 0.8806(9) | 0.2889(12) | -0.0831(6) | 0.026(2) | 1 |
| F3 | 4e | 0.2497(13) | 0.1470(9) | 0.0022(8) | 0.005(1) | 1 |
| F4 | 4e | 0.6201(8) | 0.2150(12) | 0.1414(5) | 0.016(2) | 1 |
| F5 | 4e | 0.4919(9) | 0.2378(12) | 0.8735(5) | 0.019(2) | 1 |

*x,y and z are fractional atomic coordinates along three crystallographic axes.

# Uiso is isotropic atomic displacement parameter.

@occ is site occupancy factor.

Table S2

The observed inter-atomic distances around various cations of Na2MnF5(s)

| Bond | d(Å) | Bond | d(Å) | Bond | d(Å) | Bond | d(Å) |
| --- | --- | --- | --- | --- | --- | --- | --- |
| Mn1-F2 | 1.848(7) | Mn2-F5 | 1.842(7) | Na1-F1 | 2.211(8) | Na2-F2 | 2.193(8) |
| Mn1-F2 | 1.848(7) | Mn2-F5 | 1.842(7) | Na1-F4 | 2.303(9) | Na2-F5 | 2.249(8) |
| Mn1-F1 | 1.869(7) | Mn2-F4 | 1.888(6) | Na1-F1 | 2.348(10) | Na2-F5 | 2.259(10) |
| Mn1-F1 | 1.869(7) | Mn2-F4 | 1.888(6) | Na1-F3 | 2.362(9) | Na2-F4 | 2.301(9) |
| Mn1-F3 | 2.068(10) | Mn2-F3 | 2.087(10) | Na1-F2 | 2.603(10) | Na2-F3 | 2.449(9) |
| Mn1-F3 | 2.068(10) | Mn2-F3 | 2.087(10) | Na1-F2 | 2.681(9) | Na2-F4 | 2.623(9) |
|  |  |  |  |  |  | Na2-F1 | 2.764(10) |
| Average | 1.929(8) | Average | 1.939(8) | Average | 2.418(9) | Average | 2.406(9) |

Table S3

Experimental values of the molar heat capacity at constant pressure* for Na2MnF5(s) from 2 to 300 K

| @T/K | # Cp / J K-1 mol-1 |  | @T/K | # Cp / J K-1 mol-1 |  | @T/K | # Cp / J K-1 mol-1 |
| --- | --- | --- | --- | --- | --- | --- | --- |
| 2.02 | 0.044 | 40.205 |  | 30.38 | 161.023 |  | 139.90 |
| 2.57 | 0.096 | 42.726 |  | 33.17 | 165.044 |  | 141.81 |
| 3.12 | 0.19 | 45.243 |  | 36.02 | 169.038 |  | 144.30 |
| 3.69 | 0.32 | 47.759 |  | 38.91 | 173.059 |  | 146.29 |
| 4.25 | 0.45 | 50.220 |  | 41.84 | 177.096 |  | 148.56 |
| 4.81 | 0.59 | 53.818 |  | 46.01 | 181.127 |  | 150.61 |
| 5.37 | 0.73 | 57.340 |  | 50.24 | 185.149 |  | 152.92 |
| 5.93 | 0.88 | 60.864 |  | 54.38 | 189.173 |  | 154.57 |
| 6.49 | 1.02 | 64.375 |  | 58.46 | 193.193 |  | 156.40 |
| 7.06 | 1.18 | 67.914 |  | 61.94 | 197.215 |  | 158.82 |
| 7.62 | 1.36 | 71.442 |  | 65.72 | 201.279 |  | 162.02 |
| 8.19 | 1.56 | 74.963 |  | 69.53 | 205.302 |  | 163.95 |
| 8.75 | 1.81 | 78.487 |  | 73.16 | 209.303 |  | 165.40 |
| 9.32 | 2.10 | 82.001 |  | 76.90 | 213.339 |  | 167.47 |
| 9.88 | 2.46 | 85.521 |  | 80.56 | 217.339 |  | 168.99 |
| 10.46 | 2.90 | 89.053 |  | 83.73 | 221.363 |  | 170.79 |
| 11.02 | 3.33 | 92.580 |  | 87.30 | 225.344 |  | 171.94 |
| 11.02 | 3.32 | 96.119 |  | 90.74 | 227.656 |  | 172.51 |
| 12.03 | 4.00 | 99.636 |  | 94.09 | 231.405 |  | 173.99 |
| 13.03 | 4.75 | 103.167 |  | 97.40 | 236.416 |  | 176.06 |
| 14.04 | 5.56 | 106.683 |  | 100.56 | 241.439 |  | 177.27 |
| 15.04 | 6.39 | 110.206 |  | 103.53 | 246.449 |  | 178.98 |
| 16.04 | 7.24 | 113.719 |  | 106.65 | 251.452 |  | 180.46 |
| 17.04 | 8.06 | 117.248 |  | 109.16 | 256.460 |  | 182.20 |
| 18.04 | 8.88 | 120.746 |  | 112.37 | 261.486 |  | 183.02 |
| 19.05 | 9.74 | 124.786 |  | 115.56 | 266.499 |  | 184.74 |
| 20.037 | 10.59 | 128.812 |  | 118.63 | 271.499 |  | 186.33 |
| 22.569 | 12.75 | 132.836 |  | 121.34 | 276.493 |  | 188.08 |
| 25.089 | 14.97 | 136.854 |  | 124.61 | 281.516 |  | 189.60 |
| 27.611 | 17.30 | 140.891 |  | 126.91 | 286.516 |  | 190.79 |
| 30.131 | 19.77 | 144.917 |  | 129.55 | 291.523 |  | 191.63 |
| 32.649 | 22.28 | 148.960 |  | 132.16 | 296.548 |  | 190.11 |
| 35.167 | 24.92 | 152.964 |  | 134.58 | 301.497 |  | 191.70 |
| 37.684 | 27.60 | 157.006 |  | 136.98 |  |  |  |

*The standard uncertainty in pressure is 0.6 kPa with 0.68 level of confidence.

# The standard uncertainty in Cp is within ± 1.5% and ± 4.5% of the measured Cp value of Na2MnF5(s) at temperatures between 100-300 K and 2-100 K, respectively with 0.68 level of confidence.

@The standard uncertainty in temperature is ± 0.1% for T<20 K and ± 0.02% for T>20 K with 0.68 level of confidence.

Table S4

Parameters for low temperature (2-6.5 K), mid temperature (7-68 K), and high temperature (T > 40 K) fits of heat capacity data (in J K−1 mol−1) of Na2MnF5(s)

|  | Parameter | Na2MnF5(s) |
| --- | --- | --- |
| Low temperature fits | Temperature range / K B3 / JK-4mol-1 B5 / JK-6mol-1 B7 / JK-8mol-1 B9 / JK-10mol-1 | 2-6.5 K 5.730 × 10-3 1.224 × 10-4 -8.353 × 10-6 1.026 × 10-7 |
| Mid temperature fits | Temperature range / K | 7-68 K |
|  | A0 / JK-1mol-1 | 9.653 |
|  | A1 / JK-2mol-1 | -3.809 |
|  | A2 / JK-3mol-1 | 0.5880 |
|  | A3 / JK-4mol-1 | -4.186 × 10-2 |
|  | A4 / JK-5mol-1 | 1.830 × 10-3 |
|  | A5 / JK-6mol-1 | -5.094 × 10-5 |
|  | A6 / JK-7mol-1 | 9.151 × 10-7 |
|  | A7 / JK-8mol-1 | -1.031 × 10-8 |
|  | A8 / JK-9mol-1 | 6.656 × 10-11 |
|  | A9 / JK-10mol-1 | -1.881 × 10-13 |
| High temperature fits | Temperature range / K | 40-302 K |
|  | m / mol | 5.868 |
|  | ΘD / K | 718.7 |
|  | n / mol | 3.311 |
|  | ΘE / K | 157.9 |

Table S5

Experimental data on the molar heat capacity at constant pressure* for Na2MnF5(s) from 307 K to 573 K.

| T / K | Molar heat capacity of Na2MnF5(s) / J K-1 mol-1 |  | Percentage deviation |
| --- | --- | --- | --- |
|  | Experimental data | Fitted data |  |
| 307.9 | 188.5 | 189.4 | -0.5 |
| 317.9 | 190.5 | 190.2 | 0.1 |
| 327.0 | 191.4 | 191.0 | 0.2 |
| 337.9 | 192.5 | 192.0 | 0.3 |
| 347.9 | 193.3 | 193.0 | 0.2 |
| 357.9 | 194.3 | 194.0 | 0.2 |
| 367.9 | 195.1 | 195.0 | 0.1 |
| 378.2 | 196.0 | 196.1 | -0.1 |
| 387.9 | 196.9 | 197.1 | -0.1 |
| 397.9 | 198.1 | 198.1 | -0.0 |
| 408.4 | 199.0 | 199.2 | -0.1 |
| 417.9 | 199.9 | 200.2 | -0.2 |
| 427.9 | 201.2 | 201.2 | -0.0 |
| 437.9 | 201.8 | 202.3 | -0.2 |
| 447.9 | 203.1 | 203.3 | -0.1 |
| 457.9 | 203.8 | 204.3 | -0.2 |
| 468.6 | 205.2 | 205.3 | -0.0 |
| 477.9 | 206.5 | 206.2 | 0.2 |
| 487.9 | 207.4 | 207.2 | 0.1 |
| 497.9 | 208.3 | 208.1 | 0.1 |
| 507.9 | 209.1 | 209.0 | 0.1 |
| 517.9 | 210.3 | 209.9 | 0.2 |
| 527.9 | 211.0 | 210.8 | 0.1 |
| 537.9 | 211.8 | 211.7 | 0.0 |
| 547.9 | 212.5 | 212.6 | -0.1 |
| 556.5 | 213.2 | 213.3 | -0.0 |
| 567.9 | 214.0 | 214.2 | -0.1 |

*The standard uncertainty in pressure and temperature are 0.6 kPa and 0.4 K with 0.68 level of confidence.