Experimental investigation and thermo-economic performance analysis of silver energized Phase change material integrated solar still system

Supplementary File

Nomenclature

| Abbreviations |  |
| --- | --- |
| A | Absorber area |
| Ag | Silver |
| AgePCM | Silver-enhanced phase change materials |
| BIS | Bureau of Indian Standards |
| CNT | Carbon nanotubes |
| CPL | Cost per liter |
| CuO | Copper oxide |
| DSC | Differential scanning calorimetry |
| EDX | Energy dispersive X-ray |
| FOM | Figure of merit |
| FTIR | Fourier transform infrared |
| HT | Heat transfer |
| Lh | Latent heat of vaporization of water |
| NePCM | Nano-enhanced phase change materials |
| PBP | Payback period |
| PCM | Phase change materials |
| Ph | Distillate yield |
| SEM | Scanning electron microscope |
| SS | Solar still |
| SS-C | Conventional solar still |
| SS-AgePCM | Silver-enhanced phase change material integrated solar still |
| Ta | Ambient temperature |
| Tw | Water temperature |
| TES | Thermal energy storage |
| TDS | Total dissolved solids |
| TEMPOS | Thermal properties analyzer |
| TGA | Thermogravimetric analyzer |
| TiO2 | Titanium dioxide |
| UV-Vis | Ultraviolet visible spectrum |
| η | Efficiency |
| ₹ | Indian rupee |
| α | Optical absorbance |
| k | Thermal conductivity |
| Composite codes |  |
| AgePCM-1 | 0.2 wt% Ag dispersed phase change material |
| AgePCM-2 | 0.4 wt% Ag dispersed phase change material |
| AgePCM-3 | 0.6 wt% Ag dispersed phase change material |
| AgePCM-4 | 0.8 wt% Ag dispersed phase change material |
| AgePCM-5 | 1.0 wt% Ag dispersed phase change material |

Appendix 1 Properties of materials used in experiment

| Properties | Unit | PCM | Nanoparticle |
| --- | --- | --- | --- |
|  |  | Paraffin (A49) | Silver |
| Thermal conductivity | W m-1K-1 | 0.22 | 429 |
| Latent heat | J g-1 | 155 | - |
| Melting temperature | °C | 46 | 960 |
| Density | Kg m-3 | 910 | 10500 |
| Particle size | nm |  | 20 |
| color | - | white | black |
| Purity | % | >98 | >98 |

Appendix 2 Instruments used for Characterization

Various sensitive instruments were employed to characterize the synthesized low-temperature binary nanoparticle-dispersed phase change materials. The morphology of the nanoparticle, PCM and its Ag dispersed composites was examined with a Scanning Electron Microscope (Hitachi SU3800) equipped with a Deben Cool stage. Additionally, the EDX equipment (Oxford Instrument EDX) was attached with the SEM instrument to analyze the elemental analysis of PCM and Ag dispersed PCM. To identify the specific chemical functional groups present in the PCM and composite PCM, an Fourier Transform Infrared Spectroscopy (FT-IR) was performed using a Perkin Elmer instrument, USA. The FT-IR analysis was conducted over a wavenumber range of 400 cm⁻¹ to 4000 cm⁻¹, corresponding to the mid-infrared spectrum wavelength range of 2.5 μm to 25 μm, with a precision and spectral resolution of 0.01 cm⁻¹. The optical absorbance and transmittance of the prepared samples within the solar spectrum were analyzed using UV-Vis spectroscopy (Model: LAMBDA 750, Perkin Elmer, USA). Measurements were carried out across a wavelength range of 200 nm to 1400 nm under normal room temperature conditions. The melting temperature and latent heat characteristics of the PCM composite were evaluated using Differential Scanning Calorimetry (DSC) with the DSC 3500 Sirius instrument from NETZSCH. The DSC analysis included melting and cooling curves within a temperature range of 10°C to 75°C under a nitrogen environment, with a heating rate of 5°C/min. This analysis aimed to determine the enthalpy changes during heating and cooling, the phase transition temperatures, and the degree of supercooling. The measurement of thermal conductivity is conducted using a thermal properties analyzer (TEMPOS) instrument equipped with a twin needle SH-3 probe, at a standard room temperature of 25°C. Additionally, a commercially fabricated thermal cycler was used to evaluate the thermal resistance of the composite PCMs. The thermal cycler maintained precise temperature control cycles within a range of 30°C to 70°C, ensuring a stable environment. The system's controller employs sensors to regulate both the heating and cooling cycles. When the system reaches the desired temperature, it automatically shuts off the heating unit and activates the cooling unit, maintaining the temperature within the specified range. The Peltier cooling system, equipped with sensors, ensures that the sample temperature remains above 30°C and below 70°C. Temperature data is effortlessly acquired by a PicoLog device, which the software then converts into numerical values, simplifying the measurement process.

Appendix 3 Uncertainty analysis

The thermophysical characteristics of NePCM were determined using various analytical techniques, including TEMPOS, DSC, TGA, UV-Vis, DSC, among others. The reliability of the measurements performed was characterized by uncertainty analysis. Table summarises the uncertainty of the instruments used. Uncertainty analysis also reflects the dispersion and accuracy of values measured. The uncertainties involved in direct measurement fall under random errors, named Class A errors, and measured by statistical methods. System errors are handled by non-statistical methods and are grouped as Class B errors. The uncertainty associated with the measurements can be estimated by the following equations and the associated terms. The standard uncertainty of measured results is calculated according to specific rules for the A and B uncertainty of a particular measured value, which is commonly referred to as the combined uncertainty.

The mathematical expression gives class A uncertainty

n = total number of readings,   = average value of the measurement

Under the same conditions, when x is measured multiple times, the standard uncertainty u(x) of x to be measured is obtained by combining the class A uncertainty uA(x) and the instrument uncertainty uB2(x).

ux=uA2x+uB22(x)

When a single measurement is performed on a physical quantity, the type B uncertainty is composed of the measurement uncertainty uB1(x) and the instrument uncertainty uB2(x). The measurement uncertainty uB1(x) is caused by estimation, generally 1/10 or 1/5 of the scale value of the instrument. Instrument uncertainty uB2(x) is determined by the characteristics of the instrument itself and is defined as:

uB2x=ac

where the confidence factor c can generally be processed with a uniform distribution, is the value assigned for c is. For a single measurement x, the standard uncertainty u(x) of x to be measured is obtained by combining the class A uncertainty uB1(x) and the instrument uncertainty uB2(x).

ux=uB12x+uB22(x)

x±u(x)

Table T1: The uncertainty associated with measuring devices

| Equipment | Parameter measured | Uncertainty |
| --- | --- | --- |
| TEMPOS | Thermal conductivity | 10% |
| TGA | Thermal stability | 2% |
| Digital scanning calorimetry | Latent heat | 2% |
| Digital scanning calorimetry | Melting point | 0.2°C |
| Thermogravimetric Analyzer | Decomposition Temperature | 1°C |
| UV-Vis | Absorptivity/ Transmissivity | 0.1% |
| Microbalance | Mass of nano fillers | 0.0001 g |
| Weighing Balance | Mass of PCM | 0.001 g |
| Thermocouple | Temperature | ± 0.3 °C |
| Pyranometer | Solar irradiation | ± 3-5 W m-2 |

Appendix 4 Functional group and vibrational mode of A49 PCM and AgePCM composite

| Wavenumber | Functional group | Vibration mode | Intensity |
| --- | --- | --- | --- |
| 720 cm-1 | -(CH2)n- -HC=CH- | Rocking deformation bending | Weak |
| 1378 cm-1 | -CH3 | Symmetric bending | Weak |
| 1464 cm-1 | -CH2 and -CH3 | Deformation bending | Medium |
| 2850 cm-1 | -CH2 | Symmetric stretching | Small |
| 2914 cm-1 | -CH3 | Symmetric stretching | Strong |

Appendix 5 Heat storage and release of PCM and AgePCM

| Sample name | Heat storage |  |  | Heat release |  |  |
| --- | --- | --- | --- | --- | --- | --- |
|  | Tmo (°C) (Onset) | ∆Hm Latent heat (J g-1) | Tm (°C) Melting temperature | Tfo (°C) (Onset) | ∆Hf Latent heat (J g-1) | Tf (°C) Freezing temperature |
| PCM | 12.83 | 156.1 | 49.89 | 47.93 | 153.5 | 43.68 |
| AgePCM-1 | 12.82 | 164.0 | 49.82 | 47.43 | 159.5 | 43.18 |
| AgePCM-2 | 12.14 | 176.4 | 49.32 | 47.93 | 173.2 | 43.93 |
| AgePCM-3 | 14.0 | 170.0 | 49.83 | 47.63 | 158.1 | 44.18 |
| AgePCM-4 | 12.32 | 165.5 | 49.83 | 47.69 | 162.2 | 43.68 |
| AgePCM-5 | 12.57 | 164.7 | 50.0 | 47.43 | 162.8 | 43.18 |

Appendix 6 Heat storage and release of PCM and AgePCM after 500 cycles

| Sample name | Heat storage |  |  | Heat release |  |  |
| --- | --- | --- | --- | --- | --- | --- |
|  | Tmo (°C) (Onset) | ∆Hm Latent heat (J g-1) | Tm (°C) Melting temperature | Tfo (°C) (Onset) | ∆Hf Latent heat (J g-1) | Tf (°C) Solidification temperature |
| PCM-0 cy | 12.83 | 156.1 | 49.89 | 47.93 | 153.5 | 43.68 |
| AgePCM-0 cy | 12.32 | 165.5 | 49.83 | 47.69 | 162.2 | 43.68 |
| PCM-500 cy | 12.1 | 155 | 49.89 | 47.74 | 153.4 | 43.24 |
| AgePCM-500 cy | 14.92 | 165.1 | 49.42 | 47.68 | 162.2 | 44.18 |