Table S-I. Melting peak temperatures (DTA) and degradation peak temperatures (DTG) of different excipients (liquids lipids, solid lipids, and surfactants), placed in platinum crucibles and analyzed using a simultaneous TGA/DTA-60 thermobalance (Shimadzu), under a nitrogen atmosphere with a flow rate of 50 mL.min-1, in the temperature range between 25 and 500 °C at a heating rate of 10 °C.min-1.

| Lipid excipients | DTA Tpeak / ºC |  | DTG Tpeak / ºC |  |
| --- | --- | --- | --- | --- |
|  | Raw material | Binary mixtures | Raw material | Binary mixtures |
| Stearic Acid | 62.7 | 62.3 | 261.9 | 263.4 |
| Lauric Acid | 46.7 | 46.5 | 210.3 | 212.5 |
| Oleic Acid | - | - | 263.7 | 270.5 |
| Palmitic Acid | 64.4 | 63.1 | 250.6 | 250.1 |
| Capmul® | - | - | 205.9/298.5 | 227.7 / 302.7 |
| Captex® | - | - | 324.6 | 319.6 |
| Compritol® 888 | 73.3 | 72.8 | 421.7 | 402.7 |
| Cetyltrimethylammonium Bromide | 107.9 | 107 | 319.6 | 234.1 / 370.7 |
| Kolliphor® RH40 | - | - | 410.8 | 408.8 |
| Miglyol® 812N | - | - | 329.3 | 319.2 |
| Isopropyl Myristate | - | - | 211.4 | 297.2 |
| Glyceryl Monostearate | 63.4 | 63.8 | 271.2 / 414.7 | 298.2 / 398.8 |
| Sesame Oil | - | - | 410.3 | 406.6 |
| Soybean Oil | - | - | 416.7 | 408.7 |
| Span® 60 | 56.4 | 56.1 | 410.4 | 396.1 |
| Span® 80 | - | - | 419.4 | 380.5 |
| Span® 85 | - | - | 410.3 | 394.6 |
| Sodium Taurodeoxycholate | 205.7 | - | 372.4 | 364.6 |
| Medium Chain Triglycerides | - | - | 325.3 | 322.2 |
| Tween® 80 | - | - | 409.2 | 409.9 |

Table S-II: Peak areas, determined by HPLC method, of mixtures of bulk OLZ and of all freshly prepared binary mixtures and mixtures stored for 15 and 30 days under isothermal stress experimental conditions (at 60 °C).

|  |  | Peak areas |  |  |
| --- | --- | --- | --- | --- |
| Excipient | Replicate | Day 0 | Day 15 | Day 30 |
| Stearic Acid | 1 | 224.614.535 | 200.034.713 | 154.250.817 |
|  | 2 | 244.947.164 | 210.138.594 | 175.857.239 |
|  | 3 | 246.718.065 | 193.187.541 | 168.217.409 |
| Lauric Acid | 1 | 242.119.042 | 189.245.277 | 128.319.017 |
|  | 2 | 246.548.482 | 185.666.598 | 133.510.138 |
|  | 3 | 236.919.036 | 186.744.645 | 127.518.119 |
| Palmitic Acid | 1 | 230.003.257 | 202.890.586 | 156.198.531 |
|  | 2 | 227.437.498 | 210.615.800 | 162.351.854 |
|  | 3 | 240.420.053 | 209.126.834 | 162.617.620 |
| Oleic Acid | 1 | 230.970.766 | 184.980.057 | 138.414.871 |
|  | 2 | 234.290.254 | 185.102.803 | 145.712.702 |
|  | 3 | 236.634.688 | 171.999.443 | 153.691.388 |
| Capmul® | 1 | 232.931.690 | 191.883.168 | 143.885.519 |
|  | 2 | 236.669.504 | 180.362.883 | 160.586.364 |
|  | 3 | 236.833.114 | 198.925.202 | 151.808.264 |
| Captex® | 1 | 239.064.659 | 232.896.923 | 228.575.015 |
|  | 2 | 235.303.672 | 217.604.738 | 236.211.901 |
|  | 3 | 232.883.466 | 228.590.116 | 232.553.471 |
| Compritol® 888 | 1 | 237.458.257 | 228.407.620 | 228.500.105 |
|  | 2 | 233.212.816 | 225.921.621 | 234.676.804 |
|  | 3 | 237.026.086 | 227.812.250 | 234.016.598 |
| Cetyltrimethylammonium Bromide | 1 | 226.641.549 | 234.922.588 | 233.055.931 |
|  | 2 | 233.963.820 | 224.086.819 | 238.307.011 |
|  | 3 | 235.747.632 | 235.291.736 | 246.293.454 |
| Kolliphor® RH40 | 1 | 245.161.576 | 215.589.908 | 225.275.523 |
|  | 2 | 236.873.112 | 228.563.935 | 244.528.778 |
|  | 3 | 241.590.328 | 226.753.645 | 237.499.225 |
| Glyceryl Monostearate | 1 | 232.729.820 | 222.676.287 | 226.847.607 |
|  | 2 | 244.941.620 | 224.196.521 | 213.023.475 |
|  | 3 | 259.391.027 | 220.190.154 | 217.858.262 |
| Miglyol® 812N | 1 | 231.009.715 | 203.675.331 | 221.742.838 |
|  | 2 | 228.335.062 | 216.272.388 | 231.565.037 |
|  | 3 | 231.534.551 | 223.851.162 | 231.642.424 |
| Isopropyl Myristate | 1 | 239.160.727 | 223.932.866 | 232.688.533 |
|  | 2 | 234.297.027 | 228.783.856 | 232.540.477 |
|  | 3 | 234.124.704 | 219.358.024 | 242.608.852 |
| Sesame Oil | 1 | 230.993.574 | 212.516.081 | 221.735.219 |
|  | 2 | 243.291.611 | 229.834.785 | 234.839.874 |
|  | 3 | 243.396.038 | 235.347.546 | 238.357.419 |
| Soybean Oil | 1 | 239.600.052 | 219.388.827 | 215.146.637 |
|  | 2 | 234.095.477 | 237.597.725 | 228.224.767 |
|  | 3 | 239.004.726 | 231.254.463 | 242.518.178 |
| Olanzapine | 1 | 227.483.693 | 222.617.228 | 239.664.412 |
|  | 2 | 230.756.560 | 230.423.017 | 235.254.062 |
|  | 3 | 236.892.154 | 234.580.718 | 249.624.501 |
| Span® 60 | 1 | 234.971.949 | 202.395.967 | 205.427.419 |
|  | 2 | 262.096.296 | 203.301.710 | 209.992.143 |
|  | 3 | 247.009.266 | 140.219.720 | 221.405.504 |
| Span® 80 | 1 | 223.929.786 | 181.141.848 | 217.488.050 |
|  | 2 | 238.459.606 | 220.811.358 | 214.369.632 |
|  | 3 | 237.661.022 | 223.725.803 | 213.753.324 |
| Span® 85 | 1 | 247.132.059 | 212.920.391 | 216.357.040 |
|  | 2 | 243.383.126 | 218.546.838 | 222.522.851 |
|  | 3 | 251.372.073 | 220.537.212 | 225.718.776 |
| Sodium Taurodeoxycholate | 1 | 233.538.958 | 214.797.569 | 224.097.751 |
|  | 2 | 237.631.209 | 228.415.385 | 226.636.780 |
|  | 3 | 240.620.159 | 229.838.510 | 229.132.197 |
| Medium Chain Triglycerides | 1 | 238.258.486 | 216.147.585 | 229.836.754 |
|  | 2 | 241.511.472 | 207.270.896 | 235.496.946 |
|  | 3 | 263.136.303 | 229.277.591 | 229.222.820 |
| Tween® 80 | 1 | 237.684.525 | 226.273.538 | 214.271.165 |
|  | 2 | 237.781.934 | 228.344.409 | 239.848.335 |
|  | 3 | 240.418.909 | 227.294.376 | 226.642.022 |