Supplementary Information

Revisiting Thermorheological Simplicity in Crumb Rubber Modified Bitumen Using Fractional Maxwell Modelling

List of Tables

Table 1S Goodness of Fit of the Fractional Maxwell Model to the Measured Storage and Loss Moduli	9

Table 2S STA Samples fractional maxwell parameter variation	10

Table 3S LTA Samples Fractional Maxwell Parameter Variation	11

List of Figures

Figure 1S Experimental and Predicted G’ and G” for CRMB-5 (Unaged Condition)	2

Figure 2S Experimental and Predicted G’ and G” for CRMB-10 (Unaged Condition)	2

Figure 3S Experimental and Predicted G’ and G” for CRMB-15 (Unaged Condition)	3

Figure 4S Experimental and Predicted G’ and G” for CRMB-22 (Unaged Condition)	3

Figure 5S Experimental and Predicted G’ and G” for CRMB-30 (Unaged Condition)	4

Figure 6S Experimental and Predicted G’ and G” for CRMB-5 (STA Condition)	4

Figure 7S Experimental and Predicted G’ and G” for CRMB-10 (STA Condition)	5

Figure 8S Experimental and Predicted G’ and G” for CRMB-15 (STA Condition)	5

Figure 9S Experimental and Predicted G’ and G” for CRMB-22 (STA Condition)	6

Figure 10S Experimental and Predicted G’ and G” for CRMB-5 (LTA Condition)	6

Figure 11S Experimental and Predicted G’ and G” for CRMB-10 (LTA Condition)	7

Figure 12S Experimental and Predicted G’ and G” for CRMB-15 (LTA Condition)	7

Figure 13S Experimental and Predicted G’ and G” for CRMB-22 (LTA Condition)	8

Figure 1S Experimental and Predicted G’ and G” for CRMB-5 (Unaged Condition)

Figure 2S Experimental and Predicted G’ and G” for CRMB-10 (Unaged Condition)

Figure 3S Experimental and Predicted G’ and G” for CRMB-15 (Unaged Condition)

Figure 4S Experimental and Predicted G’ and G” for CRMB-22 (Unaged Condition)

Figure 5S Experimental and Predicted G’ and G” for CRMB-30 (Unaged Condition)

Figure 6S Experimental and Predicted G’ and G” for CRMB-5 (STA Condition)

Figure 7S Experimental and Predicted G’ and G” for CRMB-10 (STA Condition)

Figure 8S Experimental and Predicted G’ and G” for CRMB-15 (STA Condition)

Figure 9S Experimental and Predicted G’ and G” for CRMB-22 (STA Condition)

Figure 10S Experimental and Predicted G’ and G” for CRMB-5 (LTA Condition)

Figure 11S Experimental and Predicted G’ and G” for CRMB-10 (LTA Condition)

Figure 12S Experimental and Predicted G’ and G” for CRMB-15 (LTA Condition)

Figure 13S Experimental and Predicted G’ and G” for CRMB-22 (LTA Condition)

Table 1S Goodness of Fit of the Fractional Maxwell Model to the Measured Storage and Loss Moduli

| Bitumen | Condition | Temp (oC) | R2 (G′) | R2 (G′′) | NRMSE G′ (%) | NRMSE G′′ (%) | Max deviation (log units) |
| --- | --- | --- | --- | --- | --- | --- | --- |
| CRMB-5 | Unaged | 10 | 0.9986 | 0.9987 | 1.16 | 1.14 | 0.0568 |
|  |  | 30 | 0.9985 | 0.9991 | 1.15 | 0.91 | 0.0089 |
|  |  | 50 | 0.9837 | 0.9951 | 3.90 | 2.11 | 0.1568 |
|  |  | 70 | 0.9841 | 0.9996 | 3.92 | 0.58 | 0.0437 |
|  | STA | 10 | 0.9978 | 0.9947 | 1.44 | 2.27 | 0.0587 |
|  |  | 30 | 0.9990 | 0.9998 | 0.97 | 0.43 | 0.0428 |
|  |  | 50 | 0.9861 | 0.9969 | 3.55 | 1.68 | 0.1154 |
|  |  | 70 | 0.9855 | 0.9984 | 3.97 | 1.23 | 0.1213 |
|  | LTA | 30 | 0.9993 | 0.9998 | 0.80 | 0.44 | 0.0352 |
|  |  | 50 | 0.9941 | 0.9985 | 2.31 | 1.18 | 0.0782 |
|  |  | 70 | 0.9885 | 0.9978 | 3.34 | 1.43 | 0.1377 |
| CRMB-10 | Unaged | 10 | 0.9985 | 0.9979 | 1.21 | 1.44 | 0.0523 |
|  |  | 30 | 0.9995 | 0.9998 | 0.70 | 0.38 | 0.0103 |
|  |  | 50 | 0.9914 | 0.9964 | 2.79 | 1.79 | 0.0883 |
|  |  | 70 | 0.9963 | 0.9991 | 1.93 | 0.93 | 0.0573 |
|  | STA | 10 | 0.9917 | 0.9899 | 2.67 | 3.09 | 0.0382 |
|  |  | 30 | 0.9992 | 0.9992 | 0.88 | 0.88 | 0.0249 |
|  |  | 50 | 0.9832 | 0.9940 | 3.85 | 2.32 | 0.0832 |
|  |  | 70 | 0.9820 | 0.9879 | 3.91 | 3.21 | 0.1030 |
|  | LTA | 30 | 0.9997 | 0.9998 | 0.49 | 0.48 | 0.0210 |
|  |  | 50 | 0.9982 | 0.9992 | 1.25 | 0.88 | 0.0351 |
|  |  | 70 | 0.9920 | 0.9975 | 2.75 | 1.50 | 0.1100 |
| CRMB-15 | Unaged | 10 | 0.9988 | 0.9983 | 1.05 | 1.29 | 0.0434 |
|  |  | 30 | 0.9982 | 0.9978 | 1.27 | 1.44 | 0.0634 |
|  |  | 50 | 0.9649 | 0.9750 | 5.62 | 4.69 | 0.1466 |
|  |  | 70 | 0.9938 | 0.9990 | 2.49 | 0.99 | 0.0123 |
|  | STA | 10 | 0.9891 | 0.9867 | 3.00 | 3.36 | 0.0689 |
|  |  | 30 | 0.9996 | 0.9990 | 0.62 | 0.98 | 0.0051 |
|  |  | 50 | 0.9899 | 0.9964 | 2.99 | 1.80 | 0.0625 |
|  |  | 70 | 0.9913 | 0.9899 | 2.84 | 2.94 | 0.1178 |
|  | LTA | 30 | 0.9997 | 0.9999 | 0.52 | 0.25 | 0.0232 |
|  |  | 50 | 0.9989 | 0.9995 | 1.00 | 0.71 | 0.0289 |
|  |  | 70 | 0.9938 | 0.9980 | 2.41 | 1.34 | 0.0967 |
| CRMB-22 | Unaged | 10 | 0.9983 | 0.9974 | 1.27 | 1.56 | 0.0347 |
|  |  | 30 | 0.9983 | 0.9978 | 1.26 | 1.42 | 0.0548 |
|  |  | 50 | 0.9984 | 0.9967 | 1.18 | 1.71 | 0.0777 |
|  |  | 70 | 0.9982 | 0.9989 | 1.32 | 0.99 | 0.0010 |
|  | STA | 10 | 0.9991 | 0.9983 | 0.93 | 1.23 | 0.0310 |
|  |  | 30 | 0.9993 | 0.9982 | 0.83 | 1.29 | 0.0476 |
|  |  | 50 | 0.9968 | 0.9985 | 1.70 | 1.15 | 0.0596 |
|  |  | 70 | 0.9509 | 0.9777 | 6.84 | 4.48 | 0.1553 |
|  | LTA | 10 | 0.9986 | 0.9982 | 1.15 | 1.31 | 0.0301 |
|  |  | 30 | 0.9986 | 0.9988 | 1.12 | 1.06 | 0.0426 |
|  |  | 50 | 0.9148 | 0.9741 | 8.71 | 4.83 | 0.1070 |
|  |  | 70 | 0.9991 | 0.9992 | 0.96 | 0.85 | 0.0353 |
| CRMB-30 | Unaged | 10 | 0.9975 | 0.9980 | 1.55 | 1.44 | 0.0613 |
|  |  | 30 | 0.9992 | 0.9974 | 0.83 | 1.55 | 0.0629 |
|  |  | 50 | 0.9979 | 0.9983 | 1.45 | 1.26 | 0.0403 |
|  |  | 70 | 0.7634 | 0.9867 | 15.15 | 3.58 | 0.0798 |
|  | STA | 10 | 0.9817 | 0.9885 | 4.34 | 3.28 | 0.1990 |
|  |  | 30 | 0.9979 | 0.9921 | 1.40 | 2.73 | 0.0942 |
|  |  | 50 | 0.9977 | 0.9989 | 1.43 | 1.00 | 0.0409 |
|  |  | 70 | 0.9928 | 0.9951 | 2.68 | 2.13 | 0.0190 |
|  | LTA | 10 | 0.9986 | 0.9982 | 1.15 | 1.31 | 0.0301 |
|  |  | 30 | 0.9986 | 0.9988 | 1.12 | 1.06 | 0.0426 |
|  |  | 50 | 0.9148 | 0.9741 | 8.71 | 4.83 | 0.1070 |
|  |  | 70 | 0.9991 | 0.9992 | 0.96 | 0.85 | 0.0353 |

Table 2S STA Samples Fractional Maxwell Parameter Variation

| Bitumen | Temp. (°C) | G(Pa) | τ (s) | α | Log c |
| --- | --- | --- | --- | --- | --- |
| CRMB-5 | 10 | 4.19×10⁷ | 1.77×10⁻² | 0.6071 | 6.56 |
|  | 30 | 1.28×10⁷ | 1.24×10⁻³ | 0.7316 | 4.98 |
|  | 50 | 8.14×10⁵ | 1.69×10⁻³ | 0.8498 | 3.55 |
|  | 70 | 1.00×10⁵ | 1.58×10⁻³ | 0.9297 | 2.40 |
| CRMB-10 | 10 | 4.04×10⁷ | 1.30×10⁻² | 0.5595 | 6.55 |
|  | 30 | 1.56×10⁷ | 7.85×10⁻⁴ | 0.6786 | 5.09 |
|  | 50 | 1.37×10⁶ | 7.75×10⁻⁴ | 0.7463 | 3.82 |
|  | 70 | 1.00×10⁵ | 2.29×10⁻³ | 0.8418 | 2.78 |
| CRMB-15 | 10 | 6.11×10⁷ | 3.09×10⁻³ | 0.5459 | 6.42 |
|  | 30 | 3.45×10⁷ | 1.19×10⁻⁴ | 0.6380 | 5.03 |
|  | 50 | 3.57×10⁶ | 1.02×10⁻⁴ | 0.6623 | 3.91 |
|  | 70 | 7.11×10⁵ | 1.09×10⁻⁴ | 0.7132 | 3.03 |
| CRMB-22 | 10 | 4.43×10⁷ | 3.46×10⁻³ | 0.5429 | 6.31 |
|  | 30 | 2.41×10⁷ | 1.00×10⁻⁴ | 0.5867 | 5.04 |
|  | 50 | 2.37×10⁶ | 1.06×10⁻⁴ | 0.5864 | 4.04 |
|  | 70 | 9.45×10⁵ | 1.01×10⁻⁴ | 0.6933 | 3.21 |
| CRMB-30 | 10 | 2.87×10⁷ | 8.50×10⁻³ | 0.4915 | 6.44 |
|  | 30 | 1.94×10⁷ | 1.00×10⁻⁴ | 0.5098 | 5.25 |
|  | 50 | 2.65×10⁶ | 1.01×10⁻⁴ | 0.5171 | 4.36 |
|  | 70 | 7.09×10⁵ | 1.01×10⁻⁴ | 0.5569 | 3.63 |

Table 3S LTA Samples Fractional Maxwell Parameter Variation

| Bitumen | Temp. (°C) | G (Pa) | τ(s) | α | Log c |
| --- | --- | --- | --- | --- | --- |
| CRMB-5 | 10 | 8.12×107 | 9.92×10⁻2 | 0.5342 | 7.37 |
|  | 30 | 1.97×10⁷ | 1.04×10⁻³ | 0.6588 | 5.33 |
|  | 50 | 1.48×10⁶ | 1.31×10⁻³ | 0.7712 | 3.95 |
|  | 70 | 1.37×10⁵ | 2.02×10⁻³ | 0.8805 | 2.76 |
| CRMB-10 | 10 | 5.34×107 | 1.92×10⁻2 | 0.5232 | 6.83 |
|  | 30 | 1.72×10⁷ | 9.83×10⁻⁴ | 0.6272 | 5.35 |
|  | 50 | 3.96×10⁶ | 2.87×10⁻⁴ | 0.6991 | 4.12 |
|  | 70 | 1.81×10⁵ | 1.63×10⁻³ | 0.8070 | 3.01 |
| CRMB-15 | 10 | 3.39×107 | 9.11×10⁻2 | 0.5276 | 6.98 |
|  | 30 | 1.69×10⁷ | 7.24×10⁻⁴ | 0.6312 | 5.25 |
|  | 50 | 4.83×10⁶ | 1.52×10⁻⁴ | 0.6905 | 4.05 |
|  | 70 | 2.21×10⁵ | 1.01×10⁻³ | 0.7858 | 2.99 |
| CRMB-22 | 10 | 4.26×10⁷ | 4.46×10⁻³ | 0.5121 | 6.39 |
|  | 30 | 2.34×10⁷ | 1.01×10⁻⁴ | 0.5769 | 5.06 |
|  | 50 | 4.45×10⁶ | 1.02×10⁻⁴ | 0.6592 | 4.02 |
|  | 70 | 5.42×10⁵ | 1.46×10⁻⁴ | 0.6011 | 3.43 |