# Supporting Information

# A Method to Improve the Quality of Silica Nanoparticles (SNPs) over Increasing Storage Durations

School of Materials, The University of Manchester, Manchester, M13 9PL, UK

Corresponding authors E-mail: Huw.Owens@manchester.ac.uk

Table S1 Average diameters of the original and centrifuged SNPs (Batch 3 ethanol) over one month (DLS results)

|  | Diameter of SNP (nm) |  |
| --- | --- | --- |
| Volume of ethanol (ml) | O-SNPs | C-SNPs |
| 100 | 224.87 | 190.90 |
| 95 | 253.43 | 216.50 |
| 91 | 298.83 | 230.33 |
| 90 | 310.30 | 267.60 |
| 85 | 366.07 | 283.93 |
| 80 | 389.80 | 321.43 |
|  | O-SNPs after one week | C-SNPs after one week |
| 100 | 254.13 | 188.40 |
| 95 | 288.53 | 208.40 |
| 91 | 319.53 | 244.90 |
| 90 | 350.40 | 257.00 |
| 85 | 346.30 | 300.63 |
| 80 | 405.27 | 306.97 |
|  | O-SNPs after two weeks | C-SNPs after two weeks |
| 100 | 257.30 | 188.30 |
| 95 | 288.87 | 215.80 |
| 91 | 309.70 | 232.47 |
| 90 | 341.10 | 265.10 |
| 85 | 345.73 | 285.53 |
| 80 | 390.40 | 294.90 |
|  | O-SNPs after four weeks | C-SNPs after four weeks |
| 100 | 262.83 | 187.30 |
| 95 | 303.23 | 218.40 |
| 91 | 323.37 | 234.07 |
| 90 | 385.70 | 279.07 |
| 85 | 388.53 | 298.07 |
| 80 | 425.23 | 329.53 |