Supplementary Information

Interaction of Biopolymers with Graphene for Bio-electronic Applications

Ahmed M. Bayoumy1,2, 3, Medhat Ibrahim4*, Ahmed Osman5, 6, Ahmed Abdelmoneim1, 2

1 Nanoscience Department, Basic and Applied Sciences Institute, Egypt-Japan University of Science and Technology, New Borg El Arab, Alexandria 21934, Egypt

2 Graphene Center of Excellence for Energy and Electronic Applications, Egypt-Japan University of Science and Technology, Alexandria 21934, Egypt

3 Biophysics Group, Physics Department, Faculty of Science, Ain Shams University, Cairo 11566, Egypt

4 Spectroscopy Department, National Research Centre, 33 El-Bohouth St. 12622 Dokki, Giza, Egypt

5 Biotechnology Department, Basic and Applied Sciences Institute, Egypt-Japan University of Science and Technology, New Borg El Arab, Alexandria 21934, Egypt

6 Biochemistry Department, Faculty of Science, Ain Shams University, Cairo 11566, Egypt

Rheological features of the formulated G/Biopolymer composite inks were investigated by a rheometer (Malvern Panalytical KINEXUS PRO Rheometer) that is used to measure viscosity at various shear rates (10-1000 s-1). Kinetic viscosity of G/CMC biocomposite ink was measured to equal 2.26 cP at 200s-1 shear rate while that of G/Cs one is 2.69 cP at 200s-1 shear rate. The printing parameters were adjusted to print a continuous homogenous line, as the illustrated example in figure S1.

Fig. S1: A live image of the printed continuous uniform line captured by the camera implemented in the printer.