Donor Moiety Engineering in D-D-π-A-π-A Quinoxaline Sensitizers for Efficient Dye-Sensitized Solar Cells

Aisha R. Al-Marhabia, Reda M. El-Shishtawyb,c, Khalid O. Al-Footyb, Kenan Ozel*d, Abdullah Atilgane, and Abdullah Yildizf

a Chemistry Department, Al-Qunfudah University College, Umm Al-Qura University, Makkah, Saudi Arabia

b Chemistry Department, Faculty of Science, King Abdulaziz University, Jeddah 21589, Saudi Arabia

c Dyeing, Printing and Textile Auxiliaries Department, Textile Research and Technology Institute, National Research Centre, 33 EL Buhouth St., Dokki, Giza, 12622, Egypt

d Department of Electrical and Energy, GAMA Vocational School, Ankara University, Ankara, Turkey

e Central Research Laboratory Application and Research Center, Ankara Yildirim Beyazit University, Ankara 06010, Turkey

f Department of Energy Systems Engineering, Faculty of Engineering and Natural Sciences, Ankara Yildirim Beyazıt University, Ankara 06010, Turkey

Supplementary Materials

Scheme S1. The synthetic route to QX-D1, QX-D2, and QX-D3 dyes.

Fig. S1. UV-Vis absorption spectra of QX-D1, QX-D2, and QX-D3 in THF solutions at a concentration (C = 1×10-5 M).

Fig. S2. Normalized absorption and emission for (A) QX-D1, (B) QX-D2, and (C) QX-D3 dyes in THF solutions.

Fig. S3. Cyclic voltammograms of QX-D1, QX-D2, and QX-D3 dyes and ferrocene as internal reference in THF solutions.

Table S1

Optical and electrochemical data for QX-D1, QX-D2, and QX-D3 dyes measured in THF solutions (C = 1×10-5 M).

| Compound | Absorption |  | Emission | Stokes shift (cm-1) | intercept (nm) | Eg (eV) | Eox(onset) vs. Ag/AgCl (V) | HOMO (eV) | LUMO (eV) |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  | max (nm) | M-1 cm-1) | em (nm) |  |  |  |  |  |  |
| QX-D1 | 511 | 23434 | 594 | 2734 | 562 | 2.21 | 0.73 | -5.07 | -2.86 |
| QX-D2 | 542 | 29825 | 587 | 1414 | 570 | 2.18 | 0.56 | -4.90 | -2.72 |
| QX-D3 | 526 | 23214 | 639 | 3362 | 592 | 2.09 | 0.79 | -5.13 | -3.04 |
| Fc/Fc+ |  |  |  |  |  |  | 0.46 |  |  |

Fig. S4. Frontier molecular orbital energy levels obtained at B3LYP/6-31G(d,p) in THF solvent compared with the experimental data.