Supporting Information

Optimization of Non-thermal Plasma-assisted Catalytic Oxidation for Methane Emissions Abatement as the Exhaust Aftertreatment Technology

Rahman Gholami1, Cristina Stere1, Sarayute Chansai1, Alexandre Goguet2, Peter Hinde3, Paul Millington 3, Amit Singhania1 and Christopher Hardacre1*

1 School of Chemical Engineering and Analytical Science, The University of Manchester, Manchester M13 9PL, UK.

2 School of Chemical Engineering and Chemistry, The Queen’s University of Belfast, Belfast BT9 5AG, U.K.

3 Johnson Matthey Technology Centre, Reading, UK

* Email: c.hardacre@manchester.ac.uk

S.1 Catalyst characterization

Nitrogen (N2) adsorption-desorption analysis was performed at −196 °C using a Micromeritics ASAP2020 to determine the specific surface area of the catalysts (based on the BET method). Before analysis, the catalysts were dried under vacuum at 300 °C for 3 h. The BET surface area of Al2O3 was 218 m2/g. A slight decrease in the surface area was observed with the loading of the noble metal, corresponding to 183 m2/g and 170 m2/g for the 2 wt% and 10 wt% Pd loading, respectively.

Fig. S1 shows the XRD patterns of the 2 wt% and 10 wt% Pd catalysts. The XRD patterns of materials were obtained by PANalytical X'Pert Pro X-ray diffractometer using CuKα emission lines from a generator operating at 40 keV and 40 mA. XRD scan was performed at 2θ = 10°–90° with a step size of 0.033°. Several peaks are assigned to the support and to PdO species and no Pd clusters are observed. As expected, 10 wt% Pd/Al2O3 has higher degree of PdO crystallinity than 2 wt% Pd/Al2O3, however, the PdO crystallite size of 10 wt% Pd/Al2O3 (4 nm) was smaller than 2 wt% Pd/Al2O3 (9 nm).

Fig. S1 XRD patterns for fresh (a) 2 wt% Pd/Al2O3 and (b) 10 wt% Pd/Al2O3 catalysts. PdO (⬤)

Fig. S2 Plasma SIE as a function of the applied peak voltage at various temperatures in NTP-catalytic CH4 oxidation. Reaction conditions are 30 kHz, 10 wt% Pd/Al2O3, 0.5 kPa CH4, 10 kPa O2, 7 kPa H2O, 5.5 kPa CO2 and 0.1 kPa NO in N2 with 171,429 mL g-1 h-1 GHSV. Room temperature (RT) is assumed to be 20 °C

Fig. S3 Plasma SIE as a function of temperature at various applied voltages in NTP-catalytic CH4 oxidation. Reaction conditions are 30 kHz, 10 wt% Pd/Al2O3, 0.5 kPa CH4, 10 kPa O2, 7 kPa H2O, 5.5 kPa CO2 and 0.1 kPa NO in N2 with 171,429 mL g-1 h-1 GHSV

Fig. S4 Surface plot of Plasma SIE, temperature and CH4 conversion in NTP-catalytic CH4 oxidation. Reaction conditions are 30 kHz, 10 wt% Pd/Al2O3, 0.5 kPa CH4, 10 kPa O2, 7 kPa H2O, 5.5 kPa CO2 and 0.1 kPa NO in N2 with 171,429 mL g-1 h-1 GHSV

Fig. S5 Schematics of the dual-stage setup: upstream plasma reactor, followed by a thermal NH3-SCR reactor

S2. Plasma gas phase reactions considered in the manuscript from references ESI Section S2 [22, 50–56]

O2 + e- → e- + O2*										(S1)

N2 + e- → e- + N2* 										(S2)

N2 + 2·O → 2NO 										(S3)

N2 + 2·O → NO + ·N										(S4)

N2 + ·OH → NO + ·H 										(S5)

NO + ·N → N2O 										(S6)

NO2 + ·N → N2O + ·O 										(S7)

NO2 + ·NH2→ N2O +H2O 									(S8)

·O + NO → NO2 										(S9)

O3 + NO → NO2 +O2 										(S10)

e- + NO2 → e- +NO + ·O 									(S11)

·O + NO2 → NO +O2 										(S12)

·N + NO2 → N2 +O2 										(S13)

·N + NO → N2 + ·O 										(S14)

O3 + NO2 → NO3 +O2 										(S15)

e- + NH3 → ·NH2 + ·H 										(S16)

·O + NH3 → ·NH2 + ·OH 									(S17)

·H + NH3 → ·NH2 + H2 										(S18)

·OH + NH3 → ·NH2 + H2O 									(S19)

·NH2 + NO → N2 + H2O 									(S20)

·NH2 + NO2 → N2 + H2O 									(S21)

NO2 + NH3 → N2 + H2O 									(S22)

N2O + ·O→ 2NO 										(S23)

e- + H2O → e- +·H + ·OH 									(S24)

·O + H2O → ·OH + ·OH 									(S25)

CH4 + e-→ CH4* + 2 e- 										(S26)

CH4 + e-→ ·CH3 + ·H + e-  									(S27)

e- + CH4 → ·C+H2 + H2 + e- 									(S28)

e- + ·CH3 → ·CH2 + ·H+ e- 									(S29)

e- + ·CH3 → ·CH + H2 + e- 									(S30)

e- + ·CH2 → ·CH + ·H + e- 									(S31)

·O + CH4 → CO + 2H2										 (S32)

·O + CH4 → CO + H2O										 (S33)

·O + CO → CO2										  (S34)

CH4 + ½ O2 → CO + 2H2 									  (S35)

22. 	Baylet A, Marécot P, Duprez D, et al (2012) Synergetic effect of plasma/catalysis hybrid system for CH4 removal. Appl Catal B Environ 113–114:31–36. https://doi.org/10.1016/j.apcatb.2011.10.026

50. 	Wang W, Snoeckx R, Zhang X, et al (2018) Modeling plasma-based CO2 and CH4 conversion in mixtures with N2, O2, and H2O: The bigger plasma chemistry picture. J Phys Chem C 122:8704–8723. https://doi.org/10.1021/acs.jpcc.7b10619

51. 	Wu J, Xia Q, Wang H, Li Z (2014) Catalytic performance of plasma catalysis system with nickel oxide catalysts on different supports for toluene removal: Effect of water vapor. Appl Catal B Environ 156–157:265–272. https://doi.org/10.1016/j.apcatb.2014.03.017

52. 	Falkenstein Z, Coogan JJ (1997) Microdischarge behaviour in the silent discharge of nitrogen - oxygen and water - air mixtures. J Phys D Appl Phys 30:817–825. https://doi.org/10.1088/0022-3727/30/5/015

53. 	Zhang J, Liu Y, Yao X, et al (2020) Enhanced moisture resistance of Cu/Ce catalysts for CO oxidation via plasma−catalyst interactions. Chemosphere 261:127739.  https://doi.org/10.1016/j.chemosphere.2020.127739

54. 	Wang Z, Kuang H, Zhang J, et al (2019) Nitrogen oxide removal by non-thermal plasma for marine diesel engines. RSC Adv 9:5402–5416. https://doi.org/10.1039/C8RA09217F

55. 	Snoeckx R, Heijkers S, Van Wesenbeeck K, et al (2016) CO2 conversion in a dielectric barrier discharge plasma: N2 in the mix as a helping hand or problematic impurity? Energy Environ Sci 9:999–1011. https://doi.org/10.1039/C5EE03304G

56. 	Pavlovich MJ, Ono T, Galleher C, et al (2014) Air spark-like plasma source for antimicrobial NOX generation. J Phys D Appl Phys 47:505202. https://doi.org/10.1088/0022-3727/47/50/505202