PHAM-D-19-00437

Supplemental Material

Figure S1. Pellet mass and TAF strength consistency in a batch of pellets. The standard deviations for pellet mass and TAF strength were ± 0.32 mg and ± 0.38 mg, respectively.

Figure S2. Kinetics of TAF hydrolysis in PBS buffer. Initial TAF concentration was 10 µg/ml, PBS solution [PO43-] = 11.9 mM [NaCl]= 137 mM; pH 7.4 phosphate-buffered saline adjusted to pH 7.0 with 1N HCl and pH 8.0 with 1 N NaOH. Reaction temperature 37 °C at 80 RPM on an orbital shaker. TAF concentration measured by HPLC described in the methods.

Figure S3. The effect of e-beam sterilization on release rate. Average daily release of TAF equivalent per cm lumen length from implants with Tecoflex™ EG-85A RCM (2.2 mm OD, 150 µm thickness) with core formulation 96:2:2 TAF:NaCl:MgSt before (, n=5) and after (, n=9) e-beam sterilization. Error bars represent standard deviation.

Figure S4. The dissolution of TAF implants after storage at various temperatures. Average daily release of TAF equivalent per cm lumen length from implants with Tecoflex™ EG-85A RCM (2.2 mm OD, 150 µm thickness, 1.6 cm lumen length) with core pellet composition of 96:2:2 TAF:NaCl:MgSt at a zero time point () and after storage at -20 °C for 1 year (), room temperature for 1 year (), and 40°C for 6 months (). Error bars represent standard deviation (n=5).

TABLES

Table S-I. Extrusion conditions for tubing of various polymers and geometries

| Polymer | Outer diameter (mm) | Wall thickness (µm) | Zone temperaturesa (hopper to die, °C) | Drawn down ratio | Draw ratio balance |
| --- | --- | --- | --- | --- | --- |
| Tecoflex™ EG-85A | 2.2 | 150 | 140/185/185/165/140 | 26.44 | 0.99 |
| Tecoflex™ EG-85A | 2.2 | 200 | 135/160/180/180/135 | 26.44 | 0.99 |
| Tecoflex™ EG-85A | 2.2 | 360 | 135/160/180/180/135 | 7.77 | 1.03 |
| Tecoflex™ EG-85A | 3.6 | 150 | 135/165/195/190/140 | 10.80 | 1.00 |
| Tecoflex™ 75:25 EG-85A:93A | 2.2 | 150 | 135/160/180/180/135 | 27.53 | 1.00 |
| Tecoflex™ 50:50 EG-85A:93A | 2.2 | 150 | 135/160/180/180/135 | 27.53 | 1.00 |
| Tecoflex™ 25:75 EG-85A:93A | 2.2 | 150 | 145/165/190/180/130 | 19.47 | 0.99 |
| Tecoflex™ EG-93A | 2.2 | 150 | 140/165/195/165/135 | 19.40 | 0.95 |
| Celanese PEVA | 2.2 | 150 | 170/170/170/160/100 | 26.44 | 0.99 |
| 87.5:12.5 Tecoflex™ EG-85A: Tecophilic™ HP-60D-20 | 2.2 | 150 | 150/170/190/175/120 | 19.47 | 0.95 |

aThe first three zone temperatures are for the barrel, and the last two are for the die.

Table S-II. Geometries and loading for all implants

| PEU | Outer diameter (mm) | Wall thickness (µm) | Lumen length (cm) | TAF loading (mg; means ± SD) | Unit Length TAF loading (mg/cm) | TAF in vitro unit length release rate (µg/cm/day; means ± SD)a | Study |
| --- | --- | --- | --- | --- | --- | --- | --- |
| Tecoflex™ EG-85A | 2.2 | 150 | 0.8 | 16.8 ± 0.4 | 21.0 | 102 ± 20 | Figure 6, 7 and 8; polymer blend; salt concentrationc |
| Tecoflex™ EG-85A | 2.2 | 150 | 1.6 | 33.9 ± 0.3 | 21.2 | 112 ± 24 | Figure 6, 7 and 8; stability; sterilizationc |
| Tecoflex™ EG-85A | 2.2 | 150 | 3.7 | 87.3 ± 0.6 | 23.6 | 105 ± 26 | Figures 6 and 7 |
| Tecoflex™ EG-85A | 2.2 | 200 | 1.0 | 16.6 ± 0.3 | 16.6 | 64 ± 16 | Figures 6 and 7 |
| Tecoflex™ EG-85A | 2.2 | 360 | 1.9 | 18.8 ± 1.6 | 9.9 | 22 ± 8 | Figures 6 and 7 |
| Tecoflex™ EG-85A | 3.6 | 150 | 3.8 | 271.3 ± 2.4 | 71.4 | 269 ± 67 | Figures 6 and 7 |
| 75:25 Tecoflex™ EG-85A:93A | 2.2 | 150 | 0.9 | 15.8 ± 0.3 | 17.5 | 67 ± 17 | Polymer blend |
| 50:50 Tecoflex™ EG-85A:93A | 2.2 | 150 | 0.9 | 16.0 ± 0.3 | 17.7 | 41 ± 14 | Polymer blend |
| 25:75 Tecoflex™ EG-85A:93A | 2.2 | 150 | 1.5 | 24.6 ± 0.5 | 16.4 | 23 ± 8 | Polymer blend |
| 0:100 Tecoflex™ EG-85A:93A | 2.2 | 150 | 1.1 | 15.8 ± 0.3 | 14.4 | 15 ± 5 | Polymer blend |
| PEVA (28% vinyl acetate content) | 2.2 | 150 | 1.3 | 24.3 ± 0.6 | 18.7 | 0.6 ± 1 | Polymer blend |
| 87.5:12.5 Tecoflex™ EG-85A:Tecophilic™ HP-60D-20 | 2.2 | 150 | 1.4 | 24.8 ± 0.5 | 17.7 | 95 ± 23 | Polymer blend |
| Tecoflex™ EG-85A | 2.2 | 150 | 1.2 | 27.9 ± 0.3 | 23.2 | 65 ± 17 | Salt concentration |
| Tecoflex™ EG-85A | 2.2 | 150 | 1.2 | 26.9 ± 0.9 | 22.4 | 99 ± 27 | Salt concentration |
| Tecoflex™ EG-85Ab | 2.2 | 150 | 1.2 | 25.1 ± 0.6 | 20.9 | 187 ± 57 | Salt concentration |
| Tecoflex™ EG-85A | 2.2 | 150 | 1.6 | 34.0 ± 0.3 | 21.3 | 100 ± 23 | Stability |
| Tecoflex™ EG-85A | 2.2 | 150 | 1.6 | 34.0 ± 0.4 | 21.3 | 95 ± 20 | Stability |
| Tecoflex™ EG-85A | 2.2 | 150 | 1.6 | 34.0 ± 0.1 | 21.3 | 87 ± 14 | Stability |
| Tecoflex™ EG-85A | 2.2 | 150 | 1.6 | 33.6 ± 0.2 | 21.0 | 93 ± 17 | Sterilization |

aAverage over days 7 to 91

bAverage over days 7 to 63 due to depletion of contents

cThese implants are called generation A implants in Su et al. (27)

Table S-III. Table of individual masses of TAF and its related species measured in release media

each day for the same set of implants shown in Figure 8B

| Day | TAF (µg/day)a | PMPA monoamidate (µg/day) | monophenyl PMPA (µg/day) | TFV (µg/day) |
| --- | --- | --- | --- | --- |
| 1 | 18.8 ± 3.2 | 4.3 ± 0.8 | 0.0 ± 0.0 | 0.4 ± 0.2 |
| 2 | 29.7 ± 5.4 | 3.7 ± 3.9 | 0.0 ± 0.0 | 0.0 ± 0.0 |
| 3 | 34.8 ± 3.9 | 6.7 ± 2.4 | 0.0 ± 0.0 | 0.0 ± 0.0 |
| 5 | 31.7 ± 21.3 | 16.0 ± 14.1 | 0.0 ± 0.0 | 10.6 ± 22.0 |
| 7 | 65.0 ± 11.6 | 10.8 ± 7.1 | 0.0 ± 0.0 | 3.2 ± 2.8 |
| 10 | 69.1 ± 5.6 | 17.6 ± 1.2 | 0.0 ± 0.0 | 0.4 ± 0.2 |
| 14 | 99.2 ± 8.8 | 6.4 ± 3.7 | 0.0 ± 0.0 | 3.3 ± 1.2 |
| 21 | 91.1 ± 4.5 | 19.3 ± 3.1 | 0.0 ± 0.0 | 2.2 ± 1.1 |
| 25 | 96.8 ± 3.1 | 16.2 ± 0.7 | 0.0 ± 0.0 | 6.2 ± 0.8 |
| 30 | 102.7 ± 4.9 | 10.2 ± 0.0 | 0.0 ± 0.0 | 9.6 ± 0.7 |
| 37 | 82.9 ± 4.6 | 21.3 ± 3.4 | 0.0 ± 0.0 | 2.6 ± 0.1 |
| 42 | 106.6 ± 7.2 | 21.7 ± 1.4 | 0.0 ± 0.0 | 7.8 ± 0.6 |
| 49 | 81.0 ± 7.0 | 20.5 ± 1.1 | 0.0 ± 0.0 | 0.0 ± 0.0 |
| 56 | 110.8 ± 6.1 | 15.4 ± 1.7 | 0.0 ± 0.0 | 0.0 ± 0.0 |
| 63 | 67.1 ± 4.6 | 35.6 ± 2.9 | 0.0 ± 0.0 | 3.5 ± 0.5 |
| 70 | 99.2 ± 25.9 | 59.9 ± 19.3 | 0.0 ± 0.0 | 0.0 ± 0.0 |
| 77 | 107.6 ± 6.7 | 3.5 ± 0.3 | 0.0 ± 0.0 | 3.2 ± 2.2 |
| 85 | 82.9 ± 8.5 | 62.1 ± 9.4 | 0.0 ± 0.0 | 4.0 ± 0.2 |
| 91 | 99.4 ± 4.9 | 43.3 ± 11.0 | 0.0 ± 0.0 | 4.9 ± 2.1 |
| 98 | 138.3 ± 8.2 | 32.8 ± 4.0 | 0.0 ± 0.0 | 5.6 ± 0.4 |
| 105 | 118.8 ± 17.6 | 27.5 ± 2.1 | 0.0 ± 0.0 | 7.4 ± 1.0 |
| 112 | 81.4 ± 40.4 | 28.7 ± 12.7 | 1.4 ± 0.0 | 7.4 ± 0.5 |
| 119 | 9.3 ± 17.1 | 9.3 ± 13.3 | 0.0 ± 0.0 | 1.2 ± 1.3 |
| 126 | 0.0 ± 0.0 | 1.6 ± 0.0 | 0.0 ± 0.0 | 12.2 ± 8.5 |
| 133 | 2.4 ± 1.5 | 0.6 ± 1.7 | 1.3 ± 0.0 | 4.3 ± 0.3 |
| 140 | 0.0 ± 0.0 | 0.7 ± 0.0 | 0.0 ± 0.0 | 8.0 ± 2.0 |
| 147 | 0.0 ± 0.0 | 3.6 ± 0.0 | 0.0 ± 0.0 | 4.9 ± 2.2 |
| 154 | 0.0 ± 0.0 | 0.0 ± 0.0 | 0.0 ± 0.0 | 1.7 ± 0.9 |
| 164 | 0.7 ± 0.2 | 7.9 ± 3.0 | 0.0 ± 0.0 | 0.0 ± 0.0 |
| 169 | 0.0 ± 0.0 | 0.0 ± 0.0 | 0.0 ± 0.0 | 0.7 ± 0.9 |
| 175 | 0.0 ± 0.0 | 1.4 ± 0.5 | 0.0 ± 0.0 | 0.7 ± 0.8 |

aUsing tenofovir alafenamide hemifumarate molecular weight