Modulating nitrogenase activity of encapsulated diazotrophs through oxygen-regulated microenvironments and carbon availability in alginate hydrogel beads

Prashant Dahal1,2, Senthil Subramanian3*, Srinivas Janaswamy1,4*

1Department of Dairy and Food Science, South Dakota State University, Brookings, SD 57007, USA.

2Department of Food, Bioprocessing and Nutrition Sciences, North Carolina State University, Raleigh, NC 27606, USA.

3College of Natural Sciences, South Dakota State University, Brookings, SD 57007, USA.

4Department of Agronomy, Horticulture and Plant Science, South Dakota State University, Brookings, SD 57007, USA.

*Corresponding authors

Email: Senthil.Subramanian@sdstate.edu, Srinivas.Janaswamy@sdstate.edu

Fig. S1. FTIR spectra for sodium alginate powder.

Fig. S2. FTIR spectra for alginate beads.

Fig. S3. FTIR spectra for sugar added Ca2+-alginate beads.

# Table T1. FTIR spectra of sodium alginate powder and ion-crosslinked alginate beads.

| Functional group | Alginate powder | Ca-Alg | Sr-Alg | Zn-Alg | Cu-Alg | Ni-Alg | Al-Alg |
| --- | --- | --- | --- | --- | --- | --- | --- |
|  | 623 | 607 | 629 | 605 | 607 | 605 | 608 |
|  | * | 750 | * | * | * | * | * |
| C-OH stretching | 1032 | 1000 | 1000 | 1027 | 1026 | 1015 |  |
|  | 1386 | * | * | * | * | * | * |
| Symmetric -C-O-O stretching | 1418 | 1467 | * | 1405 | 1432 | 1435 | 1460 |
| Asymmetric C-O-O | 1608 | 1723 | 1663 | 1704 | 1710 | 1719 | 1777 |
|  |  |  |  |  | 2152 | 2158 |  |
| Aliphatic C-H | 2939 | 2975 | 2998 | 2906 | 2973 | 2989 | 2997 |
| O-H stretching | 3417 | 3511 | 3479 | 3576 | 3557 | 3655 | 3678 |

# Table T2. The significant FTIR absorption peaks (cm-1) of sodium-alginate powder and Ca-alginate beads.

| Functional group | Ca-Control | Ca-Arabinose | Ca-Glucose | Ca-Galactose |
| --- | --- | --- | --- | --- |
| C-OH stretching | 1032 | 985 | 1032 | 988 |
| Symmetric -C-O-O stretching | 1371 | 1469 | 1435 | 1469 |
| Asymmetric C-O-O | 1714 | 1784 | 1709 | 1775 |
| Aliphatic C-H | 2955 | 2936 | 2974 | 2928 |
| O-H stretching | 3498 | 3499 | 3491 | 3500 |

# Table T3. The significant FTIR absorption peaks (cm-1) of sodium-alginate powder and Sr-alginate beads.

| Functional group | Sr-Control | Sr-Arabinose | Sr-Glucose | Sr-Galactose |
| --- | --- | --- | --- | --- |
| C-OH stretching | 1068 | 1068 | 1060 | 1068 |
| Symmetric -C-O-O stretching | 1387 | 1387 | 1387 | 1387 |
| Asymmetric C-O-O | 1734 | 1734 | 1734 | 1734 |
| Aliphatic C-H | 2991 | 2991 | 2991 | 2991 |
| O-H stretching | 3497 | 3497 | 3497 | 3492 |

# Table T4. Bulk-equivalent oxygen concentrations (nmol L⁻¹) and corresponding oxygen content per bead (nmol bead⁻¹) for alginate beads crosslinked with different cations.

| Bead type | Bulk-equivalent O₂ (nmol/L) | O₂ content (nmol/bead) |
| --- | --- | --- |
| Ca alginate | 59.9 ± 16.4 | 1.50 ± 0.41 |
| Zn alginate | 94.4 ± 32.4 | 2.36 ± 0.81 |
| Sr alginate | 77.5 ± 18.8 | 1.94 ± 0.47 |
| Ni alginate | 188.3 ± 39.6 | 4.70 ± 0.99 |
| Cu alginate | 215.0 ± 42.8 | 5.38 ± 1.07 |
| Al alginate | 89.4 ± 25.6 | 2.23 ± 0.64 |