Hydrogenation of Alkynyl Substituted Aromatics Over Rhodium/Silica.

Joseph W. Gregory and S David Jackson*

Centre for Catalysis Research, School of Chemistry, University of Glasgow, Glasgow G12 8QQ, Scotland, UK

Supplementary Data.

The activation energy for phenylacetylene was determined by measuring the first order rate constants over a temperature range of 313 – 343 K.

| Temp (K) | 1/T | k (min-1) | ln(k) |
| --- | --- | --- | --- |
| 313 | 0.0031949 | 0.023 | -3.7723 |
| 323 | 0.0030960 | 0.049 | -3.0159 |
| 333 | 0.0030030 | 0.0781 | -2.5498 |
| 343 | 0.0029155 | 0.1614 | -1.8239 |

The linear relationship between 1/T and ln(k) was analysed:

|  | Regression Output: |  |  |
| --- | --- | --- | --- |
| Constant |  |  | 17.887046345159 |
| Std Err of Y Est |  |  | 0.0879413729418242 |
| R Squared |  |  | 0.992293301549774 |
| No. of Observations |  |  | 4 |
| Degrees of Freedom |  |  | 2 |
| X Coefficient(s) |  | -6774.33531303681 |  |
| Std Err of Coef. |  | 422.149077676783 |  |

From the x-coefficient an activation energy of 56.3 kJ.mol-1 was calculated with an error of ±3.5 kJ.mol-1.

The activation energy for 1-phenyl-1-propyne was determined by measuring the first order rate constants over a temperature range of 313 – 343 K.

| Temp (K) | 1/T | k (min-1) | ln(k) |
| --- | --- | --- | --- |
| 313 | 0.0031949 | 0.0294 | -3.52676 |
| 323 | 0.0030960 | 0.04899 | -3.01614 |
| 333 | 0.0030030 | 0.0923 | -2.38271 |
| 343 | 0.0029155 | 0.1028 | -2.27497 |

The linear relationship between 1/T and ln(k) was analysed:

|  | Regression Output: |  |  |
| --- | --- | --- | --- |
| Constant |  |  | 15.4689378985295 |
| Std Err of Y Est |  |  | 0.0645851416470318 |
| R Squared |  |  | 0.99365048224137 |
| No. of Observations |  |  | 3 |
| Degrees of Freedom |  |  | 1 |
| X Coefficient(s) |  | -5953.64964972949 |  |
| Std Err of Coef. |  | 475.923140475551 |  |

From the x-coefficient an activation energy of 49.5 kJ.mol-1 was calculated with an error of ±4.0 kJ.mol-1.

The reaction profile for the phenylacetylene/1-phenyl-1-propyne competitive hydrogenation is shown in the figure.