Supplementary Information

Methanol dynamics in H-ZSM-5 with Si/Al ratio of 25: A Quasi-Elastic Neutron Scattering (QENS) study

Santhosh K. Matam*, C. Richard A. Catlow, Ian P. Silverwood, Alexander J. O’Malley*

UK Catalysis Hub, Research Complex at Harwell, Science and Technology Facilities Council, Rutherford Appleton Laboratory, OX11 0FA, UK

Santhosh K. Matam, C. Richard A. Catlow, Ian P. Silverwood & Alexander J. O’Malley

Cardiff Catalysis Institute, School of Chemistry, Cardiff University, Cardiff, CF10 3AT, UK

Santhosh K. Matam & C. Richard A. Catlow

Department of Chemistry, University College London, 20 Gordon St., London WC1E 6BT, UK

C. Richard A. Catlow

ISIS Pulsed Neutron and Muon Facility, Science and Technology Facilities Council, Rutherford Appleton Laboratory, OX11 0QX, UK

Ian P. Silverwood

Centre of Sustainable and Circular Technologies, Department of Chemistry, University of Bath, Bath, BA2 7AY, UK

Alexander J. O’Malley

*Corresponding author e-mail: santhosh.matam@rc-harwell.ac.uk; a.o’malley@bath.ac.uk; Website: www.ukcatalysishub.co.uk

Fig. S1. QENS spectra of methanol loaded H-ZSM-5 at 298 K. Experimental data (filled circles), total fit (solid black line) and the Lorentzian function (red). Selected spectra are shown for clarity.

Fig, S2. QENS spectra of methanol loaded H-ZSM-5 at 323 K. Experimental data (filled circles), total fit (solid black line) and the Lorentzian function (red). Selected spectra are shown for clarity.

Fig. S3. (A): QENS spectra of methanol loaded H-ZSM-5 at 348 K. Experimental data (filled circles), total fit (solid black line) and the Lorentzian function (red). Selected spectra are shown for clarity. (B): Experimental EISF data of methanol loaded H-ZSM-5 at 348 K are modelled by including a fraction of immobile methanol in different theoretical models. Mobile methanol fraction is shown in the parenthesis of panel (B) and confined volume radius of 2.75 Å is considered. (C): The Q independent at lower Q (< 1.25 Q2) represents the HWHM of the Lorentzian function that fits reasonably well to the Volino–Dianoux confined diffusion model. The Q dependent of the Lorentzian function HWHM at higher Q > 1 Q2) fits well to the Chudley–Elliot jump diffusion model. The Q2 value corresponding to the 2.75 Å radius of the confined sphere of the Volino–Dianoux model is indicated by the dashed black vertical line. EISF (in B) and HWHM (in C) values at Q of 1.58 and 1.67 are not considered due to contribution from Bragg peaks.

Fig. S4. (A): QENS spectra of methanol loaded H-ZSM-5 at 373 K. Experimental data (filled circles), total fit (solid black line) and the Lorentzian function (red). Selected spectra are shown for clarity. (B): Experimental EISF data of methanol loaded H-ZSM-5 at 373 K are modelled by including a fraction of immobile methanol in different theoretical models. Mobile methanol fraction is shown in the parenthesis of panel (B) and confined volume radius of 2.75 Å is considered. (C): The Q independent at lower Q (< 1.25 Q2) represents the HWHM of the Lorentzian function that fits reasonably well to the Volino–Dianoux confined diffusion model. The Q dependent of the Lorentzian function HWHM at higher Q > 1 Q2) fits well to the Chudley–Elliot jump diffusion model. The Q2 value corresponding to the 2.75 Å radius of the confined sphere of the Volino–Dianoux model is indicated by the dashed black vertical line. EISF (in B) and HWHM (in C) values at Q of 1.58 and 1.67 are not considered due to contribution from Bragg peaks.