Supplementary Information (SI)

Table S1: Assignment of the DRIFTS bands and thermal stability range of adsorbates.

| Species | ṽ (vibration mode) / cm-1 | Temperature range | Ref. |
| --- | --- | --- | --- |
| Hydroxyl | 3697 (νOH), 3665 (νOH), 3626 (νOH) | -100 °C–250 °C | [23, 34, 35] |
| Polyoxymethylene | 2981 (νCH2), 2921 (νCH2), 2786 (νCH2) 1470 (δCH2), 1433 (ωCH2), 1382 (ωCH2), 1239 (RCO),1104 (RCO), 947 (RCO) | -100 °C–50 °C | [25, 26] |
| [CH2O]n oligomers | 2938 (νCH2), 1406 (δCH2) | 50 °C–100 °C | [23, 24] |
| Methoxy | 2970 (νCH2), 2860 (νCH2), 1174, (CO) 1091 (νa,CO), 1069 (νCO) | 50 °C–150 °C | [23, 26, 28] |
| Formate | 2960 (νa,COO+ δCH), 2875 (νCH), 1564 (νa,COO), 1378 (δCH), 1355 (νs,COO) | 50 °C–250 °C | [23, 24, 26] |
| Carbonate | 1573 (νCO), 1311 (νas,OCO), 1285(νas,COO) | 100 °C–300 °C | [19, 29, 30] |
| Water | 3600–3000 (νOH), 1644 (δOH) | -100 °C–300 °C | [19, 23, 27] |

100

Figure S1: XRD patterns of the investigated materials, exclusively containing -Fe2O3.

500

Figure S2: LRS of the investigated materials, exclusively containing -Fe2O3.

Figure S3: Relation of the CH4 conversion at 550 () and 500 °C () (left) and the CH2O conversion at 250 () and 200 °C () with the BET surface areas of the catalysts; the lines are a guide for the eyes.

0

0.25

Figure S4: DRIFT spectra of the Fe25 catalyst after CH2O exposure (50 °C) and subsequent flushing with N2 at 50 °C (―), 100 °C (dashed ―), 150 °C (―), 200 °C (dashed ―) and 250 °C (―). Conditions: y(CH2O) = 500 ppm, y(O2) = 5 vol%, N2 balance, F = 200 ml min-1 (STP).

Figure S5: Gas phase fractions (CH2O (―), CH3OH (―), CO2 (―)) and temperature profile (dashed line) during DRIFTS experiment.

0

0.35

Figure S6: DRIFT spectrum of the Fe25 catalyst after CH2O exposure at -100 °C. Conditions: y(CH2O) = 500 ppm, y(O2) = 5 vol%, N2 balance, F = 200 ml min-1 (STP).

CH2O

CH3OH

C balance

Blank

Figure S7: Step function experiment using the Fe25 catalyst. Conditions: y(CH2O) = 500 ppm, y(O2) = 5 vol%, N2 balance, T = 150 °C, S.V. = 100,000 h-1 (STP).

CH2O

CH3OH

CO2

C balance

Blank

Figure S8: Step function experiment using the Fe25 catalyst. Conditions: y(CH2O) = 500 ppm, y(O2) = 5 vol%, N2 balance, T = 200 °C, S.V. = 100,000 h-1 (STP).