Supplementary material: Characterization of Unmodified and Zinc-modified ZSM-5 Zeolites with Temperature-programmed Desorption of Ammonia and Isopropylamine

Ellen Järvinena,*, Jorge A. Velascoa, Reetta Karinena, Riikka L. Puurunena

aDepartment of Chemical and Metallurgical Engineering, School of Chemical Engineering, Aalto University, P.O. Box 16100, 00076 Aalto, Finland

*Corresponding author: ellen.jarvinen@aalto.fi

# Fusion program for X-ray fluorescence analysis sample preparation

The fusion program used to prepare fused bead analysis samples for the X-ray fluorescence elemental analysis is presented in Table S1.

Table S1. The fusion program used to prepare the X-ray fluorescence analysis samples, where “Rocking angle” and “Speed” are parameters specific to the Katanax X-300 automated fusion instrument

| Step | Temperature | Time | Temperature ramp | Rocking angle | Speed |
| --- | --- | --- | --- | --- | --- |
| 1 | 1050 °C | 2 min | – | 0 ° | 0 % |
| 2 | 1050 °C | 0 min | “Fast” | 0 ° | 0 % |
| 3 | 1050 °C | 6 min | “Fast” | 25 ° | 100 % |
| 4 | 1050 °C | 0 min | “Fast” | 30 ° | 5 % |
| 5 | 1050 °C | 0 min | “Fast” | 30 ° | 5 % |
| 6 | 1050 °C | 3 min | “Fast” | 30 ° | 5 % |
| Pouring | – | – | – | 135 ° | 100 % |
| Cooling, static | – | 1 min | – | 130 ° | 50 % |
| Cooling, flow | – | 5 min | – | 90 ° | 30 % |

# Calibration parameters for the temperature-programmed desorption result quantification

The calibration parameters used in the quantification of the NH3-TPD and IPAm-TPD results are shown in Table S2 and Table S3, respectively

Table S2 NH3-TPD calibration parameters, where Ical is the average area of the integrated peaks and Vcal the

| Analysis | Sample mass (g) | Ical (-) | Vcal (cm3 STP) |
| --- | --- | --- | --- |
| H-ZSM-5-23 | 0.1044 | 7.2895 | 0.0369 |
| H-ZSM-5-50 | 0.1013 | 6.0067 | 0.0368 |
| Zn/H-ZSM-5-50 | 0.0482 | 7.6282 | 0.0367 |
| H-ZSM-5-280 | 0.1019 | 6.4577 | 0.0369 |
| γ-Al2O3 | 0.1036 | 6.2263 | 0.0370 |
| H-ZSM-5-50 (saturation 50 °C) | 0.1012 | 5.7800 | 0.0370 |
| H-ZSM-5-50 (saturation 100 °C) | 0.1022 | 5.7967 | 0.0370 |
| H-ZSM-5-50 (saturation 120 °C) | 0.1020 | 6.8121 | 0.0369 |
| H-ZSM-5-50 (saturation 150 °C) | 0.0993 | 6.7906 | 0.0371 |
| H-ZSM-5-50 (saturation 200 °C) | 0.1025 | 6.1313 | 0.0371 |

Table S3 IPAm-TPD calibration parameters, where k and b are the slope and the intercept of the calibration curve, respectively

| Analysis | Sample mass (g) | k | b |
| --- | --- | --- | --- |
| H-ZSM-5-23 | 0.0991 | 0.00283985 | -0.00591144 |
| H-ZSM-5-50 | 0.1013 | 0.00286686 | -0.00696580 |
| Zn/H-ZSM-5-50 | 0.0511 | 0.00268284 | 0.00107240 |
| H-ZSM-5-280 | 0.1017 | 0.00270677 | -0.00947695 |
| γ-Al2O3 | 0.1007 | 0.00255366 | 0.03102852 |

# Repeatability of the temperature-programmed desorption analyses

Repeatability of the NH3-TPD and IPAm-TPD methods was determined with three repeat analyses of H-ZSM-5-50. The quantitative results as well as their average, standard deciation, and relative standard deviation are presented in Table S4 for NH3-TPD and Table S5 for IPAm-TPD.

Table S4 Results of three repeat NH3-TPD analyses of H-ZSM-5-50

| Repeat | Total acidity (µmol/g) |
| --- | --- |
| 1 | 685 |
| 2 | 695 |
| 3 | 647 |
| Average | 675 |
| Standard deviation | 25 |
| Relative standard deviation | 4 % |

Table S5 Results of tree repeat IPAm-TPD analyses of H-ZSM-5-50

| Repeat | Brønsted acidity (µmol/g) |
| --- | --- |
| 1 | 368 |
| 2 | 400 |
| 3 | 385 |
| Average | 384 |
| Standard deviation | 16 |
| Relative standard deviation | 4 % |

# Curve fitting to the temperature-programmed desorption results at different saturation temperatures

The curve fitting to the NH3-TPD analysis data obtained using the saturation temperatures 50, 100, 120, 150, and 200 °C was performed with the AutoChem software. The resulting plots are presented in Fig. S1–Fig. S5, and details of the fits are included in Table S6–Table S10.

Fig. S1 Gaussian curve fits to the NH3-TPD data obtained with the saturation temperature 50 °C

Table S6 Curve fit details for the NH3-TPD data obtained with the saturation temperature 50 °C

| Peak | Left X | Right X | Peak max. X | Height | Peak area | Res. error | Shape |
| --- | --- | --- | --- | --- | --- | --- | --- |
| 1-1 | 0.13 | 58.85 | 7.71 | 13.04906 | 83.74653 |  | Gaussian |
| 1-2 | 0.13 | 58.85 | 14.80 | 18.47741 | 200.03974 |  | Gaussian |
| 1-3 | 0.13 | 58.85 | 34.15 | 10.89850 | 162.14872 | 3.3593e-02 | Gaussian |

Fig. S2 Gaussian curve fits to the NH3-TPD data obtained with the saturation temperature 100 °C

Table S7 Curve fit details for the NH3-TPD data obtained with the saturation temperature 100 °C

| Peak | Left X | Right X | Peak max. X | Height | Peak area | Res. error | Shape |
| --- | --- | --- | --- | --- | --- | --- | --- |
| 1-1 | 0.35 | 53.92 | 10.84 | 13.98119 | 132.89994 |  | Gaussian |
| 1-2 | 0.35 | 53.92 | 29.12 | 9.84479 | 147.90697 | 4.7995e-02 | Gaussian |

Fig. S3 Gaussian curve fits to the NH3-TPD data obtained with the saturation temperature 120 °C

Table S8 Curve fit details for the NH3-TPD data obtained with the saturation temperature 120 °C

| Peak | Left X | Right X | Peak max. X | Height | Peak area | Res. error | Shape |
| --- | --- | --- | --- | --- | --- | --- | --- |
| 1-1 | 0.48 | 54.18 | 9.51 | 12.13440 | 102.37765 |  | Gaussian |
| 1-2 | 0.48 | 54.18 | 26.77 | 11.17958 | 172.16653 | 5.7309e-02 | Gaussian |

Fig. S4 Gaussian curve fits to the NH3-TPD data obtained with the saturation temperature 150 °C

Table S9 Curve fit details for the NH3-TPD data obtained with the saturation temperature 150 °C

| Peak | Left X | Right X | Peak max. X | Height | Peak area | Res. error | Shape |
| --- | --- | --- | --- | --- | --- | --- | --- |
| 1-1 | 0.27 | 47.66 | 8.45 | 5.58021 | 47.70388 |  | Gaussian |
| 1-2 | 0.27 | 47.66 | 24.00 | 11.34026 | 167.52540 | 6.1646e-02 | Gaussian |

Fig. S5 Gaussian curve fits to the NH3-TPD data obtained with the saturation temperature 200 °C

Table S10 Curve fit details for the NH3-TPD data obtained with the saturation temperature 200 °C

| Peak | Left X | Right X | Peak max. X | Height | Peak area | Res. error | Shape |
| --- | --- | --- | --- | --- | --- | --- | --- |
| 1-1 | 0.36 | 47.76 | 18.73 | 10.21733 | 160.56161 | 6.5606e-02 | Gaussian |