Supplementary Material

Simultaneous voltammetric determination of neurodegenerative biomarkers at nanomolar levels using a Fe3O4 nanoparticle-decorated glassy carbon microsphere nanocomposite

Matheus B. Souza a, Jaqueline S. Santos b, Rafael N. Barros c, Fernanda A. Trenkel d, Leonardo M. S. Gomes d, Luis H. C. Andrade d, Sandro M. Lima d, Antonio R. Fiorucci d, Etenaldo F. Santiago d, Gilberto J. Arruda d *

a Chemistry Postgraduate Program, Analytics Department, São Paulo State University (UNESP), Araraquara, SP, Brazil.

b Genetics Department, Luiz de Queiroz College of Agriculture (ESALQ), University of São Paulo (USP), Piracicaba, SP, Brazil

c Department of Bioprocess Engineering and Biotechnology, Federal University of Paraná (UFPR), Curitiba, PR, Brazil.

d Natural Resources Postgraduate Program, Center for Natural Resources Study (CERNA), Mato Grosso do Sul State University (UEMS), Dourados, MS, Brazil.

*Corresponding author:

Gilberto José de Arruda (arruda@uems.br)

Fig. S1: CVs dataset for A) OGPE, B) GCM/OGPE, C) NaOH/GCM/OGPE and D) Fe3O4/GCM/OGPE electrodes. E) Ip as a function of v1/2. F) enlargement of figure E. a) 25 mV s-1; b) 50 mV s-1; c) 75 mV s-1; d) 100 mV s-1; e) 125 mV s-1; f) 150 mV s-1; g) 175 mV s-1; h) 200 mV s-1. 1 mM ferrocene monocarboxylic acid in 0.5 M KCl.

Fig. S2: (A) CVs and (B) Nyquist plot for OGPE, GCM/OGPE, NaOH/GCM/OGPE, and Fe3O4/GCM/OGPE electrodes. 10 mM ferrocenemonocarboxylic acid in 0.5 M KCl. v = 100 mV s-1.

Table S1: Values obtained for the physicochemical parameters derived from EIS (n = 3).

| Electrodes | ECSA 10-2 cm2 | Cdl 10-6 | Rs Ω | Rct 103 Ω | RF 10-2 | Kº 10-4 cm s-1 | D 10-2 cm2 s-1 | χ² 10-4 |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
| OGPE | 755.4 ± 3.9 | 0.4 ± 0.0 | 48.0 ± 3.9 | 2.1 ± 0.4 | 85.8 ± 1.0 | 1.3 ± 0.0 | 0.6 ± 0.2 | 52.9 |
| GCM/OGPE | 789.9 ± 7.9 | 0.4 ± 0.1 | 53.7 ± 2.6 | 1.0 ± 0.1 | 89.8 ± 0.9 | 3.1 ± 0.0 | 1.0 ± 0.0 | 87.6 |
| NaOH/GCM/OGPE | 763.4 ± 5.0 | 0.3 ± 0.0 | 70.4 ± 1.3 | 1.2 ± 0.1 | 86.8 ± 0.0 | 2.6 ± 0.1 | 1.2 ± 0.0 | 73.0 |
| Fe3O4/GCM/OGPE | 791.0 ± 0.1 | 0.3 ± 0.0 | 44.7 ± 0.7 | 1.4 ± 0.2 | 89.9 ± 1.6 | 2.0 ± 0.1 | 1.2 ± 0.0 | 67.6 |

SD = Standard deviation; Ageometric = 8,8 × 10-2 cm2; RF (Roughness factor) = AElectrochemically /Ageometric.; ECSA = Electrochemically Surface area

Fig. S3: Individual analytical curves for DA, 5-HT and L-Trp with CPE/GC/Fe3O4 electrode. a) DA 0.039 µM, 5-HT and L-Trp 0.078 µM b) DA 0.078 µM 0.156 µM to 5-HT and L-Trp c) DA 0.156 µM, 5-HT and L-Trp 0.312 µM d) DA 0.312 µM, 5-HT and L-Trp 0.625 µM, e) DA 0.625 µM, 5-HT and L-Trp 1.250 µM f) DA 1.250 µM, 5-HT and L-Trp 2.500 µM g) DA 2.500 µM, 5-HT and L-Trp 5.000 µM h) DA 5.000 µM, 5-HT and L-Trp 10.000 µM i) DA 10.000 µM, 5-HT and L-Trp 20.000 µM.

Table S2: Optimization of the instrumental parameters of the pulse application in the SWV.

| Parameter | Range | Optimized |
| --- | --- | --- |
| Step potential (mV) | 1.0 – 15.0 | 7.0 |
| Amplitude (mV) | 10.0 – 70.0 | 40.0 |
| Frequency (Hz) | 2.5 – 10.0 | 7.5 |

Fig. S4: Repeatability, precision, and stability study. A) Ep; B) Ip. [DA] = [5-HT] = [TRP] = 100 nM. [PB] = 0.2 M pH 7.5