Field performance of an innovative downpipe roof runoff treatment system: effect of roof material, stormwater characteristics, and system age on metals removal

Jessika Souza de Carvalho, Ricardo Bello-Mendoza, Aisling O’Sullivan

Supplementary Materials

Section 1: Flow-weighted mean concentrations (FWMC)

Intra-event samples were collected during a single rain event from the galvanised roof (sixteen samples), where Zn is predominantly in dissolved form, and the aluminium roof (nine samples), where Al is mostly in particulate form. Sampling intervals were chosen to capture variations within each rain event. Flow-weighted mean concentrations were calculated following equation S1. This involved weighing the metal concentrations by the volume of runoff during each sampling interval to obtain an average concentration representative of the entire rain event.

FWMC=1n(ci*ti*qi)1n(ti*qi)							Eq. (S1)

Where: ci= concentration in the ith sample; ti= time window for the ith sample, and qi= flow in the ith sample.

A relationship between FWMC and the first flush (FF) was established for each of the two roof types. For the galvanised roof, the FWMC was 1175.3 µg/L, and the FF concentration was 2723.3 µg/L, resulting in an FWMC/FF ratio of 0.43. For the aluminium roof, the FWMC was 130.3 µg/L, and the FF concentration was 1592.7 µg/L, resulting in an FWMC/FF ratio of 0.08. The FWMC/FF ratio from the galvanised roof was used to estimate the FWMC of Cu from the copper roof and Zn from the Zincalume® roof, both metals mostly in dissolved form, from the respective metal FF concentrations. For Al from the Zincalume® roof, the FWMC/FF ratio from the aluminium roof was applied, as both are predominantly in particulate form. The same procedure was applied to the 30 events sampled throughout the study to estimate the FWMC from the measured FF concentrations.

Given that the rain intensities of the two sampled events were 0.9 mm/hr and 2.1 mm/hr, and the average rain intensity of the 30 events is 1.4 mm/hr, it is assumed that these sampled events are representative of the rain event characteristics of the entire study. Mass loadings were subsequently calculated based on FWMC and volume from each rain event (equation S2), with event volumes calculated according to equation S3.

Mass loading=volume x flow weighted mean concentrations		Eq. (S2)

Volume=rain intensity x roof area  x rain duration x roof runoff coefficient 0.95	Eq. (S3)

Section 2: Roof, rainfall and runoff characteristics

Fig. S1. Correlation between inlet concentrations and antecedent dry days (ADD): (a) DCu from copper roof, (n=20); (b) PCu from copper roof, (n=20); (c) DZn from galvanised steel roof, (n=23); and (d) DZn from Zincalume® roof, (n=25).

Table S1: Metal roof characteristics.

|  | Roof material |  |  |  |
| --- | --- | --- | --- | --- |
|  | Aluminium | Galvanised Steel | Copper | Zincalume® |  |
| Primary metal | Aluminium (Al) | Zinc (Zn) | Copper (Cu) | Zinc (Zn) and Aluminium (Al) |  |
| Indicative age (years) | 10 | 5 | 40 | 40 |  |
| Indicative lifespan | 50 - 80 | 40 - 60 | 90 - 150 | 50 - 75 |  |
| Orientation | North | West | North | Southeast |  |
| Contributing run-off area (m2) | 213 | 229 | 51 | 385 |  |

Table S2: Total (sum of dissolved and particulate) Cu, Zn and Al concentrations (mg/L) in roof runoff.

| Roof |  |  |  | Cooper |  |  | Galvanised |  |  | Zincalume® |  |  |  |  |  | Aluminium |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| Metal |  |  |  | Cu |  |  | Zn |  |  | Zn |  |  | Al |  |  | Al |  |  |
| Event | Season | Year | Age of the System (days) | In | Out | Removed (%) | In | Out | Removed (%) | In | Out | Removed (%) | In | Out | Removed (%) | In | Out | Removed (%) |
| 1 | Spring | 2021 | 17 | 3.8 | 0.1 | 96.6 |  |  |  | 1.3 | 0.1 | 93.3 | 0.8 | 0.6 | 24.0 | 2.5 | 0.8 | 66.0 |
| 2 |  |  | 25 | 1.8 | 0.2 | 91.1 | 4.6 | 0.2 | 95.0 | 1.2 | 0.1 | 89.1 | 0.1 | 0.1 | -6.0 | 0.2 | 0.1 | 50.9 |
| 3 |  |  | 32 |  |  |  | 1.5 | 0.2 | 83.5 | 1.1 | 0.3 | 69.4 | 0.1 | 0.1 | 62.9 | 0.1 | 0 | 73.9 |
| 4 | Summer |  | 89 | 1.2 | 0 | 96.1 | 4.1 | 0.5 | 88.3 | 2.4 | 0.3 | 88.4 | 0.1 | 0.1 | -27.1 | 0.5 | 0.3 | 51.3 |
| 5 |  |  | 91 | 1.2 | 0.1 | 89.6 | 1.2 | 0.7 | 36.8 | 0.5 | 0.6 | -22.8 | 0 | 0 | 44.6 | 0 | 0.1 | -115.6 |
| 6 |  | 2022 | 117 | 4.3 | 0.5 | 89.0 | 12.1 | 2.7 | 77.8 | 5.9 | 1.8 | 68.9 | 0.7 | 1.1 | -51.2 | 1.7 | 1.3 | 27.1 |
| 7 |  |  | 124 | 2.8 | 0.4 | 87.3 | 8 | 0.9 | 88.9 | 6 | 0.7 | 89.1 | 0.4 | 0 | 91.7 | 0.3 | 0.1 | 58.4 |
| 8 |  |  | 128 | 1.5 | 0.3 | 82.6 | 2.7 | 0.5 | 80.4 | 1.1 | 0.6 | 48.6 | 0.1 | 0.1 | 47.6 | 1.2 | 0.1 | 95.0 |
| 9 |  |  | 129 |  |  |  | 3.6 | 1 | 72.3 | 0.6 | 0.2 | 61.7 | 0.1 | 0 | 46.7 | 0.0 | 0.0 | -83.5 |
| 10 |  |  | 131 | 1.5 | 0.5 | 65.4 | 3.7 | 1.7 | 54.1 | 1.6 | 0.9 | 44.3 | 0.5 | 0.3 | 28.0 | 0.6 | 0.4 | 31.7 |
| 11 |  |  | 138 | 1.6 | 0.1 | 92.3 | 1.5 | 0.7 | 50.0 | 0.8 | 0.5 | 39.7 | 0.2 | 0.2 | -8.9 | 0.3 | 0.3 | -0.9 |
| 12 |  |  | 140 |  |  |  | 1 | 0.3 | 67.7 | 0.4 | 0.2 | 58.1 | 0 | 0.1 | -59.8 |  |  |  |
| 13 | Autumn |  | 171 |  |  |  | 21.2 | 1.5 | 93.0 | 2.1 | 1.6 | 23.1 | 11.2 | 1.6 | 86.0 | 0.5 | 0 | 92.2 |
| 14 |  |  | 185 | 2.5 | 2.7 | -8.5 | 3.2 | 1.7 | 46.6 | 2.5 | 0.8 | 68.9 | 2.6 | 0.5 | 81.4 | 2.2 | 0.1 | 95.6 |
| 15 |  |  | 233 | 18.9 | 1.1 | 94.3 | 6.8 | 2.3 | 66.2 | 1.5 | 1.5 | -1.7 | 1.7 | 1.6 | 7.4 | 1.1 | 1.7 | -58.2 |
| 16 | Winter |  | 259 | 2.7 | 0.3 | 87.9 |  |  |  | 1.7 | 0.8 | 55.6 | 1.8 | 0.3 | 85.3 | 1.1 | 1.8 | -65.3 |
| 17 |  |  | 293 | 6.2 | 0.5 | 92.4 |  |  |  | 4.4 | 1.3 | 70.6 | 2.8 | 0.3 | 89.8 | 1.3 | 0.4 | 70.0 |
| 18 |  |  | 297 |  |  |  |  |  |  | 4.1 | 1 | 74.8 | 1.5 | 0.4 | 75.9 |  |  |  |
| 19 |  |  | 342 | 3.6 | 0.6 | 82.1 | 2.6 | 1.7 | 34.8 | 3.5 | 1.2 | 66.8 | 0.2 | 0.2 | -5.3 | 0.3 | 0 | 87.8 |
| 20 |  |  | 342 | 7.2 | 1.2 | 83.6 | 2.5 | 2.3 | 7.9 | 3.2 | 1.2 | 61.9 | 0.2 | 0.6 | -155.5 | 0.1 | 0.2 | -22.6 |

Table S2 (Continued): Total (sum of dissolved and particulate) Cu, Zn and Al concentrations (mg/L) in roof runoff.

| Roof |  |  |  | Cooper |  |  | Galvanised |  |  | Zincalume® |  |  |  |  |  | Aluminium |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| Metal |  |  |  | Cu |  |  | Zn |  |  | Zn |  |  | Al |  |  | Al |  |  |
| Event | Season | Year | Age of the System (days) | In | Out | Removed (%) | In | Out | Removed (%) | In | Out | Removed (%) | In | Out | Removed (%) | In | Out | Removed (%) |
| 21 | Spring | 2022 | 354 | 13.1 | 2.5 | 80.9 | 5.1 | 4.8 | 4.9 | 5.7 | 3.1 | 44.8 | 1 | 0.2 | 79.1 | 0.5 | 0.2 | 52.5 |
| 22 |  |  | 359 | 18.8 | 1.5 | 91.9 | 2.5 | 1.5 | 39.5 | 2.4 | 1.8 | 26.0 | 1.1 | 1.9 | -76.3 | 0.5 | 0.1 | 75.2 |
| 23 |  |  | 377 | 5.6 | 1 | 82.3 | 1.4 | 1.5 | -6.7 | 2.3 | 1.1 | 54.0 | 0.9 | 0.1 | 90.1 | 0.2 | 0.1 | 48.4 |
| 24 | Summer |  | 405 | 8.2 | 1.2 | 85.7 | 4.6 | 2.1 | 53.8 | 1.6 | 1.7 | -7.5 | 0.7 | 0.2 | 68.0 | 1.8 | 0.2 | 91.5 |
| 25 |  |  | 455 |  |  |  | 2.9 | 1.7 | 42.1 |  |  |  |  |  |  |  |  |  |
| 26 |  |  | 457 |  |  |  | 2.4 | 0.9 | 63.1 |  |  |  |  |  |  |  |  |  |
| 27 |  | 2023 | 477 |  |  |  | 14.6 | 2.4 | 83.4 | 3.5 | 5.4 | -53.4 |  |  |  | 7.9 | 6.8 | 12.8 |
| 28 |  |  | 514 | 3.3 | 1.4 | 58.4 | 3.4 | 2.4 | 30.0 |  |  |  |  |  |  | 0.4 | 1.5 | -297.0 |
| 29 |  |  | 515 | 2.9 | 0.9 | 70.4 | 3.5 | 1 | 72.4 | 2.7 | 1.3 | 52.8 | 0.5 | 0.7 | -41.1 | 0.2 | 0.5 | -189.7 |
| 30 | Autumn |  | 542 | 5.1 | 1.2 | 77.0 | 2.7 | 1.7 | 37.2 |  |  |  | 0.2 | 0.2 | 32.5 | 2 | 2 | 1.3 |
| Mean ± Standard deviation |  |  |  | 5.2 ± 5.1 | 0.8 ± 0.7 | 80.4 ± 22.1 | 4.8 ± 4.6 | 1.5 ± 0.9 | 56.3 ± 28.1 | 2.4 ± 1.6 | 1.2 ± 1.2 | 48.6 ± 36.1 | 1.1 ± 2.1 | 1.1 ± 2.8 | 23.4 ± 63.2 | 1.1 ± 1.6 | 0.7 ± 1.4 | 9.6 ± 95.7 |
| Coefficient of variation (CV) |  |  |  | 0.9 | 0.9 | 0.3 | 0.9 | 0.7 | 0.5 | 0.7 | 1.0 | 0.7 | 1.9 | 1.2 | 2.7 | 1.5 | 1.9 | 10 |

Table S3: Total, dissolved and particulate Al, Cu and Zn inlet concentrations (µg/L) from each roof type.

|  | Total Al Concentrations |  |  |  | Dissolved Al Concentrations |  |  |  | Particulate Al Concentrations |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  | Copper | Galvanised | Zincalume | Aluminium | Copper | Galvanised | Zincalume | Aluminium | Copper | Galvanised | Zincalume | Aluminium |
| Avg | 6537.9 | 5838.4 | 1141.7 | 1100.3 | 7.8 | 43.2 | 99.9 | 53.6 | 6530.1 | 5802.8 | 1041.9 | 1046.7 |
| Min | 101.7 | 322.7 | 35.3 | 40.4 | 0.6 | 8.1 | 22.9 | 12.3 | 99.3 | 283.0 | 6.4 | 26.8 |
| Max | 35391.8 | 52693.5 | 11237.8 | 7853.4 | 16.0 | 187.0 | 345.6 | 370.5 | 35376.8 | 52586.9 | 10985.5 | 7482.9 |
| Med | 3295.4 | 2714.7 | 486.3 | 488.6 | 8.5 | 25.4 | 89.4 | 32.6 | 3286.6 | 2651.1 | 394.3 | 440.2 |
| St D | 8976.0 | 10438.4 | 2202.0 | 1582.3 | 4.6 | 40.5 | 75.3 | 71.4 | 8974.6 | 10426.9 | 2168.9 | 1517.7 |
|  | Total Cu Concentrations |  |  |  | Dissolved Cu Concentrations |  |  |  | Particulate Cu Concentrations |  |  |  |
|  | Copper | Galvanised | Zincalume | Aluminium | Copper | Galvanised | Zincalume | Aluminium | Copper | Galvanised | Zincalume | Aluminium |
| Avg | 5346.4 | 34.4 | 25.1 | 16.9 | 2420.2 | 12.3 | 13.8 | 10.2 | 2926.1 | 22.2 | 11.3 | 6.7 |
| Min | 1161.8 | 5.5 | 3.9 | 3.3 | 960.6 | 2.8 | 2.3 | 2.1 | 87.0 | 0.0 | 0.0 | 0.0 |
| Max | 18904.8 | 192.2 | 99.6 | 34.7 | 7415.9 | 31.2 | 39.5 | 26.5 | 14807.4 | 187.0 | 75.6 | 19.6 |
| Med | 3432.3 | 23.8 | 21.9 | 15.8 | 1857.6 | 10.8 | 14.6 | 7.3 | 1065.9 | 12.2 | 6.1 | 4.3 |
| St D | 5189.8 | 38.0 | 20.9 | 9.1 | 1592.4 | 8.1 | 9.4 | 7.0 | 4010.0 | 39.2 | 16.0 | 6.5 |
|  | Total Zn Concentrations |  |  |  | Dissolved Zn Concentrations |  |  |  | Particulate Zn Concentrations |  |  |  |
|  | Copper | Galvanised | Zincalume | Aluminium | Copper | Galvanised | Zincalume | Aluminium | Copper | Galvanised | Zincalume | Aluminium |
| Avg | 188.47 | 4754.05 | 2462.28 | 941.29 | 106.44 | 3605.86 | 2422.44 | 929.26 | 79.28 | 1141.26 | 39.84 | 12.04 |
| Min | 46.30 | 997.13 | 425.73 | 382.67 | 39.99 | 949.82 | 363.69 | 295.45 | 0.00 | 0.00 | 0.00 | 0.00 |
| Max | 649.22 | 21249.91 | 6029.07 | 1908.35 | 184.41 | 13548.79 | 6029.07 | 1908.35 | 492.59 | 9491.17 | 401.12 | 104.09 |
| Med | 131.90 | 3324.81 | 2205.63 | 843.78 | 104.71 | 2724.19 | 2137.30 | 820.65 | 26.40 | 213.62 | 0.00 | 0.00 |
| St D | 149.16 | 4642.51 | 1665.88 | 462.25 | 44.98 | 2997.80 | 1688.44 | 463.55 | 130.95 | 2518.18 | 90.87 | 30.11 |

Table S4: Volume, flow-weighted mean concentrations, and total mass loading from each roof type.

| Roof | Copper Roof |  |  | Galvanised Roof |  |  | Zincalume Roof - Zn |  |  | Zincalume Roof - Al |  |  | Aluminium Roof |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| Event | Volume (L) | FWMC (µg/L) | Mass loading (g) | Volume (L) | FWMC (µg/L) | Mass loading (g) | Volume (L) | FWMC (µg/L) | Mass loading (g) | Volume (L) | FWMC (µg/L) | Mass loading (g) | Volume (L) | FWMC (µg/L) | Mass loading (g) |  |
| 1 | 1230.6 | 1652.7 | 2.0 |  |  |  | 9290.1 | 565.0 | 5.2 | 9290.1 | 64.8 | 0.6 | 5125.2 | 196.2 | 1.0 |  |
| 2 | 1056.2 | 754.2 | 0.8 | 4742.6 | 1979.9 | 9.4 | 7973.4 | 499.4 | 4.0 | 7973.4 | 5.6 | 0.0 | 4398.8 | 19.3 | 0.1 |  |
| 3 |  |  |  | 87.0 | 650.6 | 0.1 | 146.3 | 453.4 | 0.1 | 146.3 | 11.5 | 0.0 | 80.7 | 11.9 | 0.0 |  |
| 4 | 4980.7 | 499.6 | 2.5 | 22364.1 | 1787.8 | 40.0 | 37599.1 | 1055.2 | 39.7 | 37599.1 | 9.1 | 0.3 | 20743.0 | 42.3 | 0.9 |  |
| 5 | 319.8 | 511.9 | 0.2 | 1435.8 | 502.2 | 0.7 | 2414.0 | 197.7 | 0.5 | 2414.0 | 2.8 | 0.0 | 1331.7 | 3.2 | 0.0 |  |
| 6 | 67.8 | 1830.4 | 0.1 | 304.6 | 5216.0 | 1.6 | 512.1 | 2553.0 | 1.3 | 512.1 | 56.1 | 0.0 | 282.5 | 138.4 | 0.0 |  |
| 7 | 533.0 | 1193.2 | 0.6 | 2393.1 | 3451.8 | 8.3 | 4023.3 | 2602.0 | 10.5 | 4023.3 | 31.0 | 0.1 | 2219.6 | 21.2 | 0.0 |  |
| 8 | 174.4 | 653.3 | 0.1 | 783.2 | 1178.7 | 0.9 | 1316.7 | 465.6 | 0.6 | 1316.7 | 10.0 | 0.0 | 726.4 | 92.7 | 0.1 |  |
| 9 |  |  |  | 130.5 | 1572.8 | 0.2 | 219.5 | 243.1 | 0.1 | 219.5 | 4.2 | 0.0 |  |  |  |  |
| 10 | 484.5 | 664.9 | 0.3 | 2175.5 | 1582.9 | 3.4 | 3657.5 | 685.2 | 2.5 | 3657.5 | 38.5 | 0.1 | 2017.8 | 48.8 | 0.1 |  |
| 11 | 38.8 | 678.5 | 0.0 | 174.0 | 631.3 | 0.1 | 292.6 | 326.5 | 0.1 | 292.6 | 16.1 | 0.0 | 161.4 | 25.2 | 0.0 |  |
| 12 |  |  |  | 7179.2 | 430.3 | 3.1 | 12069.8 | 183.7 | 2.2 | 12069.8 | 3.9 | 0.0 |  |  |  |  |
| 13 |  |  |  | 52.2 | 9171.0 | 0.5 | 87.8 | 914.4 | 0.1 | 87.8 | 899.0 | 0.1 | 48.4 | 38.1 | 0.0 |  |
| 14 | 1915.9 | 1056.9 | 2.0 | 8602.9 | 1380.9 | 11.9 | 14463.4 | 1078.1 | 15.6 | 14463.4 | 209.3 | 3.0 | 7979.3 | 175.4 | 1.4 |  |
| 15 | 48.5 | 8129.0 | 0.4 | 217.6 | 2948.1 | 0.6 | 365.8 | 647.3 | 0.2 | 365.8 | 135.0 | 0.0 | 201.8 | 87.9 | 0.0 |  |
| 16 | 474.8 | 1177.0 | 0.6 |  |  |  | 3584.4 | 736.6 | 2.6 | 3584.4 | 145.0 | 0.5 | 1977.4 | 88.7 | 0.2 |  |
| 17 | 862.4 | 2654.1 | 2.3 |  |  |  | 6510.4 | 1909.1 | 12.4 | 6510.4 | 227.5 | 1.5 | 3591.7 | 100.6 | 0.4 |  |
| 18 |  |  |  |  |  |  | 26553.5 | 1789.9 | 47.5 | 26553.5 | 118.3 | 3.1 |  |  |  |  |
| 19 | 38.8 | 1553.2 | 0.1 | 174.0 | 1105.4 | 0.2 | 292.6 | 1499.1 | 0.4 | 292.6 | 12.4 | 0.0 | 161.4 | 27.1 | 0.0 |  |
| 20 | 96.9 | 3076.0 | 0.3 | 435.1 | 1065.0 | 0.5 | 731.5 | 1361.4 | 1.0 | 731.5 | 17.8 | 0.0 | 403.6 | 11.6 | 0.0 |  |
| 21 | 203.5 | 5632.1 | 1.1 | 913.7 | 2199.3 | 2.0 | 1536.2 | 2462.7 | 3.8 | 1536.2 | 81.0 | 0.1 | 847.5 | 39.1 | 0.0 |  |
| 22 | 67.8 | 8074.4 | 0.5 | 304.6 | 1086.5 | 0.3 | 512.1 | 1044.3 | 0.5 | 512.1 | 86.5 | 0.0 | 282.5 | 36.2 | 0.0 |  |
| 23 | 106.6 | 2427.1 | 0.3 | 478.6 | 622.4 | 0.3 | 804.7 | 989.4 | 0.8 | 804.7 | 73.7 | 0.1 | 443.9 | 12.4 | 0.0 |  |
| Table S4 (Continued): Volume, flow-weighted mean concentrations, and total mass loading from each roof type. Roof; Copper Roof; Galvanised Roof; Zincalume Roof - Zn; Zincalume Roof - Al; Aluminium Roof. Event; Volume (L); FWMC (µg/L); Mass loading (g); Volume (L); FWMC (µg/L); Mass loading (g); Volume (L); FWMC (µg/L); Mass loading (g); Volume (L); FWMC (µg/L); Mass loading (g); Volume (L); FWMC (µg/L); Mass loading (g). 24; 387.6; 3505.0; 1.4; 1740.4; 1989.3; 3.5; 2926.0; 678.7; 2.0; 2926.0; 58.0; 0.2; 1614.2; 147.9; 0.2. 25; 174.0; 1248.1; 0.2. 26; 3959.4; 1032.9; 4.1. 27; 2915.2; 6322.4; 18.4; 4901.1; 1523.6; 7.5; 2703.9; 628.3; 1.7. 28; 23.3; 1398.6; 0.0; 104.4; 1488.9; 0.2; 96.9; 30.7; 0.0. 29; 1694.8; 1267.8; 2.1; 7609.9; 1525.7; 11.6; 12793.9; 1165.0; 14.9; 12793.9; 39.3; 0.5; 7058.3; 13.9; 0.1. 30; 715.4; 2186.5; 1.6; 3212.3; 1175.3; 3.8; 5400.7; 18.3; 0.1; 2979.5; 163.4; 0.5. SUM; 19.4; 125.8; 176.1; 10.7; 6.8. |

Table S5: Rainfall characteristics from sampled events

| Event | Season | Rain Event Date |  | Age System (days) | Rain Depth (mm) | Average Intensity (mm/hr) | Peak Intensity (mm/hr) | ADD (days) | Duration (hr) |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  |  | Year | Date | 17/09/2021 | UC Weather Station |  |  |  |  |
| 1 | Spring | 2021 | 04th October | 17 | 25.4 | 1.2 | 4.8 | 4.0 | 22.1 |
| 2 |  |  | 12th October | 25 | 21.8 | 1.3 | 9.6 | 0.4 | 16.7 |
| 3 |  |  | 19th October | 32 | 0.4 | 0.2 | 2.4 | 0.4 | 2.3 |
|  |  |  |  |  | 15.9 ± 13.51 | 0.9 ± 0.62 | 5.6 ± 3.67 | 1.6 ± 2.09 | 13.7 ± 10.20 |
| 4 | Summer | 2021 | 15th December | 89 | 102.8 | 2.8 | 16.8 | 3.1 | 36.6 |
| 5 |  |  | 17th December | 91 | 6.6 | 1.1 | 9.6 | 0.4 | 6.1 |
|  |  |  |  |  | 54.7 ± 68 | 1.9 ± 1.2 | 13.2 ± 5.1 | 1.8 ± 1.9 | 21.3 ± 21.6 |
| 6 | Summer | 2022 | 12th January | 117 | 1.4 | 8.4 | 12.0 | 6.4 | 0.2 |
| 7 |  |  | 19th January | 124 | 11.0 | 0.9 | 9.6 | 7.0 | 11.8 |
| 8 |  |  | 23rd January | 128 | 3.6 | 0.6 | 4.8 | 2.9 | 6.3 |
| 9 |  |  | 24th January | 129 | 0.6 | 0.1 | 2.4 | 0.5 | 6.6 |
| 10 |  |  | 26th January | 131 | 10.0 | 1.2 | 9.6 | 0.5 | 8.3 |
| 11 |  |  | 02nd February | 138 | 0.8 | 0.7 | 2.4 | 0.4 | 1.1 |
| 12 |  |  | 04th February | 140 | 37.6 | 0.9 | 7.2 | 0.3 | 34.7 |
|  |  |  |  |  | 9.3 ± 13.2 | 1.8 ± 2.9 | 6.9 ± 3.8 | 2.6 ± 3 | 9.9 ± 11.7 |
| 13 | Autumn | 2022 | 07th March | 171 | 0.2 | 1.2 | 2.4 | 5.2 | 0.2 |
| 14 |  |  | 21st March | 185 | 39.6 | 1.7 | 19.2 | 4.6 | 23.8 |
| 15 |  |  | 08th May | 233 | 1.0 | 2.0 | 7.2 | 2.2 | 0.5 |
|  |  |  |  |  | 13.6 ± 22.5 | 1.6 ± 0.4 | 9.6 ± 8.7 | 4 ± 1.6 | 8.2 ± 13.5 |
| 16 | Winter | 2022 | 03rd June | 259 | 9.8 | 2.9 | 14.4 | 1.7 | 3.4 |
| 17 |  |  | 07th June | 293 | 17.8 | 0.9 | 7.2 | 6.6 | 18.9 |
| 18 |  |  | 11st July | 297 | 72.6 | 3.4 | 9.6 | 2.0 | 21.5 |
| 19 |  |  | 25th August | 342 | 0.8 | 0.6 | 9.6 | 3.1 | 1.3 |
| 20 |  |  | 25th August | 342 | 2.0 | 0.4 | 9.6 | 0.7 | 5.3 |
|  |  |  |  |  | 19.4 ± 26.9 | 1.5 ± 1.3 | 9.2 ± 3.2 | 3.3 ± 2.3 | 10.9 ± 8.6 |
| 21 | Spring | 2022 | 06th September | 354 | 4.2 | 0.4 | 9.6 | 11.1 | 9.7 |
| 22 |  |  | 11st Setember | 359 | 1.4 | 1.7 | 9.6 | 5.2 | 0.8 |
| 23 |  |  | 29th Setember | 377 | 2.2 | 0.2 | 9.6 | 1.3 | 9.8 |
|  |  |  |  |  | 2.6 ± 1.4 | 0.8 ± 0.8 | 9.6 ± 0 | 5.8 ± 4.9 | 6.8 ± 5.1 |
| 24 | Summer | 2022 | 27th October | 405 | 8 | 0.6 | 2.4 | 8.8 | 13.8 |
| 25 |  |  | 16th December | 455 | 0.8 | 0.6 | 2.4 | 1.0 | 1.4 |
| 26 |  |  | 18th December | 457 | 18.2 | 0.7 | 7.2 | 1.7 | 28.0 |
| 27 | Summer | 2023 | 07th January | 477 | 13.4 | 1.2 | 26.4 | 10.5 | 11.0 |
| 28 |  |  | 14th February | 514 | 0.4 | 1.6 | 2.4 | 2.9 | 0.3 |
| 29 |  |  | 15th February | 515 | 35 | 1.1 | 28.8 | 0.6 | 33.0 |
|  |  |  |  |  | 12.6 ± 13 | 0.9 ± 0.4 | 11.6 ± 12.6 | 4.2 ± 4.3 | 14.6 ± 13.5 |
| 30 | Autumn | 2023 | 13th March | 542 | 14.8 | 2.1 | 9.6 | 3.8 | 6.9 |

*Rainfall characteristics: rain event is defined as any rain depth >=0.2mm within a 6hr period; rain depth is the total depth recorded during a rain event; duration is the time from the first record of rain to the last, culminating with 6 hrs with no record of rain; antecedent dry days (ADD) are the days since the previous qualified rain event; average intensity is the rainfall depth divided by event duration; peak intensity (5min) is the peak rain depth recorded during 5-min interval; bold: average ± standard deviation.

Table S6: Total, dissolved and particulate Al, Cu and Zn concentrations removal efficiency (%) from each roof type.

|  | Total Al Removal Efficiency |  |  |  | Dissolved Al Removal Efficiency |  |  |  | Particulate Al Removal Efficiency |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  | Copper | Galvanised | Zincalume | Aluminium | Copper | Galvanised | Zincalume | Aluminium | Copper | Galvanised | Zincalume | Aluminium |
| Avg | 79.2 | 67.7 | 23.4 | 13.3 | -14.5 | 44.3 | 59.6 | 31.2 | 79.5 | 73.5 | -3.8 | 8.0 |
| Min | -86.4 | -18.0 | -155.5 | -297.0 | -619.3 | -30.8 | -45.6 | -55.8 | -86.7 | -6.7 | -199.0 | -321.3 |
| Max | 99.8 | 99.3 | 91.7 | 95.6 | 85.8 | 89.4 | 96.2 | 80.4 | 99.8 | 100.0 | 91.8 | 99.1 |
| Med | 94.1 | 79.1 | 38.5 | 50.9 | 31.0 | 50.0 | 68.3 | 36.9 | 94.3 | 81.6 | 20.7 | 50.4 |
| St Dev | 41.1 | 30.7 | 63.2 | 95.8 | 151.7 | 36.0 | 30.0 | 39.8 | 41.1 | 26.9 | 88.6 | 108.0 |
|  | Total Cu Removal Efficiency |  |  |  | Dissolved Cu Removal Efficiency |  |  |  | Particulate Cu Removal Efficiency |  |  |  |
|  | Copper | Galvanised | Zincalume | Aluminium | Copper | Galvanised | Zincalume | Aluminium | Copper | Galvanised | Zincalume | Aluminium |
| Avg | 80.4 | 56.8 | 43.0 | 21.1 | 77.9 | 33.3 | 40.2 | 14.3 | 75.5 | 37.4 | 41.2 | 5.5 |
| Min | -8.5 | 14.6 | -171.0 | -158.8 | 55.1 | -78.5 | -133.4 | -245.0 | -117.1 | -524.5 | -452.5 | -249.8 |
| Max | 96.6 | 100.0 | 95.0 | 83.6 | 96.9 | 68.6 | 95.0 | 83.6 | 100.0 | 100.0 | 100.0 | 100.0 |
| Med | 86.5 | 58.1 | 58.5 | 31.7 | 81.4 | 46.3 | 45.9 | 34.0 | 94.7 | 80.0 | 83.9 | 83.9 |
| St Dev | 22.1 | 23.4 | 62.4 | 64.0 | 12.8 | 33.9 | 42.8 | 70.5 | 48.0 | 130.8 | 119.1 | 119.4 |
|  | Total Zn Removal Efficiency |  |  |  | Dissolved Zn Removal Efficiency |  |  |  | Particulate Zn Removal Efficiency |  |  |  |
|  | Copper | Galvanised | Zincalume | Aluminium | Copper | Galvanised | Zincalume | Aluminium | Copper | Galvanised | Zincalume | Aluminium |
| Avg | 44.4 | 56.3 | 48.6 | 92.0 | 31.0 | 51.2 | 53.2 | 95.7 | 58.0 | 75.4 | -3.6 | -3.9 |
| Min | -162.2 | -6.7 | -53.4 | 67.0 | -162.2 | -4.9 | -44.3 | 77.0 | -186.4 | -96.9 | -220.2 | -396.9 |
| Max | 91.6 | 95.0 | 93.3 | 99.3 | 93.2 | 95.5 | 95.5 | 99.5 | 100.0 | 100.0 | 100.0 | 100.0 |
| Med | 66.2 | 58.6 | 56.8 | 96.1 | 58.7 | 49.0 | 58.4 | 97.4 | 100.0 | 92.7 | 91.3 | 94.8 |
| St Dev | 60.9 | 28.1 | 36.1 | 8.8 | 70.0 | 30.1 | 31.7 | 4.9 | 95.5 | 48.5 | 140.3 | 219.8 |