Roadmap to sustainable plastic waste management: a focused study on recycling PET for triboelectric nanogenerator production in Singapore and India

Wei Liang Lai, Shreya Sharma, Sunanda Roy, Pradip Kumar Maji, Bhasha Sharma, Seeram Ramakrishna, Kheng Lim Goh

Supplementary Section 1: Economic values of PET plastic.

Table S-1. Details used to derive and calculate for the recyclate value of PET plastic.

| Region | No. of times recycled? | Currency | Estimated economic value, RVi-1 | Retained mechanical performance factor, m |  | Reclaimed recyclate, rp | Recycling cost, P (USD) | Recyclate value, RVi (USD) | Reference of mechanical performance |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  |  |  | (USD/mt) | (0 ≤ m < 1) |  |  |  |  |  |
|  |  |  |  | Rupture strain (%) | Factor | (0 ≤ rp < 1) |  |  |  |
| Enlongation at break (%), eB |  |  |  |  |  |  |  |  |  |
| South-East Asia (Singapore) | 0 | USD | 1341 | 42 | 1.000 | 1 | 50 | 1291.00 | Del Mar Castro López M, Ares Pernas AI, Abad López MJ, Latorre AL, López Vilariño JM, González Rodríguez MV. Assessing changes on poly(ethylene terephthalate) properties after recycling: Mechanical recycling in laboratory versus postconsumer recycled material. Mater Chem Phys 2014;147:884–94. https://doi.org/10.1016/j.matchemphys.2014.06.034. |
|  | 1 |  | 610 | 35 | 0.833 | 0.97 |  | 443.08 |  |
|  | 2 |  | 427 | 5.7 | 0.136 | 0.94 |  | 4.47 |  |
|  | 3 |  | 299 | 2.6 | 0.062 | 0.91 |  | -33.16 |  |
|  | 4 |  | 209 | 1.6 | 0.038 | 0.88 |  | -42.99 |  |
|  | 5 |  | 146 | 0.7 | 0.017 | 0.85 |  | -47.93 |  |
| South Asia (India) | 0 | USD | 1090 | 42 | 1.000 | 1 | 50 | 1040.00 | Del Mar Castro López M, Ares Pernas AI, Abad López MJ, Latorre AL, López Vilariño JM, González Rodríguez MV. Assessing changes on poly(ethylene terephthalate) properties after recycling: Mechanical recycling in laboratory versus postconsumer recycled material. Mater Chem Phys 2014;147:884–94. https://doi.org/10.1016/j.matchemphys.2014.06.034. |
|  | 1 |  | 680 | 35 | 0.833 | 0.97 |  | 499.67 |  |
|  | 2 |  | 476 | 5.7 | 0.136 | 0.94 |  | 10.72 |  |
|  | 3 |  | 333 | 2.6 | 0.062 | 0.91 |  | -31.24 |  |
|  | 4 |  | 233 | 1.6 | 0.038 | 0.88 |  | -42.19 |  |
|  | 5 |  | 163 | 0.7 | 0.017 | 0.85 |  | -47.69 |  |
| Impact strength (kJ/m2) , acU |  |  |  |  |  |  |  |  |  |
| South-East Asia (Singapore) | 0 | USD | 1341 | 135 | 1.000 | 1 | 50 | 1291.00 | Del Mar Castro López M, Ares Pernas AI, Abad López MJ, Latorre AL, López Vilariño JM, González Rodríguez MV. Assessing changes on poly(ethylene terephthalate) properties after recycling: Mechanical recycling in laboratory versus postconsumer recycled material. Mater Chem Phys 2014;147:884–94. https://doi.org/10.1016/j.matchemphys.2014.06.034. |
|  | 1 |  | 610 | 71 | 0.526 | 0.97 |  | 261.19 |  |
|  | 2 |  | 427 | 25 | 0.185 | 0.94 |  | 24.33 |  |
|  | 3 |  | 299 | 16 | 0.119 | 0.91 |  | -17.75 |  |
|  | 4 |  | 209 | 6 | 0.044 | 0.88 |  | -41.83 |  |
|  | 5 |  | 146 | 6 | 0.044 | 0.85 |  | -44.48 |  |
| South Asia (India) | 0 | USD | 1090 | 135 | 1.000 | 1 | 50 | 1040.00 | Del Mar Castro López M, Ares Pernas AI, Abad López MJ, Latorre AL, López Vilariño JM, González Rodríguez MV. Assessing changes on poly(ethylene terephthalate) properties after recycling: Mechanical recycling in laboratory versus postconsumer recycled material. Mater Chem Phys 2014;147:884–94. https://doi.org/10.1016/j.matchemphys.2014.06.034. |
|  | 1 |  | 680 | 71 | 0.526 | 0.97 |  | 296.90 |  |
|  | 2 |  | 476 | 25 | 0.185 | 0.94 |  | 32.86 |  |
|  | 3 |  | 333 | 16 | 0.119 | 0.91 |  | -14.09 |  |
|  | 4 |  | 233 | 6 | 0.044 | 0.88 |  | -40.89 |  |
|  | 5 |  | 163 | 6 | 0.044 | 0.85 |  | -43.84 |  |
| Viscosity (Pa.s), h |  |  |  |  |  |  |  |  |  |
| South-East Asia (Singapore) | 0 | USD | 1341 | 350 | 1.000 | 1 | 50 | 1291.00 | Schyns ZOG, Shaver MP. Mechanical Recycling of Packaging Plastics: A Review. Macromol Rapid Commun 2021;42:1–27. https://doi.org/10.1002/marc.202000415. La Mantia FP, Vinci M. Recycling poly(ethyleneterephthalate). Polym Degrad Stab 1994;45:121–5. https://doi.org/10.1016/0141-3910(94)90187-2. |
|  | 1 |  | 610 | 300 | 0.857 | 0.97 |  | 457.17 |  |
|  | 2 |  | 427 | 180 | 0.514 | 0.94 |  | 156.42 |  |
|  | 3 |  | 299 | 150 | 0.429 | 0.91 |  | 66.61 |  |
|  | 4 |  | 209 | 130 | 0.371 | 0.88 |  | 18.31 |  |
|  | 5 |  | 146 | 110 | 0.314 | 0.85 |  | -11.00 |  |
| South Asia (India) | 0 | USD | 1090 | 350 | 1.000 | 1 | 50 | 1040.00 |  |
|  | 1 |  | 680 | 300 | 0.857 | 0.97 |  | 515.37 |  |
|  | 2 |  | 476 | 180 | 0.514 | 0.94 |  | 180.11 |  |
|  | 3 |  | 333 | 150 | 0.429 | 0.91 |  | 79.87 |  |
|  | 4 |  | 233 | 130 | 0.371 | 0.88 |  | 26.16 |  |
|  | 5 |  | 163 | 110 | 0.314 | 0.85 |  | -6.46 |  |
| Degree of crystallinity (%), D |  |  |  |  |  |  |  |  |  |
| South-East Asia (Singapore) | 0 | USD | 1341 | 21.5 | 1.000 | 1 | 50 | 1291.00 | Schyns ZOG, Shaver MP. Mechanical Recycling of Packaging Plastics: A Review. Macromol Rapid Commun 2021;42:1–27. https://doi.org/10.1002/marc.202000415. La Mantia FP, Vinci M. Recycling poly(ethyleneterephthalate). Polym Degrad Stab 1994;45:121–5. https://doi.org/10.1016/0141-3910(94)90187-2. |
|  | 1 |  | 610 | 21.8 | 1.014 | 0.97 |  | 549.96 |  |
|  | 2 |  | 427 | 23 | 1.070 | 0.94 |  | 379.38 |  |
|  | 3 |  | 299 | 24 | 1.116 | 0.91 |  | 253.73 |  |
|  | 4 |  | 209 | 24.5 | 1.140 | 0.88 |  | 159.58 |  |
|  | 5 |  | 146 | 25.2 | 1.172 | 0.85 |  | 95.46 |  |
| South Asia (India) | 0 | USD | 1090 | 21.5 | 1.000 | 1 | 50 | 1040.00 |  |
|  | 1 |  | 680 | 21.8 | 1.014 | 0.97 |  | 618.80 |  |
|  | 2 |  | 476 | 23 | 1.070 | 0.94 |  | 428.66 |  |
|  | 3 |  | 333 | 24 | 1.116 | 0.91 |  | 288.27 |  |
|  | 4 |  | 233 | 24.5 | 1.140 | 0.88 |  | 183.65 |  |
|  | 5 |  | 163 | 25.2 | 1.172 | 0.85 |  | 112.39 |  |