Excess secondary sludge reuse: H2O2 treatment - thermal adsorbent synthesis

Ana Udaondo1,2, Vicente Montes*,2, Olga Gimeno1, Francisco Javier Rivas1

1 Department of Chemical Engineering and Physical Chemistry, university institute of water, climate change and sustainability, University of Extremadura, Badajoz, Spain

2 Department of Organic and Inorganic Chemistry, university institute of water, climate change and sustainability, University of Extremadura, Badajoz, Spain

SUPLEMENTARY INFORMATION

Fig. S1. Reactor used in the H2O2 treatment of secondary sludge.

Fig. S2. Thermal sewage sludge treatment in the presence of hydrogen peroxide. Influence of temperature on the final concentration of up: Proteins. Middle: Soluble Chemical oxygen demand (s-COD). Bottom: Soluble Total Organic Carbon (s-TOC)

Fig. S3. Thermal sewage sludge treatment in the presence of hydrogen peroxide. Linear correlation between proteins and COD extracellular polymeric substances with sludge volumetric index after 30 min. ▲, s-EPS ●, l-EPS

Table S1. Elemental and XRF analysis pf synthetized adsorbents. Data in weight percentage

|  | C | H | N | P | Fe | Al | Si | Ca | Mg | Ni |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| DS | 29.7 | 3.96 | 2.93 | 4.49 | 4.34 | 3.87 | 3.35 | 2.29 | 1.00 | - |
| S400 | 25.9 | 2.03 | 2.11 | 4.65 | 4.24 | 4.17 | 3.90 | 2.41 | 1.23 | 0.02 |
| S700 | 15.2 | 0.06 | 0.36 | 7.20 | 7.44 | 6.87 | 5.54 | 3.84 | 1.91 | - |
| SKOH | 6.5 | 1.96 | - | 1.15 | 8.44 | 6.62 | 8.30 | 5.04 | 2.46 | - |
| SNN | 10.1 | 0.18 | 1.19 | 6.36 | 7.27 | 5.79 | 5.87 | 3.46 | 1.51 | 0.02 |
|  | K | S | Ti | Cl | Zn | Mn | Cu | Sr | Cr |  |
| DS | 0.58 | 0.49 | 0.21 | 0.10 | 0.07 | 0.06 | 0.03 | 0.01 | - |  |
| S400 | 0.64 | 0.18 | 0.19 | - | 0.06 | 0.06 | 0.02 | 0.004 | 0.02 |  |
| S700 | 0.87 | 0.24 | 0.29 | - | 0.09 | 0.10 | 0.05 | 0.02 | 0.03 |  |
| SKOH | 2.27 | 0.34 | 0.39 | - | 0.08 | 0.11 | 0.09 | 0.02 | 0.04 |  |
| SNN | 1.06 | 0.10 | 0.31 | - | 0.13 | 0.07 | 0.05 | 0.02 | 0.02 |  |

DS=Dehydrated sludge