Enhanced adsorption of phenolic compounds using biomass-derived high surface area activated carbon: Isotherms, Kinetics and Thermodynamics

Praveengouda Patil1, Gautham Jeppu1, Manjunath Singanodi Vallabha2, Chikmagalur Raju Girish1*

1Department of Chemical Engineering, Manipal Institute of Technology,

Manipal Academy of Higher Education, Manipal-576104, Karnataka, India

2Department of Civil Engineering, BMS College of Engineering, Bengaluru-560019, India

*Corresponding author email id: cr.girish@manipal.edu

# SUPPLEMENTARY FILE

List of Tables

# Table S1. Impacts of phenolic compounds on human being.

# Table S2. List of Isotherms used in the present investigation.

# Table S3. Kinetic models: linear and non-linear forms.

# Table S4. Proximate and Ultimate analysis.

# Table S5. Elemental composition before and after adsorption from EDS.

# Table S6. Optimum operational conditions for isotherm studies.

# Table S7. Thermodynamic parameters for adsorption of Phenol and 2,4-DCP on CFPAC.

# Table S8. Isosteric heat of adsorption parameters for phenol and 2,4-DCP.

# Table S9. Cost analysis for preparation of CFPAC.

# Table S1. Impacts of phenolic compounds on human being.

| Exposure | Hazards |
| --- | --- |
| Inhalation | Irritation in respiratory system |
| Oral | Fatal death |
| Eyes | Severe damage and blindness |
| Skin | Irritation and corrosive damage to skin, burns are developed on skin |
| Chronic exposure | Headache, nausea, issue in swallowing, vomit, and diarrhoea. The phenol can also damage liver and kidney |

# Table S2. List of Isotherms used in the present investigation

| Isotherm | Equation |  | Ref. |
| --- | --- | --- | --- |
|  | Linear Form | Non-Linear form |  |
| Langmuir Isotherm | Ceqm=1KL*qm+Ceqm | qe=qm*KL*Ce1+KL*Ce | (Girish and Ramachandra Murty 2014) |
| Freundlich Isotherm | lnqe=1nlnCe+lnKF | qe=KF*Ce1n | (Karri, Sahu, and Jayakumar 2017) |
| Redlich-Peterson model | lnCeqe=βlnCe-lnARP | qe=ARP*Ce1+KRP*Ceβ | (Dehmani et al. 2022) |
| Temkin model | qe=RTbT*lnAT+RTbT*lnCe | qe=RTbT*lnAT*Ce | (Gama et al. 2022) |

where, qm is maximum quantity of phenol/2,4-DCP on unit mass of CFPAC, Ce is aqueous concentration of pollutant (phenol/2,4-DCP) at equilibrium, KL, KF, ARP, KRP, β, AT, bT are constants of Langmuir, Freundlich, RP isotherm and Temkin isotherm.

# Table S3. Kinetic models: linear and non-linear forms

| Types of equation | Linear form | Non-linear form | References |
| --- | --- | --- | --- |
| Pseudo-first-order | lnqe-qt=lnqe-k1*t | qt=qe*1-e-k1t | (Sriramoju, Dash, and Majumdar 2021) |
| Pseudo-second-order | tq=1k2*qe2+1qet | qt=k2*qe2*t1+k2*qe*t | (Mohammadi, Darijani, and Karimi 2020) |
| Intraparticle diffusion | qt=Kpi*t0.5+Ci | - | (Lütke et al. 2019) |

Where, qt is adsorption capacity (mg/g) of pollutant at a given time “t”, qe is experimental adsorption capacity of pollutant at equilibrium, k1 (min-1) and k2 (g/mg/min) is rate constant of pseudo-first-order and pseudo-second-order model respectively (Yu et al. 2021). Further, Kpi is diffusion constant (mg/g/min1/2) and Ci is thickness of boundary layer (Kuśmierek, Szala, and Światkowski 2016).

# Table S4. Proximate and Ultimate analysis

| Proximate Analysis | % Moisture | %Volatile matter | % Ash | %Fixed Carbon |
| --- | --- | --- | --- | --- |
| Value (%) | 8.495 | 32.995 | 3.385 | 55.125 |
| Ultimate Analysis | Carbon | Hydrogen | Nitrogen | Sulphur |
| Value (%) | 49 | 7.41 | 0.86 | 0.07 |

# Table S5. Elemental composition before and after adsorption from EDS

| Condition | Element | C | O | Na | P | K | Cl |
| --- | --- | --- | --- | --- | --- | --- | --- |
| Before adsorption | wt/% | 90.65 | 7.735 | 0.28 | 1.19 | 0.145 | 0 |
| After adsorption: Phenol | wt/% | 90.03 | 8.19 | 0.285 | 1.22 | 0.28 | 0 |
| After adsorption :2,4-Dichlorophenol | wt/% | 87.28 | 8.5 | 0.21 | 0.785 | 0.17 | 3.04 |

# Table S6. Optimum operational conditions for isotherm studies

| Conditions | Phenol | 2,4-DCP |
| --- | --- | --- |
| Concentration (mg/L) | 25 | 50 |
| pH | 2 | 2 |
| Temperature (oC) | 20 | 20 |
| Agitation speed (rpm) | 150 | 120 |
| Adsorbent dosage (g/L) | 1.6 | 0.6 |

# Table S7. Thermodynamic parameters for adsorption of Phenol and 2,4-DCP on CFPAC

| Adsorbate | Co (mg/L) | ∆G kJ/mol |  |  |  |  | ∆H kJ/mol | ∆S kJ/mol/K |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  |  | 283K | 293K | 303K | 313K | 323K |  |  |
| PHENOL | 25 | -3.395 | -3.653 | -1.117 | -0.673 | -1.685 | -22.161 | -0.066 |
|  | 50 | -2.081 | -2.437 | -0.801 | -0.509 | -0.850 | -14.872 | -0.045 |
|  | 100 | -0.756 | -1.170 | 0.087 | 0.715 | 0.167 | -11.642 | -0.038 |
|  | 150 | -0.084 | -0.596 | 0.883 | 1.096 | 0.896 | -10.721 | -0.037 |
|  | 200 | 0.180 | -0.297 | 1.011 | 1.487 | 1.316 | -11.565 | -0.041 |
|  | 300 | 0.819 | 0.209 | 1.624 | 1.726 | 1.014 | -4.967 | -0.020 |
|  | 400 | 1.067 | 0.640 | 2.301 | 2.267 | 1.413 | -5.967 | -0.025 |
|  | 500 | 1.386 | 1.232 | 2.426 | 2.782 | 1.177 | -2.335 | -0.014 |
|  | 600 | 1.534 | 1.429 | 2.334 | 2.636 | 3.159 | -11.148 | -0.111 |
| 2,4-DICHLOROPHENOL | 25 | -7.835 | -7.203 | -6.571 | -5.939 | -5.307 | -25.72 | -0.063 |
|  | 50 | -7.060 | -6.489 | -5.918 | -5.347 | -4.776 | -23.22 | -0.057 |
|  | 100 | -4.887 | -4.459 | -4.030 | -3.602 | -3.173 | -17.01 | -0.043 |
|  | 150 | -3.506 | -3.127 | -2.748 | -2.369 | -1.990 | -14.23 | -0.038 |
|  | 200 | -2.518 | -2.257 | -1.995 | -1.734 | -1.472 | -9.92 | -0.026 |
|  | 300 | -1.239 | -0.937 | -0.636 | -0.335 | -0.034 | -9.76 | -0.030 |
|  | 400 | -0.551 | -0.143 | 0.265 | 0.673 | 1.081 | -12.09 | -0.041 |
|  | 500 | 0.261 | 0.513 | 0.765 | 1.018 | 1.270 | -6.88 | -0.025 |
|  | 600 | 0.247 | 0.715 | 1.183 | 1.652 | 2.120 | -13.01 | -0.047 |

# Table S8. Isosteric heat of adsorption parameters for phenol and 2,4-DCP

| Pollutant | qe (mg/g) | ΔHx (kJ/mol) |
| --- | --- | --- |
| Phenol | 10 | 15.953 |
|  | 20 | 9.576 |
|  | 30 | 6.151 |
|  | 40 | 5.034 |
|  | 50 | 5.045 |
|  | 70 | 2.018 |
|  | 90 | 2.172 |
|  | 100 | 0.596 |
| 2,4-DICHLOROPHENOL | 40 | 24.146 |
|  | 80 | 21.406 |
|  | 140 | 14.257 |
|  | 190 | 10.754 |
|  | 230 | 6.821 |
|  | 280 | 5.626 |
|  | 320 | 5.887 |
|  | 360 | 3.122 |
|  | 390 | 5.210 |

# Table S9. Cost analysis for preparation of CFPAC

| Description of item |  | Unit cost | No. of Units |  | Price (INR) |  | Price (USD) |
| --- | --- | --- | --- | --- | --- | --- | --- |
| For 1Kg of CFPAC |  |  |  |  |  |  |  |
| 1. | Biomass | 0 |  |  |  | 0 | 0 |
| 2. | Electricity | 7.5 |  | 4 |  | 30 | 0.36 |
| 3. | Chemicals |  |  |  |  | 380 | 4.59 |
| 4. | DI Water |  |  |  |  | 24 | 0.29 |
| Total |  |  |  |  |  | 434 | 5.24 |

# List of Figures

# Fig. S1 Nitrogen adsorption/ desorption isotherms of CFPAC

# Fig. S2 Non-linear model fit of isotherms for phenol (a), (b) and 2,4-DCP (c), (d) at pH 2 and pH 5

# Fig. S3 Influence of initial concentration on the separation factor (RL)

# Fig. S4 Langmuir isotherm at different temperatures a) Phenol and b) 2,4-DCP

# Fig. S5 Pseudo-First-Order (a) and (c), Pseudo-Second-Order (b) and (d) non-linear kinetics for phenol, 2,4-DCP

# Fig. S6 Pseudo first order and Pseudo second order model fit for Phenol (a) and (b) and 2,4-DCP (c) and (d)

# Fig. S7 Plot of ln(k2) vs 1/T for determining activation energy

# Fig. S8 Intraparticle diffusion plot of a) Phenol b) 2,4-DCP

# Fig. S9 Isosteric heat of adsorption for (a) phenol (b) 2,4-DCP on CFPAC and plot of ΔHx vs Loading for phenol (c) and (d) 2,4-DCP

# Fig S10 SEM-EDS after adsorption of phenol and 2,4-DCP

# Fig. S11 FTIR spectra before and after adsorption of phenol and 2,4-DCP

# Fig. S1 Nitrogen adsorption/ desorption isotherms of CFPAC

Fig. S2 Non-linear model fit of isotherms for phenol (a), (b) and 2,4-DCP (c), (d) at pH 2 and pH 5

# Fig. S3 Influence of initial concentration on the separation factor (RL)

# Fig. S4 Langmuir isotherm at different temperatures a) Phenol and b) 2,4-DCP

# Fig. S5 Pseudo-First-Order (a) and (c), Pseudo-Second-Order (b) and (d) non-linear kinetics for phenol, 2,4-DCP

# Fig. S6 Pseudo first order and Pseudo second order model fit for Phenol (a) and (b) and 2,4-DCP (c) and (d)

# Fig. S7 Plot of ln(k2) vs 1/T for determining activation energy

# Fig. S8 Intraparticle diffusion plot of a) Phenol b) 2,4-DCP

# Fig. S9. Isosteric heat of adsorption for (a) phenol (b) 2,4-DCP on CFPAC and plot of ΔHx vs Loading for phenol (c) and (d) 2,4-DCP

- (b)

# Fig S10 SEM-EDS after adsorption of (a) phenol and (b) 2,4-DCP

# Fig. S11 FTIR spectra before and after adsorption of phenol and 2,4-DCP