Electronic Supporting Information (ESI)

Figure S1. Packing of the water molecules in the channels formed by the CaO8 units in the crystal network of gypsum (a), and subhydrate of calcium sulfate CaSO4·0.69H2O (b). Water channels are highlighted in blue.

Table S1. Unit cell parameters of investigated crystals selected from the surface of A. maritima leaves and the SEM images illustrating their morphology.

| Population | Sample | Type of experiment | Bravais lattice type | Unit cell parameters a, b, c, α, β, γ [Å,°] | Compound | An image of the spot from the crystal was selected. |
| --- | --- | --- | --- | --- | --- | --- |
| Metal tolerant (control) | B_K_1_1_1-1 | pre | mC | 6.29(6) 15.16(14) 5.65(7) 90.4(9) 114(1) 89.7(7) | Gypsum |  |
| Metal tolerant (control) | B_K_2_1_1-1 | pre | mC | 6.266(17) 15.16(5) 5.679(10) 90.0 114.3(3) 90.0 | Gypsum |  |
| Metal tolerant (control) | B_K_2_1_1-2 | pre | mC | 6.266(15) 15.25(3) 5.66(3) 90.0 114.4(4) 90.0 | Gypsum |  |
| Metal tolerant (control) | B_K_2_1_1-3 | pre | mC | 6.29(2) 15.11(3) 5.695(15) 90.0 114.2(4) 90.0 | Gypsum |  |
| Metal tolerant (control) | B_K_4_1_4-3 | pre | mP | 6.205(13) 7.237(9) 9.42(2) 90.0 102.5(3) 90.0 | Syngenite |  |
| Metal tolerant (control) | B_K_4_1_4-4 | full | mP | 6.2246(4) 7.1218(4) 9.7273(7) 90 104.138(7) 90 | Syngenite |  |
| Metal tolerant (control) | B_K_4_1_8-3 | pre | mP | 6.2(2) 7.1(5) 9.72(10) 90(2) 104(2) 90(4) | Syngenite |  |
| Metal tolerant (control) | B_K_5_1_6-2 | Pre | mC | 6.24(6) 15.3(3) 5.65(3) 90.0 114.2(9) 90.0 | Gypsum |  |
| Metal tolerant (control) | B_K_5_1_6-3 | Full | mC | 6.265(2) 15.138(3) 5.6774(14) 90 114.35(4) 90 | Gypsum |  |
| Metal tolerant (control) | B_K_5_1_8-1 | pre | mP | 6.25(5) 7.18(4) 9.73(8) 87.7(6) 102.8(7) 89.9(6) | Syngenite |  |
| Metal tolerant (control) | B_K_5_1_8-4 | pre | mP | 6.249(6) 7.135(7) 9.778(10) 90.0 103.97(10) 90.0 | Syngenite |  |
| Metal tolerant (control) | B_K_5_1_8-6 | pre | mP | 6.219(13) 7.083(18) 9.714(17) 89.8(3) 104.5(3) 90.3(4) | Syngenite |  |
| Metal tolerant (control) | B_K_5_1_8-7 | pre | mP | 6.220(7) 7.144(9) 9.725(12) 90.0 104.25(13) 90.0 | Syngenite |  |
| Metal tolerant (control) | B_K_5_1_10-2 | pre | mC | 6.250(2) 15.110(9) 5.6600(18) 90.00(4) 114.39(4) 90.00(4) | Gypsum |  |
| Metal tolerant (control) | B_K_6_1_9-1 | pre | mC | 6.30(8) 15.3(2) 5.72(6) 89(1) 113(1) 89(1) | Gypsum |  |
| Metal tolerant (control) | B_K_6_1_9-2 | pre | mC | 6.27(3) 15.12(6) 5.66(3) 89.8(4) 114.0(4) 89.9(4) | Gypsum |  |
| Metal tolerant (control) | B_K_6_2_6-1 | full | mP | 6.11490(14) 12.1502(2) 9.0272(2) 90 104.507(3) 90 | Picromerite |  |
| Metal tolerant (control) | B_K_6_2_6-2 | pre | mP | 6.101(13) 12.123(16) 9.002(16) 89.85(19) 104.3(2) 89.94(15) | Picromerite |  |
| Metal tolerant (control) | B_K_6_2_6-3 | pre | mP | 6.14(2) 12.17(4) 9.03(3) 90.2(3) 104.9(3) 90.4(3) | Picromerite |  |
| Metal tolerant (control) | B_K_6_2_13-1 | pre | mP | 6.10(2) 12.116(6) 9.001(19) 89.8(2) 104.3(3) 90.13(15) | Picromerite |  |
| Metal tolerant (control) | B_K_8_1_2-1 | pre | mC | 6.3(2) 15.07(14) 5.6(2) 89(3) 116(6) 89(3) | Gypsum |  |
| Metal tolerant (control) | B_K_8_1_2-2 | pre | mC | 6.260(5) 15.125(6) 5.668(4) 90.0 114.37(8) 90.0 | Gypsum |  |
| Metal tolerant (control) | B_K_8_2_4-1 | pre | mP | 6.202(9) 7.079(12) 9.71(2) 90.0 104.1(2) 90.0 | Syngenite |  |
| Metal tolerant (control) | B_K_8_2_9-3 | pre | mP | 6.38(3) 7.29(5) 9.7(2) 91.0(8) 105(1) 90.0(5) | Syngenite |  |
| Metal intolerant (control) | L_K_10_1_2-1 | full | mC | 6.2598(5) 15.1329(8) 5.6732(5) 90 114.335(10) 90 | Gypsum |  |
| Metal intolerant (control) | L_K_10_1_2-3 | pre | mC | 6.24(15) 15.11(12) 5.66(5) 90.3(7) 114.6(8) 89.8(7) | Gypsum |  |
| Metal intolerant (control) | L_K_10_1_4-1 | pre | mC | 6.28(4) 15.16(3) 5.69(2) 90.0 114.6(5) 90.0 | Gypsum |  |
| Metal intolerant (control) | L_K_10_1_4-2 | pre | mC | 6.29(5) 14.99(7) 5.69(6) 91.2(6) 114.5(9) 88.6(5) | Gypsum |  |
| Metal intolerant (control) | L_K_10_1_4-3 | pre | mC | 6.25(12) 15.1(2) 5.66(5) 90(1) 114(1) 90(2) | Gypsum |  |
| Metal intolerant (control) | L_K_10_1_5-1 | pre | mC | 6.289(19) 15.12(8) 5.684(14) 89.8(3) 114.2(3) 90.1(3) | Gypsum |  |
| Metal intolerant (control) | L_K_10_1_5-3 | pre | mC | 6.23(10) 14.9(3) 5.66(10) 90.8(10) 114(2) 89(1) | Gypsum |  |
| Metal intolerant (control) | L_K_10_2_5-1 | pre | mC | 6.25(2) 15.16(6) 5.71(3) 89.8(4) 114.4(4) 90.1(3) | Gypsum |  |
| Metal intolerant (control) | L_K_10_2_9-1 | pre | mP | 6.23(3) 7.18(6) 9.54(7) 90.4(6) 104.2(5) 90.2(5) | Syngenite |  |
| Metal intolerant (control) | L_K_11_1_5-3 | pre | mC | 6.25(7) 15.30(14) 5.68(10) 90.0 115(2) 90.0 | Gypsum |  |
| Metal intolerant (control) | L_K_12_1_1-1 | pre | mC | 6.31(7) 15.17(7) 5.71(3) 90.0 114.4(9) 90.0 | Gypsum |  |
| Metal intolerant (control) | L_K_12_1_8-1 | pre | mC | 6.306(18) 15.08(8) 5.72(3) 90.0 114.5(5) 90.0 | Gypsum |  |
| Metal intolerant (control) | L_K_12_1_8-2 | pre | mC | 6.26(7) 15.19(7) 5.65(4) 90.1(5) 113.9(9) 91.0(7) | Gypsum |  |
| Metal intolerant (control) | L_K_12_1_8-3 | pre | mC | 6.26(2) 15.172(15) 5.669(16) 90.0 114.2(3) 90.0 | Gypsum |  |
| Metal intolerant (control) | L_K_12_2_2-2 | pre | mP | 6.26(2) 7.12(2) 9.71(2) 90.0 105.0(6) 90.0 | Syngenite |  |
| Metal intolerant (control) | L_K_13_2_6-1 | pre | mC | 6.27(2) 15.12(5) 5.675(13) 90.0 114.4(3) 90.0 | Gypsum |  |
| Metal intolerant (control) | L_K_13_2_7-1 | pre | mC | 6.27(4) 15.11(9) 5.70(3) 90.0 114.3(7) 90.0 | Gypsum |  |
| Metal intolerant (control) | L_K_14_1_9-1 | pre | mC | 6.257(9) 15.126(16) 5.674(10) 90.0 114.30(18) 90.0 | Gypsum |  |
| Metal intolerant (control) | L_K_14_1_9-3 | pre | mC | 6.16(9) 15.12(15) 5.88(11) 91(1) 114(2) 90(1) | Gypsum |  |
| Metal intolerant (control) | L_K_14_1_10-1 | pre | mC | 6.26(2) 15.14(5) 5.69(2) 89.9(3) 114.6(4) 90.0(3) | Gypsum |  |
| Metal intolerant (control) | L_K_14_1_10-2 | pre | mC | 6.26(2) 15.14(5) 5.69(2) 89.9(3) 114.6(4) 90.0(3) | Gypsum |  |
| Metal intolerant (control) | L_K_14_2_6+7-3 | pre | mC | 6.24(6) 15.15(3) 5.70(3) 90.0 114.2(7) 90.0 | Gypsum |  |
| Metal intolerant (control) | L_K_14_2_9-1 | pre | mC | 6.23(6) 15.05(6) 5.646(18) 90.0 114.3(7) 90.0 | Gypsum |  |
| Metal intolerant (control) | L_K_15_1_12-2 | pre | mP | 6.241(7) 7.097(14) 9.728(15) 90.0 104.9(3) 90.0 | Syngenite |  |
| Metal intolerant (control) | L_K_15_1_12-3 | pre | mP | 6.218(8) 7.100(14) 9.73(2) 90.0 104.48(14) 90.0 | Syngenite |  |
| Metal intolerant (control) | L_K_15_1_13-1 | pre | mP | 6.225(12) 7.11(2) 9.72(3) 90.0 104.14(19) 90.0 | Syngenite |  |
| Metal intolerant (control) | L_K_15_1_13-2 | pre | mP | 6.20(2) 7.115(15) 9.72(2) 90.0 104.0(3) 90.0 | Syngenite |  |
| Metal intolerant (control) | L_K_15_1_15-1 | pre | mP | 6.219(10) 7.120(17) 9.71(6) 90.0 103.9(3) 90.0 | Syngenite |  |
| Metal intolerant (control) | L_K_15_1_15-2 | pre | mP | 6.22(4) 7.11(2) 9.73(2) 90.0 104.6(3) 90.0 | Syngenite |  |
| Metal intolerant (control) | L_K_16_1_3-3 | pre | mC | 6.29(8) 15.18(17) 5.69(5) 89.9(8) 114.6(10) 88.2(9) | Gypsum |  |
| Metal intolerant (control) | L_K_16_1_9-1 | pre | mC | 6.29(18) 15.09(6) 5.67(10) 90.0 115(3) 90.0 | Gypsum |  |
| Metal tolerant (+ Pb) | B_Pb_17_2-1 | pre | oP | 6.48(2) 5.391(10) 9.24(2) 90.0 90.0 90.0 | Niter |  |
| Metal tolerant (+ Pb) | B_Pb_17_2-2 | pre | oP | 6.425(14) 5.425(12) 9.20(2) 89.70(18) 89.90(18) 89.92(18) | Niter |  |
| Metal tolerant (+ Pb) | B_Pb_17_2-3 | pre | oP | 6.422(8) 5.413(5) 9.165(12) 90.0 90.0 90.0 318.6(6) | Niter |  |
| Metal tolerant (+ Pb) | B_Pb_17_1_6-1 | pre | oP | 6.44(2) 5.400(8) 9.206(14) 90.0 90.0 90.0 | Niter |  |
| Metal tolerant (+ Pb) | B_Pb_17_1_6-2 | pre | oP | 6.426(4) 5.4197(14) 9.169(3) 90.0 90.0 90.0 | Niter |  |
| Metal tolerant (+ Pb) | B_Pb_17_1_6-3 | pre | oP | 6.420(7) 5.416(5) 9.159(3) 90.0 90.0 90.0 | Niter |  |
| Metal tolerant (+ Pb) | B_Pb_17_1_6-4 | pre | oP | 6.428(3) 5.422(3) 9.169(3) 90.0 90.0 90.0 | Niter |  |
| Metal tolerant (+ Pb) | B_Pb_17_1_6-5 | pre | oP | 6.441(2) 5.4278(18) 9.150(11) 90.0 90.0 90.0 | Niter |  |
| Metal tolerant (+ Pb) | B_Pb_17_1_4_1 | pre | oP | 6.425(6) 5.417(5) 9.164(5) 90.0 90.0 90.0 | Niter |  |
| Metal tolerant (+ Pb) | B_Pb_17_1_4-2 | full | oP | 6.27222) 5.39305(16) 9.1392(3) 90 90 90 | Niter |  |
| Metal tolerant (+ Pb) | B_Pb_17_1_4-3 | pre | oP | 6.43(2) 5.397(9) 9.194(12) 90.0 90.0 90.0 | Niter |  |
| Metal tolerant (+ Pb) | B_Pb_20_2_6-1 | full | hP | 6.9332(4) 6.9332(4) 6.3460(4) 90 90 120 | CaSO4·0.69H2O |  |
| Metal tolerant (+ Pb) | B_Pb_20_2_6-2 | pre | hP | 6.934(16) 6.934(16) 6.35(2) 90.0 90.0 120.0 | CaSO4·0.69H2O |  |
| Metal tolerant (+ Pb) | B_Pb_21_1_2-2 | pre | mC | 6.270(12) 15.22(3) 5.682(15) 90.09(18) 114.4(2) 89.74(17) | Gypsum |  |
| Metal tolerant (+ Pb) | B_Pb_21_1_2-3 | pre | mC | 6.31(12) 15.13(10) 5.67(17) 90.0 115(4) 90.0 | Gypsum |  |
| Metal tolerant (+ Pb) | B_Pb_21_1_3-1 | pre | mC | 6.34(4) 15.26(2) 5.71(3) 90.0 114.6(7) 90.0 | Gypsum |  |
| Metal tolerant (+ Pb) | B_Pb_21_1_9-1 | pre | mC | 6.272(17) 15.21(5) 5.70(4) 90.0 114.8(6) 90.0 | Gypsum |  |
| Metal tolerant (+ Pb) | B_Pb_21_1_9-2 | pre | mC | 6.216(15) 15.13(3) 5.660(16) 90.0 113.9(4) 90.0 | Gypsum |  |
| Metal tolerant (+ Pb) | B_Pb_21_1_9-3 | pre | mC | 6.28(6) 14.97(17) 5.68(4) 90.0 114(1) 90.0 | Gypsum |  |
| Metal tolerant (+ Pb) | B_Pb_21_1_10-1 | pre | mC | 6.32(4) 15.26(4) 5.67(7) 90.0 115(1) 90.0 | Gypsum |  |
| Metal tolerant (+ Pb) | B_Pb_21_1_10-2 | pre | mC | 6.1(7) 15.4(3) 5.5(5) 90.0 112(14) 90.0 | Gypsum |  |
| Metal tolerant (+ Pb) | B_Pb_22_1_7-1 | pre | mC | 6.31(6) 15.23(5) 5.67(5) 90.0 114(1) 90.0 | Gypsum |  |
| Metal tolerant (+ Pb) | B_Pb_22_1_7-2 | pre | mC | 6.23(2) 15.09(4) 5.647(19) 90.0 114.2(4) 90.0 | Gypsum |  |
| Metal tolerant (+ Pb) | B_Pb_22_1_7-3 | pre | mC | 6.04(17) 15.2(2) 5.8(3) 88(2) 111(4) 92(2) | Gypsum |  |
| Metal tolerant (+ Pb) | B_Pb_23_1-1 | pre | mC | 6.32(4) 15.05(8) 5.71(3) 90.0(4) 115.5(6) 89.0(5) | Gypsum |  |
| Metal tolerant (+ Pb) | B_Pb_23_1-5 | pre | mC | 6.18(5) 15.36(11) 5.64(3) 90.1(5) 113.6(6) 88.8(6) | Gypsum |  |
| Metal tolerant (+ Pb) | B_Pb_23_2-1 | pre | mC | 6.250(14) 15.210(17) 5.700(17) 89.3(2) 113.9(3) 90.36(15) | Gypsum |  |
| Metal tolerant (+ Pb) | B_Pb_23_2-3 | pre | mC | 6.26(2) 15.23(2) 5.680(10) 90.0 114.5(3) 90.0 | Gypsum |  |
| Metal tolerant (+ Pb) | B_Pb_23_2-6 | full | mC | 6.2783(15) 15.217(3) 5.6738(13) 90 114.21(3) 90 | Gypsum |  |
| Metal tolerant (+ Pb) | B_Pb_24_1_3-1 | pre | oP | 6.426(10) 5.416(5) 9.192(9) 90.0 90.0 90.0 | Niter |  |
| Metal tolerant (+ Pb) | B_Pb_24_1_3-2 | pre | oP | 6.428(18) 5.388(12) 9.162(12) 90.0 90.0 90.0 | Niter |  |
| Metal tolerant (+ Pb) | B_Pb_24_1_3-3 | pre | oP | 6.4351(17) 5.423(3) 9.159(4) 90.0 90.0 90.0 | Niter |  |
| Metal tolerant (+ Pb) | B_Pb_24_1_1-2 | pre | oP | 6.4(4) 5.4(2) 9(1) 90.0 92(7) 90.0 | Niter |  |
| Metal intolerant (+ Pb) | L_Pb_26_2_10-3 | pre | mC | 6.45(11) 14.9(2) 5.9(2) 90.0 114(4) 90.0 | Gypsum |  |
| Metal intolerant (+ Pb) | L_Pb_26_2_13-4 | pre | mC | 6.25(4) 15.1(5) 5.66(3) 90(1) 114.4(6) 90(1) | Gypsum |  |
| Metal intolerant (+ Pb) | L_Pb_26_2-12 | pre | mC | 6.20(9) 15.18(4) 5.67(3) 89.8(3) 114.3(9) 90.0(6) | Gypsum |  |
| Metal intolerant (+ Pb) | L_Pb_26_2-15 | pre | mC | 6.28(4) 15.14(10) 5.69(3) 91.0(5) 114.8(6) 89.1(5) | Gypsum |  |
| Metal intolerant (+ Pb) | L_Pb_27_1_3-2 | pre | mC | 6.282(7) 15.26(2) 5.697(9) 90.0 114.07(17) 90.0 | Gypsum |  |
| Metal intolerant (+ Pb) | L_Pb_27_1_3-3 | pre | mC | 6.277(9) 15.270(16) 5.664(9) 90.0 114.09(17) 90.0 | Gypsum |  |
| Metal intolerant (+ Pb) | L_Pb_27_1_3-4 | pre | mC | 6.25(3) 15.27(13) 5.65(2) 90.1(5) 114.1(5) 89.6(5) | Gypsum |  |
| Metal intolerant (+ Pb) | L_Pb_27_1_2-1 | pre | oP | 6.439(11) 5.439(16) 9.19(2) 90.0 90.0 90.0 | Niter |  |
| Metal intolerant (+ Pb) | L_Pb_27_1_2-2 | pre | mC | 6.43(6) 15.08(2) 5.62(5) 90.0 113(1) 90.0 | Gypsum |  |
| Metal intolerant (+ Pb) | L_Pb_27_1_2-3 | pre | mC | 6.28(2) 15.19(3) 5.674(13) 90.0 113.9(4) 90.0 | Gypsum |  |
| Metal intolerant (+ Pb) | L_Pb_27_1_2-5 | pre | oP | 6.438(11) 5.409(12) 9.21(3) 90.0 90.0 90.0 | Niter |  |
| Metal intolerant (+ Pb) | L_Pb_27_1_1-1 | pre | oP | 6.275(16) 5.362(11) 9.206(14) 90.0 90.0 90.0 | Niter |  |
| Metal intolerant (+ Pb) | L_Pb_27_1_1-2 | pre | oP | 6.388(10) 5.446(5) 9.216(17) 90.0 90.0 90.0 | Niter |  |
| Metal intolerant (+ Pb) | L_Pb_27_1_1-3 | pre | oP | 6.431(7) 5.404(5) 9.207(10) 90.0 90.0 90.0 | Niter |  |
| Metal intolerant (+ Pb) | L_Pb_27_1_1-4 | pre | oP | 6.432(11) 5.403(12) 9.219(19) 90.0 90.4(2) 90.0 | Niter |  |
| Metal intolerant (+ Pb) | L_Pb_28_1_5-3 | pre | mC | 6.3(3) 15.1(4) 5.66(16) 90(2) 114(4) 90(3) | Gypsum |  |
| Metal intolerant (+ Pb) | L_Pb_28_1_9-1 | full | mC | 6.2562(14) 15.1356(15) 5.6698(10) 90 114.43(3) 90 | Gypsum |  |
| Metal intolerant (+ Pb) | L_Pb_28_1_9-2 | pre | mC | 6.25(4) 15.1(5) 5.66(3) 90(1) 114.4(6) 90(1) | Gypsum |  |
| Metal intolerant (+ Pb) | L_Pb_28_1_9-3 | pre | mC | 6.26(6) 15.10(3) 5.66(4) 90.0 114.5(8) 90.0, | Gypsum |  |
| Metal intolerant (+ Pb) | L_Pb_29_1_8-1 | pre | mC | 6.272(12) 15.14(3) 5.672(10) 90.0 114.8(3) 90.0 | Gypsum |  |
| Metal intolerant (+ Pb) | L_Pb_29_1_9-1 | pre | mC | 6.20(13) 15.14(10) 5.75(19) 90.0 115(3) 90.0 | Gypsum |  |
| Metal intolerant (+ Pb) | L_Pb_29_1_9-2 | pre | mC | 6.27(6) 15.10(5) 5.67(3) 90.0 114.6(10) 90.0 | Gypsum |  |
| Metal intolerant (+ Pb) | L_Pb_29_1_9-3 | pre | mC | 6.22(6) 15.1(2) 5.68(6) 90.0 114(1) 90.0 | Gypsum |  |
| Metal intolerant (+ Pb) | L_Pb_30_1_1-1 | pre | mC | 6.24(7) 15.28(5) 5.70(5) 90.0 115(1) 90.0 | Gypsum |  |
| Metal intolerant (+ Pb) | L_Pb_30_1_1-3 | pre | mC | 6.19(5) 15.16(7) 5.85(5) 90.2(5) 113.7(8) 89.3(5) | Gypsum |  |
| Metal intolerant (+ Pb) | L_Pb_30_1_5-2 | pre | mC | 6.291(5) 15.226(14) 5.656(4) 90.0 114.17(8) 90.0 | Gypsum |  |
| Metal intolerant (+ Pb) | L_Pb_30_1_5-3 | pre | mC | 6.329(19) 15.21(4) 5.700(13) 90.0 114.5(3) 90.0 | Gypsum |  |
| Metal intolerant (+ Pb) | L_Pb_30_1-2 | pre | mC | 6.286(7) 15.305(11) 5.690(6) 90.0 114.23(13) 90.0 | Gypsum |  |
| Metal intolerant (+ Pb) | L_Pb_30_1-3 | pre | mC | 6.310(7) 15.245(10) 5.692(7) 90.0 114.28(15) 90.0 | Gypsum |  |
| Metal intolerant (+ Pb) | L_Pb_30_1_2-2 | pre | mC | 6.28(3) 15.24(3) 5.71(3) 90.0 114.5(6) 90.0 | Gypsum |  |
| Metal intolerant (+ Pb) | L_Pb_31_1_12-3 | pre | oP | 6.28(4) 5.40(5) 9.14(5) 90.0 90.0 90.0 | Niter |  |
| Metal intolerant (+ Pb) | L_Pb_31_2_13-2 | pre | oP | 6.24(3) 5.352(15) 9.27(2) 90.0 90.0 90.0 | Niter |  |
| Metal intolerant (+ Pb) | L_Pb_31_2_14-1 | pre | mC | 6.286(9) 15.207(17) 5.700(6) 90.02(11) 114.44(16) 90.02(9) | Gypsum |  |
| Metal intolerant (+ Pb) | L_Pb_31_2_14-2 | pre | mC | 6.277(15) 15.181(16) 5.687(8) 90.0 114.4(2) 90.0 | Gypsum |  |
| Metal intolerant (+ Pb) | L_Pb_31_2_10-3 | pre | mC | 6.265(7) 15.13(3) 5.659(5) 90.0 114.35(13) 90.0 | Gypsum |  |
| Metal intolerant (+ Pb) | L_Pb_31_1_9-1 | pre | oP | 6.281(3) 5.400(4) 9.126(8) 90.0 90.0 90.0 | Niter |  |
| Metal intolerant (+ Pb) | L_Pb_31_1_12-1 | pre | oP | 6.26(2) 5.375(7) 9.192(12) 90.0 90.0 90.0 | Niter |  |
| Metal intolerant (+ Pb) | L_Pb_31_1_12-2 | pre | oP | 6.268(3) 5.393(5) 9.142(3) 90.0 90.0 90.0 | Niter |  |
| Metal intolerant (+ Pb) | L_Pb_31_1_12-3 | pre | oP | 6.266(7) 5.370(7) 9.171(9) 90.0 90.0 90.0 | Niter |  |
| Metal intolerant (+ Pb) | L_Pb_31_1_13-1 | full | oP | 6.2730(4) 5.3930(3) 9.1408(7) 90.0 90.0 90.0 | Niter |  |
| Metal intolerant (+ Pb) | L_Pb_31_2_4-1 | pre | oP | 6.278(14) 5.38(2) 9.191(16) 90.0 90.0 90.0 | Niter |  |
| Metal intolerant (+ Pb) | L_Pb_31_2_4-2 | pre | oP | 6.271(11) 5.327(8) 9.285(19) 90.0 90.0 90.0 | Niter |  |

Where: pre – X-Ray diffraction screening; full – complete X-Ray diffraction measurement.

Table S2. Bond lengths for gypsum [Å].

| Atom | Atom | Length/Å |  | Atom | Atom | Length/Å |
| --- | --- | --- | --- | --- | --- | --- |
| Ca1 | Ca11 | 4.0415(14) |  | Ca1 | O22 | 2.542(2) |
| Ca1 | Ca12 | 4.0415(14) |  | Ca1 | O25 | 2.542(2) |
| Ca1 | S13 | 3.1283(7) |  | S1 | Ca12 | 3.1283(7) |
| Ca1 | S12 | 3.1283(7) |  | S1 | Ca13 | 3.1283(7) |
| Ca1 | O12 | 2.531(2) |  | S1 | O16 | 1.475(2) |
| Ca1 | O14 | 2.360(2) |  | S1 | O1 | 1.475(2) |
| Ca1 | O15 | 2.531(2) |  | S1 | O26 | 1.478(2) |
| Ca1 | O1 | 2.360(2) |  | S1 | O2 | 1.478(2) |
| Ca1 | O1W | 2.362(2) |  | O1 | Ca12 | 2.531(2) |
| Ca1 | O1W4 | 2.362(2) |  | O2 | Ca12 | 2.542(2) |

13/2-X,1/2-Y,2-Z; 21/2-X,1/2-Y,1-Z; 33/2-X,1/2-Y,1-Z; 41-X,+Y,3/2-Z; 51/2+X,1/2-Y,1/2+Z; 61-X,+Y,1/2-Z

Table S3. Values of valence angles for gypsum [ º].

| Atom | Atom | Atom | Angle/˚ |  | Atom | Atom | Atom | Angle/˚ |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
| Ca11 | Ca1 | Ca12 | 106.51(4) |  | O1W | Ca1 | Ca12 | 79.67(6) |
| S13 | Ca1 | Ca12 | 60.602(19) |  | O1W4 | Ca1 | S13 | 104.04(6) |
| S13 | Ca1 | Ca11 | 118.49(2) |  | O1W | Ca1 | S11 | 104.04(6) |
| S11 | Ca1 | Ca12 | 118.49(2) |  | O1W4 | Ca1 | S11 | 76.86(6) |
| S11 | Ca1 | Ca11 | 60.602(19) |  | O1W | Ca1 | S13 | 76.86(6) |
| S11 | Ca1 | S13 | 178.67(4) |  | O1W | Ca1 | O15 | 77.74(8) |
| O1 | Ca1 | Ca11 | 35.66(5) |  | O1W4 | Ca1 | O15 | 131.69(8) |
| O11 | Ca1 | Ca11 | 32.94(5) |  | O1W | Ca1 | O11 | 131.69(8) |
| O14 | Ca1 | Ca11 | 91.70(6) |  | O1W4 | Ca1 | O11 | 77.74(8) |
| O1 | Ca1 | Ca12 | 91.70(6) |  | O1W4 | Ca1 | O1W | 98.01(13) |
| O15 | Ca1 | Ca11 | 115.23(6) |  | O1W4 | Ca1 | O21 | 80.01(8) |
| O11 | Ca1 | Ca12 | 115.23(6) |  | O1W | Ca1 | O21 | 76.20(8) |
| O15 | Ca1 | Ca12 | 32.94(5) |  | O1W | Ca1 | O25 | 80.01(8) |
| O14 | Ca1 | Ca12 | 35.66(5) |  | O1W4 | Ca1 | O25 | 76.20(8) |
| O11 | Ca1 | S11 | 27.73(5) |  | O21 | Ca1 | Ca12 | 113.76(5) |
| O14 | Ca1 | S11 | 82.89(5) |  | O21 | Ca1 | Ca11 | 88.45(5) |
| O11 | Ca1 | S13 | 151.30(5) |  | O25 | Ca1 | Ca11 | 113.76(5) |
| O15 | Ca1 | S13 | 27.73(5) |  | O25 | Ca1 | Ca12 | 88.45(5) |
| O14 | Ca1 | S13 | 96.23(5) |  | O21 | Ca1 | S13 | 153.06(5) |
| O1 | Ca1 | S11 | 96.23(5) |  | O25 | Ca1 | S13 | 27.85(5) |
| O15 | Ca1 | S11 | 151.30(5) |  | O25 | Ca1 | S11 | 153.06(5) |
| O1 | Ca1 | S13 | 82.89(5) |  | O21 | Ca1 | S11 | 27.85(5) |
| O11 | Ca1 | O15 | 139.61(10) |  | O25 | Ca1 | O21 | 143.39(11) |
| O1 | Ca1 | O14 | 98.26(11) |  | Ca13 | S1 | Ca11 | 178.67(4) |
| O1 | Ca1 | O11 | 68.60(8) |  | O1 | S1 | Ca11 | 52.97(8) |
| O14 | Ca1 | O15 | 68.60(8) |  | O16 | S1 | Ca13 | 52.97(8) |
| O1 | Ca1 | O15 | 85.02(5) |  | O16 | S1 | Ca11 | 127.99(9) |
| O14 | Ca1 | O11 | 85.02(5) |  | O1 | S1 | Ca13 | 127.99(9) |
| O14 | Ca1 | O1W | 85.44(8) |  | O16 | S1 | O1 | 110.84(17) |
| O1 | Ca1 | O1W | 159.71(7) |  | O1 | S1 | O26 | 111.03(11) |
| O14 | Ca1 | O1W4 | 159.71(7) |  | O1 | S1 | O2 | 106.38(11) |
| O1 | Ca1 | O1W4 | 85.44(8) |  | O16 | S1 | O26 | 106.38(11) |
| O15 | Ca1 | O21 | 141.46(6) |  | O16 | S1 | O2 | 111.03(11) |
| O1 | Ca1 | O25 | 81.44(7) |  | O2 | S1 | Ca13 | 125.63(8) |
| O1 | Ca1 | O21 | 124.04(7) |  | O26 | S1 | Ca11 | 125.63(8) |
| O15 | Ca1 | O25 | 55.57(6) |  | O2 | S1 | Ca11 | 53.44(8) |
| O14 | Ca1 | O25 | 124.04(7) |  | O26 | S1 | Ca13 | 53.44(8) |
| O14 | Ca1 | O21 | 81.44(7) |  | O2 | S1 | O26 | 111.25(18) |
| O11 | Ca1 | O25 | 141.46(6) |  | Ca1 | O1 | Ca11 | 111.40(8) |
| O11 | Ca1 | O21 | 55.57(6) |  | S1 | O1 | Ca11 | 99.30(11) |
| O1W4 | Ca1 | Ca11 | 79.67(6) |  | S1 | O1 | Ca1 | 148.89(12) |
| O1W | Ca1 | Ca11 | 164.63(6) |  | S1 | O2 | Ca11 | 98.71(10) |
| O1W4 | Ca1 | Ca12 | 164.63(6) |  |  |  |  |  |

11/2-X,1/2-Y,1-Z; 23/2-X,1/2-Y,2-Z; 33/2-X,1/2-Y,1-Z; 41-X,+Y,3/2-Z; 51/2+X,1/2-Y,1/2+Z; 61-X,+Y,1/2-Z

Table S4. Values of torsion angles for gypsum [ º].

| A | B | C | D | Angle/˚ |  | A | B | C | D | Angle/˚ |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| Ca11 | S1 | O1 | Ca1 | 170.8(3) |  | O13 | S1 | O2 | Ca11 | -122.40(11) |
| Ca12 | S1 | O1 | Ca1 | -8.0(3) |  | O2 | S1 | O1 | Ca1 | 172.5(2) |
| Ca12 | S1 | O1 | Ca11 | -178.83(4) |  | O23 | S1 | O1 | Ca11 | -119.45(11) |
| Ca12 | S1 | O2 | Ca11 | 178.82(4) |  | O23 | S1 | O1 | Ca1 | 51.3(3) |
| O13 | S1 | O1 | Ca11 | 122.53(11) |  | O2 | S1 | O1 | Ca11 | 1.73(14) |
| O13 | S1 | O1 | Ca1 | -66.7(2) |  | O23 | S1 | O2 | Ca11 | 119.32(10) |
| O1 | S1 | O2 | Ca11 | -1.72(14) |  |  |  |  |  |  |

11/2-X,1/2-Y,1-Z; 23/2-X,1/2-Y,1-Z; 31-X,+Y,1/2-Z

Table S5. Bond lengths for niter [Å].

| Atom | Atom | Length/Å |  | Atom | Atom | Length/Å |
| --- | --- | --- | --- | --- | --- | --- |
| O2 | K11 | 2.8031(12) |  | K1 | O15 | 2.8464(8) |
| O2 | K12 | 2.8879(5) |  | K1 | O14 | 2.8094(9) |
| O2 | K13 | 2.8879(5) |  | K1 | O18 | 2.8464(8) |
| O2 | N1 | 1.2568(19) |  | K1 | O19 | 2.8094(9) |
| O1 | K1 | 2.8601(8) |  | K1 | O110 | 2.8602(8) |
| O1 | K12 | 2.8465(8) |  | K1 | N1 | 3.2363(14) |
| O1 | K14 | 2.8094(9) |  | K1 | N15 | 3.2471(8) |
| O1 | N1 | 1.2544(11) |  | K1 | N17 | 3.2471(8) |
| K1 | O25 | 2.8879(5) |  | N1 | O110 | 1.2544(11) |
| K1 | O26 | 2.8031(12) |  | N1 | K12 | 3.2471(8) |
| K1 | O27 | 2.8879(5) |  | N1 | K13 | 3.2471(8) |

11/2+X,+Y,1/2-Z; 23/2-X,1-Y,-1/2+Z; 33/2-X,-Y,-1/2+Z; 42-X,1-Y,1-Z; 53/2-X,1-Y,1/2+Z; 6-1/2+X,+Y,1/2-Z; 73/2-X,-Y,1/2+Z; 83/2-X,-1/2+Y,1/2+Z; 92-X,-1/2+Y,1-Z; 10+X,1/2-Y,+Z

Table S6. Values of valence angles for niter [ º].

| Atom | Atom | Atom | Angle/˚ |  | Atom | Atom | Atom | Angle/˚ |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
| K11 | O2 | K12 | 102.92(2) |  | O17 | K1 | O19 | 167.28(3) |
| K11 | O2 | K13 | 102.92(2) |  | O14 | K1 | O1 | 79.32(3) |
| K12 | O2 | K13 | 138.05(5) |  | O18 | K1 | O110 | 72.592(18) |
| N1 | O2 | K11 | 127.45(9) |  | O17 | K1 | O1 | 123.067(8) |
| N1 | O2 | K13 | 94.93(4) |  | O18 | K1 | O1 | 104.491(18) |
| N1 | O2 | K12 | 94.93(4) |  | O17 | K1 | O110 | 68.85(3) |
| K14 | O1 | K1 | 100.68(3) |  | O110 | K1 | O1 | 167.28(3) |
| K14 | O1 | K13 | 101.22(3) |  | O14 | K1 | O17 | 72.592(18) |
| K13 | O1 | K1 | 136.82(3) |  | O14 | K1 | O18 | 69.89(4) |
| N1 | O1 | K13 | 96.98(7) |  | O1 | K1 | O19 | 44.69(3) |
| N1 | O1 | K14 | 131.36(8) |  | O17 | K1 | N1 | 144.654(18) |
| N1 | O1 | K1 | 95.76(7) |  | O19 | K1 | N1 | 22.684(17) |
| O25 | K1 | O26 | 77.08(2) |  | O19 | K1 | N17 | 144.79(3) |
| O26 | K1 | O27 | 138.05(5) |  | O1 | K1 | N1 | 22.684(17) |
| O25 | K1 | O27 | 77.08(2) |  | O1 | K1 | N17 | 100.70(3) |
| O25 | K1 | O18 | 142.462(19) |  | O1 | K1 | N16 | 144.79(3) |
| O25 | K1 | O19 | 74.19(3) |  | O110 | K1 | N1 | 144.654(18) |
| O25 | K1 | O14 | 142.462(19) |  | O18 | K1 | N1 | 95.30(3) |
| O25 | K1 | O1 | 74.19(3) |  | O14 | K1 | N16 | 124.21(3) |
| O25 | K1 | O110 | 100.36(3) |  | O17 | K1 | N16 | 90.88(3) |
| O25 | K1 | O17 | 100.36(3) |  | O18 | K1 | N17 | 124.21(3) |
| O27 | K1 | N16 | 128.92(3) |  | O110 | K1 | N16 | 22.55(3) |
| O27 | K1 | N17 | 22.68(3) |  | O19 | K1 | N16 | 100.70(3) |
| O26 | K1 | N1 | 100.37(2) |  | O14 | K1 | N1 | 95.30(3) |
| O27 | K1 | N1 | 100.37(2) |  | O17 | K1 | N17 | 22.55(3) |
| O25 | K1 | N17 | 92.09(3) |  | O14 | K1 | N17 | 67.10(3) |
| O26 | K1 | N17 | 128.92(3) |  | O110 | K1 | N17 | 90.88(3) |
| O26 | K1 | N16 | 22.68(3) |  | O18 | K1 | N16 | 67.10(3) |
| O25 | K1 | N1 | 68.85(4) |  | N1 | K1 | N16 | 122.12(2) |
| O25 | K1 | N16 | 92.09(3) |  | N17 | K1 | N16 | 112.29(4) |
| O1 | K1 | O27 | 80.28(3) |  | N1 | K1 | N17 | 122.12(2) |
| O14 | K1 | O26 | 140.37(3) |  | O2 | N1 | K1 | 161.26(10) |
| O19 | K1 | O26 | 80.28(3) |  | O2 | N1 | K12 | 62.39(3) |
| O110 | K1 | O26 | 44.54(3) |  | O2 | N1 | K13 | 62.39(3) |
| O1 | K1 | O26 | 122.76(3) |  | O19 | N1 | O2 | 119.90(7) |
| O17 | K1 | O27 | 44.54(3) |  | O1 | N1 | O2 | 119.90(7) |
| O19 | K1 | O27 | 122.76(3) |  | O1 | N1 | O19 | 120.18(13) |
| O110 | K1 | O27 | 110.06(3) |  | O1 | N1 | K12 | 161.24(9) |
| O14 | K1 | O27 | 72.57(3) |  | O1 | N1 | K1 | 61.56(7) |
| O18 | K1 | O26 | 72.57(3) |  | O19 | N1 | K1 | 61.56(7) |
| O18 | K1 | O27 | 140.37(3) |  | O1 | N1 | K13 | 60.47(5) |
| O17 | K1 | O26 | 110.06(3) |  | O19 | N1 | K12 | 60.47(5) |
| O18 | K1 | O17 | 110.39(2) |  | O19 | N1 | K13 | 161.24(9) |
| O18 | K1 | O19 | 79.32(3) |  | K12 | N1 | K13 | 112.29(4) |
| O14 | K1 | O19 | 104.491(18) |  | K1 | N1 | K12 | 109.86(3) |
| O110 | K1 | O19 | 123.067(8) |  | K1 | N1 | K13 | 109.86(3) |
| O14 | K1 | O110 | 110.39(2) |  |  |  |  |  |

11/2+X,+Y,1/2-Z; 23/2-X,-Y,-1/2+Z; 33/2-X,1-Y,-1/2+Z; 42-X,1-Y,1-Z; 5-1/2+X,+Y,1/2-Z; 63/2-X,-Y,1/2+Z; 73/2-X,1-Y,1/2+Z; 82-X,-1/2+Y,1-Z; 9+X,1/2-Y,+Z; 103/2-X,-1/2+Y,1/2+Z

Table S7. Values of torsion angles for niter [ º].

| A | B | C | D | Angle/˚ |  | A | B | C | D | Angle/˚ |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| K11 | O2 | N1 | O1 | 90.86(12) |  | K1 | O1 | N1 | O2 | 158.58(12) |
| K11 | O2 | N1 | O12 | -90.86(12) |  | K13 | O1 | N1 | O2 | 19.92(13) |
| K13 | O2 | N1 | O12 | 158.72(11) |  | K15 | O1 | N1 | O2 | -91.73(14) |
| K13 | O2 | N1 | O1 | -19.55(13) |  | K1 | O1 | N1 | O12 | -19.69(13) |
| K14 | O2 | N1 | O1 | -158.73(11) |  | K13 | O1 | N1 | O12 | -158.35(11) |
| K14 | O2 | N1 | O12 | 19.55(13) |  | K15 | O1 | N1 | O12 | 89.99(14) |
| K11 | O2 | N1 | K13 | 110.41(3) |  | K13 | O1 | N1 | K1 | -138.65(4) |
| K14 | O2 | N1 | K1 | -69.59(3) |  | K15 | O1 | N1 | K1 | 109.69(8) |
| K11 | O2 | N1 | K14 | -110.41(3) |  | K15 | O1 | N1 | K13 | -111.66(8) |
| K13 | O2 | N1 | K14 | 139.17(6) |  | K13 | O1 | N1 | K14 | -71.8(3) |
| K13 | O2 | N1 | K1 | 69.59(3) |  | K1 | O1 | N1 | K14 | 66.8(3) |
| K11 | O2 | N1 | K1 | 180.0 |  | K15 | O1 | N1 | K14 | 176.53(18) |
| K14 | O2 | N1 | K13 | -139.17(6) |  | K1 | O1 | N1 | K13 | 138.65(4) |

11/2+X,+Y,1/2-Z; 2+X,1/2-Y,+Z; 33/2-X,1-Y,-1/2+Z; 43/2-X,-Y,-1/2+Z; 52-X,1-Y,1-Z

Table S8. Bond lengths for syngenite [Å].

| Atom | Atom | Length/Å |  | Atom | Atom | Length/Å |
| --- | --- | --- | --- | --- | --- | --- |
| Ca1 | O11 | 2.5457(19) |  | O2 | K111 | 2.858(2) |
| Ca1 | O1 | 2.5458(19) |  | O2 | S1 | 1.480(3) |
| Ca1 | O1W | 2.461(3) |  | O3 | K112 | 2.850(2) |
| Ca1 | O4 | 2.5185(18) |  | O3 | K111 | 2.955(2) |
| Ca1 | O42 | 2.4427(18) |  | O3 | K110 | 2.955(2) |
| Ca1 | O43 | 2.4427(18) |  | O3 | K18 | 2.850(2) |
| Ca1 | O41 | 2.5185(18) |  | O3 | S1 | 1.480(3) |
| Ca1 | O54 | 2.401(3) |  | O4 | Ca12 | 2.4427(18) |
| Ca1 | O64 | 2.703(3) |  | O4 | K112 | 3.3844(19) |
| Ca1 | S1 | 3.1441(11) |  | O4 | S2 | 1.4780(18) |
| Ca1 | S2 | 3.1105(10) |  | O5 | Ca113 | 2.401(3) |
| Ca1 | S24 | 3.1267(10) |  | O5 | K18 | 2.671(2) |
| K1 | K11 | 3.4591(11) |  | O5 | K112 | 2.671(2) |
| K1 | O15 | 2.9452(19) |  | O5 | S2 | 1.479(3) |
| K1 | O1W | 2.962(2) |  | O6 | Ca113 | 2.703(3) |
| K1 | O26 | 2.900(2) |  | O6 | K113 | 2.745(2) |
| K1 | O27 | 2.858(2) |  | O6 | K114 | 2.745(2) |
| K1 | O37 | 2.955(2) |  | O6 | S2 | 1.470(3) |
| K1 | O38 | 2.850(2) |  | S1 | K111 | 3.3371(9) |
| K1 | O43 | 3.3844(19) |  | S1 | K112 | 3.7717(9) |
| K1 | O58 | 2.671(2) |  | S1 | K16 | 3.4703(9) |
| K1 | O64 | 2.745(2) |  | S1 | K110 | 3.3371(9) |
| K1 | S17 | 3.3371(9) |  | S1 | K19 | 3.4703(9) |
| K1 | S16 | 3.4703(9) |  | S1 | K18 | 3.7717(10) |
| O1 | K19 | 2.9452(19) |  | S1 | O11 | 1.4814(18) |
| O1 | S1 | 1.4814(18) |  | S2 | Ca113 | 3.1267(10) |
| O1W | K11 | 2.962(2) |  | S2 | K18 | 3.6156(9) |
| O2 | K110 | 2.858(2) |  | S2 | K112 | 3.6156(9) |
| O2 | K16 | 2.900(2) |  | S2 | O41 | 1.4780(18) |
| O2 | K19 | 2.900(2) |  |  |  |  |

1+X,1/2-Y,+Z; 21-X,1-Y,1-Z; 31-X,-1/2+Y,1-Z; 41+X,+Y,+Z; 52-X,-1/2+Y,1-Z; 62-X,-Y,1-Z; 7+X,+Y,-1+Z; 81-X,-Y,1-Z; 92-X,1/2+Y,1-Z; 10+X,+Y,1+Z; 11+X,1/2-Y,1+Z; 121-X,1/2+Y,1-Z; 13-1+X,+Y,+Z; 14-1+X,1/2-Y,+Z

Table S9. Values of valence angles for syngenite [ º].

| Atom | Atom | Atom | Angle/˚ |  | Atom | Atom | Atom | Angle/˚ |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
| O11 | Ca1 | O1 | 55.41(8) |  | S17 | K1 | O44 | 152.57(4) |
| O1 | Ca1 | O62 | 122.82(6) |  | S17 | K1 | S15 | 98.11(2) |
| O11 | Ca1 | O62 | 122.82(6) |  | Ca1 | O1 | K19 | 101.56(6) |
| O1 | Ca1 | S1 | 27.71(4) |  | S1 | O1 | Ca1 | 99.23(9) |
| O11 | Ca1 | S1 | 27.71(4) |  | S1 | O1 | K19 | 97.74(9) |
| O11 | Ca1 | S2 | 87.83(5) |  | Ca1 | O1W | K11 | 102.62(8) |
| O11 | Ca1 | S22 | 98.61(5) |  | Ca1 | O1W | K1 | 102.62(8) |
| O1 | Ca1 | S2 | 87.83(5) |  | K11 | O1W | K1 | 71.46(6) |
| O1 | Ca1 | S22 | 98.61(5) |  | K19 | O2 | K15 | 78.31(7) |
| O1W | Ca1 | O11 | 148.16(5) |  | K110 | O2 | K15 | 101.60(2) |
| O1W | Ca1 | O1 | 148.16(5) |  | K111 | O2 | K19 | 101.60(2) |
| O1W | Ca1 | O41 | 78.15(7) |  | K111 | O2 | K15 | 164.88(10) |
| O1W | Ca1 | O4 | 78.15(7) |  | K111 | O2 | K110 | 74.48(7) |
| O1W | Ca1 | O62 | 68.61(8) |  | K110 | O2 | K19 | 164.88(10) |
| O1W | Ca1 | S1 | 162.93(7) |  | S1 | O2 | K19 | 99.66(11) |
| O1W | Ca1 | S2 | 76.09(6) |  | S1 | O2 | K111 | 95.27(11) |
| O1W | Ca1 | S22 | 96.63(6) |  | S1 | O2 | K15 | 99.66(11) |
| O43 | Ca1 | O11 | 129.48(6) |  | S1 | O2 | K110 | 95.27(11) |
| O41 | Ca1 | O11 | 75.05(6) |  | K18 | O3 | K110 | 96.08(3) |
| O4 | Ca1 | O1 | 75.05(6) |  | K111 | O3 | K110 | 71.66(7) |
| O41 | Ca1 | O1 | 100.28(6) |  | K18 | O3 | K112 | 79.98(7) |
| O44 | Ca1 | O1 | 129.48(6) |  | K18 | O3 | K111 | 149.14(10) |
| O4 | Ca1 | O11 | 100.28(6) |  | K112 | O3 | K110 | 149.14(10) |
| O43 | Ca1 | O1 | 74.35(6) |  | K112 | O3 | K111 | 96.08(3) |
| O44 | Ca1 | O11 | 74.35(6) |  | S1 | O3 | K112 | 117.68(11) |
| O43 | Ca1 | O1W | 80.12(5) |  | S1 | O3 | K110 | 91.43(11) |
| O44 | Ca1 | O1W | 80.12(5) |  | S1 | O3 | K111 | 91.43(11) |
| O43 | Ca1 | O4 | 68.65(7) |  | S1 | O3 | K18 | 117.68(11) |
| O44 | Ca1 | O41 | 68.65(7) |  | Ca13 | O4 | Ca1 | 111.35(7) |
| O41 | Ca1 | O4 | 56.00(8) |  | Ca13 | O4 | K112 | 92.04(5) |
| O44 | Ca1 | O43 | 153.70(9) |  | Ca1 | O4 | K112 | 114.95(6) |
| O44 | Ca1 | O4 | 123.38(5) |  | S2 | O4 | Ca13 | 147.00(11) |
| O43 | Ca1 | O41 | 123.38(5) |  | S2 | O4 | Ca1 | 98.87(9) |
| O44 | Ca1 | O62 | 78.36(4) |  | S2 | O4 | K112 | 86.76(8) |
| O4 | Ca1 | O62 | 136.45(6) |  | Ca113 | O5 | K18 | 114.24(7) |
| O41 | Ca1 | O62 | 136.45(6) |  | Ca113 | O5 | K112 | 114.24(7) |
| O43 | Ca1 | O62 | 78.36(4) |  | K112 | O5 | K18 | 86.59(8) |
| O43 | Ca1 | S1 | 102.00(4) |  | S2 | O5 | Ca113 | 104.90(14) |
| O4 | Ca1 | S1 | 86.80(5) |  | S2 | O5 | K112 | 118.37(9) |
| O44 | Ca1 | S1 | 102.00(4) |  | S2 | O5 | K18 | 118.37(9) |
| O41 | Ca1 | S1 | 86.80(5) |  | Ca113 | O6 | K114 | 102.34(7) |
| O43 | Ca1 | S2 | 95.96(4) |  | Ca113 | O6 | K113 | 102.34(7) |
| O41 | Ca1 | S22 | 151.25(4) |  | K113 | O6 | K114 | 78.11(7) |
| O43 | Ca1 | S22 | 82.61(4) |  | S2 | O6 | Ca113 | 92.24(13) |
| O4 | Ca1 | S2 | 28.00(4) |  | S2 | O6 | K114 | 137.53(6) |
| O4 | Ca1 | S22 | 151.25(4) |  | S2 | O6 | K113 | 137.53(6) |
| O44 | Ca1 | S22 | 82.61(4) |  | Ca1 | S1 | K18 | 92.12(2) |
| O44 | Ca1 | S2 | 95.96(4) |  | Ca1 | S1 | K15 | 80.06(2) |
| O41 | Ca1 | S2 | 28.00(4) |  | Ca1 | S1 | K110 | 148.762(12) |
| O52 | Ca1 | O11 | 74.59(7) |  | Ca1 | S1 | K111 | 148.762(12) |
| O52 | Ca1 | O1 | 74.59(7) |  | Ca1 | S1 | K112 | 92.12(2) |
| O52 | Ca1 | O1W | 123.83(9) |  | Ca1 | S1 | K19 | 80.06(2) |
| O52 | Ca1 | O44 | 88.36(5) |  | K111 | S1 | K110 | 62.43(2) |
| O52 | Ca1 | O4 | 145.86(6) |  | K19 | S1 | K18 | 171.51(3) |
| O52 | Ca1 | O41 | 145.86(6) |  | K15 | S1 | K112 | 171.51(3) |
| O52 | Ca1 | O43 | 88.36(5) |  | K111 | S1 | K15 | 113.95(3) |
| O52 | Ca1 | O62 | 55.22(8) |  | K111 | S1 | K19 | 81.89(2) |
| O52 | Ca1 | S1 | 73.25(6) |  | K19 | S1 | K112 | 118.462(16) |
| O52 | Ca1 | S22 | 27.20(6) |  | K18 | S1 | K112 | 58.10(2) |
| O52 | Ca1 | S2 | 160.08(7) |  | K111 | S1 | K18 | 103.65(2) |
| O62 | Ca1 | S1 | 128.46(6) |  | K110 | S1 | K112 | 103.65(2) |
| O62 | Ca1 | S2 | 144.70(6) |  | K110 | S1 | K15 | 81.89(2) |
| O62 | Ca1 | S22 | 28.02(6) |  | K19 | S1 | K15 | 63.70(2) |
| S2 | Ca1 | S1 | 86.84(3) |  | K111 | S1 | K112 | 74.495(19) |
| S22 | Ca1 | S1 | 100.44(3) |  | K110 | S1 | K18 | 74.495(19) |
| S2 | Ca1 | S22 | 172.72(4) |  | K110 | S1 | K19 | 113.95(3) |
| K11 | K1 | S15 | 121.851(12) |  | K15 | S1 | K18 | 118.462(16) |
| O16 | K1 | K11 | 102.70(4) |  | O1 | S1 | Ca1 | 53.06(8) |
| O16 | K1 | O1W | 138.43(6) |  | O11 | S1 | Ca1 | 53.05(8) |
| O16 | K1 | O37 | 128.20(6) |  | O1 | S1 | K19 | 57.24(8) |
| O16 | K1 | O44 | 100.04(5) |  | O11 | S1 | K111 | 158.07(8) |
| O16 | K1 | S15 | 25.02(4) |  | O11 | S1 | K110 | 95.71(8) |
| O16 | K1 | S17 | 102.49(4) |  | O1 | S1 | K15 | 107.59(8) |
| O1W | K1 | K11 | 54.27(3) |  | O11 | S1 | K15 | 57.24(8) |
| O1W | K1 | O44 | 59.19(5) |  | O1 | S1 | K18 | 115.26(8) |
| O1W | K1 | S15 | 162.19(6) |  | O11 | S1 | K18 | 69.56(8) |
| O1W | K1 | S17 | 93.42(5) |  | O1 | S1 | K112 | 69.56(8) |
| O25 | K1 | K11 | 129.16(3) |  | O11 | S1 | K112 | 115.26(8) |
| O27 | K1 | K11 | 52.76(3) |  | O11 | S1 | K19 | 107.59(8) |
| O25 | K1 | O16 | 49.03(6) |  | O1 | S1 | K110 | 158.07(8) |
| O27 | K1 | O16 | 79.49(6) |  | O1 | S1 | K111 | 95.71(8) |
| O25 | K1 | O1W | 172.51(7) |  | O1 | S1 | O11 | 106.07(15) |
| O27 | K1 | O1W | 102.69(5) |  | O2 | S1 | Ca1 | 126.42(12) |
| O27 | K1 | O25 | 78.40(2) |  | O2 | S1 | K110 | 58.52(9) |
| O27 | K1 | O37 | 49.08(7) |  | O2 | S1 | K112 | 132.91(9) |
| O25 | K1 | O37 | 105.96(7) |  | O2 | S1 | K19 | 55.47(8) |
| O27 | K1 | O44 | 152.04(5) |  | O2 | S1 | K111 | 58.52(9) |
| O25 | K1 | O44 | 122.53(5) |  | O2 | S1 | K18 | 132.91(9) |
| O25 | K1 | S15 | 24.87(5) |  | O2 | S1 | K15 | 55.47(8) |
| O27 | K1 | S17 | 26.21(5) |  | O2 | S1 | O1 | 109.98(10) |
| O27 | K1 | S15 | 82.59(5) |  | O2 | S1 | O11 | 109.98(10) |
| O25 | K1 | S17 | 84.39(5) |  | O3 | S1 | Ca1 | 124.20(12) |
| O37 | K1 | K11 | 54.17(3) |  | O3 | S1 | K111 | 62.26(9) |
| O38 | K1 | K11 | 129.99(4) |  | O3 | S1 | K18 | 41.99(8) |
| O38 | K1 | O16 | 126.00(5) |  | O3 | S1 | K19 | 141.72(6) |
| O38 | K1 | O1W | 89.16(6) |  | O3 | S1 | K110 | 62.26(9) |
| O37 | K1 | O1W | 70.19(7) |  | O3 | S1 | K112 | 41.99(8) |
| O38 | K1 | O25 | 83.98(6) |  | O3 | S1 | K15 | 141.72(6) |
| O38 | K1 | O27 | 120.57(7) |  | O3 | S1 | O11 | 110.70(10) |
| O38 | K1 | O37 | 83.92(3) |  | O3 | S1 | O1 | 110.70(10) |
| O37 | K1 | O44 | 127.56(6) |  | O3 | S1 | O2 | 109.39(16) |
| O38 | K1 | O44 | 82.62(6) |  | Ca1 | S2 | Ca113 | 172.72(4) |
| O38 | K1 | S15 | 102.90(4) |  | Ca1 | S2 | K18 | 95.72(2) |
| O37 | K1 | S17 | 26.31(5) |  | Ca113 | S2 | K18 | 78.03(2) |
| O37 | K1 | S15 | 123.53(5) |  | Ca1 | S2 | K112 | 95.72(2) |
| O38 | K1 | S17 | 96.44(5) |  | Ca113 | S2 | K112 | 78.03(2) |
| O44 | K1 | K11 | 101.06(3) |  | K112 | S2 | K18 | 60.86(2) |
| O44 | K1 | S15 | 108.86(4) |  | O4 | S2 | Ca1 | 53.13(7) |
| O58 | K1 | K11 | 133.29(4) |  | O41 | S2 | Ca113 | 126.42(7) |
| O58 | K1 | O16 | 64.35(6) |  | O41 | S2 | Ca1 | 53.13(7) |
| O58 | K1 | O1W | 104.27(7) |  | O4 | S2 | Ca113 | 126.42(7) |
| O58 | K1 | O25 | 78.00(7) |  | O41 | S2 | K112 | 117.03(8) |
| O58 | K1 | O27 | 143.84(7) |  | O41 | S2 | K18 | 69.16(8) |
| O58 | K1 | O37 | 166.37(7) |  | O4 | S2 | K112 | 69.16(8) |
| O58 | K1 | O38 | 83.55(7) |  | O4 | S2 | K18 | 117.03(8) |
| O58 | K1 | O44 | 45.09(6) |  | O41 | S2 | O4 | 106.24(14) |
| O58 | K1 | O62 | 82.47(5) |  | O41 | S2 | O5 | 109.42(10) |
| O58 | K1 | S17 | 162.30(5) |  | O4 | S2 | O5 | 109.42(10) |
| O58 | K1 | S15 | 64.85(5) |  | O5 | S2 | Ca1 | 124.82(11) |
| O62 | K1 | K11 | 50.94(4) |  | O5 | S2 | Ca113 | 47.90(10) |
| O62 | K1 | O16 | 77.25(6) |  | O5 | S2 | K18 | 40.53(7) |
| O62 | K1 | O1W | 61.34(7) |  | O5 | S2 | K112 | 40.53(7) |
| O62 | K1 | O27 | 89.82(6) |  | O6 | S2 | Ca1 | 127.54(11) |
| O62 | K1 | O25 | 126.15(7) |  | O6 | S2 | Ca113 | 59.74(11) |
| O62 | K1 | O38 | 142.66(8) |  | O6 | S2 | K18 | 128.20(9) |
| O62 | K1 | O37 | 104.55(5) |  | O6 | S2 | K112 | 128.20(9) |
| O62 | K1 | O44 | 63.19(6) |  | O6 | S2 | O4 | 112.04(10) |
| O62 | K1 | S17 | 107.00(4) |  | O6 | S2 | O41 | 112.04(10) |
| O62 | K1 | S15 | 102.08(5) |  | O6 | S2 | O5 | 107.64(15) |
| S17 | K1 | K11 | 58.783(12) |  |  |  |  |  |

1+X,1/2-Y,+Z; 21+X,+Y,+Z; 31-X,1-Y,1-Z; 41-X,-1/2+Y,1-Z; 52-X,-Y,1-Z; 62-X,-1/2+Y,1-Z; 7+X,+Y,-1+Z; 81-X,-Y,1-Z; 92-X,1/2+Y,1-Z; 10+X,+Y,1+Z; 11+X,1/2-Y,1+Z; 121-X,1/2+Y,1-Z; 13-1+X,+Y,+Z; 14-1+X,1/2-Y,+Z

Table S10. Values of torsion angles for syngenite [ º].

| A | B | C | D | Angle/˚ |  | A | B | C | D | Angle/˚ |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| Ca1 | O1 | S1 | K11 | 179.66(5) |  | K16 | O2 | S1 | O1 | 159.20(9) |
| Ca1 | O1 | S1 | K12 | -72.32(8) |  | K11 | O2 | S1 | O3 | -37.43(4) |
| Ca1 | O1 | S1 | K13 | -109.25(7) |  | K15 | O2 | S1 | O3 | -140.17(5) |
| Ca1 | O1 | S1 | K14 | 62.29(7) |  | K16 | O2 | S1 | O3 | 37.43(4) |
| Ca1 | O1 | S1 | K15 | 103.12(8) |  | K14 | O2 | S1 | O3 | 140.17(5) |
| Ca1 | O1 | S1 | K16 | 175.32(17) |  | K11 | O3 | S1 | Ca1 | -144.16(3) |
| Ca1 | O1 | S1 | O17 | 2.25(15) |  | K16 | O3 | S1 | Ca1 | 144.16(4) |
| Ca1 | O1 | S1 | O2 | 121.13(11) |  | K12 | O3 | S1 | Ca1 | 46.53(9) |
| Ca1 | O1 | S1 | O3 | -117.88(12) |  | K13 | O3 | S1 | Ca1 | -46.53(9) |
| Ca18 | O4 | S2 | Ca1 | 156.5(2) |  | K13 | O3 | S1 | K15 | 75.1(2) |
| Ca18 | O4 | S2 | Ca19 | -32.6(2) |  | K12 | O3 | S1 | K15 | 168.13(6) |
| Ca1 | O4 | S2 | Ca19 | 170.94(5) |  | K13 | O3 | S1 | K14 | -168.13(6) |
| Ca1 | O4 | S2 | K12 | 75.94(8) |  | K16 | O3 | S1 | K14 | 22.56(16) |
| Ca18 | O4 | S2 | K12 | -127.57(17) |  | K11 | O3 | S1 | K14 | 94.25(10) |
| Ca1 | O4 | S2 | K13 | 114.76(7) |  | K11 | O3 | S1 | K15 | -22.56(16) |
| Ca18 | O4 | S2 | K13 | -88.76(19) |  | K16 | O3 | S1 | K15 | -94.25(10) |
| Ca18 | O4 | S2 | O47 | 157.94(11) |  | K13 | O3 | S1 | K12 | -93.06(18) |
| Ca1 | O4 | S2 | O47 | 1.45(16) |  | K13 | O3 | S1 | K11 | 97.63(6) |
| Ca1 | O4 | S2 | O5 | 119.49(11) |  | K11 | O3 | S1 | K16 | 71.69(7) |
| Ca18 | O4 | S2 | O5 | -84.0(2) |  | K12 | O3 | S1 | K11 | -169.32(12) |
| Ca18 | O4 | S2 | O6 | 35.3(2) |  | K16 | O3 | S1 | K11 | -71.69(7) |
| Ca1 | O4 | S2 | O6 | -121.20(11) |  | K16 | O3 | S1 | K13 | -169.32(12) |
| Ca19 | O5 | S2 | Ca1 | 180.000(0) |  | K12 | O3 | S1 | K13 | 93.06(18) |
| Ca19 | O5 | S2 | K13 | 128.80(9) |  | K12 | O3 | S1 | K16 | -97.63(6) |
| Ca19 | O5 | S2 | K12 | -128.80(9) |  | K11 | O3 | S1 | K12 | 169.32(12) |
| Ca19 | O5 | S2 | O4 | 121.99(9) |  | K12 | O3 | S1 | K14 | -75.1(2) |
| Ca19 | O5 | S2 | O47 | -121.99(9) |  | K13 | O3 | S1 | K16 | 169.32(12) |
| Ca19 | O5 | S2 | O6 | 0.000(1) |  | K16 | O3 | S1 | K12 | 97.63(6) |
| Ca19 | O6 | S2 | Ca1 | 180.000(0) |  | K11 | O3 | S1 | K13 | -97.63(6) |
| Ca19 | O6 | S2 | K13 | -40.13(6) |  | K12 | O3 | S1 | O1 | 105.19(10) |
| Ca19 | O6 | S2 | K12 | 40.13(6) |  | K11 | O3 | S1 | O1 | -85.49(11) |
| Ca19 | O6 | S2 | O47 | 120.35(9) |  | K13 | O3 | S1 | O1 | 12.13(15) |
| Ca19 | O6 | S2 | O4 | -120.35(9) |  | K11 | O3 | S1 | O17 | 157.18(9) |
| Ca19 | O6 | S2 | O5 | 0.000(1) |  | K16 | O3 | S1 | O17 | 85.49(11) |
| K15 | O1 | S1 | Ca1 | -103.12(8) |  | K16 | O3 | S1 | O1 | -157.18(9) |
| K15 | O1 | S1 | K11 | 76.53(5) |  | K12 | O3 | S1 | O17 | -12.13(15) |
| K15 | O1 | S1 | K16 | 72.2(2) |  | K13 | O3 | S1 | O17 | -105.19(10) |
| K15 | O1 | S1 | K14 | -40.83(7) |  | K13 | O3 | S1 | O2 | 133.47(9) |
| K15 | O1 | S1 | K12 | -175.45(3) |  | K11 | O3 | S1 | O2 | 35.84(3) |
| K15 | O1 | S1 | K13 | 147.63(7) |  | K12 | O3 | S1 | O2 | -133.47(9) |
| K15 | O1 | S1 | O17 | -100.87(11) |  | K16 | O3 | S1 | O2 | -35.84(4) |
| K15 | O1 | S1 | O2 | 18.01(13) |  | K13 | O4 | S2 | Ca19 | 56.18(8) |
| K15 | O1 | S1 | O3 | 139.00(11) |  | K13 | O4 | S2 | Ca1 | -114.76(7) |
| K14 | O2 | S1 | Ca1 | -39.83(5) |  | K13 | O4 | S2 | K12 | -38.82(6) |
| K16 | O2 | S1 | Ca1 | -142.57(4) |  | K13 | O4 | S2 | O47 | -113.30(10) |
| K11 | O2 | S1 | Ca1 | 142.57(4) |  | K13 | O4 | S2 | O5 | 4.73(11) |
| K15 | O2 | S1 | Ca1 | 39.83(5) |  | K13 | O4 | S2 | O6 | 124.04(11) |
| K11 | O2 | S1 | K15 | 102.742(16) |  | K12 | O5 | S2 | Ca19 | 128.80(9) |
| K16 | O2 | S1 | K13 | 78.95(4) |  | K13 | O5 | S2 | Ca19 | -128.80(9) |
| K11 | O2 | S1 | K16 | -74.85(8) |  | K13 | O5 | S2 | Ca1 | 51.20(9) |
| K15 | O2 | S1 | K16 | -177.60(8) |  | K12 | O5 | S2 | Ca1 | -51.20(9) |
| K11 | O2 | S1 | K14 | -177.60(9) |  | K12 | O5 | S2 | K13 | -102.40(19) |
| K15 | O2 | S1 | K13 | -98.64(12) |  | K13 | O5 | S2 | K12 | 102.40(18) |
| K14 | O2 | S1 | K15 | -79.66(9) |  | K13 | O5 | S2 | O47 | 109.22(10) |
| K16 | O2 | S1 | K15 | 177.60(9) |  | K13 | O5 | S2 | O4 | -6.81(15) |
| K15 | O2 | S1 | K14 | 79.66(9) |  | K12 | O5 | S2 | O47 | 6.81(15) |
| K15 | O2 | S1 | K12 | 178.30(4) |  | K12 | O5 | S2 | O4 | -109.22(10) |
| K14 | O2 | S1 | K16 | 102.742(16) |  | K13 | O5 | S2 | O6 | -128.80(9) |
| K15 | O2 | S1 | K11 | -102.742(16) |  | K12 | O5 | S2 | O6 | 128.80(9) |
| K14 | O2 | S1 | K11 | 177.60(9) |  | K19 | O6 | S2 | Ca19 | -111.07(18) |
| K14 | O2 | S1 | K12 | 98.64(12) |  | K110 | O6 | S2 | Ca1 | -68.93(18) |
| K16 | O2 | S1 | K11 | 74.85(8) |  | K19 | O6 | S2 | Ca1 | 68.93(18) |
| K16 | O2 | S1 | K14 | -102.742(16) |  | K110 | O6 | S2 | Ca19 | 111.07(18) |
| K11 | O2 | S1 | K13 | 4.10(11) |  | K110 | O6 | S2 | K13 | 70.9(2) |
| K11 | O2 | S1 | K12 | -78.95(4) |  | K19 | O6 | S2 | K12 | -70.9(2) |
| K14 | O2 | S1 | K13 | -178.30(4) |  | K19 | O6 | S2 | K13 | -151.20(13) |
| K16 | O2 | S1 | K12 | -4.10(11) |  | K110 | O6 | S2 | K12 | 151.20(13) |
| K11 | O2 | S1 | O1 | 84.35(11) |  | K19 | O6 | S2 | O47 | 9.3(2) |
| K15 | O2 | S1 | O1 | -18.40(12) |  | K19 | O6 | S2 | O4 | 128.58(17) |
| K14 | O2 | S1 | O1 | -98.06(9) |  | K110 | O6 | S2 | O4 | -9.3(2) |
| K16 | O2 | S1 | O17 | -84.35(11) |  | K110 | O6 | S2 | O47 | -128.58(17) |
| K15 | O2 | S1 | O17 | 98.06(9) |  | K19 | O6 | S2 | O5 | -111.07(18) |
| K14 | O2 | S1 | O17 | 18.39(12) |  | K110 | O6 | S2 | O5 | 111.07(18) |
| K11 | O2 | S1 | O17 | -159.20(9) |  |  |  |  |  |  |

1+X,1/2-Y,1+Z; 21-X,-Y,1-Z; 31-X,1/2+Y,1-Z; 42-X,-Y,1-Z; 52-X,1/2+Y,1-Z; 6+X,+Y,1+Z; 7+X,1/2-Y,+Z; 81-X,1-Y,1-Z; 9-1+X,+Y,+Z; 10-1+X,1/2-Y,+Z

Table S11. Bond lengths for picromerite [Å].

| Atom | Atom | Length/Å |  | Atom | Atom | Length/Å |
| --- | --- | --- | --- | --- | --- | --- |
| Mg1 | O1W1 | 2.1007(12) |  | K1 | O37 | 2.8485(14) |
| Mg1 | O1W | 2.1007(12) |  | K1 | O48 | 2.8016(13) |
| Mg1 | O2W1 | 2.0172(13) |  | K1 | S16 | 3.4343(6) |
| Mg1 | O2W | 2.0172(13) |  | K1 | S1 | 3.5743(5) |
| Mg1 | O3W1 | 2.0912(12) |  | O1 | S1 | 1.4800(13) |
| Mg1 | O3W | 2.0912(12) |  | O2 | K16 | 2.8981(14) |
| O1W | K12 | 2.9718(13) |  | O2 | S1 | 1.4697(13) |
| O3W | K13 | 3.0850(13) |  | O3 | K19 | 2.8485(14) |
| K1 | O1W4 | 2.9717(13) |  | O3 | K16 | 2.9028(13) |
| K1 | O3W5 | 3.0850(13) |  | O3 | S1 | 1.4827(13) |
| K1 | O1 | 2.7045(13) |  | O4 | K18 | 2.8016(13) |
| K1 | O2 | 3.3091(14) |  | O4 | S1 | 1.4843(12) |
| K1 | O26 | 2.8981(14) |  | S1 | K16 | 3.4343(6) |
| K1 | O36 | 2.9028(13) |  |  |  |  |

11-X,2-Y,1-Z; 21-X,1/2+Y,1/2-Z; 3+X,1+Y,+Z; 41-X,-1/2+Y,1/2-Z; 5+X,-1+Y,+Z; 6-X,1-Y,1-Z; 7-X,-1/2+Y,1/2-Z; 81-X,1-Y,1-Z; 9-X,1/2+Y,1/2-Z

Table S12. Values of valence angles for picromerite [ º].

| Atom | Atom | Atom | Angle/˚ |  | Atom | Atom | Atom | Angle/˚ |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
| O1W | Mg1 | O1W1 | 180.00(9) |  | O37 | K1 | O3W5 | 64.49(3) |
| O2W | Mg1 | O1W | 89.39(5) |  | O36 | K1 | O3W5 | 92.47(4) |
| O2W | Mg1 | O1W1 | 90.61(5) |  | O37 | K1 | O26 | 95.43(4) |
| O2W1 | Mg1 | O1W1 | 89.39(5) |  | O37 | K1 | O2 | 147.77(4) |
| O2W1 | Mg1 | O1W | 90.61(5) |  | O36 | K1 | O2 | 86.12(3) |
| O2W | Mg1 | O2W1 | 180.0 |  | O37 | K1 | O36 | 104.27(3) |
| O2W | Mg1 | O3W | 90.44(5) |  | O36 | K1 | S16 | 25.32(3) |
| O2W1 | Mg1 | O3W1 | 90.44(5) |  | O37 | K1 | S16 | 106.26(3) |
| O2W | Mg1 | O3W1 | 89.56(5) |  | O37 | K1 | S1 | 126.22(3) |
| O2W1 | Mg1 | O3W | 89.56(5) |  | O36 | K1 | S1 | 106.03(3) |
| O3W1 | Mg1 | O1W1 | 90.35(5) |  | O48 | K1 | O1W4 | 85.19(4) |
| O3W | Mg1 | O1W1 | 89.65(5) |  | O48 | K1 | O3W5 | 76.88(4) |
| O3W1 | Mg1 | O1W | 89.65(5) |  | O48 | K1 | O2 | 69.83(4) |
| O3W | Mg1 | O1W | 90.35(5) |  | O48 | K1 | O26 | 118.14(4) |
| O3W | Mg1 | O3W1 | 180.0 |  | O48 | K1 | O36 | 85.16(4) |
| Mg1 | O1W | K12 | 137.71(5) |  | O48 | K1 | O37 | 140.37(4) |
| Mg1 | O3W | K13 | 128.09(5) |  | O48 | K1 | S16 | 98.30(3) |
| O1W4 | K1 | O3W5 | 78.52(3) |  | O48 | K1 | S1 | 85.67(3) |
| O1W4 | K1 | O2 | 97.08(3) |  | S16 | K1 | S1 | 85.511(13) |
| O1W4 | K1 | S16 | 164.99(3) |  | S1 | O1 | K1 | 114.12(7) |
| O1W4 | K1 | S1 | 80.18(3) |  | K16 | O2 | K1 | 111.86(4) |
| O3W5 | K1 | O2 | 146.68(4) |  | S1 | O2 | K16 | 98.34(7) |
| O3W5 | K1 | S16 | 116.48(3) |  | S1 | O2 | K1 | 88.03(6) |
| O3W5 | K1 | S1 | 153.41(3) |  | K19 | O3 | K16 | 122.48(5) |
| O1 | K1 | O1W4 | 72.32(4) |  | S1 | O3 | K16 | 97.81(6) |
| O1 | K1 | O3W5 | 150.36(4) |  | S1 | O3 | K19 | 126.12(7) |
| O1 | K1 | O2 | 45.69(4) |  | S1 | O4 | K18 | 122.95(7) |
| O1 | K1 | O26 | 73.23(4) |  | K16 | S1 | K1 | 94.489(13) |
| O1 | K1 | O36 | 117.14(4) |  | O1 | S1 | K16 | 105.96(5) |
| O1 | K1 | O37 | 104.02(4) |  | O1 | S1 | K1 | 43.68(5) |
| O1 | K1 | O48 | 105.39(4) |  | O1 | S1 | O3 | 108.11(7) |
| O1 | K1 | S16 | 92.70(3) |  | O1 | S1 | O4 | 110.06(7) |
| O1 | K1 | S1 | 22.21(3) |  | O2 | S1 | K1 | 67.71(6) |
| O26 | K1 | O1W4 | 142.51(4) |  | O2 | S1 | K16 | 56.61(6) |
| O26 | K1 | O3W5 | 132.62(4) |  | O2 | S1 | O1 | 108.93(8) |
| O26 | K1 | O2 | 68.14(4) |  | O2 | S1 | O3 | 109.77(8) |
| O26 | K1 | O36 | 49.20(4) |  | O2 | S1 | O4 | 110.22(8) |
| O26 | K1 | S1 | 73.43(3) |  | O3 | S1 | K1 | 136.21(5) |
| O2 | K1 | S16 | 70.79(2) |  | O3 | S1 | K16 | 56.87(5) |
| O26 | K1 | S16 | 25.05(3) |  | O3 | S1 | O4 | 109.72(7) |
| O2 | K1 | S1 | 24.26(2) |  | O4 | S1 | K16 | 143.97(5) |
| O36 | K1 | O1W4 | 168.07(4) |  | O4 | S1 | K1 | 111.80(5) |
| O37 | K1 | O1W4 | 79.06(4) |  |  |  |  |  |

11-X,2-Y,1-Z; 21-X,1/2+Y,1/2-Z; 3+X,1+Y,+Z; 41-X,-1/2+Y,1/2-Z; 5+X,-1+Y,+Z; 6-X,1-Y,1-Z; 7-X,-1/2+Y,1/2-Z; 81-X,1-Y,1-Z; 9-X,1/2+Y,1/2-Z

Table S13. Values of torsion angles for picromerite [ º].

| A | B | C | D | Angle/˚ |  | A | B | C | D | Angle/˚ |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| K1 | O1 | S1 | K11 | -79.53(6) |  | K12 | O3 | S1 | K11 | -140.45(9) |
| K1 | O1 | S1 | O2 | -20.00(9) |  | K11 | O3 | S1 | K1 | 56.91(8) |
| K1 | O1 | S1 | O3 | -139.23(7) |  | K12 | O3 | S1 | O1 | -42.86(10) |
| K1 | O1 | S1 | O4 | 100.95(8) |  | K11 | O3 | S1 | O1 | 97.59(7) |
| K11 | O2 | S1 | K1 | -111.81(5) |  | K12 | O3 | S1 | O2 | -161.56(8) |
| K1 | O2 | S1 | K11 | 111.81(5) |  | K11 | O3 | S1 | O2 | -21.11(8) |
| K1 | O2 | S1 | O1 | 14.79(7) |  | K11 | O3 | S1 | O4 | -142.37(6) |
| K11 | O2 | S1 | O1 | -97.02(7) |  | K12 | O3 | S1 | O4 | 77.18(9) |
| K1 | O2 | S1 | O3 | 132.98(6) |  | K13 | O4 | S1 | K1 | -80.66(7) |
| K11 | O2 | S1 | O3 | 21.17(8) |  | K13 | O4 | S1 | K11 | 53.22(12) |
| K11 | O2 | S1 | O4 | 142.13(6) |  | K13 | O4 | S1 | O1 | -127.57(8) |
| K1 | O2 | S1 | O4 | -106.06(6) |  | K13 | O4 | S1 | O2 | -7.40(10) |
| K12 | O3 | S1 | K1 | -83.54(9) |  | K13 | O4 | S1 | O3 | 113.59(8) |

1-X,1-Y,1-Z; 2-X,1/2+Y,1/2-Z; 31-X,1-Y,1-Z

Table S14. Bond lengths for subhydrate CaSO4·0.69H2O [Å].

| Atom | Atom | Length/Å |  | Atom | Atom | Length/Å |
| --- | --- | --- | --- | --- | --- | --- |
| Ca1 | Ca11 | 4.0958(4) |  | Ca1 | S17 | 3.17317(18) |
| Ca1 | O12 | 2.503(3) |  | O1 | Ca11 | 2.503(3) |
| Ca1 | O13 | 2.423(4) |  | O1 | S1 | 1.456(3) |
| Ca1 | O1 | 2.423(4) |  | O2 | Ca18 | 2.442(4) |
| Ca1 | O14 | 2.503(3) |  | O2 | Ca11 | 2.645(4) |
| Ca1 | O1W | 2.503(9) |  | O2 | S1 | 1.466(3) |
| Ca1 | O25 | 2.442(4) |  | S1 | Ca11 | 3.17317(17) |
| Ca1 | O22 | 2.645(4) |  | S1 | Ca19 | 3.17321(17) |
| Ca1 | O26 | 2.442(4) |  | S1 | O110 | 1.456(3) |
| Ca1 | O24 | 2.645(4) |  | S1 | O210 | 1.466(3) |
| Ca1 | S12 | 3.17321(17) |  |  |  |  |

11+Y-X,1-X,1/3+Z; 21-Y,+X-Y,-1/3+Z; 3-Y+X,-Y,4/3-Z; 41-X,-X+Y,5/3-Z; 51-Y+X,1-Y,4/3-Z; 6+X,-1+Y,+Z; 71-Y,+X-Y,2/3+Z; 8+X,1+Y,+Z; 91+Y-X,1-X,-2/3+Z; 10+Y,+X,1-Z

Table S15. Values of valence angles for CaSO4·0.69H2O [ º].

| Atom | Atom | Atom | Angle/˚ |  | Atom | Atom | Atom | Angle/˚ |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
| O1 | Ca1 | Ca11 | 34.38(7) |  | O25 | Ca1 | O14 | 69.37(12) |
| O12 | Ca1 | Ca11 | 108.34(8) |  | O25 | Ca1 | O12 | 82.67(13) |
| O13 | Ca1 | Ca11 | 124.78(12) |  | O26 | Ca1 | O14 | 82.67(13) |
| O14 | Ca1 | Ca11 | 83.06(7) |  | O26 | Ca1 | O1W | 140.23(8) |
| O13 | Ca1 | O12 | 117.30(9) |  | O25 | Ca1 | O1W | 140.23(8) |
| O1 | Ca1 | O12 | 78.32(13) |  | O25 | Ca1 | O22 | 87.89(13) |
| O14 | Ca1 | O12 | 143.6(2) |  | O26 | Ca1 | O25 | 79.55(16) |
| O1 | Ca1 | O14 | 117.30(9) |  | O26 | Ca1 | O24 | 87.89(13) |
| O13 | Ca1 | O14 | 78.32(13) |  | O25 | Ca1 | O24 | 122.91(10) |
| O13 | Ca1 | O1 | 131.6(2) |  | O26 | Ca1 | O22 | 122.91(10) |
| O1 | Ca1 | O1W | 65.78(11) |  | O24 | Ca1 | O22 | 141.52(16) |
| O13 | Ca1 | O1W | 65.78(11) |  | O24 | Ca1 | S17 | 27.30(7) |
| O1 | Ca1 | O22 | 96.63(11) |  | O26 | Ca1 | S17 | 85.20(9) |
| O1 | Ca1 | O25 | 152.43(14) |  | O22 | Ca1 | S17 | 151.78(9) |
| O14 | Ca1 | O22 | 142.79(10) |  | O22 | Ca1 | S12 | 27.29(7) |
| O1 | Ca1 | O26 | 75.18(13) |  | O24 | Ca1 | S12 | 151.78(9) |
| O13 | Ca1 | O24 | 96.63(11) |  | O25 | Ca1 | S17 | 95.81(9) |
| O13 | Ca1 | O26 | 152.43(14) |  | O26 | Ca1 | S12 | 95.81(9) |
| O1 | Ca1 | O24 | 67.30(11) |  | O25 | Ca1 | S12 | 85.20(9) |
| O13 | Ca1 | O25 | 75.18(13) |  | S17 | Ca1 | Ca11 | 58.669(17) |
| O14 | Ca1 | O24 | 53.80(11) |  | S12 | Ca1 | Ca11 | 120.855(13) |
| O13 | Ca1 | O22 | 67.30(11) |  | S17 | Ca1 | S12 | 178.69(8) |
| O12 | Ca1 | O22 | 53.80(11) |  | Ca1 | O1 | Ca11 | 112.50(12) |
| O12 | Ca1 | O24 | 142.79(10) |  | S1 | O1 | Ca11 | 103.35(19) |
| O13 | Ca1 | S17 | 86.56(7) |  | S1 | O1 | Ca1 | 142.45(19) |
| O14 | Ca1 | S17 | 26.51(8) |  | Ca18 | O2 | Ca11 | 107.18(11) |
| O12 | Ca1 | S17 | 154.42(9) |  | S1 | O2 | Ca11 | 96.84(19) |
| O1 | Ca1 | S12 | 86.56(7) |  | S1 | O2 | Ca18 | 136.8(2) |
| O13 | Ca1 | S12 | 92.90(7) |  | Ca11 | S1 | Ca19 | 178.69(8) |
| O12 | Ca1 | S12 | 26.51(8) |  | O1 | S1 | Ca11 | 50.14(14) |
| O1 | Ca1 | S17 | 92.90(7) |  | O110 | S1 | Ca11 | 128.91(15) |
| O14 | Ca1 | S12 | 154.42(9) |  | O110 | S1 | Ca19 | 50.14(14) |
| O1W | Ca1 | Ca11 | 71.91(4) |  | O1 | S1 | Ca19 | 128.91(15) |
| O1W | Ca1 | O14 | 108.20(10) |  | O1 | S1 | O110 | 111.6(3) |
| O1W | Ca1 | O12 | 108.20(10) |  | O1 | S1 | O210 | 111.43(18) |
| O1W | Ca1 | O22 | 70.76(8) |  | O110 | S1 | O210 | 106.0(2) |
| O1W | Ca1 | O24 | 70.76(8) |  | O110 | S1 | O2 | 111.43(18) |
| O1W | Ca1 | S12 | 89.34(4) |  | O1 | S1 | O2 | 106.0(2) |
| O1W | Ca1 | S17 | 89.34(4) |  | O2 | S1 | Ca11 | 55.86(15) |
| O22 | Ca1 | Ca11 | 128.12(8) |  | O2 | S1 | Ca19 | 125.04(16) |
| O24 | Ca1 | Ca11 | 34.72(8) |  | O210 | S1 | Ca19 | 55.86(15) |
| O26 | Ca1 | Ca11 | 71.69(8) |  | O210 | S1 | Ca11 | 125.04(16) |
| O25 | Ca1 | Ca11 | 142.34(9) |  | O2 | S1 | O210 | 110.5(3) |
| O26 | Ca1 | O12 | 69.37(12) |  |  |  |  |  |

11+Y-X,1-X,1/3+Z; 21-Y,+X-Y,-1/3+Z; 3-Y+X,-Y,4/3-Z; 41-X,-X+Y,5/3-Z; 5+X,-1+Y,+Z; 61-Y+X,1-Y,4/3-Z; 71-Y,+X-Y,2/3+Z; 8+X,1+Y,+Z; 91+Y-X,1-X,-2/3+Z; 10+Y,+X,1-Z

Table S16. Values of torsion angles for CaSO4·069H2O [ º].

| A | B | C | D | Angle/˚ |  | A | B | C | D | Angle/˚ |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| Ca1 | O1 | S1 | Ca11 | -162.5(5) |  | Ca14 | O2 | S1 | Ca12 | 54.6(3) |
| Ca1 | O1 | S1 | Ca12 | 18.6(5) |  | Ca14 | O2 | S1 | Ca11 | -124.2(3) |
| Ca11 | O1 | S1 | Ca12 | -178.84(7) |  | Ca11 | O2 | S1 | Ca12 | 178.85(7) |
| Ca11 | O1 | S1 | O13 | -123.31(19) |  | Ca11 | O2 | S1 | O1 | 1.7(2) |
| Ca1 | O1 | S1 | O13 | 74.1(4) |  | Ca11 | O2 | S1 | O13 | 123.31(19) |
| Ca11 | O1 | S1 | O23 | 118.41(19) |  | Ca14 | O2 | S1 | O1 | -122.6(3) |
| Ca11 | O1 | S1 | O2 | -1.8(2) |  | Ca14 | O2 | S1 | O13 | -0.9(4) |
| Ca1 | O1 | S1 | O23 | -44.1(5) |  | Ca11 | O2 | S1 | O23 | -119.16(17) |
| Ca1 | O1 | S1 | O2 | -164.4(4) |  | Ca14 | O2 | S1 | O23 | 116.6(3) |

11+Y-X,1-X,1/3+Z; 21+Y-X,1-X,-2/3+Z; 3+Y,+X,1-Z; 4+X,1+Y,+Z