S2. Material outputs and energy consumption for the off-site treatment of 1 tonne of slags from MSWI. 
	Parameter
	
	Unit

	Outputs
	
	

	Aluminum scrap 
	13.3
	kg

	Iron scrap
	78.1
	kg

	Inert material
	751
	kg

	Water
	70
	kg

	Waste to landfill
	87.6
	kg

	Energy consumption
	
	

	Electricity 
	4
	kWh
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