Supplementary Material

Comparison of three different zeolites to activate peroxymonosulfate for the degradation of the pharmaceutical ciprofloxacin in water

Efraím A. Serna-Galvisa,b, Carlos Mendoza-Merlanob, Johana Arboleda-Echavarríab,c, Ricardo A. Torres-Palmaa, Adriana Echavarría-Isazab,*

a Grupo de Investigación en Remediación Ambiental y Biocatálisis (GIRAB), Instituto de Química, Facultad de Ciencias Exactas y Naturales, Universidad de Antioquia UdeA, Calle 70 # 52-21, Medellín, Colombia

b Grupo de Catalizadores y Adsorbentes (CATALAD), Instituto de Química, Facultad de Ciencias Exactas y Naturales, Universidad de Antioquia UdeA, Calle 70 # 52-21, Medellín, Colombia

c Escuela de Microbiología, Universidad de Antioquia UdeA, Calle 70 # 52-21, Medellín, Colombia

*Corresponding author: adriana.echavarria@udea.edu.co

Supplementary figures

A

B

C

Fig. S1. Determination of the basicity of the considered zeolites by CO2 adsorption (TPD-CO2 results). A. ZY, B. ZB, and C. CP814C*.

A

B

Fig. S2. Structures of the target pollutants A. Methyl Orange (MO).

B. Ciprofloxacin (CIP) and its pKa1.

Supplementary tables

Table S1. Elemental composition of ZY.

| Element | Si | Al | Na | O |
| --- | --- | --- | --- | --- |
| Weight Composition (%) | 20.7 | 8.3 | 14.1 | 56.9 |

Table S2.  Oxygen surface composition (percentage) for the basic groups on the ZY surface before and after interaction with PMS.

| Zeolite* | Al-O- | Si-O- |
| --- | --- | --- |
| ZY before interaction | 40.0 | 20.7 |
| ZY after interaction | 33.4 | 8.8 |

*Before the interaction with PMS, the AlO- and SiO-

moieties on ZY have Na+ as compensation cations.

Fig. S3. Degradation of MO by the ZY/PMS system at different initial pHs. Experimental conditions: [Zeolite]= 0.2 g L-1, [PMS]= 500 µmol L-1, and [MO]= 30.6 µmol L-1, pH nat: 5.6.

Fig. S4.  Spectra of methyl orange solution without treatment (MO) and after 10 min of the treatment using the ZY/PMS system (MO treated by ZY/PMS).

Fig. S5. Reuse cycles for the MO treatment by ZY/PMS. Experimental conditions: [Z4A]= 0.2 g L-1, [PMS]= 500 µmol L-1, and [MO]= 30.6 µmol L-1.

Table S3. Composition of the simulated hospital wastewater (HWW).

| Component | Concentration (mg L-1) |  | Concentration (µmol L-1) |  |  |
| --- | --- | --- | --- | --- | --- |
| NaCl |  | 76 |  | 1300 |
| NH4Cl |  | 50 |  | 940 |
| Na2SO4 |  | 100.5 |  | 710 |
| KCl |  | 100 |  | 1340 |
| KH2PO4 |  | 50 |  | 370 |
| CaCl2-2H2O |  | 50 |  | 340 |
| Urea |  | 1260 |  | 2100 |
| pH |  | 6.5 |  |  |