Table S1: Summary of prepared and tested specimens in stage 1.

| Samples | DSM 33 OD600=5 [ml] | DSM 33 OD600=2.5 [ml] | pH adjusted to 6.8 ± 0.2 (1M HCl) [ml] | MICP solutiona [ml] |
| --- | --- | --- | --- | --- |
| WCF-G-01 | 10+10b | - | - | 10 |
| WCF-G-02 | - | 10+10b | - | 10 |
| WCF-G-03 | 10 | - | 2 | 10 |
| WCF-G-04 | 10+10b | - | 2 | 10 |
| WCF-G-05 | - | 10+10b | 2 | 10 |

a solutions were added consistently every 48 to 72 hours

b repeated addition of bacterial suspension

Table S2: Summary of prepared and tested specimens in stage 2.

| Samples | MICP treatment | DSM 33 OD600=5 [ml] | Salineb [ml] | MICP (biocementation) solutionc [ml] |
| --- | --- | --- | --- | --- |
| WCF-G14 | 14 days | 10 | - | 10 |
| WCF-G30 | 30 days | 10 | - | 10 |
| WCF-G60 | 60 days | 10 | - | 10 |
| WCF-G90 | 90 days | 10 | - | 10 |
| WCF-H14 | 14 days | 10 | - | 10 |
| WCF-H30 | 30 days | 10 | - | 10 |
| WCF-H60 | 60 days | 10 | - | 10 |
| WCF-H90 | 90 days | 10 |  | 10 |
| WCF-S-G90a | 90 days | - | 10 | - |
| WCF-S-H90a | 90 days | - | 10 | - |

a  sterile samples

b, c solutions were added consistently every 48 to 72 hours

Table S3: Classification of samples based on their compactness.

| Samples | 1 | 2 | 3 |
| --- | --- | --- | --- |
| WCF-G-01 | Medium | Medium | Poor |
| WCF-G-02 | Poor | Poor | Poor |
| WCF-G-03 | Medium | Poor | High |
| WCF-G-04 | Poor | Poor | Poor |
| WCF-G-05 | Poor | Poor | Poor |

Table S4: Classification of samples based on their compactness.

| Samples | 1 | 2 | 3 | 4 | 5 | 6 |
| --- | --- | --- | --- | --- | --- | --- |
| WCF-S-G90 | Poor | Poor | Poor | Poor | Poor | Poor |
| WCF-G14 | Poor | Poor | Poor | Medium | Poor | Poor |
| WCF-G30 | Poor | Poor | Medium | Medium | Medium | Medium |
| WCF-G60 | Medium | Medium | Medium | Poor | Poor | Medium |
| WCF-G90 | Medium | Medium | Poor | Poor | Medium | Medium |
| WCF-S-H90 | Medium | Medium | Medium | Medium | Medium | Medium |
| WCF-H14 | High | High | High | Medium | Medium | Medium |
| WCF-H30 | High | High | High | Medium | Medium | High |
| WCF-H60 | High | Medium | High | High | High | High |
| WCF-H90 | Medium | High | High | High | High | High |