Supplementary data for

Synthesis of Metal Organic Framework-based Hydrogel for Microplastics Removal from Aquatic Environments

Thi Trang Luu1,2, Shudi Mao1, Dai Quyet Truong1, Yihan Shi1, Thi Ngoc Oanh Duon1, Qiang Fu1, Van Manh Do3, Saravanamuthu Vigneswaran1, Tien Vinh Nguyen1*

1Faculty of Engineering and IT, University of Technology Sydney (UTS), Sydney, NSW 2007, Australia

2Faculty of Urban Infrastructure and Environment Engineering, Hanoi Architectural University, Hanoi, 100000, Vietnam

3Institute of Science and Technology for Energy and Environment, Vietnam Academy of Science and Technology (VAST), Hanoi, 100000, Vietnam

*Correspondence: tien.nguyen@uts.edu.au

Table

Table S1 Quantitative comparison of the most intense diffraction peak of ZIF-8.1 and ZIF-8.2.

| Sample | Peak position (2Ɵ/ o) | Peak intensity (a.u.) | FWHM (o) |
| --- | --- | --- | --- |
| ZIF-8.1 | 17.66 | 18.38 | 0.18 |
| ZIF-8.2 | 12.66 | 12.73 | 0.42 |

Table S2 Cost estimation for the lab-scale filtration column (Filtration rate: 1.7 m h⁻¹; Each hydrogel filter: used for 6 cycles, 4 hours/cycle before being replaced; Total volume of filtrated water/year:10.5 m3)

| (1) Chemical cost for 40g product (1 year operation) | Price (AUD) |  | (2) Energy consumption for material fabrication (0.35AUD/kWh) |  | Price (AUD) |  |
| --- | --- | --- | --- | --- | --- | --- |
| ZIF preparation | 0.80 |  | ZIF preparation |  | 0.01 |  |
| 10 wt% PVA solution | 0.66 |  | 10 wt% PVA solution |  | 0.01 |  |
| PEGDA | 0.31 |  | Hydrogel mixture |  | 0.01 |  |
| LAP | 0.01 |  | UV irradiation (for 365 pieces) |  | 1.28 |  |
| Total (1) | 1.78 |  | Total (2) | 1.31 |  |  |
| Treatment cost/annual: (1) + (2): 3.09 AUD |  |  |  |  |  |  |
| Treatment cost/m3 treated water: 0.3 AUD |  |  |  |  |  |  |

Figure

Fig. S1. Preparing the laundry wastewater with high strength MPs

Fig. S2. Microplastics analysis using the PerkinElmer Spectrum 3 FTIR spectrometer equipped with a Spotlight 200i microscope (PerkinElmer, USA) ng

Fig. S3. XRD patterns of (a) ZIF-8.1 and (b) ZIF-8.2 synthesized under different HMIM:Zn molar ratios. The original diffraction patterns are presented separately for clarity, while the overlaid comparison is shown in Figure 1 of the main manuscript.

Fig. S4. Photographs of the ZIF-based hydrogel before and after freeze-drying. The freeze-dried material can be stored under ambient conditions without special preservation

.

Fig. S5. Photograph of the laboratory-scale fixed-bed column setup employed to evaluate the microplastic removal performance of the ZIF-8/hydrogel composite under continuous-flow condition

Fig. S6. SEM-EDS elemental mapping of ZIF-8.1@H6mg hydrogel composite, illustrating the spatial distribution of the primary elements carbon (C), oxygen (O), and zinc (Zn) within the material.

Fig. S7(i). SEM image of the ZIF-8.1@H6mg sample after the sixth filtration cycle, showing retained nanoscale microplastic particles on the hydrogel surface.

(ii). SEM image of ZIF-8.1@H6mg after the sixth filtration cycle and regeneration, showing the persistence of ZIF-8 nanocrystals on the hydrogel surface.