electronic supplementary material

Policies and support in relation to LCA

Supporting a transition towards sustainable circular economy: sensitivity analysis for the interpretation of LCA for the recovery of electric and electronic waste

Lucia Rigamonti1 • Alida Falbo1 • Luca Zampori2 • Serenella Sala2

Received: 26 November 2015 / Accepted: 14 November 2016

© Springer-Verlag Berlin Heidelberg 2016

Responsible editor: Zbigniew Stanislaw Klos

1 Politecnico di Milano, Department of Civil and Environmental Engineering, P. L. da Vinci 32, 20133 Milano, Italy

2 European Commission, Joint Research Centre, Institute for Environment and Sustainability, Sustainability Assessment Unit, via Enrico Fermi 2749, 21027 Ispra (Va), Italy

 Serenella Sala

serenella.sala@jrc.ec.europa.eu

Content:

- Appendix A: addendum to case study

- Table A1: Components separated from small household appliances (R4): percentage of the plant input (equal to 100%), treatment process and corresponding recovered material and/or energy.

- Table A2: Avoided primary materials and energy associated with the treatment of 1 tonne of R4

- Appendix B: addendum to sensitivity of toxicity-related impacts

- Table B1: Impact indicators of toxicity-related impact categories associated with the treatment of 1 tonne of R4 (with long-term emissions and without long-term emissions)

- Figure B1: Contribution analysis of the human toxicity (cancer effects) impact indicator associated with the treatment of 1 tonne of R4 (with long-term emissions)

- Table B2: Contribution analysis of the human toxicity (cancer effects) impact indicator associated with the treatment of 1 tonne of R4 with and without long-term emissions

- Table B3: Focus on the contribution of steel and ferrous metals to the human toxicity (cancer effects) impact indicator

- Table B4: Focus on the contribution of PWBs to the human toxicity (cancer effects) impact indicator

- Figure B2: Contribution analysis of the human toxicity (non-cancer effects) impact indicator associated with the treatment of 1 tonne of R4 (with long-term emissions)

- Table B5: Contribution analysis of the human toxicity (non-cancer effects) impact indicator associated with the treatment of 1 tonne of R4 with and without long-term emissions

- Table B6: Focus on the contribution of PWBs to the human toxicity (non-cancer effects) impact indicator

- Table B7: Focus on the contribution of cables to the human toxicity (non-cancer effects) impact indicator

- Figure B3: Contribution analysis of the freshwater ecotoxicity impact indicator associated with the treatment of 1 tonne of R4 (with long-term emissions)

- Table B8: Contribution analysis of the freshwater ecotoxicity impact indicator associated with the treatment of 1 tonne of R4 with and without long-term emissions

- Table B9: Focus on the contribution of PWBs to the freshwater ecotoxicity impact indicator

- Table B10: Focus on the contribution of steel and ferrous metals to the freshwater ecotoxicity impact indicator

- Appendix C: addendum to sensitivity of resource-related impacts

- Table C1: Characterization factors (kg Sb eq/kg) of selected mineral resources in comparable methods

- Table C2: Contribution analysis of the mineral resource depletion indicator calculated by different characterization models (values in %)

Appendix A

Table A1: Components separated from small household appliances (R4): percentage of the plant input (equal to 100%), treatment process and corresponding recovered material and/or energy.

| Separated components from small household appliances (R4) | % | Treatment process | Recovered material / energy |
| --- | --- | --- | --- |
| Aluminium | 1.4 | Material recycling in smelter | Secondary aluminium ingots |
| Brass* | 0.2 | Not included* | Not included* |
| Cables | 2.8 | Shredding and separation of materials | Copper to material recycling and plastic to energy recovery |
| Capacitors | 0.2 | Disposal to hazardous waste incineration | Electricity and heat |
| Engines | 7.1 | Shredding and separation of materials | Plastic to energy recovery; aluminium, iron and copper to material recycling in smelter; PWBs with precious metals to specific processes |
| Hard disk** | 0.6 | Shredding and separation of materials | Not included** |
| Other batteries and accumulators (45% Li-ion and 55% NiMH batteries) | 0.1 | Li-ion batteries to mechanical process | Plastic to energy recovery; steel and non- ferrous metals to material recycling in smelter; MnO2 to recycler and Co powder to cobalt industry |
|  |  | NiMH batteries to pyrometallurgical process | Plastic to energy recovery |
|  |  |  | Recovery of Ni-Co-Fe residues was not included in the study |
| Plastic mix | 31.3 | Energy recovery | Electricity and heat |
| Other waste to landfill | 1.0 | Disposal to inert waste landfill | - |
| Pb batteries | 0.2 | Shredding and remelting of the lead acid in shaft furnace | Secondary lead |
| Power supplies** | 1.8 | Shredding and separation of materials | Not included |
| Printed Wiring Boards | 3.0 | Material recycling in smelter and further refinery | Secondary copper; secondary nickel; secondary lead; secondary precious metals (gold, silver, palladium) |
| Steel and ferrous metals | 50.1 | Material recycling in smelter | Liquid secondary steel |
| Toners and cartridges | 0.2 | Disposal to municipal waste incineration | Electricity and heat |
| Wood | 0.1 | Material recycling | Particle board |

*Neither the treatment process nor the recovered materials were included in the model due to a lack of information.

**Only the treatment process was modelled, whereas the recovered materials were not included in the model due to a lack of information.

Table A2: Avoided primary materials and energy associated with the treatment of 1 tonne of R4

| Avoided primary materials and energy | Unit of measure | Amount |
| --- | --- | --- |
| Aluminium | kg | 15.2 |
| Cobalt | kg | 0.1 |
| Copper | kg | 29.1 |
| Gold | kg | 0.005 |
| Lead | kg | 1.70 |
| Manganese dioxide | kg | 0.005 |
| Nickel | kg | 1.04 |
| Palladium | kg | 0.01 |
| Plywood from virgin wood | m3 | 0.0005 |
| Silver | kg | 0.18 |
| Steel | kg | 490 |
| Electricity | kWh | 675 |
| Thermal energy | MJ | 1504 |

Appendix B

Table B1: Impact indicators of toxicity-related impact categories associated with the treatment of 1 tonne of R4 (with long-term emissions and without long-term emissions)

| Impact category | Unit | With long-term emissions (A) | Without long-term emissions (B) | A-B; ((A-B)/A) |
| --- | --- | --- | --- | --- |
| Human toxicity, cancer effects | CTUh | 0.00163 | 0.00045 | 0.00118 (72.5%) |
| Human toxicity, non-cancer effects | CTUh | -0.0071 | -0.00068 | -0.00643 (90.4%) |
| Freshwater ecotoxicity | CTUh | -123811 | 872 | -124684 (100.7%) |

Figure B1: Contribution analysis of the human toxicity (cancer effects) impact indicator associated with the treatment of 1 tonne of R4 (with long-term emissions)

Table B2: Contribution analysis of the human toxicity (cancer effects) impact indicator associated with the treatment of 1 tonne of R4 with and without long-term emissions

| Human toxicity (cancer effects) | With long-term emissions (A) CTUh | Without long-term emissions (B) CTUh | A-B *; ((A-B)/A) CTUh; (%) |
| --- | --- | --- | --- |
| Total | 0.00163 | 0.00045 | 0.00118 (72.5%) |
| Transport of separated components | 7.13E-07 | 1.71E-07 | 5.42E-07 (76.0%) |
| Infrastructure | 7.52E-07 | 1.72E-07 | 5.79E-07 (77.1%) |
| Energy consumption | 1.04E-06 | 1.57E-07 | 8.80E-07 (84.9%) |
| Cables | -2.36E-05 | -1.64E-06 | -2.20E-05 (93.1%) |
| Printed wiring boards | -2.14E-04 | -1.03E-05 | -2.04E-04 (95.2%) |
| Steel and ferrous metals | 1.73E-03 | 4.23E-04 | 1.31E-03 (75.5%) |
| Aluminum | -3.71E-05 | -9.37E-06 | -2.77E-05 (74.7%) |
| Wood | -3.86E-09 | -1.26E-09 | -2.61E-09 (67.4%) |
| Pb batteries | -6.34E-07 | -2.45E-07 | -3.89E-07 (61.3%) |
| Li-ion batteries | 3.90E-07 | 1.11E-07 | 2.79E-07 (71.6%) |
| NiMH batteries | 1.09E-08 | 4.32E-09 | 6.59E-09 (60.4%) |
| Engines | 1.59E-04 | 4.22E-05 | 1.17E-04 (73.5%) |
| Plastic mix | 8.15E-06 | 2.93E-06 | 5.22E-06 (64.0%) |
| Toners and cartridges | 3.40E-08 | 1.62E-08 | 1.78E-08 (52.4%) |
| Capacitors incineration | 1.81E-06 | 4.59E-07 | 1.35E-06 (74.6%) |
| Others waste | 2.97E-09 | 7.49E-10 | 2.22E-09 (74.7%) |
| Treatment of power supplies and hard disk | 1.86E-07 | 1.91E-08 | 1.67E-07 (89.7%) |

* In bold type the mayor positive and negative differences (analyzed in detail in tables B3 and B4).

Table B3: Focus on the contribution of steel and ferrous metals to the human toxicity (cancer effects) impact indicator

| Human toxicity (cancer effects) |  | With long-term emissions |  |  |  |  | Without long-term emission |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| Process |  | Total value (CTUh) | Contribution of the main process/total of all processes (%) | Contribution of steel and ferrous metals to the total value (CTUh) | Contribution of steel and ferrous metals/total value (%) | B/A (%) | Total value (CTUh) | Contribution of the main process/total of all processes (%) | Contribution of steel and ferrous metals to the total value (CTUh) | Contribution of steel and ferrous metals/total value (%) | B/A (%) |
| All processes |  | 0.00163 | - | 0.00173 (A) | 106.3 | - | 0.00045 | - | 0.00042 (A) | 94.5 | - |
| Main process: Disposal, slag, unalloyed electr. steel, 0% water, to residual material landfill/CH U |  | 0.00281 | 173 | 0.00254 (B) | 90.3 | 147 | 0.00068 | 151 | 0.00061 (B) | 90.3 | 144 |
| Main substance for the main process | Compartment/ Sub-compartment | Total value for the main process (CTUh) | Contribution of the substance/ total of the main process (%) | Contribution of steel and ferrous metals to the total value for the main process(CTUh) (C) | Contribution of steel and ferrous metals/total value for the main process(%) | C/B (%) | Total value for the main process (CTUh) | Contribution of the substance/total of the main process (%) | Contribution of steel and ferrous metals to the total value for the main process (CTUh) (C) | Contribution of steel and ferrous metals/total value for the main process (%) | C/B (%) |
| Chromium VI | water/groundwater, long-term | 0.00214 | 75.9 | 0.00193 | 90.3 | 75.9 | - | - | - | - | - |
| Chromium VI | water/river | 0.00068 | 24.0 | 0.00061 | 90.3 | 24.0 | 0.00068 | 100 | 0.00061 | 90.3 | 100 |

| Human toxicity (cancer effects) |  | With long-term emissions |  |  |  |  | Without long-term emission |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| Process |  | Total value (CTUh) | Contribution of the main process/total of all processes (%) | Contribution of PWBs to the total value (CTUh) | Contribution of PWBs/total value (%) | B/A (%) | Process |  | Total value (CTUh) | Contribution of the main process/total of all processes (%) | Contribution of PWBs to the total value (CTUh) | Contribution of PWBs/total value (%) | B/A (%) |
| All processes |  | 0.00163 | - | -0.00021 (A) | -13 | - | All processes |  | 0.000448 | - | -0.000010 (A) | -2.3 | - |
| Main process1: Disposal, sulfidic tailings, off-site/GLO U |  | -0.00023 | -14% | -0.00019 (B) | 83 | 88 | Main process 2: Copper, primary, at refinery/GLO U |  | -0.000003 | -1 | -0.000003 (B) | 96.6 | 32.3 |
| Main substances for the main process 1 | Compartment/ Sub-compartment | Total value for the main process (CTUh) | Contribution of the substance/total of the main process (%) | Contribution of PWBs to the total value for the main process (CTUh) (C) | Contribution of PWBs/total value for the main process (%) | C/B (%) | Main substance for the main process 2 | Compartment/ Sub-compartment | Total value for the main process (CTUh) | Contribution of the substance/total of the main process (%) | Contribution of PWBs to the total value for the main process (CTUh) (C) | Contribution of PWBs/total value for the main process (%) | C/B (%) |
| Chromium VI | water/groundwater, long-term | -0.00019 | 84.0 | -0.00016 | 83.4 | 84 | Arsenic | air/low. Pop. | -0.0000017 | 50.0 | -0.0000017 | 96.6 | 50.0 |
|  |  |  |  |  |  |  | Process |  | Total value (CTUh) | Contribution of the main process/total of all processes (%) | Contribution of PWBs to the total value (CTUh) | Contribution of PWBs/total value (%) | D/A (%) |
| Arsenic | water/groundwater, long-term | -0.000033 | 14.6 | -0.000028 | 83.4 | 15 | Main process 3: Ferrochromium, high-carbon, 68% Cr, at plant/GLO U |  | -0.000004 | -1 | -0.0000022 (D) | 53.9 | 21.5% |
|  |  |  |  |  |  |  | Main substance for the main process 3 | Compartment/ Sub-compartment | Total value for the main process (CTUh) | Contribution of the substance/total of the main process (%) | Contribution of PWBs to the total value for the main process (CTUh) (F) | Contribution of PWBs/total value for the main process (%) | F/D (%) |
|  |  |  |  |  |  |  | Chromium VI | air/low pop | -0.0000039 | 95 | -0.0000021 | 53.9 | 95.2 |

# Table B4: Focus on the contribution of PWBs to the human toxicity (cancer effects) impact indicator

Figure B2: Contribution analysis of the human toxicity (non-cancer effects) impact indicator associated with the treatment of 1 tonne of R4 (with long-term emissions)

Table B5: Contribution analysis of the human toxicity (non-cancer effects) impact indicator associated with the treatment of 1 tonne of R4 with and without long-term emissions

| Human toxicity (cancer effects) | With long-term emissions (A) CTUh | Without long-term emissions (B) CTUh | A-B *; ((A-B)/A) CTUh; (%) |
| --- | --- | --- | --- |
| Total | -0.0071 | -0.00068 | -0.00643 (90.4%) |
| Transport of separated components | 2.09E-06 | 9.45E-07 | 1.15E-06 (54.9%) |
| Infrastructure | 6.49E-06 | 1.80E-06 | 4.69E-06 (72.2%) |
| Energy consumption | 3.48E-06 | 8.59E-07 | 2.62E-06 (75.3%) |
| Cables | -5.51E-04 | 3.66E-05 | -5.88E-04 (106.6%) |
| Printed wiring boards | -6.14E-03 | -7.90E-04 | -5.35E-03 (87.1%) |
| Steel and ferrous metals | 4.89E-05 | 7.22E-05 | -2.32-E05 (47.5%) |
| Aluminum | 4.80E-07 | 1.09E-05 | -1.04E-05 (2161%) |
| Wood | -8.79E-08 | -8.12E-08 | -6.63E-09 (7.5%) |
| Pb batteries | -2.32E-05 | -1.77E-05 | -5.50E-06 (23.7%) |
| Li-ion batteries | -1.08E-06 | -7.71E-08 | -9.99E-07 (92.8%) |
| NiMH batteries | 2.58E-07 | 2.45E-07 | 1.31E-08 (5.1%) |
| Engines | -4.60E-04 | 4.78E-06 | -4.60E-04 (99.9%) |
| Plastic mix | 1.73E-06 | 3.03E-06 | -1.30E-06 (75.2%) |
| Toners and cartridges | -7.10E-08 | -1.46E-08 | -5.64E-08 (79.4%) |
| Capacitors incineration | 5.06E-07 | 6.86E-07 | -1.81E-07 (35.7%) |
| Others waste | 7.09E-09 | 3.95E-9 | 3.14E-09 (44.3%) |
| Treatment of Power supplies and hard disk | 6.61E-07 | 1.50E-07 | 5.10E-07 (77.2%) |

* In bold type the mayor differences (analyzed in detail in tables B6 and B7).

| Human toxicity (non-cancer effects) |  | With long-term emissions |  |  |  |  | Without long-term emission |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| Process |  | Total value (CTUh) | Contribution of the main process/total of all processes (%) | Contribution of PWBs to the total value (CTUh) | Contribution of PWBs/total value (%) | B/A (%) | Process |  | Total value (CTUh) | Contribution of the main process/total of all processes (%) | Contribution of PWBs to the total value (CTUh) | Contribution of PWBs/total value (%) | B/A (%) |
| All processes |  | -0.0071 | - | -0.0061 (A) | 86.3 | - | All processes |  | -0.00068 | - | -0.00079 (A) | 116.0 | - |
| Main process 1: Disposal, sulfidic tailings,off-site/GLO U |  | -0.0064 | 90 | -0.0053 (B) | 83.4 | 87 | Main process 2: Copper, primary, at refinery/GLO U |  | -0.00050 | 73 | -0.00048 (B) | 96.6 | 61.0 |
| Main substances for the main process 1 | Compartment/ Sub-compartment | Total value for the main process (CTUh) | Contribution of the substance/total of the main process (%) | Contribution of PWBs to the total value for the main process (CTUh) (C) | Contribution of PWBs/total value for the main process (%) | C/B (%) | Main substances for the main process 2 | Compartment/ Sub-compartment | Total value for the main process (CTUh) | Contribution of the substance/total of the main process (%) | Contribution of PWBs to the total value for the main process (CTUh) (C) | Contribution of PWBs/total value for the main process (%) | C/B (%) |
| Zinc | water/groundwater, long-term | -0.00388 | 60.6 | -0.0032 | 83.4 | 60.6 | Lead | air/low. Pop. | -0.000169 | 33.9 | -0.000164 | 96.6 | 33.9 |
| Arsenic | water/groundwater, long-term | -0.0024 | 38.2 | -0.0020 | 83.4 | 38.2 | Arsenic | air/low. Pop. | -0.000117 | 23.4 | -0.000113 | 96.6 | 23.4 |
|  |  |  |  |  |  |  | Cadmium | air/low. Pop. | -0.000115 | 23.1 | -0.000111 | 96.6 | 23.1 |

Table B6: Focus on the contribution of PWBs to the human toxicity (non-cancer effects) impact indicator

| Human toxicity (non-cancer effects) |  | With long-term emissions |  |  |  |  | Without long-term emission |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| Process |  | Total value (CTUh) | Contribution of the main process/total of all processes (%) | Contribution of cables to the total value (CTUh) | Contribution of cables/total value (%) | B/A (%) | Process |  | Total value (CTUh) | Contribution of the main process/total of all processes (%) | Contribution of cables to the total value (CTUh) | Contribution of cables/total value (%) | B/A (%) |
| All processes |  | -0.0071 | - | -0.00055 (A) | 7.8 | - | All processes |  | -0.00068 | - | 0.000037 (A) | -5.4 | - |
| Main process 1: Disposal, sulfidic tailings, off-site/GLO U |  | -0.0064 | 90 | -0.00059 (B) | 9.2 | 107 | Main process 2: Copper, secondary, at refinery/RER U RAEE RL |  | 0.00015 | -22 | 0.000105 (B) | 68.8 | 287 |
| Main substances for the main process 1 | Compartment/ Sub-compartment | Total value for the main process (CTUh) | Contribution of the substance/total of the main process (%) | Contribution of cables to the total value for the main process (CTUh) (C) | Contribution of cables/total value for the main process (%) | C/B (%) | Main substance for the main process 2 | Compartment/ Sub-compartment | Total value for the main process (CTUh) | Contribution of the substance/total of the main process (%) | Contribution of cables to the total value for the main process (CTUh) (C) | Contribution of cables/total value for the main process (%) | C/B (%) |
| Zinc | water/groundwater, long-term | -0.0039 | 60.6 | -0.00036 | 9.2 | 60.6 | Zinc | air/low. Pop. | 0.00013 | 85.2 | 0.00009 | 68.8 | 85.2 |
| Arsenic | water/groundwater, long-term | -0.0024 | 38.2 | -0.00022 | 9.2 | 38.2 |  |  |  |  |  |  |  |

Table B7: Focus on the contribution of cables to the human toxicity (non-cancer effects) impact indicator

Figure B3: Contribution analysis of the freshwater ecotoxicity impact indicator associated with the treatment of 1 tonne of R4 (with long-term emissions)

Table B8: Contribution analysis of the freshwater ecotoxicity impact indicator associated with the treatment of 1 tonne of R4 with and without long-term emissions

| Freshwater ecotoxicity | With long-term emissions (A) CTUh | Without long-term emissions (B) CTUh | A-B *; ((A-B)/A) CTUh; (%) |
| --- | --- | --- | --- |
| Total | -123811 | 872 | -124684 (101%) |
| Transport of separated components | 4.73E+01 | 6.98E+00 | 4.04E+01 (85.3%) |
| Infrastructure | 1.40E+02 | 6.73E+00 | 1.33E+02 (95.2%) |
| Energy consumption | 8.91E+01 | 8.32E+00 | 8.07E+01 (90.7%) |
| Cables | -5.62E+03 | -2.88E+01 | -5.60E+03 (99.5%) |
| Printed wiring boards | -1.40 E+05 | -4.72E+03 | -1.35E+05 (96.6%) |
| Steel and ferrous metals | 2.42E+04 | 4.52E+03 | 1.97E+04 (81.3%) |
| Aluminium | -1.34E+03 | -1.04E+02 | -1.24E+03 (92.2%) |
| Wood | -2.77E-01 | -5.28E-02 | -2.24E-01 (80.9%) |
| Pb batteries | -1.76E+02 | -2.57E+01 | -1.51E+02 (85.4%) |
| Li-ion batteries | -1.73E+01 | 1.01E+00 | -1.83E+01 (106%) |
| NiMH batteries | 2.55E+00 | 2.99E-01 | 2.25E+00 (88.3%) |
| Engines | -9.37E+03 | 2.81E+02 | -9.65E+03 (103%) |
| Plastic mix | 7.79E+03 | 8.09E+02 | 6.99E+03 (89.6%) |
| Toners and cartridges | 3.24E+01 | 5.26E+00 | 2.72E+01 (83.8%) |
| Capacitors incineration | 1.68E+02 | 1.19E+02 | 4.88E+01 (29.1%) |
| Others waste | 1.51E-01 | 2.77E-02 | 1.23E (81.6%) |
| Treatment of Power supplies and hard disk | 1.71E+01 | 5.98E-01 | 1.65E+01 (96.5%) |

* In bold type the mayor positive and negative differences (analyzed in detail in tables B9 and B10).

# Table B9: Focus on the contribution of PWBs to the freshwater ecotoxicity impact indicator

| Freshwater ecotoxicity |  | With long-term emissions |  |  |  |  | Without long-term emission |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| Process |  | Total value (CTUh) | Contribution of the main process/total of all processes (%) | Contribution of PWBs to the total value (CTUh) | Contribution of PWBs/total value (%) | B/A (%) | Process |  | Total value (CTUh) | Contribution of the main process/total of all processes (%) | Contribution of PWBs to the total value (CTUh) | Contribution of PWBs/total value (%) | B/A (%) |
| All processes |  | -123811 | - | -139767 (A) | 113 | - | All processes |  | 872 | - | -4724 (A) | -512 |  |
| Main process 1: Disposal, sulfidic tailings, off-site/GLO U |  | -159353 | 129% | -132847 (B) | 83.4 | 95% | Main process 2: Gold, from combined gold-silver production, at refinery/PG U |  | -1249 | -143 | -1207 (B) | 96.6 | 25.5 |
| Main substance for the main process 1 | Compartment/ Sub-compartment | Total value for the main process (CTUh) | Contribution of the substance/total of the main process (%) | Contribution of PWBs to the total value (CTUh) (C) | Contribution of PWBs/total value (%) | C/B (%) | Main substance for the main process 2 | Compartment/ Sub-compartment | Total value for the main process (CTUh) | Contribution of the substance/total of the main process (%) | Contribution of PWBs to the total value for the main process (CTUh) (C) | Contribution of PWBs/total value for the main process (%) | C/B (%) |
| Zinc | water/groundwater, long-term | -116879 | 73.4% | -97526 | 83.4 | 73.4 | Zinc | water river | -1382 | 111 | -1335 | 96.6 | 111 |
|  |  |  |  |  |  |  | Process |  | Total value (CTUh) | Contribution of the main process/total of all processes (%) | Contribution of PWBs to the total value (CTUh) | Contribution of PWBs/total (%) | D/A (%) |
|  |  |  |  |  |  |  | Main process 3: Gold, from combined gold-silver production, at refinery/PE U |  | -1486 | -170 | -1436 (D) | 96.6 | 30.4 |
|  |  |  |  |  |  |  | Main substance for the main process 3 | Compartment/ Sub-compartment | Total value for the main process (CTUh) | Contribution of the substance/total of the main process (%) | Contribution of PWBs to the total value for the main process (CTUh) (F) | Contribution of PWBs/total value for the main process (%) | F/D (%) |
|  |  |  |  |  |  |  | Zinc | water river | -1007 | 67.7 | -972.7 | 96.6 | 67.7 |

Table B10: Focus on the contribution of steel and ferrous metals to the freshwater ecotoxicity impact indicator

| Freshwater ecotoxicity |  | With long-term emissions |  |  |  |  | Without long-term emission |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| Process |  | Total value (CTUh) | Contribution of the main process/total of all processes (%) | Contribution of steel and ferrous metals to the total value (CTUh) | Contribution of steel and ferrous metals/total value (%) | B/A (%) | Process |  | Total value (CTUh) | Contribution of the main process/total of all processes (%) | Contribution of steel and ferrous metals to the total value (CTUh) | Contribution of steel and ferrous metals/total value (%) | B/A (%) |
| All processes |  | -123811 | - | -24193 (A) | -19.6% | - | All processes |  | 872 | - | 4517 (A) | 517.7 | - |
| Main process 1: Disposal, slag, unalloyed electr. steel, 0% water, to residual material landfill/CH U |  | 37886 | -31% | 34200 (B) | 90.3% | -141 | Main process 2: Disposal, slag, unalloyed electr. steel, 0% water, to residual material landfill/CH U |  | 6730 | 771 | 6075 (B) | 90.3 | 134 |
| Main substances for the main process 1 | Compartment/ Sub-compartment | Total value for the main process (CTUh) | Contribution of the substance/total of the main process (%) | Contribution of steel and ferrous metals to the total value (CTUh) (C) | Contribution of steel and ferrous metals/total value (%) | C/B (%) | Main substance for the main process 2 | Compartment/ Sub-compartment | Total value for the main process (CTUh) | Contribution of the substance/total of the main process (%) | Contribution of steel and ferrous metals to the total value for the main process (CTUh) (C) | Contribution of steel and ferrous metals/total value for the main process (%) | C/B (%) |
| Chromium VI | water/groundwater, long-term | 21162 | 55.9 | 19103 | 90.3 | 55.9 | Zinc | water river | 6699 | 99.5 | 6048 (C) | 90.3 | 99.5 |
| Vanadium | water/groundwater, long-term | 9057 | 23.9 | 8176 | 90.3 | 23.9 |  |  |  |  |  |  |  |
| Chromium VI | water/river | 6699 | 17.7 | 6048 | 90.3 | 17.7 |  |  |  |  |  |  |  |

# Appendix C

# Table C1: Characterization factors (kg Sb eq/kg) of selected mineral resources in comparable methods

| Minerals | AADP (2011) | AADP (2015) | ILCD | CML 2012 (a) | CML 2012 (b) | CML 2012 (c) |
| --- | --- | --- | --- | --- | --- | --- |
| aluminium (Al) | 5.34E-06 | 3.00E-10 | 2.53E-05 | 1.09E-09 | 2.53E-05 | 2.14E-05 |
| bromine (Br) |  |  |  | 4.39E-03 |  |  |
| cadmium (Cd) | 3.19E-01 | 3.08E+00 | 1.11E+00 | 1.57E-01 | 1.11E+00 | 1.92E+00 |
| chromium (Cr) |  | 9.03E-05 | 1.96E-05 | 4.43E-04 | 1.96E-05 | 3.77E-05 |
| cobalt (Co) | 2.08E-01 | 1.04E-03 | 2.56E-02 | 1.57E-05 | 2.56E-02 | 4.89E-02 |
| copper (Cu) | 1.57E-03 | 5.41E-04 | 2.50E-03 | 1.37E-03 | 2.50E-03 | 3.94E-03 |
| fluorspar |  |  | 2.62E-03 |  |  |  |
| gallium (Ga) |  | 3.82E-06 | 6.30E-03 | 1.46E-07 |  |  |
| gold (Au) |  | 1.59E+00 | 3.60E+01 | 5.20E+01 | 3.60E+01 | 3.99E+01 |
| indium (In) |  | 7.48E-01 | 5.55E+02 | 6.89E-03 | 5.55E+02 | 1.15E+03 |
| iodine (I) |  |  | 2.22E-03 | 2.50E-02 | 2.22E-03 | 3.10E-03 |
| iron (Fe) | 2.38E-06 | 2.75E-08 | 1.66E-06 | 5.24E-08 | 1.66E-06 | 3.64E-06 |
| lead (Pb) | 1.02E-03 | 4.80E-04 | 1.50E-02 | 6.34E-03 | 1.50E-02 | 2.67E-02 |
| lithium (Li) |  | 2.42E-06 | 1.33E-02 | 1.15E-05 | 1.33E-02 | 4.38E-02 |
| magnesium (Mg) |  | 8.61E-10 | 2.48E-06 | 2.02E-09 |  |  |
| manganese (Mn) |  | 7.57E-05 | 2.35E-05 | 2.54E-06 | 2.35E-05 | 5.80E-04 |
| molybdenum (Mo) |  | 6.17E-03 | 7.11E-02 | 1.78E-02 | 7.11E-02 | 1.46E-01 |
| nickel (Ni) | 3.91E-02 | 3.03E-05 | 4.18E-03 | 6.53E-05 | 4.18E-03 | 1.69E-02 |
| palladium (Pd) |  | 6.93E+00 | 9.36E+00 | 5.71E-01 | 9.36E+00 | 4.99E+00 |
| phosphorus (P) |  |  | 6.21E-05 | 5.52E-06 | 6.21E-05 | 2.54E-04 |
| platinum (Pt) |  | 6.93E+00 | 9.09E+00 | 2.22E+00 | 9.09E+00 | 4.85E+00 |
| rhenium (Re) |  | 2.54E-03 | 3.19E+01 | 6.03E-01 | 3.19E+01 | 2.66E+02 |
| silver (Ag) |  | 2.28E-01 | 8.42E+00 | 1.18E+00 | 8.42E+00 | 8.16E+00 |
| sodium sulfate |  |  | 9.92E-06 |  |  |  |
| sulfur (S) |  |  | 3.91E-04 | 1.93E-04 | 3.91E-04 | 1.05E-03 |
| talc |  |  | 1.18E-03 |  |  |  |
| tantalum (Ta) |  | 2.52E-03 | 1.15E+01 | 4.06E-05 | 1.15E+01 | 2.28E+01 |
| tellurium (Te) |  |  | 7.21E+00 | 4.07E+01 | 7.21E+00 | 1.12E+01 |
| tin (Sn) |  | 1.52E-03 | 1.15E-01 | 1.62E-02 | 1.15E-01 | 7.77E-02 |
| vermiculite |  |  | 1.11E-03 |  |  |  |
| zinc (Zn) | 1.70E-03 | 8.60E-05 | 3.65E-03 | 5.38E-04 | 3.65E-03 | 8.05E-03 |
| zirconium (Zr) |  | 1.19E-06 | 1.64E-02 | 5.44E-06 | 1.64E-02 | 2.30E-02 |

Table C2: Contribution analysis of the mineral resource depletion indicator calculated by different characterization models (values in %)

| Minerals | AADP (2011) | AADP (2015) | ILCD | CML 2012 (a) | CML 2012 (b) | CML 2012 (c) | EDIP 97 | EPS 2000 | ReCiPe 2008 | Supply Risk (1) | Supply Risk (2) | Supply Risk (3) |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| aluminium (Al) | -1.36E-02 | -3.72E-06 | -2.12E-02 | -2.05E-06 | -2.13E-02 | -1.59E-02 | -2.06E-01 | -7.12E-03 | -7.79E-02 | -4.13E+01 | -4.04E+00 | -2.78E-02 |
| bromine (Br) |  |  |  | -3.23E-06 |  |  |  |  |  |  |  |  |
| cadmium (Cd) | 3.09E-04 | 1.45E-02 | 3.56E-04 | 1.12E-04 | 3.57E-04 | 5.45E-04 | 5.57E-04 | 1.80E-04 |  |  |  |  |
| chromium (Cr) |  | 3.16E-03 | 4.65E-05 | 2.34E-03 | 4.66E-05 | 7.94E-05 | 9.92E-03 | 3.89E-03 | 6.09E-02 | 2.74E-01 | 1.92E+00 | 1.38E-03 |
| cobalt (Co) | -3.19E+00 | -7.77E-02 | -1.30E-01 | -1.77E-04 | -1.30E-01 | -2.20E-01 | -7.56E-01 | -2.50E-02 | -5.27E-03 | -9.45E-01 | -7.24E+01 |  |
| copper (Cu) | -6.58E+00 | -1.11E+01 | -3.47E+00 | -4.22E+00 | -3.47E+00 | -4.86E+00 | -3.08E+00 | -5.57E+00 | -6.09E+01 | -3.49E+01 | -1.20E-01 | -4.54E+00 |
| Fluorspar |  |  | -1.72E-01 |  |  |  |  |  |  |  |  |  |
| gallium (Ga) |  | -5.84E-13 | -6.52E-11 | -3.36E-15 |  |  |  | -4.24E-11 |  | -2.16E-09 | -2.87E-07 |  |
| gold (Au) |  | -6.38E+00 | -9.76E+00 | -3.15E+01 | -9.78E+00 | -9.62E+00 | -6.76E+00 | -6.25E+00 | -1.96E+01 | -4.67E-03 | -2.36E-06 |  |
| indium (In) |  | 4.95E-05 | 2.49E-03 | 6.88E-08 | 2.49E-03 | 4.58E-03 |  | 4.22E-06 |  | 9.24E-07 | 1.16E-04 |  |
| iodine (I) |  |  | -1.59E-07 | -3.99E-06 | -1.60E-07 | -1.98E-07 |  | -2.94E-06 |  |  |  |  |
| iron (Fe) | -9.77E-08 | -5.51E-09 | -2.25E-08 | -1.59E-09 | -2.26E-08 | -4.38E-08 | -1.77E-07 | -2.52E-07 | -1.40E-05 | -7.77E-04 | -1.62E-04 |  |
| lead (Pb) | -2.42E-01 | -5.56E-01 | -1.18E+00 | -1.11E+00 | -1.18E+00 | -1.86E+00 | -1.22E+00 | -2.65E-01 | -1.43E-01 |  |  |  |
| lithium (Li) |  | -5.15E-11 | -1.92E-08 | -3.69E-11 | -1.92E-08 | -5.62E-08 |  | -3.76E-09 |  | -1.07E-07 | -8.29E-08 |  |
| magnesium (Mg) |  | -8.13E-13 | -1.58E-10 | -2.88E-13 |  |  |  |  |  | -1.85E-05 | -1.28E-02 | -2.08E-10 |
| manganese (Mn) |  | -1.27E-03 | -2.66E-05 | -6.43E-06 | -2.67E-05 | -5.86E-04 | -3.12E-03 | -1.24E-04 | -8.96E-02 | -5.59E-02 | -5.47E-03 | -3.50E-05 |
| molybdenum (Mo) |  | -2.14E+00 | -1.67E+00 | -9.30E-01 | -1.67E+00 | -3.04E+00 | -2.86E+00 | -9.63E-01 | -5.02E+00 | -2.31E+00 | -7.24E+00 |  |
| nickel (Ni) | -9.02E+01 | -3.41E-01 | -3.18E+00 | -1.11E-01 | -3.19E+00 | -1.14E+01 | -1.29E+01 | -2.36E+00 | -9.84E+00 | -2.10E+01 | -1.11E-01 |  |
| palladium (Pd) |  | -5.03E+01 | -4.60E+00 | -6.26E-01 | -4.61E+00 | -2.18E+00 | -1.77E+01 | -7.07E+01 | -1.93E+00 |  |  |  |
| phosphorus (P) |  |  | -8.42E-04 | -1.67E-04 | -8.43E-04 | -3.06E-03 |  | -1.17E-03 | 0.00E+00 | -1.69E+00 | -1.73E+01 |  |
| platinum (Pt) |  | -1.66E-04 | -1.47E-05 | -8.01E-06 | -1.48E-05 | -6.99E-06 | -5.31E-05 | -2.33E-04 | -2.72E-04 | -2.19E-07 | -3.34E-06 |  |
| rhenium (Re) |  | -3.98E-09 | -3.38E-06 | -1.43E-07 | -3.39E-06 | -2.51E-05 |  | -1.52E-05 |  | -1.08E-08 | -4.02E-08 |  |
| silver (Ag) |  | -2.92E+01 | -7.29E+01 | -2.29E+01 | -7.31E+01 | -6.29E+01 | -3.36E+01 | -9.04E+00 | -2.55E+00 | -7.24E-01 | -1.00E+00 | -9.57E+01 |
| sodium sulfate |  |  | -1.89E-04 |  |  |  |  |  |  |  |  |  |
| sulfur (S) |  |  | -2.05E-04 | -2.25E-04 | -2.05E-04 | -4.91E-04 |  |  |  |  |  |  |
| talc |  |  | -1.92E-04 |  |  |  |  |  |  |  |  |  |
| tantalum (Ta) |  | 8.29E-07 | 2.57E-04 | 2.01E-09 | 2.57E-04 | 4.52E-04 | 5.42E-04 | 8.53E-07 |  | 1.58E-06 | 9.65E-07 |  |
| tellurium (Te) |  |  | -3.08E+00 | -3.87E+01 | -3.08E+00 | -4.26E+00 | -2.13E+01 | -4.91E+00 |  | -9.30E-03 | -1.53E-05 |  |
| tin (Sn) |  | -1.59E-04 | -8.18E-04 | -2.56E-04 | -8.19E-04 | -4.89E-04 | -1.21E-03 | -1.63E-04 | -9.28E-03 | -6.66E-04 | -1.64E-03 |  |
| vermiculite |  |  | -6.20E-07 |  |  |  |  |  |  |  |  |  |
| zinc (Zn) | 2.66E-01 | 6.57E-02 | 1.89E-01 | 6.20E-02 | 1.89E-01 | 3.70E-01 | 2.46E-01 | 5.71E-02 | 1.20E-01 | 2.67E+00 | 3.28E-01 | 2.48E-01 |
| zirconium (Zr) |  | 5.54E-10 | 5.17E-07 | 3.83E-10 | 5.18E-07 | 6.46E-07 | 1.18E-06 | 7.62E-09 |  |  |  |  |