Process simulation-based LCA: Li-ion battery recycling case study

Supplementary Information

Yvonne Kaye Perocillo*1, Eric Pirard2 and Angélique Léonard1

*Corresponding author. Email: yperocillo@uliege.be

Description: This document discusses in detail how the process simulation was modelled.

TABLE OF CONTENTS

Process simulation-based LCA: Li-ion battery recycling case study	1

1	HSC Chemistry®	2

2	NMC battery cell composition	3

3	Hydrometallurgical Recycling of Black mass	5

3.1	Slurry Preparation	5

3.2	Leaching	6

3.3	Purification	8

3.4	Precipitation	9

3.4.1	Mixed Ni-Co-Mn Precipitation	9

3.4.2	Lithium carbonate precipitation	10

3.5	Filtration	10

4	Pyrometallurgical Recycling of Black mass	11

4.1	Reduction Smelting	11

5	References	14

# HSC Chemistry®

The HSC Chemistry® 10 software includes a Flowsheet Simulation (Sim) module which was used to simulate the hydrometallurgical and the pyrometallurgical phase in the treatment of waste Li-ion battery cells. For these simulations, the software uses the thermodynamic and chemical data of a wide variety of substances and compounds collected in its own database. Some of the substances needed for this study however were not available in the HSC database. They had to be registered manually and their thermodynamic data was sourced from literature or from HSC’s estimates, as shown in Table 1.

Table 1. Summary of substances/compounds that are not available in the HSC Chemistry® database that was used in this simulation.

| Substance | Data Source |
| --- | --- |
| Polyvinylidene difluoride (PVDF, C2H2F2) | [1] |
| Lithium hexafluorophosphate (LiPF6) | [2], HSC Estimates |
| NMC cathode material (LiNi0.6Mn0.2Co0.2O2) | HSC Estimates |

A feature of the Sim module is the Gibbs wizard. This feature allows for users to calculate the equilibrium amounts of the output. The equilibrium temperature, pressure, as well as the amounts of input and the expected outputs (as phases) can be specified while the software automatically does the backround thermodynamic calculation [3]. This module was used in almost all the process steps of each simulation, both hydro and pyro processes, except for the heaters, and filter in the hydrometallurgical process.

Both the heaters and filters in the Sim module of HSC are few of the equipments that have ready-made unit models i.e., predefined formula and parameters to calculate the output. You only need to make sure that the input and output streams are connected to this model correctly, and indicate the parameters required (e.g., %moisture for filters, type of flow for the heaters, etc.).

# NMC battery cell composition

The composition of the feed battery cell and black mass used as feed in the process simulation was calculated from the cited literature.

Table 2. Average material contents of an NMC cell  based on Wang et al. (2016).

| Materials | Wt (kg) | Wt% | Phases | Wt (kg) | Wt (%) | Remarks |
| --- | --- | --- | --- | --- | --- | --- |
| Al | 3.60 | 8.51% | Al | 3.42 | 8.09% | Assumed to be from a mix of the cathode current collector and the cell casing |
|  |  |  | Al2O3 | 0.18 | 0.43% | Those from cell casing is assumed to be partly oxidized (5% of the total Al content). |
| Co | 0.80 | 1.89% |  |  |  | Assumed to be from the NMC cathode active material, which is assumed as NMC622 |
| Cu | 6.90 | 16.31% | Cu | 6.90 | 16.31% | Assumed to be from the anode current collector |
| Li | 1.00 | 2.36% |  |  |  | Assumed to be from the NMC cathode active material, which is assumed as NMC622 |
| Mn | 3.20 | 7.57% |  |  |  | Assumed to be from the NMC cathode active material, which is assumed as NMC622 |
| Ni | 3.40 | 8.04% |  |  |  | Assumed to be from the NMC cathode active material, which is assumed as NMC622 |
| Graphite | 8.70 | 20.57% | C | 8.70 | 20.57% |  |
| Carbon black | 0.80 | 1.89% | C | 0.80 | 1.89% |  |
| LiPF6 | 6.20 | 14.66% | LiPF6 | 6.20 | 14.66% |  |
| Ethylene carbonate (EC)/others | 4.40 | 10.40% |  | 4.40 | 10.40% | Other electrolyte components assumed to only ethylene carbonate |
| Binders | 1.20 | 2.84% | PVDF | 1.20 | 2.84% | Assumed to be polyvinylidene difluoride (PVDF) based on Jung (2023) |
| Plastics | 2.10 | 4.96% | PPE | 2.10 | 4.96% | Assumed to be from the separator, usually polyethylene (PE) and polypropylene (PPE) in commercial cells (Vuorilento, 2018). Assumed to only be PPE. |
|  |  |  | LiNi0.6Mn0.2Co0.2O2 | 8.40 | 19.86% | Assumed balance is the NCM622 |
| TOTAL | 42.30 | 100.0% |  | 42.30 | 100% |  |

Table 3. NMC622 black mass composition based on (Woeste et al. 2024).

| Element | From literature | Possible Phases | kg | % | Remark |
| --- | --- | --- | --- | --- | --- |
| Al | 1.92% | Al | 18.23 | 1.82% | From current collector residues, assumed to be in pure form as required for the battery |
|  |  | Al2O3 | 0.96 | 0.10% | Assumed oxidized Al is about 5% of the total Al. Assumed to be from the cell casing since it is in the exterior of the battery. |
| Cu | 1.30% | Cu | 12.95 | 1.30% | From current collector residues, assumed to be in pure form as required for the battery |
| C | 29.24% | C | 292.42 | 29.24% | Graphite used is assumed pure C |
| Fe | 4.56% | Fe | 0.00 | 0.00% | Assumed to be not present in this case since there are no Fe sources from the NMC cell based on Wang et al (2016). |
| Li | 4.52% | LiPF6 | 0.53 | 0.05% |  |
| Ni | 22.92% |  |  |  |  |
| Mn | 7.15% |  |  |  |  |
| Co | 7.58% | LiNMC622 | 623.68 | 62.37% |  |
| Others | 20.82% | PVDF | 51.23 | 5.12% |  |
| TOTAL | 100.00% |  | 1000.00 | 100.00% |  |

# Hydrometallurgical Recycling of Black mass

## Slurry Preparation

The recovered black mass (BM) from the pretreatment of the waste Li-ion batteries’ (LIBs) cells, with the composition shown in Table 2, was first prepared as a slurry before the leaching stage. Note that for the calculation of the BM recovery, it was assumed that an average 20 hour operation per day treats 1000-kg waste LIBs cells that produces 244.63 kg of BM during pretreatment (See Supplementart File No.1). This is equivalent to ~12 kg/hr of BM prepared as slurry for the hydrometallurgical treatment. Due to this low value, the simulation feed was assumed to be 1000 kg/hr of BM instead.

Table 4. Initial  black mass composition of the modeled waste Li-ion battery cells used in the simulation. Based on the calculations from Supplementary Document No. 1.

| Phases | % |
| --- | --- |
| Al | 1.82 |
| Al2O3 | 0.10 |
| Cu | 1.30 |
| C | 29.24 |
| LiPF6 | 0.05 |
| NMC cathode material (LiNi0.6Mn0.2Co0.2O2) | 62.37 |
| PVDF | 5.12 |
| Total | 100 |

To prepare the black mass slurry, 1600 kg/m3 slurry density was assumed (about ~60% solids). This was based on authors’ industrial experience. Since the phases present in the black mass has the possibility of reacting with water, an inspection of these possible reactions are summarized in Table 3. This then became the basis for the inputs and outputs in the Gibbs wizard of the software.

Table 5. Summary of assumed reactions during the slurry preparation.

| Reactions | Assumptions |
| --- | --- |
| Al + H2O | No reaction based on solubility rules. |
| Al2O3 + H2O | No reaction based on solubility rules. |
| Cu + H2O | No reaction based on activity series. |
| C + H2O | No reaction, graphite is known to be hydrophobic. |
| LiPF6 + H2O → LiF + POF3 + 2HF | Based on reported reactions by Hider et al and Aurbach et al as seen in [4]. |
| LiNi0.6Mn0.2Co0.2O2 + H2O | Li dissolution is expected while it is assumed that Ni, Mn, and Co are not based on [5]. |
| PVDF + H2O | Considered to be a non-reactive thermoplastic so assumed to have no reaction with water. |

The inputs and possible outputs for leaching is summarized in Table 4. Note that the outputs are only a possibility and not necessarily present in the final simulation output since it will depend on the thermodynamic calculation.

Table 6. Inputs and outputs for slurry preparation unit process indicated in the Gibbs wizard.

| INPUTS | OUTPUTS |
| --- | --- |
| Gas Phase | Gas Phase |
|  | HF, POF3 |
| Water Phase | Water Phase |
| H2O | Same as input plus Li+ |
| Solid Phase | Solid Phase |
| Al2O3, Al, Cu, C, LiNi0.6Mn0.2Co0.2O2, F6LiP, PVDF | Except F6LiP, same as inputs plus LiF |

## Leaching

This stage of the process is the heart of a hydrometallurgical process because this is where targetted extraction of the desired metals begins. This occurs by dissolving the metals (in this case Ni, Co, Mn, and Li) trapped in the black mass and into the solution using a lixiviant and producing a pregrant liquor solution (PLS). Process parameters are then carefully controlled to keep these metals in the solution until they are ready to be recovered by precipitation, solvent extraction, cystallization, etc.

To simulate this stage of the process in the software, a mix of literature and process know-how were needed. Target temperature and pH, 90°C and 3.2±0.1, were mainly based on experiments by Guimarães et al. (2022). This is because they avoided the use of reductants (e.g. hydrogen peroxide (H2O2)) during the leaching of critical metals from Li-ion batteries with NMC111 cathodes. They leached the black mass with sulfuric acid (H2SO4) without reductant addition and yielded complete extraction of Ni, Co, and Li, and 93% extraction of Mn into the pregnant liquor under optimal laboratory test conditions. To achieve the temperature target in the simulation, a heat exchanger was used.

The lixiviant used was sulfuric acid (H2SO4) which is assumed to be 100% pure. Considering this and the assumed results of the BM slurry preparation discussed earlier, some reactions shown below (Table 5) were considered to be possible during leaching.

Table 7. Summary of assumed reactions during leaching.

| H2SO4 + H2O → H+ + HSO4- HSO4- → H+ + SO42- | Dissociation of sulfuric acid (H2SO4) in water. Full dissociation is assumed. |
| --- | --- |
| Al + H2SO4 → Al2(SO4)3 + H2 | Usual reaction between Al and concentrated H2SO4 |
| Al2O3 + H2SO4 → Al2(SO4)3 + H2O | Usual reaction between Al2O3 and concentrated H2SO4 |
| Cu + 2H2SO4 → CuSO4 + 2H2O + SO2 | Usual reaction between Cu and concentrated H2SO4 |
| 3Fe + 8H2SO4 → FeSO4 + Fe2(SO4)3 + 4SO2 + 8H2O | Usual reaction between Fe and concentrated H2SO4. Note Fe represents stainless steel. |
| C + 2H2SO4 → CO2 + 2SO2 + H2O | Common reaction between C and concentrated H2SO4 |
| 2LiF + H2SO4 → Li2SO4 + 2HF | Common reaction between LiF and concentrated H2SO4 |
| Li+ + SO42- → Li2SO4 | Possible reaction of metallic ions with sulfate ions. |
| Co+2 + SO42- → CoSO4 |  |
| Mn+2 + SO42- → MnSO4 |  |

It should be noted that these reactions aren’t necessarily completed during leaching. Depending on the system’s parameters e.g., temperature, pH, etc., the reactants and products could occur interchangeably or even diffuse through the solution as ions. Taking this in consideration, the reactants and products in the presumed reactions are indicated as possible outputs in the Gibbs wizard, except for the sulfates of the target metals (Table 6). They were assumed to exist as ions only because they could end up filtered as solids in the next steps in the simulation.

Table 8. Inputs and outputs for leaching unit process indicated in the Gibbs wizard.

| INPUTS | OUTPUTS |
| --- | --- |
| Gas Phase | Gas Phase |
|  | HF, H2O, CO2, SO2 |
| Water Phase | Water Phase |
| Output from slurry preparation plus H2SO4 | Same as input minus H2SO4. Other outputs are H+, SO4-2, Ni+2, Al+3, Cu+2 and ionic phases of Al2(SO4)3, CuSO4, FeSO4, Fe2(SO4)3, NiSO4, Li2SO4, CoSO4, and MnSO4 |
| Solid Phase | Solid Phase |
| Al2O3, Al, Cu, C, LiNi0.6Mn0.2Co0.2O2, PVDF, LiF | Al2O3, Al, Cu, C, Fe, PVDF |

Notice that the gas phase of the input is empty. This is because all gas products are assumed to be vented out of the tank and not pumped along to the next process. This is the same for all succeding steps. Also due to the high temperature, it is also assumed that some water vapor could form and was also indicated as a possible process output.

## Purification

The objective of this stage in the process is to concentrate the PLS by removing any impurities that was leached along with the target metals as ions. By controlling the pH with the help of a reagent, in this case hydrated lime (Ca(OH)2), the impurities (i.e., Al and Cu) can be precipitated as hydroxides and later separated from the purified PLS by filtration. The formation of gysum is also common when lime is used to neutralize sulfuric acid.

For the simulation, hydrated lime was introduced as a pulp with assumed 45% solids based on author’s industry experience, i.e., concentrated but just enough without clogging pipings and pumps. The target temperature was set at 60°C to make sure that Li stays on the solution [9], while the pH is set at 6.5±0.5 which is enough to make sure that any Al, Cu, or Fe ions precipitate into hydroxides and be removed from the PLS, without precipitating the target metals [7]. Table 7 summarizes some assumed reactions in the reactor, while Table 8 the indicated inputs and outputs in the Gibbs wizard.

Table 9. Summary of assumed reactions during purification.

| Ca(OH)2 → Ca2+ + 2(OH)- | Dissolution of hydrated lime in water |
| --- | --- |
| Ca(OH)2 + H2SO4 → CaSO4●2H2O | Formation of gypsum |
| Al2(SO4)3 + 3Ca(OH)2 → 2Al(OH)3+ 3CaSO4 | Formation of aluminum hydroxide |
| CuSO4 + 3Ca(OH)2 → 2Cu(OH)3+ 3CaSO4 | Formation of copper hydroxide |
| FeSO4 + Ca(OH)2 → Fe(OH)2 + CaSO4 | Formation of ferrous hydroxide |
| Fe2(SO4)3 + 3Ca(OH)2 → 2Fe(OH)3 + 3CaSO4 | Formation of ferric hydroxide |

Table 10. Inputs and outputs for purification unit process indicated in the Gibbs wizard.

| INPUTS | OUTPUTS |
| --- | --- |
| Water Phase | Water Phase |
| Ouput from leaching plus output of Ca(OH)2 pulping i.e., more H2O and possibility of Ca+2, OH- | Same as input minus Al+3, Cu+2, Ca+2, OH-, and ionic phases of Al2(SO4)3, CuSO4, FeSO4, and Fe2(SO4)3 |
| Solid Phase | Solid Phase |
| Al2O3, Cu, C, Fe, PVDF, Ca(OH)2 | Al2O3, Cu, C, Fe, PVDF, Ca(OH)2, CaSO4, CaSO4●2H2O, Al(OH)3, Cu(OH)2, Fe(OH)2, Fe(OH)3 |

## Precipitation

This stage of the process was done sequentially i.e., Ni, Co, and Mn were precipitated as hydroxide and later the lithium as carbonate. Commonly in research and industry, the goal is to reuse the recovered hydroxides as precursor for new battery material. That is why the Ni, Co, and Mn were also coprecipitated in this simulation. However, it should be noted that lithium carbonate (Li2CO3) will need to be further refined before battery application [8]. Also note that after each precipitation stage, the precipitates were filtered for recovery. Table 9 summarizes the possible reactions considered during this phase in the process.

Table 11. Summary of assumed reactions during precipitation.

| NaOH → Na+ + (OH)- | Dissolution of NaOH in water |
| --- | --- |
| NiSO4 + 2NaOH → Ni(OH)2 + Na2SO4 | Precipitation of Ni(OH)2 |
| MnSO4 + 2NaOH → Mn(OH)2 + Na2SO4 | Precipitation of Mn(OH)2 |
| CoSO4 + 2NaOH → Co(OH)2 + Na2SO4 | Precipitation of Co(OH)2 |
| Na2CO3 → Na+ + (CO3)-2 | Dissolution of Na2CO3 in water |
| Li2SO4 + Na2CO3 → Li2CO3 + Na2SO4 | Precipitation of Li2CO3 |

The reagents used to precipitate the target metals, as well as control the pH in each stage, were sodium hydroxide (NaOH), and sodium carbonate (Na2CO3), respectively. They are introduced into the reactor as slurry with 45% solids, like the hydrated lime used in the purification.

### Mixed Ni-Co-Mn Precipitation

Like the previous step the, target temperature was set at 60°C to make sure that Li stays on the solution [9]. The pH was set at 11.5±0.5 based on [7], [10]. Summary of the inputs and outputs considered in the Gibbs wizard are shown in Table 10.

Table 12: Inputs and outputs for precipitation of mixed Ni-Co-Mn hydroxide unit process indicated in the Gibbs wizard.

| INPUTS | OUTPUTS |
| --- | --- |
| Water Phase | Water Phase |
| Ouput from purification plus output of NaOH pulping i.e., more H2O and possibility of Na+, OH- | Same as input minus Ni2+, Mn2+, Co2+, and ionic phases of NiSO4, CoSO4, and MnSO4 |
| Solid Phase | Solid Phase |
| No solids from PLS since removed during filtration. Some undisolved NaOH could be present from the pulping. | NaOH, Na2SO4, Ni(OH)2, Mn(OH)2, Co(OH)2 |

### Lithium carbonate precipitation

Target temperature is set at 50°C based on experiments by Battaglia and colleagues [11]. They suggest increasing the temperature, but for this case the lower temperature was first used to ensure that unnecessary energy use is avoided. For the pH, different values are found in literature that was used to precipitate lithium carbonate (Li2CO3) using Na2CO3 as precipitant i.e., ~12 [9] and 14 [12]. Both were tested in the simulation. However, the simulation was not able to reach the pH of 14 despite very high feed rate of Na2CO3. The pH target was instead set to 12.8±0.3, taking into consideration the literature and simulation information. Table 11 summarizes the inputs and outputs indicated in the Gibbs wizard.

Table 13: Inputs and outputs for precipitation of Li2CO3 unit process indicated in the Gibbs wizard.

| INPUTS | OUTPUTS |
| --- | --- |
| Water Phase | Water Phase |
| Ouput from mixed Ni-Mn-Co precipitation plus output of Na2CO3 pulping i.e., more H2O and possibility of Na+, CO32- | Same as input except ionic phase of Li2SO4 |
| Solid Phase | Solid Phase |
| No solids from PLS since removed during filtration. Some undisolved Na2CO3 could be present from the pulping. | Na2SO4, Li2CO3 |

## Filtration

After purification and each precipitation stage, the slurry goes through a filter to separate the solid impurities, or the recovered materials from the PLS. Table 12 summarizes the parameters used for each filter, as required by the built-in model of HSC Sim.

Table 14. Filtration parameters used in the simulation.

| Cake moisture | 30 % |
| --- | --- |
| Washing efficiency | 95 % |
| Washing water needed | 1 m3/ton solids |
| Filtrate solids | 0 % |

Filtration produces 3 outputs, the cake or solids, the filtrate, and the used cake wash water. The filtrate and the cake wash water are all mixed into a tank before feeding it to the precipitation reactor to minimize loss of material (i.e., some metallic ions can remain attached to the solid residues and can be washed off by the cake wash water).

# Pyrometallurgical Recycling of Black mass

## Reduction Smelting

In recycling waste LIBs through pyrometallurgical processes, the chemical composition of the battery cells allow it to be processed without mechanical pretreatment [13]. This means the whole battery cell can be fed directly to the furnace, and the same was assumed for the simulation. The battery cell composition used for the model was calculated based on information from Mohr’s and colleagues’ work and shown in Table 13 [14].

Table 15. Composition of a Li-ion battery cell used in simulating the smelting process.

| Phases | % |
| --- | --- |
| Al | 8.09% |
| Al2O3 | 0.43% |
| Cu | 16.31% |
| C | 22.46% |
| LiPF6 | 25.64% |
| PVDF | 2.84% |
| PPE | 4.96% |
| LiNi0.6Mn0.2Co0.2O2 | 19.86% |
| TOTAL | 100% |

For the reductant and fuel of the process, carbon based materials are commonly used. The C and Al contained in the LIBs can fullfill this role in the process but since it is not enough, additional metallurgical coke will be needed. The composition of the coke used in the simulation was derived from an analysis by Colorado-Arango and colleagues (Table 14). The amount of coke fed to the process was set at a 1:1 ratio to the feed mass but reduced by the amount of C and Al present in the feed.

Table 16. Composition of the coke used in simulating the smelting process.

| Content | C | H2O | SiO2 | Fe2O3 | Al2O3 | CaO | Total |
| --- | --- | --- | --- | --- | --- | --- | --- |
| % | 81.88% | 0.050% | 6.825% | 6.313% | 2.508% | 2.428% | 100.00% |

As seen in Figure 2, other inputs to the reduction smelting process are quicklime (CaO) and enriched air. Quicklime here works as the slag former flux which assists in the stability of the slag system i.e. slag formation and fluidity. The amount used in the simulation was set at 5% of the feed weight. It was observed that increasing this amount results to decreased recoveries of Co. This aligns with industry practice of minimizing the amount of slag formers added in the system to make sure that target metals are not trapped in the slag.

The enriched air on the other hand is assumed to contain 80% O2, and 20% N2 and to be preheated to 250°C, based on the hot gases temperature in an iron blast furnace [15]. The amount used for the simulated process was used to control the enthalpy balance of the whole system along with the excess heat released by the process. To identify the amount of heating power required to heat the enriched air, a separate simulation (Figure 3) conducted showed that about 0.0604 kWh of heat is needed per kilo of enriched air (see Supplementary Doc. No.1).

Figure 3. The simulation model in HSC Chemistry® for the heating of enriched air.

For the smelting process, the process output temperature was arbitrarily set at 1300°C, which is the average temperature in the smelting process temperature range [13], and operated in atmospheric pressure i.e., 1.01325 bar.

The process outputs’ composition had to be defined prior to activating the Gibbs/equilibrium wizard. Table 15 summarizes the expected composition of the simulation output as shown in Figure 2. Note that this does not necessarily mean that the actual output of the simulated process will have these components.

Table 17. Outputs of the simulated reduction smelting process.

| Ouputs | ALLOY | SLAG | OFFGAS | FLYASH |
| --- | --- | --- | --- | --- |
| Components | Ni Co Cu Fe Mn Li | Al2O3 MnO2 Li2O SiO2 Fe3O4 Fe2O3 CuO CoO NiO | CO2 CO N2 O2 NO H2O HF POF3 | SiO2 Fe2O3 Al2O3 CaO MnO2 |

# References

[1]	M. Pyda, Poly(vinylidene fluoride) (PVF2) Heat Capacity, Enthalpy, Entropy, Gibbs Energy: Datasheet from ‘The Advanced THermal Analysis System (ATHAS) Databank – Polymer Thermodynamics’ Release 2014 in SpringerMaterials (https://materials.springer.com/polymerthermodynamics/docs/athas_0154). (2014). Springer-Verlag Berlin Heidelberg & Marek Pyda. [Online]. Available: https://materials.springer.com/polymerthermodynamics/docs/athas_0154

[2]	K. S. Gavrichev, G. A. Sharpataya, L. N. Golushina, V. N. Plakhotnik, and I. V. Goncharova, ‘Heat capacity and thermodynamic functions of LiPF6’, Russian Journal of Inorganic Chemistry, vol. 47, no. 7, pp. 940–944, 2002.

[3]	P. Kobylin, T. Kotiranta, and M. Loponen, ‘HSC-Sim Reactions Unit’. Metso Finland Oy, Sep. 06, 2023.

[4]	T. Kawamura, S. Okada, and J. Yamaki, ‘Decomposition reaction of LiPF6-based electrolytes for lithium ion cells’, Journal of Power Sources, vol. 156, no. 2, pp. 547–554, Jun. 2006, doi: 10.1016/j.jpowsour.2005.05.084.

[5]	M. Wood, Y. Sheng, T. J. Keever, J. Li, and D. L. Wood, ‘Stability of Ni-Rich NMC Cathode Materials in Water and Electrolyte Solutions during Aqueous Electrode Processing’, Meet. Abstr., vol. MA2017-01, no. 5, pp. 376–376, Apr. 2017, doi: 10.1149/MA2017-01/5/376.

[6]	L. F. Guimarães, A. B. Botelho Junior, and D. C. R. Espinosa, ‘Sulfuric acid leaching of metals from waste Li-ion batteries without using reducing agent’, Minerals Engineering, vol. 183, p. 107597, Jun. 2022, doi: 10.1016/j.mineng.2022.107597.

[7]	X. Zhang et al., ‘Toward sustainable and systematic recycling of spent rechargeable batteries’, Chem. Soc. Rev., vol. 47, no. 19, pp. 7239–7302, 2018, doi: 10.1039/C8CS00297E.

[8]	J. Jung and J. Zhang, ‘Hydrometallurgical Recycling of Lithium-Ion Battery Cathode Material’, in Hydrometallurgical Recycling of Lithium-Ion Battery Materials, pp. 1–31.

[9]	B. Han, R. Anwar Ui Haq, and M. Louhi-Kultanen, ‘Lithium carbonate precipitation by homogeneous and heterogeneous reactive crystallization’, Hydrometallurgy, vol. 195, p. 105386, Aug. 2020, doi: 10.1016/j.hydromet.2020.105386.

[10]	H. Zou, E. Gratz, D. Apelian, and Y. Wang, ‘A novel method to recycle mixed cathode materials for lithium ion batteries’, Green Chem., vol. 15, no. 5, p. 1183, 2013, doi: 10.1039/c3gc40182k.

[11]	G. Battaglia et al., ‘Recovery of Lithium Carbonate from Dilute Li-Rich Brine via Homogenous and Heterogeneous Precipitation’, Ind. Eng. Chem. Res., vol. 61, no. 36, pp. 13589–13602, Sep. 2022, doi: 10.1021/acs.iecr.2c01397.

[12]	P. Meshram, B. D. Pandey, and T. R. Mankhand, ‘Hydrometallurgical processing of spent lithium ion batteries (LIBs) in the presence of a reducing agent with emphasis on kinetics of leaching’, Chemical Engineering Journal, vol. 281, pp. 418–427, Dec. 2015, doi: 10.1016/j.cej.2015.06.071.

[13]	B. Makuza, Q. Tian, X. Guo, K. Chattopadhyay, and D. Yu, ‘Pyrometallurgical options for recycling spent lithium-ion batteries: A comprehensive review’, Journal of Power Sources, vol. 491, p. 229622, Apr. 2021, doi: 10.1016/j.jpowsour.2021.229622.

[14]	‘Mohr et al (2020)_Toward a cell-chemistry specific LCA of LIB recycling processes’. Accessed: Mar. 29, 2023. [Online]. Available: https://onlinelibrary.wiley.com/doi/pdfdirect/10.1111/jiec.13021

[15]	H. Yin and P. Xing, ‘Pyrometallurgical Routes for the Recycling of Spent Lithium-Ion Batteries’, in Recycling of Spent Lithium-Ion Batteries, L. An, Ed., Cham: Springer International Publishing, 2019, pp. 57–83. doi: 10.1007/978-3-030-31834-5_3.

Industrial experience was for an industrial HPAL processing plant that treats limonite ore to extract mixed Ni-Co sulphides.