Agile life cycle assessment of waste plastic pyrolysis: implications of feedstock composition and processing conditions

Md Nurus Sakib 1, Rui Shi 1,2 *

1Chemical Engineering Department, The Pennsylvania State University, 121 Chemical and Biomedical Engineering Building, University Park, Pennsylvania 16802, USA

2 Institute of Energy and the Environment, The Pennsylvania State University, Land and Water Research Building, University Park, Pennsylvania 16802, USA

*Corresponding author

Summary

This supporting information describes the main assumptions and data used in the life cycle assessment of plastic pyrolysis. It includes information on transportation distance, process energy requirements, and greenhouse gas (GHG) emission and characterization factors.

Contents

S1. Primary Assumptions for the Pyrolysis Process

S2. Carbon Contents of Feedstocks and Products

S3. Composition and Distribution of Pyrolysis Products

S4. Thermochemical Properties of Feedstocks and Products

S5. Global Warming Potential (GWP) and GHG Emission Factors

S6. Char Handling

S7. Sample GHG Emission Calculation and Sensitivity Analysis

S8. References

S1. Primary Assumptions for the Pyrolysis Process

Table S1: Assumptions considered for the overall pyrolysis plant; including the curbside transportation to the recycling facility where NRP plastic is separated

|  |  | Value | Units | References |
| --- | --- | --- | --- | --- |
| Collected waste and NRP separation stage | Transportation distance to separation facilities | 98.81 | miles | (Benavides et al. 2017; Wang et al. 2021) |
|  | Fraction of plastics in MSW | 0.177 |  |  |
|  | Separation energy (Electricity) | 0.0649 | MMBTU/wet-ton |  |
|  | Fraction NRP | 0.49 |  |  |
| Pyrolysis and upgradation stage | Plant capacity | 18120 | lb plastic/hr | (Larrain et al. 2020) |
|  | Baseline value for natural gas contribution to pyrolysis energy conversion | 12.5 | % | (Wang et al. 2021) |
|  | Baseline value for electricity contribution to pyrolysis energy conversion | 87.5 | % |  |
|  | Baseline electricity generation efficiency | 33.8 | % |  |
|  | Fuel upgradation downstream process | 0.44 | MJ/h/kg liquid processed | (Gracida-Alvarez et al. 2019) |

Plant capacity

A plant capacity of approximately 70 kt per year was selected, as this represents the minimum capacity at which plastic pyrolysis plants are typically considered economically feasible (Larrain et al. 2020). This is also roughly 45% of the total annual recyclable plastics disposed of in the state of PA. (Pennsylvania Department of Environmental Protection 2003)

S2. Carbon Contents of Feedstocks and Products

Table S2.1. The carbon contents of the feedstock and the products

| Components | Fraction C | References |
| --- | --- | --- |
| HDPE | 0.842 | Table S2.2 |
| LDPE | 0.840 |  |
| PP | 0.839 |  |
| Wax | 0.33 | (Wang et al. 2021, 2023) |
| Fuel Gas | 0.76 |  |
| Gasoline | 0.83 |  |
| Diesel | 0.87 |  |

Table S2.2. Averaged carbon contents of the feedstocks

| Feedstock | (Smeaton 2021) | Other sources | Fraction C (Averaged) |
| --- | --- | --- | --- |
| HDPE | 0.833 | 0.8503[*] | 0.842 |
| LDPE | 0.820 | 0.86[**] | 0.840 |
| PP | 0.818 | 0.86[***] | 0.839 |

[*] (Hosseini et al. 2014)

[**](Petrovic Aleksandra et al. 2022)

[***] (Yaqoob et al. 2022)

S3. Composition and Distribution of Pyrolysis Products

Table S3.1 Pyrolysis product distribution of the three plastic types at 550 °C (Marcilla et al. 2009; Onwudili et al. 2009; Jung et al. 2010; Wulan et al. 2018)

| Group | Components | Component % in HDPE | Component % in LDPE | Component % in PP |
| --- | --- | --- | --- | --- |
|  | Methane | 5.06 | 4.6 | 41.18 |
|  | Ethane | 9.82 | 7.47 | 9.84 |
|  | Ethylene | 14.25 | 12.56 | 7.49 |
| Gas | Propane | 8.63 | 12.74 | 4.22 |
|  | Propylene | 20.67 | 19.41 | 21.98 |
|  | Isobutane | 0 | 0 | 1.53 |
|  | N butane | 7.56 | 9.2 | 0 |
|  | Butene | 34.01 | 34.02 | 13.77 |
|  | Pentane | 4.21 | 6.63 | - |
|  | Pentene | 10.69 | 11.44 | - |
|  | Hexane | 3.51 | 5.52 | - |
|  | Hexene | 25.42 | 29.43 | - |
|  | Heptane | 6.79 | 8.47 | - |
|  | Heptene | 14.54 | 15.90 | - |
|  | Octane | 2.81 | 6.26 | - |
|  | Octene | 0.42 | 4.48 | - |
|  | Nonane | 2.34 | - | - |
|  | Nonene | 3.16 | 0.08 | - |
|  | Decane | 7.26 | 5.50 | - |
| Light Oil | Decene | 11.45 | 4.60 | - |
|  | 1-Hexene, 3,3-Dimethyl- | - | - | 7.82 |
|  | 2,3-Dimethyl-3-Heptene | - | - | 33.03 |
|  | Cyclohexane, 1,2,4-Trimethyl- | - | - | 27.87 |
|  | Cyclohexane, 1,1,3,5 Tetramethyl | - | - | 30.09 |
|  | Cyclohexane, 1 Ethyl 1,4 Dimethyl | - | - | 1.19 |
|  | Nonadiene | 1.60 | 0.03 | - |
|  | Decadiene | 5.79 | 1.67 | - |

Table S3.1 (Continued) Pyrolysis product distribution of the three plastic types at 550 °C (Marcilla et al. 2009; Onwudili et al. 2009; Jung et al. 2010; Wulan et al. 2018)

| Group | Components | Component % in HDPE | Component % in LDPE | Component % in PP |
| --- | --- | --- | --- | --- |
|  | N Undecane | 2.22 | 2.56 | - |
|  | Undecene | 4.30 | 3.55 | - |
|  | Dodecane | 2.07 | 3.04 | - |
|  | Dodecene | 4.15 | 4.45 | - |
|  | N Tridecane | 2.30 | 3.17 | - |
|  | Tridecene | 4.26 | 4.37 | - |
|  | N Tetradecane | 2.53 | 3.29 | - |
|  | Tetradecene | 4.70 | 4.50 | - |
|  | N Pentadecane | 2.66 | 3.77 | - |
|  | Pentadecene | 5.22 | 5.20 | - |
|  | Hexadecane | 2.83 | 4.38 | - |
|  | Hexadecene | 5.10 | 4.70 | - |
|  | Heptadecane | 3.14 | 4.50 | - |
|  | Heptadecene | 5.10 | 4.94 | - |
|  | Octadecane | 3.29 | 4.87 | - |
|  | Octadecene | 5.90 | 5.33 | - |
| Heavy Oil | Nonadecane | 3.37 | 5.36 | - |
|  | Nonadecene | 6.57 | 5.31 | - |
|  | 1,11-Dodecadiene | 2.10 | 1.62 | - |
|  | 1,12-Tridecadiene | 2.15 | 1.59 | - |
|  | 1,13-Tetradecadiene | 2.38 | 1.63 | - |
|  | Un decadiene | 2.17 | 1.29 | - |
|  | Penta decadiene | 2.64 | 1.89 | - |
|  | Hexa decadiene | 2.58 | 1.71 | - |
|  | Hepta decadiene | 2.58 | 1.79 | - |
|  | Octa decadiene | 2.98 | - | - |
|  | Icosene | 6.98 | 5.71 | - |
|  | Eicosane | 3.75 | 5.48 | - |
|  | 2,6 Dimethyl Nonane | - | - | 4.94 |
|  | 4,6 Dimethyl Dodecane | - | - | 0.65 |
|  | 4 Methyl 2 Un decene | - | - | 6.70 |
|  | Cyclooctane, Butyl- | - | - | 2.59 |
|  | Cyclohexane, 1-Ethyl-2-Propyl- | - | - | 42.09 |
|  | Cyclohexane, 2,4-Diethyl-1-Methyl- | - | - | 41.56 |
|  | Cyclooctane, 1-Methyl-3-Propyl- | - | - | 1.47 |
| Aromatics | Benzene | 100 | 100 | 50 |
|  | Toluene |  |  | 50 |

Table S3.2 Pyrolysis product distribution of the three plastic types at 600 °C ((Elordi et al. 2011; Lee et al. 2021; Park and Lee 2021; Zhou et al. 2021; Liu et al. 2023)

| Group | Components | Component % in HDPE | Component % in LDPE | Component % in PP |
| --- | --- | --- | --- | --- |
|  | Methane | 2.89 | 8.08 | 4.79 |
|  | Ethane | 1.44 | 19.00 | 13.88 |
|  | Ethylene | 22.56 | 17.10 | 1.91 |
|  | Propane | 4.69 | 28.19 | 4.79 |
| Gas | Propylene | 37.36 | 27.63 | 74.64 |
|  | Isobutane | 0.54 | - | - |
|  | N butane | 5.96 | - | - |
|  | Butene | 19.13 | - | - |
|  | Butadiene | 5.43 | - | - |
|  | Pentane | 3.51 | - | - |
|  | Pentene | 9.35 | - | - |
|  | Hexane | 6.71 | - | 1.67 |
|  | Hexene | 13.42 | - | 3.92 |
|  | Heptane | 4.37 | - | 2.81 |
|  | Heptene | 13.72 | - | 6.57 |
|  | Octane | 5.26 | 8.13 | 5.91 |
|  | Octene | 8.18 | 12.73 | 13.73 |
|  | Nonane | 5.69 | 14.11 | 4.64 |
|  | Nonene | 7.88 | 10.43 | 10.76 |
| Light Oil | Decane | 9.94 | 29.29 | 2.87 |
|  | Decene | 11.97 | 25.31 | 6.69 |
|  | Cyclohexane | - | - | 1.36 |
|  | Methylcyclohexane | - | - | 2.27 |
|  | Dimethyl cyclohexane | - | - | 4.75 |
|  | Cyclohexane, 1,2,4-Trimethyl- | - | - | 3.70 |
|  | Cyclohexene, 1-Methyl- | - | - | 4.12 |
|  | Cyclohexane, 1,1,3,5 Tetramethyl | - | - | 2.32 |
|  | Cyclohexene | - | - | 2.45 |
|  | Dimethyl Cyclohexene | - | - | 8.56 |
|  | Trimethyl Cyclohexene | - | - | 6.73 |
|  | Trimethyl Cycloheptene | - | - | 4.17 |

Table S3.2 (Continued) Pyrolysis product distribution of the three plastic types at 600 °C ((Elordi et al. 2011; Lee et al. 2021; Park and Lee 2021; Zhou et al. 2021; Liu et al. 2023)

| Group | Components | Component % in HDPE | Component % in LDPE | Component % in PP |
| --- | --- | --- | --- | --- |
|  | N Undecane | 5.48 | 3.22 | 12.72 |
|  | Undecene | 6.23 | 2.53 | 8.42 |
|  | Dodecane | 4.69 | 3.74 | 11.26 |
|  | Dodecene | 7.98 | 2.92 | 7.48 |
|  | N Tridecane | 1.78 | 3.70 | 9.84 |
|  | Tridecene | 5.47 | 4.04 | 6.53 |
|  | N Tetradecane | 0.78 | 3.86 | 7.52 |
|  | Tetradecene | 2.62 | 4.95 | 4.98 |
|  | N Pentadecane | 1.34 | 4.43 | 8.38 |
|  | Pentadecene | 4.01 | 4.78 | 5.54 |
|  | Hexadecane | 2.02 | 4.49 | 5.50 |
| Heavy Oil | Hexadecene | 4.86 | 4.62 | 3.65 |
|  | Heptadecane | 2.45 | 4.29 | 4.90 |
|  | Heptadecene | 5.75 | 4.84 | 3.27 |
|  | Octadecane | 2.84 | 4.25 | - |
|  | Octadecene | 7.59 | 4.67 | - |
|  | Nonadecane | 2.69 | 4.35 | - |
|  | Nonadecene | 7.87 | 5.45 | - |
|  | 1,11-Dodecadiene | 0.45 | 0.55 | - |
|  | 1,12-Tridecadiene | 1.62 | 0.63 | - |
|  | 1,13-Tetradecadiene | 0.56 | 0.76 | - |
|  | Penta decadiene | 0.95 | 0.81 | - |
|  | Hexa decadiene | 1.62 | 0.99 | - |
|  | Hepta decadiene | 2.23 | 0.81 | - |
|  | Octa decadiene | 2.84 | 0.90 | - |
|  | 1,19-Eicosadiene | 3.12 | 0.78 | - |
|  | Henicosene | - | 4.82 | - |
|  | Henicosane | - | 4.68 | - |
|  | Icosene | 7.26 | 4.68 | - |
|  | Eicosane | 2.84 | 4.49 | - |
|  | Benzene | 10.98 | - | 10.99 |
|  | Ethylbenzene | 21.97 | 3.56 | 38.58 |
| Aromatics | Toluene | 35.55 | 3.35 | 18.49 |
|  | Propyl benzene | 13.58 | - | 30.29 |
|  | Naphthalene, Decahydro-1-Undecyl- | - | - | 1.66 |
|  | Azulene | 17.92 | 93.09 | - |

Product distribution for the plastic-to-fuel pathway

Two types of products are considered in this study: liquid and non-condensable gas. The liquid (main product), also stated as blend stock, includes light oil, heavy oil, and aromatics (Fig. S3). Gas fraction is considered to be fuel gas.

Fig. S1 Pyrolysis yield (%) at two different temperatures obtained using the kinematic model from Kulas et al. (2021)

The product distribution using the lump kinetic model (Kulas et al. 2021) shows that in general, high LDPE fractions produce more liquid products (diesel and gasoline) while high HDPE fractions produce more fuel gas as seen in Figure S3. This finding is in line with studies based on plastic pyrolysis. Sharuddin et al. stated that among the polyolefins, LDPE produces the highest oil when pyrolyzed (Anuar Sharuddin et al. 2016). A neural network model developed using the data from non-recycled plastic data available in the literature also points out LDPE produces the highest oil yield when compared with HDPE and PP (Abnisa et al. 2019). When HDPE and PP are compared for gas yields, HDPE shows high gas production. (Hwang et al. 2001).

S4. Thermochemical Properties of Feedstocks and Products

Table S4.1 Averaged values of heat of formation, specific heat, and molecular weight for each product type (gas, light oil, heavy oils, and aromatics respectively) at 550 °C

|  | Components | Average Specific Heat (J/(mol.K)) | Average Heat of Formation (KJ/mol) | Average Molecular Weight (g/mol) |
| --- | --- | --- | --- | --- |
| Gas | PP | 41.33 | -53.16 | 24.689 |
|  | LDPE | 73.05 | -23.81 | 40.038 |
|  | HDPE | 70.28 | -19.84 | 38.864 |
| Light Oil | PP | 357.96 | -172.7 | 128.89 |
|  | LDPE | 226.67 | -90.4 | 91.388 |
|  | HDPE | 240.34 | -86.06 | 97.223 |
| Heavy Oil | PP | 451.138 | -243.355 | 156.127 |
|  | LDPE | 651.98 | -271.5 | 214.7 |
|  | HDPE | 638.76 | -247.3 | 213.84 |
| Aromatics | PP | 212.22 | 77.181 | 90.0 |
|  | LDPE | 210.9 | 82.98 | 78.11 |
|  | HDPE | 210.9 | 82.98 | 78.11 |

Table S4.2 Averaged values of heat of formation, specific heat, and molecular weight for each product type (gas, light oil, heavy oils, and aromatics respectively) at 600 °C

|  | Components | Average Specific Heat (J/(mol.K)) | Average Heat of Formation (KJ/mol) | Average Molecular Weight (g/mol) |
| --- | --- | --- | --- | --- |
| Gas | PP | 58.745 | -3.912 | 38.996 |
|  | LDPE | 57.097 | -36.664 | 32.885 |
|  | HDPE | 68.438 | 13.099 | 38.764 |
| Light Oil | PP | 292.742 | -125.093 | 112.816 |
|  | LDPE | 353.301 | -172.529 | 130.996 |
|  | HDPE | 259.001 | -110.776 | 101.670 |
| Heavy Oil | PP | 551.365 | -263.554 | 185.353 |
|  | LDPE | 671.194 | -290.377 | 219.282 |
|  | HDPE | 639.821 | -252.659 | 212.897 |
| Aromatics | PP | 280.771 | 48.582 | 103.909 |
|  | LDPE | 281.932 | 286.033 | 125.579 |
|  | HDPE | 313.864 | 90.246 | 101.399 |

Table S4.3 Higher heating values (HHV) of the plastic feedstocks considered in this study

| Components |  | HHV (MJ/kg) of repeating units | References |
| --- | --- | --- | --- |
| HDPE | 45.67 |  | (Montejo et al. 2011) |
| LDPE | 46 |  | (Zevenhoven et al. 1997) |
| PP | 46.5 |  |  |

From the HHV values, we can find the heat of formation per unit chain by (Walters et al. 2000) using the heat of combustion equation. The values of the heat of formation for plastics vary depending on the type of plastic.

Table S4.4 Heat of formation of plastics investigated in this study

| Components | Heat of Formation (MJ/kg) |
| --- | --- |
| LDPE | -2.524 |
| HDPE | -2.854 |
| PP | -2.024 |

S5. Global Warming Potential (GWP) and GHG Emission Factors

Characterization factors (Table S5) were taken from the sixth assessment report (AR6) from the  Intergovernmental Panel on Climate Change (IPCC). GHG emissions per kg of hydrogen are taken following the ‘ReCiPe Midpoint (H) V1.13’ methodology; GHG Emission for hydrogen (per kg) as the market for hydrogen, gaseous, location: GLO, is 1.560519 kg CO2 eq. (Huijbregts et al. 2016).

Table S5. Table for carbon footprint equivalency factors (IPCC AR6)

| Species | GWP-100 |
| --- | --- |
| CO2 | 1 |
| CH4 | 29.8 |
| N2O | 273 |

S6. Char Handling

In the base-case study, emissions from end-of-life and transportation for char were excluded. Emissions from char transportation were 0.006 gCO2 eq./MJ of fuel. Table S6 presents the GHG emissions for scenarios when char is considered a co-product.

Table S6. Table representing GHG emissions for char handled as a co-product

| Char handling | Averaged GHG emissions (or credit) in gCO2 eq./MJ of fuel |
| --- | --- |
| Char when credited for sequestration with displacement | -0.99 |
| Char when credited for sequestration with energy allocation | -0.93 |

S7. Sample GHG Emission Calculation and Sensitivity Analysis for Heat Loss

S7.1 Sample GHG Emission Calculation

Sample calculation for 600 °C , VRT 2, and a composition of HDPE:LDPE:PP 24%:49%:27%, with a baseline fuel-gas-to electricity conversion efficiency of 33.8%

Product yield determination

The product distribution was obtained via kinetic model (Kulas et al. 2021)

Table S7.1 Pyrolysis product distribution (fraction) at 600 °C, VRT 2

| Plastic type | Aromatics | Gas | Heavy | Light | Wax |
| --- | --- | --- | --- | --- | --- |
| HDPE | 0.007 | 0.247 | 0.311 | 0.399 | 0.036 |
| LDPE | 0.019 | 0.203 | 0.351 | 0.389 | 0.038 |
| PP | 0.025 | 0.289 | 0.195 | 0.490 | 0.002 |

The overall yield of each product species was determined using a weighted-average approach that accounted for the fraction of each plastic type in the feedstock and its respective product yield. For example,

Total aromatics fraction  =  HDPE wt% in plastic × HDPE Aromatics yield + LDPE wt% in plastic× LDPE Aromatics yield + PP wt% in plastic× PP Aromatics yield                                                                           =0.24×0.007+0.49×0.019+0.27×0.025=0.018

Following similar equations, total fractions for other species were calculated.

Total gas fraction = 0.237

Total heavy fraction = 0.299

Total light fraction = 0.419

The remaining fraction, wax, was considered to have an insignificant impact on GHG emission calculation. The only time wax was considered was when calculating carbon balance for non-combustion emissions

Of the total oil after hydro processing, it was assumed that around  81.43 % was gasoline range and the remaining were diesel range; averaged from literature data (Dutta et al. 2015; Gracida-Alvarez et al. 2019). Because the literature reported aromatics in the C11 carbon-number range, a gasoline-to-diesel distribution ratio was applied to partition these compounds into light and heavy aromatic fractions. The resulting fractions were then assigned to the light- and heavy-oil product streams, respectively.

The assumed plant capacity was 18120 lb/hr.

Total diesel produced (without considering H2 amount) = Light fraction+Heavy fraction+Aromatics fraction×Plant capacity ×Diesel ratio (18.57%) =2474.6244 lb/hr

Similarly, total gasoline produced (without considering H2 amount) = 10851.3 lb/hr

Total hydrogen required=  Total liquid processed ×329.5526556.884=161.358kghr

Hydrogen required was assumed to be proportional to liquid processed in the upgrading section. The ratio 329.55 kg hydrogen26556.884 lb liquid processed  was obtained from (Gracida-Alvarez et al. 2019).

Total blend stock produced with hydrogen amount=  Total liquid amount+Total hydrogen amount =13681.66lbhr ; As it was considered that the upgraded liquid incorporates the hydrogen mass.

Based on GREET ™ heating value ,

Averaged blend stock heating value was calculated to be 18167.28 BTU/lb of blend stock, based on diesel and gasoline fraction in the blend stock.

Although hydro processing with hydrogen in most cases increases heating values, for simpler calculation, typical diesel and gasoline heating values were considered. Throughout the calculation, heating values refer to lower heating value of the components.

Component properties determination

As a sample calculation for heat of formation, specific heat and average molecular weight for HDPE light oil fraction is provided. The assumed component fractions were obtained from (Elordi et al. 2011). Component properties were obtained from online repositories (Joback and Reid 1987; Linstrom 1997; Chemeo 2022).

Table S7.2 Average thermochemical properties and molecular weight determination for light oil from HDPE fraction

|  | Wt% from (Elordi et al. 2011) | Molecular weight (MW) g/mol | Heat of formation (HF) KJ/mol | Specific heat (SP) J/(mol.K) | Moles (M) | Mole fraction (MF) |
| --- | --- | --- | --- | --- | --- | --- |
| Equation |  |  |  |  | Wt. fractionMW | =MiMoles |
| Pentane | 0.48 | 72.151 | -146.6 | 232.9 | 0.006653 | 0.049371 |
| Pentene | 1.28 | 70.13 | -29.31 | 151.8 | 0.018252 | 0.13545 |
| Hexane | 0.92 | 86.18 | -167.7 | 206.94 | 0.010675 | 0.079224 |
| Hexene | 1.84 | 84.1608 | -41.4 | 199.69 | 0.021863 | 0.162249 |
| Heptane | 0.6 | 100.21 | -187.7 | 238.49 | 0.005987 | 0.044434 |
| Heptene | 1.88 | 98.18 | -70.59 | 243.33 | 0.019149 | 0.142105 |
| Octane | 0.72 | 114.23 | -208.4 | 297 | 0.006303 | 0.046776 |
| Octene | 1.12 | 112.24 | -82.93 | 285.74 | 0.009979 | 0.074053 |
| Nonane | 0.78 | 128.2 | -228.3 | 349.98 | 0.006084 | 0.045152 |
| Nonene | 1.08 | 126.25 | -103.6 | 331.38 | 0.008554 | 0.063484 |
| Decane | 1.36 | 142.29 | -249.7 | 397.93 | 0.009558 | 0.070931 |
| Decene | 1.64 | 140.266 | -123.4 | 378.63 | 0.011692 | 0.086769 |

For average values,

Average specific heat SP= Specific heat of each component SPi×Mole fraction of each component MFi=259Jmol K

Average heat of formation (HF)= Heat of formation for each component HFi×Mole fraction of each component MFi= -110.78kJmol

Average molecular weight (MW)= Molecular weight of each component MWi×Mole fraction of each component MFi=101.67gmol

Converting HF from unit mol to kg ,  Average HFAverage MW= -1317.05 kJ/kg

Converting SP from unit mol to kg = Average SPAverage MW=2.69kJkgK

The average values of HF, SP and MW are listed in Table S 4.2 for all types of products at 600 °C

Plastic heat of formation calculation

Heat of formation was calculated following a combustion reaction for repeating units. As an example, LDPE heat of formation is provided. Other heat of formation values are given in S 4.4

-CH2- + 32O2→CO2+H2O

Heat of formation for LDPE= -Higher heating value of CO2+Higher heating value of H2O -Higher heating value of plasticsMW of repeating unit(for unit conversion)=-2524.3 kJ/kg

The heating values of all plastics are provided in Table S4.3

Pyrolysis conversion and upgradation energy requirements determination

Conversion energy required (kJ kg⁻¹) was calculated as the difference between the weighted (multiplied with weight fractions) heat of formation of the hydrocarbon products at vapor/gas phase and the weighted heat of formation of the feed plastics, plus the sensible heat required to raise the products from 25 °C (reference point) to 600 °C, including heat losses (1% of plastic heating value).

Conversion energy required (kJ / kg plastic),

= [Weighted HF of products] - [Weighted HF of feed plastics] + [Weighted sensible heating requirement of products × (600 - 25) °C] + Heat loss

=  [ { HDPE fraction × (Aromatics fraction × HF of HDPE derived aromatics + Gas fraction × HF of HDPE derived gas + Heavy fraction × HF of HDPE derived heavy fraction + light fraction × HF of HDPE derived light fraction) + LDPE fraction × (aromatics fraction × HF of LDPE derived aromatics + Gas fraction × HF of LDPE derived gas + Heavy fraction × HF of LDPE derived heavy fraction +Light fraction × HF of LDPE derived light fraction) +PP fraction × (Aromatics fraction × HF of PP derived aromatics + gas fraction × HF of PP derived gas + heavy fraction × HF of PP derived heavy fraction + light fraction × HF of PP derived light fraction)} - (HDPE fraction × HF of HDPE + LDPE fraction × HF of LDPE +PP fraction × HF of PP) + {HDPE fraction × (aromatics fraction × SP of HDPE derived aromatics + gas fraction × SP of HDPE derived gas + heavy fraction × SP of HDPE derived heavy fraction + light fraction × SP of HDPE derived light fraction) + LDPE fraction × (aromatics fraction × SP of LDPE derived aromatics + gas fraction × SP of LDPE derived gas + heavy fraction × SP of LDPE derived heavy fraction + light fraction × SP of LDPE derived light fraction) + PP fraction × (aromatics fraction × SP of PP derived aromatics + Gas fraction × SP of PP derived gas + Heavy fraction × SP of PP  derived heavy fraction + Light fraction × SP of PP derived light fraction)} ×  (600-25) °C + Heat loss considered

= 3358.67 kJ/kg plastic

Energy required MMBTUhour

=(3358.67kJkg×0.947 kJ to BTU1000000 BTU to MMBTU × 0.4535kglb× Plant capacitylbhr) MMBTU/hr

= 26.137 MMBTU / hr

Upgrading energy required = Energy for downstream fuel upgrading + Energy required to heat up hydrogen= Total capacity × aromatics fraction + light fraction + heavy fraction× lb to kg conversion factor × fuel upgrading energy intensity × GJ to MMBTU conversion factor +  Total hydrogen required × Hydrogen specific heat capacity × 150 - 25°C × MJ to MMBTU conversion factor = 2.797 MMBTU/hr

Fuel upgrading energy intensity is provided in Table S1. A constant hydrogen specific heat capacity of 14.29 kJ·kg⁻¹·K⁻¹ was assumed for calculating the sensible heat required to increase the hydrogen temperature from 25°C to 150°C. The variation in hydrogen heat capacity over this temperature range was assumed negligible.

Pretreatment energy calculation

For pretreatment energy, scaled value from the GREET model ™ was assumed.

In GREET 2021, 161 BTU /lb liquid or approximately 0.33 MMBTU/ton liquid was assumed to be the pre-treatment energy requirement. An additional ~86% efficiency  was assumed for the motors for pre-treatment equipment like crushers/grinders (OSTI 2014).

Pretreatment energy required MMBTUhr= 1.16× 0.33 MMBTU/ton× (Total liquid amount)/2000 (ton/lb)

=2..55 MMBTU/hr

Since pre-treatment energy was considered fully sourced from electricity,

Total electricity required = (Pretreatment energy required +  Fraction electricity of total energy×Pyrolysis conversion energy)= (2.55+ 22.869)MMBTU/hr = 25.42 MMBTU/hr

Total natural gas (NG) required = (Pyrolysis conversion energy×Fraction NG of total energy + Upgradation energy required) = 6.06 MMBTU/hr

It was assumed that the liquid upgradation energy or hydro processing was fully sourced from NG. Assumed types of energy (NG or electricity) contribution fractions are listed in Table S1.

Normalized inventory values (in per lb. of blend stock unit)

Blend stock carbon content

= Carbon fraction of diesel× Diesel amount +  Carbon fraction of gasoline × Gasoline amount Total amount of blend stock

=0.813  % C / lb. blend stock

Feedstock amount = Total capacityTotal amount of blend stock =1.3244lblb blend stock

Fuel gas amount = Total fuel gasTotal amount of blend stock=0.3136 lblb blend stock

Total NG =Total NG requiredTotal amount of blend stock =0.000443MMBTUlb blendstock

Total electricity =Total electricity requiredTotal amount of blend stock =0.001858MMBTUlb blendstock

Total feedstock carbon  = Fraction of HDPE in feedstock× %C of HDPE + Fraction of LDPE in feedstock × %C of LDPE + Fraction of PP in feedstock × % C of PP× Normalized feedstock valuelb feedstocklb of blend stock=1.113 % C / lb. blend stock

Section 2 (Table S2.1 and S2.2) lists the carbon content assumed in this study for products and feedstocks.

GHG calculation

The estimation of GHG emissions followed the calculation framework employed in the GREET™ model, using the corresponding GREET™ emission factors (Wang et al. 2021, 2023). The GREET ™ 2021 version was used as the basis for process modelling as the waste plastic-to-fuel pathway and associated inventory structure and emission calculation employed in this work were followed the model. The GREET ™ 2023 model was used as a source of updated emission factors for energy and material inputs (such as emission factors for natural gas as processing fuel, emission factors for electricity generation, emission factors for waste plastic separation energy, emission factors for char handling, etc.).  The use of updated emission factors may influence the absolute carbon footprint values relative to those obtained using GREET™ 2021 emission factors. However, because all scenarios were evaluated using the same modified modeling framework and the same set of GREET™ 2023 emission factors, the comparative analysis, relative differences, and overall trends reported in this study remain internally consistent. A Sample boiler emission is listed in Table S7.3 below.

Table S7.3 Component emissions from utility/industrial boiler (>100 MMBTU/hr input)

| Component | Emissions in grams/MMBTU |
| --- | --- |
| VOC | 2.54 |
| CO | 22.21 |
| NOx | 36.4 |
| PM10 | 3.507 |
| PM25 | 3.507 |
| SOx | 0.269 |
| BC | 0.579 |
| OC | 1.501 |
| CH4 | 1.06 |
| N2O | 0.75 |
| CO2 | 59367 |
| CO2_equivalence | 59409.82 |
| GHG (g CO2 eq.) | 59646.16 |

Table S7.4 List of GHG emissions from different processes (Wang et al. 2021, 2023)

| List of emissions from different processes |  |
| --- | --- |
| Total electricity generation emissions (US Mix) | 128806 g CO2 eq. /MMBTU of electricity available at user sites |
| Emissions from Natural Gas as processing fuel (as stationary fuel) | 13382 g CO2 eq. /MMBTU of fuel |
| Emissions for industrial boiler (10-100 MMBTU/hr boiler) | 59534 g CO2 eq. /MMBTU of fuel |
| Emission for industrial boiler (> 100 MMBTU/hr ) | 59646 g CO2 eq. /MMBTU of fuel |
| GHG for transportation of MSW | 387.815 g CO2 eq. /mile/ ton of plastics transported |
| Separation of PUP energy emissions | 17240.79642 g CO2 eq. /dry ton |

Table S7.5 List of carbon ratio of pollutants (Wang et al. 2021, 2023)

| Component | Carbon ratio |
| --- | --- |
| VOC | 0.85 |
| CO | 0.43 |
| CH4 | 0.75 |
| CO2 | 0.27 |

Transportation

With an assumed distance of 98.81 miles,

GHG emissions per lb of plastic = Distance× Emission factor for transportation = 98.81 miles × 387.815 gCO2eq.per ton per mile ×1 2000    (tonlb of plastic)=19.16  g CO2 eq. / lb of plastics

Separation emission

Separation emission=  Separation emissionfactorg CO2 eq.per ton plastics ×12000× (ton/lb) =8.62  g CO2 eq. / lb of plastics

GHG emissions for NG = NG consumedMMBTUlb of blendstock× (GHG emissions for natural gas as processing fuel + GHG emissions for industrial Boiler) =32.32 g CO2eq. / lb of blendstock

GHG emissions for electricity = Electricity consumedMMBTUlb of blendstock× (Total GHG emissions for electricity generation emissions) =239.32 g CO2 eq. / lb of blendstock

Scenario 1

Internal generation of heating requirements

Since there are enough fuel gas produced, internal generation of heating completely offsets natural gas requirements.

Emissions due to internal generation

CO2 emissions for fuel gas internal combustion for heating = Total NG required MMBTUlb of blendstock× MMBTU to BTU×1heating value of fuel gas× Carbon fraction of fuel gas×1carbon ratio of pollutants for CO2× lb to grams - Total NG required MMBTUlb of blendstock × VOC from industrial boiler gramsMMBTU fuel × Carbon ratio for VOC + Total NG required MMBTUlb of blendstock × CO emission from industrial boiler gramsMMBTU fuel × Carbon ratio for CO + Total NG required MMBTUlb of blendstock × CH4 from industrial boiler gramsMMBTU fuel × Carbon ratio for CH4 ×1carbon ratio for CO2   = 25.513 g CO2 / lb of blendstock

GHG emissions from fuel gas combustion =CO2 emissions for fuel gas internal combustion for heating + Total NG required MMBTUlb of blendstock × VOC emission from boilergramsMMBTU fuel × carbon ratio for VOCcarbon ratio for CO2+ CO emission from boiler gramsMMBTU fuel × carbon ratio for COcarbon ratio for CO2+ GWP  for CH4 × CH4 emissions ingramsMMBTU+ N2O emissions ingramsMMBTU× GWP for N2O=25.636 g CO2 eq. / lb of blendstock

GWP values are given in Table S5, carbon ratios are given in Table S7.5

Remaining fuel gas to sell as energy product= Normalized fuel gas amount× Fuel gas heating value - Total NG required MMBTUlb blend stock × MMBTU to BTU=6439.96BTUlb blendstock

Non-combustion emissions

Table S7.6 Assumed VOC and CO non-combustion emissions (Wang et al. 2021)

| Component | Grams/lb product |
| --- | --- |
| VOC | 0.13 |
| CO | 0.74 |

CO2 emission for noncombustion emission= { Feedstock carbon 1lb blend stock - ( blend stock carbon 1lb blend stock + Normalized wax lblb blend stock × % C in wax + Remaining fuel gas × %C in fuel gas  fuel gas heating value)+((Total NG required × (VOC emission from industrial boiler× Carbon ratio for VOC+  CO from industrial boiler × carbon ratio for CO +  CH4 from industrial boiler × Carbon ratio for CH4) + CO2 emission from internal combustion × carbon ratio for CO2) × g to lb))}× lb to gramcarbon ratio for CO2 =84.7 g CO2 / lb of blendstock

GHG Emissions from non combustion emissions = CO2 emissions from noncombustion emission + Non combustion VOC emissiongMMBTU× carbon ratio for VOCcarbon ratio for CO2+ Noncombustion CO emission from boilergMMBTU×carbon ratio for COcarbon ratio for CO2=86.27 g CO2 eq. / lb of blendstock

GHG for hydrogen = Normalized hydrogen amount kglb blend stock× hydrogen emission factor × kg to gram = 18.4 g CO2 eq. / lb of blendstock

Emission factor for hydrogen is provided in Section S5

Total GHG emissions = Emission from transportation + Emission from separation energy×Normalized feedstock Blend stock heating value×1BTU to MMBTU  +GHG emissions from electricity use + internal combustion + non combustion + hydrogen use blend stock heating value ×1BTUto MMBTU=22370.86g CO2eq.  MMBTU of blendstock

Energy allocation

For scenario 1, after meeting internal NG demand, excess fuel gas (if any) was exported.

Energy allocation factor =Heating value of the blend stock Heating value of blend stock + Remaining fuel gas heating value=0.73829

Allocated GHG emission = Energy allocation factor× (Emission from transportation + emission from separation energy)×Normalized feedstock Blend stock heating value×1BTU to MMBTU   +(GHG emissions from (Energy allocation factor×electricity use + Energy allocation factor×internal combustion + Energy allocation factor×non combustion + Hydrogen use))/( blend stock heating value)   ×1/BTU to MMBTU=22370.86 (g CO2 eq.)/( MMBTU of blendstock)=16781.31 g CO2 eq.  MMBTU of blendstock =15.91g CO2 eq.  MJ of blendstock

A conversion factor of 1055 (MMBTU to MJ) was assumed. Hydrogen burden was not allocated since it was assumed that hydrogen was solely used for liquid oil upgradation.

Scenario 2

For scenario 2, first it was checked if remaining fuel gas could meet the electricity demand. For the assumed case, it met the demand ;

Fuel gas remaining after internal heat MMBTUlb blend stock× Fuelgas to electricity conversion efficiency > electricity requirement MMBTUlb blend stock

The efficiency was assumed to be 33.8% as baseline.

Electricity generated with the remaining fuel gas = Fuel gas amount remaining× Fuelgas to electricity conversion efficiency=2176.73BTUlb blend stock

Electricity remaining exported to gridafter meeting internal demand = Electricity generated MMBTUlb blend stock- Electricity consumed MMBTUlb blend stock=318.75  BTUlb blend stock

Emissions due to internal generation

CO2 emissions from internal combustion for electricity = Normalized fuel gas amountlblb blendstock×Fuel gas heating value BTUlb×1fuel gas heating value  ×% C fuel gascarbon ratio for CO2× lb to grams- Normalized fuel gas amount lblb blend stock× Fuel gas heating value BTUlb× BTU to MMBTU × VOC from industrial boiler × Carbon ratio for VOC + CO from industrial boiler × Carbon ratio for CO + CH4 from industrial boiler × Carbon ratio for CH4 ×1carbon ratio for CO2 =396.2 g CO2 / lb of blendstock

GHG emissions from fuel gas combustion = CO2 emissions for internal combustion + normalized fuel gas MMBTUlb blend stock× Fuel gas heating value BTUlb× BTU to MMBTU × VOC emission from boiler gramsMMBTU ×carbon ratio for VOCcarbon ratio for CO2+ CO emission from boiler gramsMMBTU ×carbon ratio for COcarbon ratio for CO2+ GWP  for CH4 × CH4 emissions in gramsMMBTU + N2O emissions in gramsMMBTU × GWP for N2O= 398.12g CO2 eq.  MMBTU of blendstock

Non-combustion emission

CO2 emission for non-combustion emission=  Feedstock carbon 1lb blend stock -  blend stock carbon1lb blend stock + Normalized wax lblb blend stock× % C in wax +Remaining fuel gas × % C fuel gascarbon ratio for CO2+Fuel gas Normalized lblb blend stock×Fuel gas heating value BTUlb× VOC emission from industrial boiler× carbon ratio for VOC+  CO from industrial boiler × carbon ratio for CO +  CH4 from industrial boiler × carbon ratio for CH4 + CO2 emission from internal combustion × carbon ratio for CO2× g to lb ×lb to gramcarbon ratio for CO2  =118.75 g CO2 / lb of blendstock

GHG Emissions from noncombustion emissions = CO2 emissions from noncombustion emission + Non combustion VOC emissiongMMBTU× carbon ratio for VOCcarbon ratio for CO2+ Noncombustion CO emission from boilergMMBTU× carbon ratio for COcarbon ratio for CO2=120.32g CO2 eq.  MMBTU of blendstock

Total GHG emissions = Emission from transportation + Emission from separation energy× Normalized feedstock blend stock heating valueBTUlb×1BTU to MMBTU  +GHG emissions from  internal combustion + non combustion + hydrogen use blend stock heating value ×1BTU to MMBTU  =  31575.69g CO2 eq.  MMBTU of blendstock

Energy allocation

For scenario 2, after meeting internal heating and electricity demand, excess fuel gas (if any) was exported.

Energy allocation factor =Heating value of the blend stock Heating value of blend stock + Exported electricity =0.9827

Allocated GHG emission = Energy allocation factor × = Emission from transportation + Emission from separation energy× Normalized feedstock Blend stock heating valueBTUlb×1BTU to MMBTU  +(Energy allocation factor × Emission from  Internal combustion + Non combustion) + hydrogen useBlend stock heating value ×1BTU to MMBTU=31048.7g CO2 eq.  MMBTU of blendstock

Total GHG emissions ing CO2 eq. MJ of fuel = 29.43 g CO2 eq. MJ of fuel

A conversion factor of 1055 (MMBTU to MJ) was assumed.

For displacement,

Displacement credit = Remaining electricity × GHG emission factor for electricity USmix=41.06g CO2 eq. lb of blend stock

Total GHG with displacement credit =Emission from transportation + Emission from separation energy× Normalized feedstock Blend stock heating valueBTUlb×1BTU to MMBTU  +  Internal combustion + Non combustion) + Hydrogen use-Displacement creditBlend stock heating value ×1BTU to MMBTU=29315.76g CO2 eq.  MMBTU of blendstock

S 7.2 Sensitivity Analysis for Varying Heat Loss

A sensitivity analysis was performed to evaluate the influence of reactor heat loss assumptions on the GHG emissions of the pyrolysis system. The base model assumed a heat loss of 1% of the heating value of typical plastic resins (0.46 MJ/kg); which accounted for approximately 14.5% of the reactor energy demand for the pyrolysis of an average plastic composition. In this study, reactor energy demand was defined as the sum of the pyrolysis conversion energy demand and reactor heat loss (equation 5 of the main manuscript). Additional scenarios corresponded to heat loss of 5% , 10% , 25%, and 46% of the reactor energy demand were evaluated to reflect potential variations in industrial scale to lab-scale operations (Zhang et al. 2020; Torres Tovar et al. 2025; Callen 2026). The selected heat-loss ranges represent conditions spanning from a highly insulated reactor to a poorly insulated lab-scale reactor. Increased heat loss resulted in higher heating demand, which subsequently increased GHG emissions linearly.

Fig. S2 Sensitivity analysis of GHG emissions to reactor thermal heat loss (HL) assumptions for pyrolysis of the average plastic mix at 550 °C with a VRT 2 with US-average plastic waste composition. The baseline case corresponds to the originally modeled heat-loss condition (~14.5% of total supplied thermal energy), while additional scenarios represent industrial to lab-scale reactor heat losses. (a) represents Scenario 1, where fuel gas was used for generating process heat only with the remaining fuel gas sold as energy product, and (b) represents Scenario 2, where fuel gas was used for cogenerating process heat and electricity with remaining electricity sold to the grid; the average plastic mix was assumed to be consisted of 49% LDPE, 27% PP, and 24% HDPE, based on the average composition of landfilled plastics in 2019 (Milbrandt et al. 2022)

In Scenario 1, GHG emissions increased gradually from 14.6 gCO2 eq/MJ at minimal heat loss (5%) to 20.4 gCO2 eq./MJ at high heat loss (46%). In Scenario 2, the absolute emissions are significantly higher across all cases, starting at 25.0 gCO2 eq./MJ and rising to 31.0 gCO2 eq./MJ at maximum heat loss. Across both scenarios, the results show that heat loss can be a key driver of environmental performance in pyrolysis-based systems and a well-insulated and optimized reactor can reduce GHG emissions to approximately 29%.

S8. References

Abnisa F, Anuar Sharuddin SD, bin Zanil MF, et al (2019) The Yield Prediction of Synthetic Fuel Production from Pyrolysis of Plastic Waste by Levenberg–Marquardt Approach in Feedforward Neural Networks Model. Polymers 11:1853. https://doi.org/10.3390/polym11111853

Anuar Sharuddin SD, Abnisa F, Wan Daud WMA, Aroua MK (2016) A review on pyrolysis of plastic wastes. Energy Conversion and Management 115:308–326. https://doi.org/10.1016/j.enconman.2016.02.037

Benavides PT, Sun P, Han J, et al (2017) Life-cycle analysis of fuels from post-use non-recycled plastics. Fuel 203:11–22. https://doi.org/10.1016/j.fuel.2017.04.070

Callen P (2026) Industrial Furnace Insulation Thickness Calculation Guide, Industrial Monitor Direct, https://industrialmonitordirect.com/blogs/knowledgebase/industrial-furnace-insulation-thickness-calculation-guide, Accessed May 2026. https://industrialmonitordirect.com/blogs/knowledgebase/industrial-furnace-insulation-thickness-calculation-guide

Chemeo (2022) Chemeo, Chemical Properties of Varying Components, https://www.chemeo.com/, Accessed June 2022

Dutta A, Sahir A, Tan E, et al (2015) Process design and economics for the conversion of lignocellulosic biomass to hydrocarbon fuels: Thermochemical research pathways with in situ and ex situ upgrading of fast pyrolysis vapors. Pacific Northwest National Laboratory (PNNL), Richland, WA (United States)

Elordi G, Olazar M, Lopez G, et al (2011) Product Yields and Compositions in the Continuous Pyrolysis of High-Density Polyethylene in a Conical Spouted Bed Reactor. Ind Eng Chem Res 50:6650–6659. https://doi.org/10.1021/ie200186m

Gracida-Alvarez UR, Winjobi O, Sacramento-Rivero JC, Shonnard DR (2019) System Analyses of High-Value Chemicals and Fuels from a Waste High-Density Polyethylene Refinery. Part 2: Carbon Footprint Analysis and Regional Electricity Effects. ACS Sustainable Chem Eng 7:18267–18278. https://doi.org/10.1021/acssuschemeng.9b04764

Hosseini S, Shrivastava M, Qi L, et al (2014) Effect of low-density polyethylene on smoke emissions from burning of simulated debris piles. Journal of the Air & Waste Management Association 64:690–703. https://doi.org/10.1080/10962247.2014.882282

Huijbregts MA, Steinmann ZJ, Elshout PM, et al (2016) ReCiPe 2016: a harmonized life cycle impact assessment method at midpoint and endpoint level report I: characterization

Hwang GC, Kim KH, Bae SY, et al (2001) Degradation of high density polyethylene, polypropylene and their mixtures in supercritical acetone. Korean Journal of Chemical Engineering 18:396–401

Joback KG, Reid RC (1987) ESTIMATION OF PURE-COMPONENT PROPERTIES FROM GROUP-CONTRIBUTIONS. Chemical Engineering Communications 57:233–243. https://doi.org/10.1080/00986448708960487

Jung S-H, Cho M-H, Kang B-S, Kim J-S (2010) Pyrolysis of a fraction of waste polypropylene and polyethylene for the recovery of BTX aromatics using a fluidized bed reactor. Fuel Processing Technology 91:277–284. https://doi.org/10.1016/j.fuproc.2009.10.009

Kulas DG, Zolghadr A, Shonnard D (2021) Micropyrolysis of Polyethylene and Polypropylene Prior to Bioconversion: The Effect of Reactor Temperature and Vapor Residence Time on Product Distribution. ACS Sustainable Chem Eng 9:14443–14450. https://doi.org/10.1021/acssuschemeng.1c04705

Larrain M, Van Passel S, Thomassen G, et al (2020) Economic performance of pyrolysis of mixed plastic waste: Open-loop versus closed-loop recycling. Journal of Cleaner Production 270:122442. https://doi.org/10.1016/j.jclepro.2020.122442

Lee N, Joo J, Lin K-YA, Lee J (2021) Waste-to-Fuels: Pyrolysis of Low-Density Polyethylene Waste in the Presence of H-ZSM-11. Polymers 13:1198. https://doi.org/10.3390/polym13081198

Linstrom P (1997) NIST Chemistry WebBook, NIST Standard Reference Database 69

Liu T, Li Y, Zhou Y, et al (2023) Efficient Pyrolysis of Low-Density Polyethylene for Regulatable Oil and Gas Products by ZSM-5, HY and MCM-41 Catalysts. Catalysts 13:382. https://doi.org/10.3390/catal13020382

Marcilla A, Beltrán MI, Navarro R (2009) Thermal and catalytic pyrolysis of polyethylene over HZSM5 and HUSY zeolites in a batch reactor under dynamic conditions. Applied Catalysis B: Environmental 86:78–86. https://doi.org/10.1016/j.apcatb.2008.07.026

Milbrandt A, Coney K, Badgett A, Beckham GT (2022) Quantification and evaluation of plastic waste in the United States. Resources, Conservation and Recycling 183:106363. https://doi.org/10.1016/j.resconrec.2022.106363

Montejo C, Costa C, Ramos P, Márquez MDC (2011) Analysis and comparison of municipal solid waste and reject fraction as fuels for incineration plants. Applied Thermal Engineering 31:2135–2140. https://doi.org/10.1016/j.applthermaleng.2011.03.041

Onwudili JA, Insura N, Williams PT (2009) Composition of products from the pyrolysis of polyethylene and polystyrene in a closed batch reactor: Effects of temperature and residence time. Journal of Analytical and Applied Pyrolysis 86:293–303. https://doi.org/10.1016/j.jaap.2009.07.008

OSTI (2014) Premium Efficiency Motor Selection and Application Guide – A Handbook for Industry, U.S. Department of Energy Office of Scientific and Technical Information. United States

Park C, Lee J (2021) Pyrolysis of polypropylene for production of fuel‐range products: Effect of molecular weight of polypropylene. Int J Energy Res 45:13088–13097. https://doi.org/10.1002/er.6635

Pennsylvania Department of Environmental Protection (2003) Statewide Waste Composition Study

Petrovic Aleksandra, Colnik Maja, Prsa Amadeja, et al (2022) Comparative Analysis of Virgin and Recycled Thermoplastic Polymer based on Thermochemical Characteristics. Chemical Engineering Transactions 94:1321–1326. https://doi.org/10.3303/CET2294220

Smeaton C (2021) Augmentation of global marine sedimentary carbon storage in the age of plastic. Limnology and Oceanography Letters 6:113–118. https://doi.org/10.1002/lol2.10187

Torres Tovar JA, Servín-Campuzano H, González-Avilés M, et al (2025) Design of an Energy-Efficient Pilot-Scale Pyrolysis Reactor Using Low-Cost Insulating Materials. Recycling 10:199. https://doi.org/10.3390/recycling10060199

Walters RN, Hackett SM, Lyon RE (2000) Heats of combustion of high temperature polymers. Fire and materials 24:245–252

Wang M, Elgowainy A, Lee U, et al (2021) Greenhouse gases, Regulated Emissions, and Energy use in Technologies Model ® (2021 Excel)

Wang M, Elgowainy A, Lee U, et al (2023) Greenhouse gases, Regulated Emissions, and Energy use in Technologies Model ® (2023 Excel)

Wulan PPDK, Sidauruk JOD, Ningtyas JA (2018) The Effect of Pyrolysis Temperature and Time of Polypropylene on Quality of Carbon Nanotube with Flame Synthesis Method. E3S Web Conf 67:03030. https://doi.org/10.1051/e3sconf/20186703030

Yaqoob L, Noor T, Iqbal N (2022) Conversion of Plastic Waste to Carbon-Based Compounds and Application in Energy Storage Devices. ACS Omega 7:13403–13435. https://doi.org/10.1021/acsomega.1c07291

Zevenhoven R, Karlsson M, Hupa M, Frankenhaeuser M (1997) Combustion and Gasification Properties of Plastics Particles. Journal of the Air & Waste Management Association 47:861–870. https://doi.org/10.1080/10473289.1997.10464461

Zhang Y, Ji G, Ma D, et al (2020) Exergy and energy analysis of pyrolysis of plastic wastes in rotary kiln with heat carrier. Process Safety and Environmental Protection 142:203–211. https://doi.org/10.1016/j.psep.2020.06.021

Zhou N, Dai L, Lv Y, et al (2021) Catalytic pyrolysis of plastic wastes in a continuous microwave assisted pyrolysis system for fuel production. Chemical Engineering Journal 418:129412. https://doi.org/10.1016/j.cej.2021.129412