# Interfacial Electric Field Engineering in Ni-ZrC Heterostructures for High-Efficiency Zinc–Air Batteries

Enmin Lv a, Jiefeng Diao b, Yilong Wang a, Hongtao Yu c, Graeme Henkelman b, Hao Zhang d, *, Xuefeng Zhang e, *, and Xinglong Dong a, *

a Key Laboratory of Materials Modification by Laser, Ion and Electron Beams (Ministry of Education), School of Materials Science and Engineering, Dalian University of Technology, Dalian 116024, P. R. China

b Department of Chemistry and the Oden Institute for Computational Engineering and Sciences, The University of Texas at Austin, Austin, TX 78712, USA

c Key Laboratory of Industrial Ecology and Environmental Engineering (Ministry of Education), School of Environmental Science and Technology, Dalian University of Technology, Dalian 116024, P. R. China

d Department of Chemical Engineering, Massachusetts Institute of Technology, Cambridge, MA 02139, USA

e Institute of Advanced Magnetic Materials, College of Materials and Environmental Engineering, Hangzhou Dianzi University, Hangzhou 110819, P. R. China

* Corresponding author. Email: dongxl@dlut.edu.cn (X. Dong), zhang@hdu.edu.cn (X. Zhang), hzhchem@mit.edu (H. Zhang)

# Fig. S1. The JK of all catalysts at 0.82 V.

# Fig. S2. (a-d) ORR polarization curves at different rotating speeds; (e-h) Corresponding K-L plots with n at different potentials.

# Fig. S3. The TOF of all catalysts at 0.82V.

# Fig. S4. XRD and XPS of (Ni/ZrC)@NC NPs after 5,000 cycles.

# Fig. S5. (a), (b) TEM, HRTEM images of (Ni/ZrC)@NC NPs after 5,000 cycles.

# Fig. S6. (a), (b) Histogram of normalized mass activity changes of (Ni/ZrC)@NC NPs and 20 wt.% Pt/C after 5000 cycles.

# Fig. S7. Nyquist plots of the impedance for all catalysts at their corresponding OCV.

# Fig. S8. Discharge curves of ZABs at a current density of 5 mA⋅cm-2.

# Table S1. The elemental contents of C, N, Ni, Zr, and O in all catalysts.

| Catalysts | Composition (at.%) |  |  |  |  |
| --- | --- | --- | --- | --- | --- |
|  | C | N | Ni | Zr | O |
| Ni@C NPs | 82.40 | / | 7.42 | / | 10.18 |
| ZrC@C NPs | 84.25 | / | / | 0.61 | 15.14 |
| (Ni/ZrC)@C NPs | 83.52 | / | 6.38 | 0.53 | 9.57 |
| (Ni/ZrC)@NC NPs | 81.69 | 0.79 | 6.57 | 0.54 | 10.41 |

# Table S2. Spectral line information of Hα utilized in constructing Boltzmann plots to determine the plasma's Te.

| λ/nm | Species | Lower level (l) configuration | Uper level (k) configuration | Ak1/106 /s-1 | EK /cm-1 | gk |
| --- | --- | --- | --- | --- | --- | --- |
| 375.01 | H | 2s | 12d | 0.36 | 108917.12 | 6 |
| 379.79 | H | 2p | 10d | 1.21 | 107832.64 | 2 |
| 388.90 | H | 2p | 8d | 2.05 | 107965.05 | 6 |
| 397.01 | H | 2p | 7d | 0.52 | 107440.45 | 7 |
| 434.05 | H | 2s | 4d | 1.83 | 107765.18 | 6 |
| 656.27 | H | 2s | 3p | 1.62 | 103245.62 | 6 |
| 656.28 | H | 2s | 3s | 2.14 | 103954.21 | 4 |

# Table S3. The values of CV of all catalysts.

| Catalysts | CV (V) |
| --- | --- |
| Ni@C NPs | 0.69 |
| ZrC@C NPs | 0.69 |
| (Ni/ZrC)@C NPs | 0.77 |
| (Ni/ZrC)@NC NPs | 0.82 |
| Pt/C | 0.81 |

# Table S4. The values of Eonset, E1/2 and JL of all catalysts.

| Catalysts | Eonset (V) | E1/2 (V) | JL (mA⋅cm−2) |
| --- | --- | --- | --- |
| Ni@C NPs | 0.78 | 0.65 | 2.61 |
| ZrC@C NPs | 0.81 | 0.65 | 3.54 |
| (Ni/ZrC)@C NPs | 0.84 | 0.76 | 5.28 |
| (Ni/ZrC)@NC NPs | 0.91 | 0.82 | 5.63 |
| Pt/C | 0.90 | 0.80 | 5.43 |

# Table S5. Summary of the electrochemical parameters of the catalysts.

| Catalysts | Cdl (mF·cm−2) | ECSAa (m2·g−1) | Jk@0.82V (mA·cm−2) | SAb@0.82V (μA·cm−2) | MA@0.82V (A·g−1) | TOF (1012·cm−2·s−1) |
| --- | --- | --- | --- | --- | --- | --- |
| Ni@C NPs | 1.60 | 44.8 | 0.05 | 1.09 | 0.52 | 1.70 |
| ZrC@C NPs | 1.65 | 46.2 | 0.13 | 2.76 | 1.27 | 4.30 |
| (Ni/ZrC)@C NPs | 3.38 | 96.64 | 0.58 | 6.01 | 5.19 | 9.37 |
| (Ni/ZrC)@NC NPs | 8.84 | 247.52 | 5.04 | 19.95 | 26.07 | 31.11 |
| Pt/C | 7.01 | 196.28 | 3.62 | 18.07 | 20.09 | 28.19 |

# Table S6. Simulated parameters of equivalent circuit from EIS results.

| Catalysts | Rs (Ω) | Rct (Ω) |
| --- | --- | --- |
| Ni@C NPs | 12.91 | 45.59 |
| ZrC@C NPs | 9.22 | 42.19 |
| (Ni/ZrC)@C NPs | 8.92 | 40.76 |
| (Ni/ZrC)@NC NPs | 5.92 | 34.05 |
| Pt/C | 6.33 | 34.84 |

# Table S7. Comparison of power density and specific capacity of liquid ZABs reported in literatures.

| Catalysts | Power density (mW·cm-2) | Specific capacity (mAh·g-1) | Reference |
| --- | --- | --- | --- |
| CoSe2-FeSe2@NC/NHC | 184.3 | 813.61 @10 mA·cm-2 | [1] |
| CoS/CoO@NGNs | 137.8 | 723.9 @20 mA·cm-2 | [2] |
| Mn-N-S-C | 209.8 | 734.01 @20 mA·cm-2 | [3] |
| CoNP@FeNC | 104.4 | - | [4] |
| Co-N/P-C | 173.9 | 790.0 | [5] |
| Co@C-CoNC | 162.8 | 810.0 @10 mA·cm-2 | [6] |
| Ag-FeNx-N-C | 180.0 | 813.0 @20 mA·cm-2 | [7] |
| Zn/Co-N@PCNFs-800 | 83.5 | 640.3 @10 mA·cm-2 | [8] |
| Fe2P/FeNi/NPC-0.5 | 158.4 | 755.08 @5 mA·cm-2 | [9] |
| CoFe-NiFe/NC | 155.0 | 777.0 @20 mA·cm-2 | [10] |
| (Ni/ZrC)@NC | 251.63 | 815.28 @5 mA·cm-2 | This work |

# Table S8. Comparison of peak power density of (Ni/ZrC)@NC NPs-based all-solid-state FZABs with other reported FZABs.

| Catalysts | Peak power density (mW·cm-2) | Reference |
| --- | --- | --- |
| CoSe2-FeSe2@NC/NHC | 61.40 | [1] |
| Mn-N-S-C | 34.05 | [3] |
| Fe2P/FeNi/NPC | 158.02 | [9] |
| CoFe-NiFe/NC | 124.50 | [10] |
| FeN4-Ti3C2Sx | 133.60 | [11] |
| Fe1/d-CN | 78.00 | [12] |
| Cop@CoNC | 121.80 | [13] |
| NiCo2O4@NiCoFe-OH | 31.80 | [14] |
| CoN-BC | 59.40 | [15] |
| Co/VN@NC | 85.00 | [16] |
| FeN3-CoN3 | 93.46 | [17] |
| FeCo-MI@TAP-900 | 67.00 | [18] |
| Fe3C/Fe@CNs | 81.24 | [19] |
| Co2P@NPAC | 75.30 | [20] |
| (Ni/ZrC)@NC | 184.22 | This work |

# References

[1] Luo Y, Wu Q, Fu Y, Wen M, Chem Eng J, 2025, 512: 162739.

[2] Tian Y, Xu L, Li M, Yuan D, Liu X, Qian J, Dou Y, Qiu J, Zhang S, Nano-Micro Lett, 2021, 13: 3.

[3] Wang Z, Deng D, Zhang W, Cheng X, Xu L, Qian J, Li H, J Energy Chem, 2025, 110: 647-656.

[4] Xue Y, Guo Y, Zhang Q, Xie Z, Wei J, Zhou Z, Nano-Micro Lett, 2022, 14: 162.

[5] Qi Y, Liang Q, Song K, Zhou X, Liu M, Li W, Liu F, Jiang Z, Zou X, Chen Z, Zhang W, Zheng W, J Energy Chem, 2024, 95: 306-314.

[6] Chandrasekaran S, Hu R, Yao L, Sui L, Liu Y, Abdelkader A, Li Y, Ren X, Deng L, Nano-Micro Lett, 2023, 15: 48.

[7] Shi K, Wang K, Li T, Li J, Ren J, Li X, Min Y, Lu Z, Tan W, Liu Q, J Energy Chem, 2024, 95: 106-116.

[8] Niu Q, Chen B, Guo J, Nie J, Guo X, Ma G, Nano-Micro Lett, 2019, 11: 8.

[9] Zeng Y, Liu Y, Gong Y, Li Z, Qiu Z, Xiong D, Du Y, Zhou L, Zhan F, Yang X, J Energy Chem, 2025, 110: 476-485.

[10] Yang X, Mao H, Zhou Z, Li K, Li C, Ye Q, Liu B, Fang Y, Cai X, Adv Funct Mater, 2024, 34: 2402933.

[11] Chen S, Liang X, Hu S, Li X, Zhang G, Wang S, Ma L, Wu CML, Zhi C, Zapien JA, Nano-Micro Lett, 2023, 15: 47.

[12] Zhao M, Liu H, Zhang H, Chen W, Sun H, Wang Z, Zhang B, Song L, Yang Y, Ma C, Han Y, Huang W, Energy Environ Sci, 2021, 14: 6455-6463.

[13] Yang H, Gao S, Rao D, Yan X, Energy Storage Mater, 2022, 46: 553-562.

[14] Li S, Yang X, Yang S, Gao Q, Zhang S, Yu X, Fang Y, Yang S, Cai X, J Mater Chem A, 2020, 8: 5601.

[15] Chen Z, Zou Y, Chen H, Zhang K, Hui B, Small, 2024, 20: 2307776.

[16] Luo Z, Gong J, Li Q, Wei F, Liu B, Isimjan TT, Yang X, Chem Eur J, 2024, 30: e202303943.

[17] Zhang X, Gao C, Li L, Yan X, Zhang N, Bao J, J Colloid Interface Sci, 2024, 676: 871-883.

[18] Zheng J, Hu G, Liu B, Liu Y, Li H, Zhao H, Yang M, Energy Storage Mater, 2024, 65: 103106.

[19] Ma Y, Zhao L, Zhang W, Zhou X, Cong X, Wang J, Liu Q, Li Z, Wang L, J Energy Storage, 2024, 103: 114168.

[20] Li S, Sun K, Liu Y, Liu S, Zhou J, Zhang W, Lu Y, Chen X, Wang X, Li B, Jiang J, Rare Met, 2024, 43: 4982-4991.