


Figure A1. Cyclic voltammograms of the GP/Co(OH)₂ electrode containing 40 wt% Co(OH)₂ recorded at a scan rate of 5 mV s⁻¹ in KOH solutions of different concentrations (0.1, 1.0, 3.0, and 6.0 M), using Ag/AgCl (sat.) as the reference electrode.
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