Supplementary Materials:

High-performance polyamide/carbon Fiber composites by fused filament fabrication: mechanical and functional Performance

Sithiprumnea Dul, Luca Fambri , Alessandro Pegoretti

Figure S1. TGA curve of PA and PA/CF pellet in nitrogen (continuous line) and air (dot line) atmosphere.

(a)	(b)

Figure S2. Resistivity of three compression moulded (a) and three 3D-printed (b) samples in the range of temperature between -16 °C and 150 °C.

(a)

(b)

Figure S3. Piezoresistivity cyclic test of the selected three PA/CF-XY specimens: (a) stress and (b) R/R0, as a function of time (50 cycles).

Table S1. Summary of resistance values at room temperature of compression molded (CM) and 3D-printed samples produced in XY configuration before and after test.

| Samples | Type test | Resistivity (·cm) |  |
| --- | --- | --- | --- |
|  |  | Before test | After test |
| PA/CF-CM | Fracture | 7.4 ± 1.2 | \\ |
|  | 1% strain test | 4.9 ± 1.6 | 4.7 ± 1.5 |
| PA/CF-XY | Fracture test | (1.4 ± 0.6)×104 | \\ |
|  | 1% strain | (1.4 ± 0.5)×104 | (6.4 ± 3.2)×104 |
|  | Cyclic strain | (0.9 ± 0.5)×104 | (0.6 ± 0.2)×104 |