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Fig. S1: Encapsulation efficiency (%) of inclusion complex. Values given are averages ± SD. from four replicates. Different letter (A, B) indicates significant differences significant differences between compound (p < 0.05). Different number (1,2) indicates significant difference between preparation method (p <0.05).



Table S1: Differential scanning calorimetry (DSC) data for inclusion complex and starting materials. Inclusion complex values in average ± SD. 
	Peak
	Onset temp (°C)
	Heat fusion (J/g)
	Heat flow (m/W)

	Linalool/βCD (co-prep)

	1
	98.81 ± 11.22
	4.28 ± 1.13
	-0.61 ± 0.15

	2
	137.75 ± 9.77
	20.28 ± 9.77
	-0.64 ± 0.92

	3
	312.27 ± 2.43
	174.60 ± 95.88
	-3.97 ±0.86

	Linalool/ βCD (kneading)

	1
	97.77 ± 8.73
	10.43 ± 0.76
	-0.38 ± 0.31

	2
	151.61 ± 88.28
	42.12 ± 24.56
	-1.25 ±  0.74

	3
	316.77 ±  1.04
	183.30 ± 12.68
	-5.32 ± 0.69

	Eugenyl acetate/ βCD (co-prep)

	1
	89.09 ± 9.08
	450.60 ± 33.58
	-9.38 ± 1.69

	2
	321.84 ± 5.92
	210.50 ± 12.51
	-9.40 ± 0.35

	Eugenyl acetate/ βCD (kneading)

	1
	85.23 ± 3.17
	29.37 ± 7.38
	-1.27 ± 0.45

	2
	145.67 ± 4.46
	29.27 ± 11.28
	-1.23 ± 0.38

	3
	213.44 ± 4.62
	17.11 ± 4.89
	-0.51 ± 0.06

	4
	320.45 ± 8.62
	208.90 ± 15.59
	-7.97 ± 2.02








	
Table S2: Thermogravimetric analysis (TGA) data for inclusion complex and starting materials. Inclusion complex values presented in average ± SD. 
	Peak
	Onset (°C)
	Midpoint (°C)
	Residue (%)

	Linalool/βCD (co-prep)

	1
	67.68 ± 11.26
	86.92 ± 28.61
	87.38 ± 4.48

	2
	99.60 ± 3.06
	127.51 ± 10.69
	82.35 ± 7.13

	3
	309.03 ± 1.16
	 325.90 ± 2.30
	4.99 ± 0.01

	Linalool/ βCD (kneading)

	1
	108.29 ± 0.98
	113.05 ± 0.92
	90.03 ± 1.22

	2
	152.43 ± 3.54
	160.31 ± 8.11
	72.97 ± 4.78

	3
	308.12  ± 1.40
	 325.51 ± 1.49
	6.34 ± 0.54

	Eugenyl acetate/ βCD (co-prep)

	1
	52.23 ± 0.27
	61.88 ± 0.56
	84.22 ± 8.53

	2
	96.75 ± 0.82
	122.53 ± 2.05
	74.65 ± 5.62

	3
	318.07 ± 1.12
	 327.05 ± 1.52
	3.59 ± 2.97

	Eugenyl acetate/ βCD (kneading)

	1
	107.75 ± 0.47
	113.05 ± 0.92
	90.03 ± 1.22

	2
	151.44 ± 8.67
	160.32  ± 8.14
	72.97 ± 4.78

	3
	 308.30 ± 6.65
	325.51 ± 1.49
	6.34 ± 0.54
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