Purification of recovered phosphoric acid by extracting aluminium with di-2-ethylhexyl phosphoric acid

Sini Reuna1*, Ari Väisänen1

1 Department of Chemistry, Renewable Natural Resources, and Chemistry of Living Environment, University of Jyväskylä, P.O. Box 35, FI-40014 Jyväskylä, Finland

*Corresponding author sini.s.reuna@jyu.fi

# Supplementary Data

Table S1. The design layout for optimization of aluminium extraction and experimental results for CCF design

| Standard order | pH | DEHPA (M) | AO | E% (Al) | c(Alorg) (mg L-1) | pH equilibrium |
| --- | --- | --- | --- | --- | --- | --- |
| C1.1 | 1.7 | 0.3 | 1:2 | 23 | 286 | 1.5 |
| C1.2 | 2.5 | 0.3 | 1:2 | 46 | 562 | 2.0 |
| C1.3 | 1.7 | 0.6 | 1:2 | 44 | 556 | 1.4 |
| C1.4 | 2.5 | 0.6 | 1:2 | 64 | 820 | 1.9 |
| C1.5 | 1.7 | 0.3 | 2:1 | 8 | 411 | 1.6 |
| C1.6 | 2.5 | 0.3 | 2:1 | 18 | 864 | 2.3 |
| C1.7 | 1.7 | 0.6 | 2:1 | 13 | 673 | 1.6 |
| C1.8 | 2.5 | 0.6 | 2:1 | 32 | 1546 | 2.2 |
| C1.9 | 2.1 | 0.45 | 1:1 | 35 | 854 | 1.8 |
| C1.10 | 2.1 | 0.45 | 1:1 | 30 | 738 | 1.8 |
| C1.11 | 2.1 | 0.45 | 1:1 | 28 | 694 | 1.8 |
| S2.1 | 1.7 | 0.45 | 1:1 | 17 | 428 | 1.6 |
| S2.2 | 2.5 | 0.45 | 1:1 | 41 | 999 | 2.1 |
| S2.3 | 2.1 | 0.3 | 1:1 | 19 | 460 | 1.9 |
| S2.4 | 2.1 | 0.6 | 1:1 | 37 | 902 | 1.8 |
| S2.5 | 2.1 | 0.45 | 1:2 | 47 | 578 | 1.7 |
| S2.6 | 2.1 | 0.45 | 2:1 | 20 | 988 | 1.9 |
| S2.7 | 2.1 | 0.45 | 1:1 | 37 | 913 | 1.9 |
| S2.8 | 2.1 | 0.45 | 1:1 | 32 | 798 | 1.9 |
| S2.9 | 2.1 | 0.45 | 1:1 | 23 | 529 | 1.9 |

Model assumption checks

The normal probability plot of residuals, the residuals versus fitted-values plot, the histogram of residuals and residuals versus order plot are presented in Figure S1. According to normal probability plot (top, left), residuals follow the straight line confirming that the residuals are normally distributed. The residuals versus fitted-values plot (top, right) display random scatter, which indicates that the residuals have constant variance, while the histogram (down, left) shows that data is not skewed. The observation order plot (down, right) shows that residuals are uncorrelated with each other.

Figure S1. Residual plots for the prediction model

Figure S2. Main effect plots of fitted means for variables in aluminium extraction.