Supporting Information (SI)

Effect of Si/Al2 ratio over BEA zeolite in steam and direct catalytic cracking of n-dodecane

Arumugam Ramesh1, Jun-Hyuk Ahn1, Su-Un Leea, Su-Ah Kang1, Temur Khujamuratov1,2, Kwang-Eun Jeong1, Tae-Wan Kim1,2, *, Chul-Ung Kim1,*

1Chemical & Process Technology Division, Korea Research Institute of Chemical Technology, 141, Gajeong-ro, Yuseong-gu, Daejeon 34114, South Korea

2Advanced Materials and Chemical Engineering Technology, University of Science & Technology, 217 Gajeong-ro, Yuseong-gu, Daejeon 34113, Republic of Korea

Fig. S1 Schematic diagram of the catalytc cracking reaction system in SCC and

DCC of n-Do.

Table S1 Experimental conditions for catalytic cracking (DCC, SCC) of n-Do over BEA zeolite catalysts

| Parameters | Values |
| --- | --- |
| Rxn. temperature (oC) Rxn. pressure (MPa) Time-on-stream (h) LHSV (h-1) of n-Do Catalyst loading (g) Catalysts (SAR) | 500 to 650 0.1 1 to 6 4.2, 5.7, 12.8, 17.0 0.675 ZSM-5(280), BEA(25) to BEA(360) |

Table S2 Comparison between BEA and ZSM-5 zeolite catalyst in similar SAR on the n-Do conversion and, light olefin selectivity and yield in DCC and SCC of n-Do (500, 650℃, LHSV = 4.2 h-1, TOS = 1, 6 h)

| Catalyst materials |  |  |  | Cracking method | n-Do conv. (wt%) |  |  | Selectivity (wt%) |  |  |  |  |  |  |  | Yield (wt%) |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  | Temp. (oC) |  | TOS (h) |  |  | H2 | Ethylene (E) |  | Propylene (P) | Butenes (B) | Paraffins | BTX | E/P ratio | Light olefin/ paraffin | E+P |  | E+P+B |
| BEA(300)-C | 550 |  | 1 | DCC | 97.5 | 0.3 | 3.3 |  | 24.4 | 25.3 | 45.0 | 0.6 | 0.14 | 1.18 | 27.0 |  | 51.6 |
| BEA(300)-C |  |  | 6 |  | 59.3 | 1.9 | 2.6 |  | 20.5 | 22.1 | 47.5 | 3.1 | 0.13 | 0.95 | 13.7 |  | 26.8 |
| ZSM-5(280)-C |  |  | 1 |  | 92.2 | 0.8 | 13.4 |  | 24.5 | 13.3 | 45.6 | 0.2 | 0.55 | 1.12 | 35.0 |  | 47.2 |
| ZSM-5(280)-C |  |  | 6 |  | 85.3 | 0.7 | 11.5 |  | 22.3 | 12.4 | 48.0 | 3.4 | 0.51 | 0.96 | 28.7 |  | 39.3 |
| BEA(300)-C | 650 |  | 1 |  | 94.6 | 1.2 | 23.3 |  | 24.8 | 13.5 | 21.1 | 0.1 | 0.94 | 2.92 | 45.5 |  | 58.3 |
| BEA(300)-C |  |  | 6 |  | 77.3 | 0.5 | 30.3 |  | 27.8 | 11.7 | 16.8 | 0.3 | 1.09 | 4.15 | 44.9 |  | 54.0 |
| ZSM-5(280)-C |  |  | 1 |  | 98.6 | 1.7 | 27.9 |  | 26.2 | 8.5 | 20.7 | 0.1 | 1.06 | 3.02 | 53.2 |  | 61.6 |
| ZSM-5(280)-C |  |  | 6 |  | 82.8 | 1.2 | 26.9 |  | 27.2 | 9.4 | 21.8 | 0.6 | 0.99 | 2.91 | 44.7 |  | 52.5 |
| BEA(300)-C | 550 |  | 1 | SCC | 91.1 | 0.3 | 4.1 |  | 33.1 | 27.8 | 32.2 | 2.0 | 0.12 | 2.02 | 33.9 |  | 59.2 |
| BEA(300)-C |  |  | 6 |  | 95.1 | 0.2 | 2.9 |  | 28.6 | 26.1 | 36.6 | 5.0 | 0.10 | 1.57 | 30.0 |  | 54.8 |
| ZSM-5(280)-C |  |  | 1 |  | 75.6 | 0.4 | 9.2 |  | 39.4 | 25.1 | 22.8 | 2.5 | 0.23 | 3.23 | 36.7 |  | 55.7 |
| ZSM-5(280)-C |  |  | 6 |  | 46.8 | 0.3 | 7.1 |  | 33.9 | 22.0 | 29.7 | 6.6 | 0.21 | 2.12 | 19.1 |  | 29.4 |
| BEA(300)-C | 650 |  | 1 |  | 97.5 | 0.8 | 12.3 |  | 36.0 | 28.0 | 16.9 | 1.7 | 0.34 | 4.51 | 47.1 |  | 74.3 |
| BEA(300)-C |  |  | 6 |  | 78.5 | 0.7 | 12.5 |  | 30.8 | 27.6 | 20.4 | 3.8 | 0.41 | 3.48 | 34.0 |  | 55.6 |
| ZSM-5(280)-C |  |  | 1 |  | 81.0 | 0.6 | 18.0 |  | 38.1 | 24.2 | 13.6 | 2.1 | 0.47 | 5.90 | 45.5 |  | 65.1 |
| ZSM-5(280)-C |  |  | 6 |  | 58.7 | 0.6 | 18.0 |  | 34.7 | 22.6 | 16.9 | 3.4 | 0.52 | 4.46 | 30.9 |  | 44.2 |

Table S3 Effect of SAR of BEA catalyst with different SAR = 25 - 360 in DCC and SCC of n-Do over BEA zeolite catalysts (550 ℃, LHSV = 17.0 h-1, TOS = 6 h)

| Catalyst materials | SAR of BEA | Cracking method | n-Do conv. (wt%) | Selectivity (wt%) |  |  |  |  |  |  |  | Yield (wt%) |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  |  |  |  | H2 | Ethylene (E) | Propylene (P) | Butenes (B) | Paraffin | BTX | E/P ratio | Light olefin/ paraffin | E+P | E+P+B |
| BEA(25)-S | 25 | DCC | 13.5 | 0.7 | 7.2 | 20.7 | 13.8 | 50.7 | 4.2 | 0.35 | 0.82 | 3.8 | 5.6 |
| BEA(38)-C | 38 |  | 17.4 | 0.4 | 5.6 | 26.6 | 14.9 | 46.3 | 5.0 | 0.21 | 1.02 | 5.6 | 8.2 |
| BEA(100)-S | 100 |  | 27.3 | 0.3 | 3.5 | 20.7 | 15.2 | 54.6 | 4.0 | 0.17 | 0.72 | 6.6 | 10.7 |
| BEA(300)-C | 300 |  | 36.6 | 0.2 | 3.1 | 21.8 | 16.9 | 53.0 | 3.6 | 0.14 | 0.79 | 9.1 | 15.3 |
| BEA(360)-C | 360 |  | 44.3 | 0.1 | 1.9 | 20.6 | 19.2 | 49.4 | 8.3 | 0.09 | 0.84 | 9.9 | 18.4 |
| BEA(25)-S | 25 | SCC | 54.4 | 0.2 | 1.4 | 26.7 | 22.7 | 46.0 | 2.7 | 0.05 | 1.10 | 15.3 | 27.7 |
| BEA(38)-C | 38 |  | 58.2 | 0.2 | 1.8 | 26.0 | 22.4 | 45.3 | 4.0 | 0.07 | 1.11 | 16.1 | 29.2 |
| BEA(100)-S | 100 |  | 74.7 | 0.2 | 1.3 | 23.8 | 23.2 | 45.1 | 6.2 | 0.05 | 1.07 | 18.7 | 36.1 |
| BEA(300)-C | 300 |  | 75.3 | 0.2 | 1.7 | 24.5 | 22.7 | 43.9 | 6.7 | 0.07 | 1.11 | 19.7 | 36.8 |
| BEA(360)-C | 360 |  | 80.3 | 0.2 | 1.8 | 25.2 | 23.4 | 42.4 | 6.7 | 0.07 | 1.19 | 27.0 | 50.3 |

Table S4 Effect of reaction temperature on the n-Do conversion and light olefin selectivity in SCC of n-Do over a typical BEA(300)-C zeolite catalyst (LHSV = 4.2 h-1, TOS = 1, 6 h)

| Rxn. temp. (oC) |  | TOS (h) | n-Do conv. (wt%) | Selectivity (wt%) |  |  |  |  |  |  |  | Yield (wt%) |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  |  |  |  | H2 | Ethylene (E) | Propylene (P) | Butenes (B) | Paraffin | BTX | E/P ratio | Light olefin/ paraffin | E+P | E+P+B |
| 500 |  | 1 | 94.0 | 0.1 | 2.3 | 28.2 | 25.9 | 42.2 | 1.0 | 0.08 | 1.34 | 28.7 | 53.0 |
|  |  | 6 | 85.3 | 0.1 | 1.5 | 24.9 | 26.0 | 42.2 | 3.1 | 0.06 | 1.24 | 22.5 | 44.7 |
| 550 |  | 1 | 90.3 | 0.3 | 4.1 | 33.1 | 28.8 | 32.2 | 2.0 | 0.12 | 2.02 | 33.9 | 60.1 |
|  |  | 6 | 95.1 | 0.2 | 2.9 | 28.6 | 27.1 | 36.6 | 5.0 | 0.10 | 1.79 | 30.0 | 55.7 |
| 600 |  | 1 | 96.9 | 0.4 | 7.6 | 36.9 | 25.2 | 27.4 | 1.5 | 0.21 | 2.54 | 43.1 | 67.6 |
|  |  | 6 | 99.6 | 0.4 | 5.3 | 32.6 | 26.7 | 29.6 | 4.5 | 0.16 | 2.18 | 37.7 | 64.3 |
| 650 |  | 1 | 98.6 | 0.8 | 11.1 | 36.3 | 28.6 | 17.9 | 1.6 | 0.31 | 4.25 | 46.7 | 74.9 |
|  |  | 6 | 77.8 | 0.7 | 11.0 | 30.4 | 27.7 | 21.9 | 4.2 | 0.36 | 3.16 | 32.2 | 53.8 |

Table S5 Effect of LHSV on the n-Do conversion and light olefin selectivity in SCC of n-Do over a typical BEA(300)-C zeolite catalyst (550 ℃, TOS = 1, 6 h)

| LHSV (h-1) | TOS (h) | n-Do conv. (wt%) | Selectivity (wt%) |  |  |  |  |  |  |  | Yield (wt%) |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  |  |  | H2 | Ethylene (E) | Propylene (P) | Butenes (B) | Paraffin | BTX | E/P ratio | Light olefin/ paraffin | E+P | E+P+B |
| 4.2 | 1 | 91.1 | 0.3 | 4.1 | 33.1 | 27.8 | 32.2 | 2.0 | 0.12 | 2.02 | 33.9 | 60.1 |
|  | 6 | 95.1 | 0.2 | 2.9 | 28.6 | 26.1 | 36.6 | 5.0 | 0.10 | 1.57 | 30.0 | 55.7 |
| 5.7 | 1 | 90.3 | 0.2 | 3.5 | 32.8 | 29.5 | 32.3 | 1.2 | 0.10 | 2.04 | 32.8 | 59.4 |
|  | 6 | 86.9 | 0.2 | 2.9 | 30.1 | 29.2 | 34.4 | 1.9 | 0.10 | 1.81 | 28.7 | 54.1 |
| 12.8 | 1 | 91.2 | 0.2 | 2.0 | 29.2 | 29.1 | 35.9 | 3.3 | 1.68 | 1.68 | 28.5 | 55.0 |
|  | 6 | 85.3 | 0.2 | 1.5 | 22.5 | 22.3 | 46.4 | 7.0 | 1.00 | 1.00 | 20.5 | 39.5 |
| 17.0 | 1 | 81.5 | 0.2 | 2.3 | 28.3 | 25.9 | 38.0 | 5.0 | 0.08 | 1.49 | 24.9 | 46.0 |
|  | 6 | 75.6 | 0.2 | 1.7 | 23.0 | 21.3 | 45.8 | 7.7 | 0.07 | 1.00 | 18.7 | 34.8 |

Table S6 Comparison with previous results on the catalytic cracking activity of n-Do over BEA and ZSM-5 catalysts in SCC and DCC

| Cracking method | Catalysts | Rxn. temp. (oC) | LHSV (h-1 ) | n-Do con. (wt%) | Light olefins yield (wt%) | References |
| --- | --- | --- | --- | --- | --- | --- |
| SCC SCC SCC SCC SCC SCC | BEA(300) BEA(300) 0.2Ni-Dsi-BEA(48) BEA (B-25(48)) BEA, DT4-DeAl(151) BEA(40) | 550 650 400 350 350 550 | 4.2 4.2 4.0 4.0 4.0 1.0 | 91.1 97.5 72.6 45.0 76.0 99.0 | 59.2 74.3 21.8 - 18.9 47.8 | This work This work 1 2 3 4 |
| DCC DCC DCC | BEA(300) Nano-BEA(38) (BEA-Co) BEA(40) | 550 550 550 | 4.2 10.0 1.0 | 97.5 97.7 98.0 | 51.6 51.4 48.0 | This work 5 4 |
| SCC SCC | ZSM-5(280) ZSM-5(50) | 550 550 | 4.2 1.0 | 75.6 98.0 | 55.7 40.0 | This work 4 |
| DCC DCC SCC DCC | ZSM-5(280) 0.2P-ZSM-5(132), washed coated ZSM-5(100) ZSM-5(50) | 550 500 450 550 | 4.2 8.0 4.0 1.0 | 92.2 52.5 75.0 95.0 | 47.2 37.7 45.1 48.0 | This work 6 7 4 |

References

1.  M.H. Ahmed, O. Muraza, A.K. Jamil, E.N. Shafei, Z.H. Yamani, K.H. Choi, Energy     & Fuels 31, 5482 (2017)

2.  M.H. Ahmed, O. Muraza, A. Galadima, A.K. Jamil, E.N. Shafei, Z.H. Yamani, K.H. Choi, Energy & Fuels 32, 5501 (2018)

3.  M.A. Sanhoo, U. Khalil, E.N. Shafei, K.H. Choi, T. Yokoi, O. Muraza, Fuel 263, 116624 (2020)

4.  E.N. Al-Shafei, M. Z. Albahar, M.F. Aljishi, A.N. Aljishi, G.A. Nasser, M.A. Sanhoo,

A. AlAsseel, Fuel 321, 124089 (2022)

5.  G.A. Nasser, M.H.M. Ahmed, M.A. Firdaus, M.A. Sanhoo, I.A. Bakare, E.N. Al-
    Shafei, O. Muraza, RSC Advances 11, 7904 (2021)

6.  H. Liu, Z. Diao, G. Liu, L. Wang, X. Zhang, Journal of Porous Materials 24, 1679 (2017)

7.  X. Xian, G. Liu, X. Zhang, L. Wang, Z. Mi, Chemical Engineering Science 65, 5588 (2010)