Electronic Supporting Information

for

Development of Surfactant-Templated Mesoporous CeO₂ with Enhanced CO Oxidation Activity: Comparative Optimization by Response Surface Methodology Using Different Surfactants

### Text S1. Materials characterization

The textural properties of the synthesized CeO₂ samples were characterized by N₂ adsorption–desorption measurements. The specific surface area was calculated using the Brunauer–Emmett–Teller (BET) method, while the pore size distribution and pore volume were derived from the adsorption isotherms.

Temperature-programmed reduction (TPR) measurements were conducted to evaluate the reducibility of the catalysts. The samples were heated at a controlled rate under a reducing atmosphere, and the consumption of the reducing gas was monitored as a function of temperature.

The surface chemical states and elemental composition of the samples were analyzed by X-ray photoelectron spectroscopy (XPS). The binding energies were determined to identify the oxidation states and surface species.

The morphology and surface structure of the samples were examined using scanning electron microscopy (SEM).

The crystalline structure and phase composition were analyzed by X-ray diffraction (XRD). Diffraction patterns were recorded and compared with standard reference data to identify the crystalline phases.

### Text S2. The Fit Summary results of CTAB-templated system

Response 1: BET surface area

| Source | Sequential p-value | Lack of Fit p-value | Adjusted R² | Predicted R² |  |
| --- | --- | --- | --- | --- | --- |
| Linear | 0.1487 | 0.1850 | 0.1719 | -0.3060 |  |
| 2FI | 0.0048 | 0.6919 | 0.6880 | 0.4241 | Suggested |
| Quadratic | 0.8595 | 0.4584 | 0.5973 | -0.4029 |  |
| Cubic | 0.4584 |  | 0.6077 |  | Aliased |

Response 2: Pore volume

| Source | Sequential p-value | Lack of Fit p-value | Adjusted R² | Predicted R² |  |
| --- | --- | --- | --- | --- | --- |
| Linear | 0.0038 | 0.0468 | 0.5461 | 0.3599 |  |
| 2FI | 0.6497 | 0.0327 | 0.4956 | -0.0711 |  |
| Quadratic | 0.0048 | 0.3127 | 0.8744 | 0.4752 | Suggested |
| Cubic | 0.3127 |  | 0.9018 |  | Aliased |

Response 3: CO conversion (T500)

| Source | Sequential p-value | Lack of Fit p-value | Adjusted R² | Predicted R² |  |
| --- | --- | --- | --- | --- | --- |
| Linear | 0.0172 | 0.0221 | 0.4221 | 0.0522 |  |
| 2FI | 0.0003 | 0.3145 | 0.8809 | 0.7635 | Suggested |
| Quadratic | 0.2656 | 0.3522 | 0.9000 | 0.6019 |  |
| Cubic | 0.3522 |  | 0.9164 |  | Aliased |

### Text S3. Detailed analysis of variance (ANOVA) results for RSM models of CTAB-templated mesoporous CeO₂

### Response 1: BET surface area

ANOVA for Reduced 2FI model

| ### Source | ### Sum of Squares | ### df | ### Mean Square | ### F-value | ### p-value |  |
| --- | --- | --- | --- | --- | --- | --- |
| ### Model | ### 5923.39 | ### 3 | ### 1974.46 | ### 10.21 | ### 0.0010 | ### significant |
| ### A-pH | ### 1822.09 | ### 1 | ### 1822.09 | ### 9.42 | ### 0.0090 |  |
| ### B-Ratio | ### 920.40 | ### 1 | ### 920.40 | ### 4.76 | ### 0.0481 |  |
| ### AB | ### 3180.90 | ### 1 | ### 3180.90 | ### 16.45 | ### 0.0014 |  |
| ### Residual | ### 2514.11 | ### 13 | ### 193.39 |  |  |  |
| ### Lack of Fit | ### 1686.53 | ### 9 | ### 187.39 | ### 0.9057 | ### 0.5884 | ### not significant |
| ### Pure Error | ### 827.58 | ### 4 | ### 206.89 |  |  |  |
| ### Cor Total | ### 8437.50 | ### 16 |  |  |  |  |

Fit Statistics

| ### Std. Dev. | ### 13.91 |  | ### R² | ### 0.7020 |
| --- | --- | --- | --- | --- |
| ### Mean | ### 102.79 |  | ### Adjusted R² | ### 0.6333 |
| ### C.V. % | ### 13.53 |  | ### Predicted R² | ### 0.4944 |
|  |  |  | ### Adeq Precision | ### 12.8353 |

### Response 2: Pore volume

ANOVA for Reduced Quadratic model

| ### Source | ### Sum of Squares | ### df | ### Mean Square | ### F-value | ### p-value |  |
| --- | --- | --- | --- | --- | --- | --- |
| ### Model | ### 0.2236 | ### 3 | ### 0.0745 | ### 26.20 | ### < 0.0001 | ### significant |
| ### A-pH | ### 0.1223 | ### 1 | ### 0.1223 | ### 42.99 | ### < 0.0001 |  |
| ### B-Ratio | ### 0.0415 | ### 1 | ### 0.0415 | ### 14.58 | ### 0.0021 |  |
| ### A² | ### 0.0598 | ### 1 | ### 0.0598 | ### 21.03 | ### 0.0005 |  |
| ### Residual | ### 0.0370 | ### 13 | ### 0.0028 |  |  |  |
| ### Lack of Fit | ### 0.0306 | ### 9 | ### 0.0034 | ### 2.13 | ### 0.2434 | ### not significant |
| ### Pure Error | ### 0.0064 | ### 4 | ### 0.0016 |  |  |  |
| ### Cor Total | ### 0.2605 | ### 16 |  |  |  |  |

Fit Statistics

| ### Std. Dev. | ### 0.0533 |  | ### R² | ### 0.8581 |
| --- | --- | --- | --- | --- |
| ### Mean | ### 0.2897 |  | ### Adjusted R² | ### 0.8253 |
| ### C.V. % | ### 18.41 |  | ### Predicted R² | ### 0.7260 |
|  |  |  | ### Adeq Precision | ### 15.1241 |

### Response 3: CO conversion (T500)

### ANOVA for Reduced 2FI model

| ### Source | ### Sum of Squares | ### df | ### Mean Square | ### F-value | ### p-value |  |
| --- | --- | --- | --- | --- | --- | --- |
| ### Model | ### 2294.95 | ### 5 | ### 458.99 | ### 21.78 | ### < 0.0001 | ### significant |
| ### A-pH* | ### 43.93 | ### 1 | ### 43.93 | ### 2.08 | ### 0.1767 |  |
| ### B-Ratio | ### 1012.05 | ### 1 | ### 1012.05 | ### 48.03 | ### < 0.0001 |  |
| ### C-T | ### 284.29 | ### 1 | ### 284.29 | ### 13.49 | ### 0.0037 |  |
| ### AC | ### 806.87 | ### 1 | ### 806.87 | ### 38.29 | ### < 0.0001 |  |
| ### BC | ### 147.80 | ### 1 | ### 147.80 | ### 7.01 | ### 0.0227 |  |
| ### Residual | ### 231.81 | ### 11 | ### 21.07 |  |  |  |
| ### Lack of Fit | ### 179.00 | ### 7 | ### 25.57 | ### 1.94 | ### 0.2727 | ### not significant |
| ### Pure Error | ### 52.80 | ### 4 | ### 13.20 |  |  |  |
| ### Cor Total | ### 2526.75 | ### 16 |  |  |  |  |

### *To ensure the hierarchy of the model, factor A-pH was retained in the reduced model even though it was not statistically significant on its own.

### Fit Statistics

| ### Std. Dev. | ### 4.59 |  | ### R² | ### 0.9083 |
| --- | --- | --- | --- | --- |
| ### Mean | ### 77.24 |  | ### Adjusted R² | ### 0.8666 |
| ### C.V. % | ### 5.94 |  | ### Predicted R² | ### 0.7383 |
|  |  |  | ### Adeq Precision | ### 15.0734 |

### Text S4. The Fit Summary results of F127-templated system

Response 1: BET surface area

| Source | Sequential p-value | Lack of Fit p-value | Adjusted R² | Predicted R² |  |
| --- | --- | --- | --- | --- | --- |
| Linear | 0.0169 | 0.0029 | 0.4238 | 0.1618 |  |
| 2FI | 0.4322 | 0.0024 | 0.4238 | -0.2607 |  |
| Quadratic | 0.0011 | 0.0545 | 0.9053 | 0.4421 | Suggested |
| Cubic | 0.0545 |  | 0.9708 |  | Aliased |

Response 2: Pore volume

| Source | Sequential p-value | Lack of Fit p-value | Adjusted R² | Predicted R² |  |
| --- | --- | --- | --- | --- | --- |
| Linear | 0.0035 | < 0.0001 | 0.5523 | 0.3328 |  |
| 2FI | 0.3876 | < 0.0001 | 0.5641 | -0.0078 |  |
| Quadratic | < 0.0001 | 0.0502 | 0.9977 | 0.9864 | Suggested |
| Cubic | 0.0502 |  | 0.9993 |  | Aliased |

Response 3: CO conversion (T500)

| Source | Sequential p-value | Lack of Fit p-value | Adjusted R² | Predicted R² |  |
| --- | --- | --- | --- | --- | --- |
| Linear | 0.0639 | 0.2305 | 0.2826 | -0.1132 |  |
| 2FI | 0.0062 | 0.7546 | 0.7152 | 0.5302 | Suggested |
| Quadratic | 0.7725 | 0.5702 | 0.6497 | -0.0458 |  |
| Cubic | 0.5702 |  | 0.6104 |  | Aliased |

### Text S5. Detailed analysis of variance (ANOVA) results for RSM models of F127-templated mesoporous CeO₂

Response 1: BET surface area

ANOVA for Reduced Quadratic model

| Source | Sum of Squares | df | Mean Square | F-value | p-value |  |
| --- | --- | --- | --- | --- | --- | --- |
| Model | 7474.67 | 6 | 1245.78 | 31.22 | < 0.0001 | significant |
| A-pH* | 175.70 | 1 | 175.70 | 4.40 | 0.0623 |  |
| B-Ratio | 3326.51 | 1 | 3326.51 | 83.36 | < 0.0001 |  |
| C-T | 685.18 | 1 | 685.18 | 17.17 | 0.0020 |  |
| BC | 786.72 | 1 | 786.72 | 19.71 | 0.0013 |  |
| A² | 242.56 | 1 | 242.56 | 6.08 | 0.0334 |  |
| B² | 2169.68 | 1 | 2169.68 | 54.37 | < 0.0001 |  |
| Residual | 399.05 | 10 | 39.91 |  |  |  |
| Lack of Fit | 341.65 | 6 | 56.94 | 3.97 | 0.1016 | not significant |
| Pure Error | 57.40 | 4 | 14.35 |  |  |  |
| Cor Total | 7873.73 | 16 |  |  |  |  |

*To ensure the hierarchy of the model, factor A-pH was retained in the reduced model even though it was not statistically significant on its own.

Fit Statistics

| Std. Dev. | 6.32 |  | R² | 0.9493 |
| --- | --- | --- | --- | --- |
| Mean | 97.19 |  | Adjusted R² | 0.9189 |
| C.V. % | 6.50 |  | Predicted R² | 0.7698 |
|  |  |  | Adeq Precision | 17.9349 |

Response 2: Pore volume

ANOVA for Reduced Quadratic model

| Source | Sum of Squares | df | Mean Square | F-value | p-value |  |
| --- | --- | --- | --- | --- | --- | --- |
| Model | 0.0639 | 8 | 0.0080 | 993.50 | < 0.0001 | significant |
| A-pH | 0.0155 | 1 | 0.0155 | 1926.97 | < 0.0001 |  |
| B-Ratio | 0.0239 | 1 | 0.0239 | 2969.97 | < 0.0001 |  |
| C-T | 0.0013 | 1 | 0.0013 | 164.99 | < 0.0001 |  |
| AB | 0.0058 | 1 | 0.0058 | 718.63 | < 0.0001 |  |
| AC | 0.0001 | 1 | 0.0001 | 7.96 | 0.0224 |  |
| A² | 0.0099 | 1 | 0.0099 | 1233.52 | < 0.0001 |  |
| B² | 0.0063 | 1 | 0.0063 | 787.62 | < 0.0001 |  |
| C² | 0.0006 | 1 | 0.0006 | 78.29 | < 0.0001 |  |
| Residual | 0.0001 | 8 | 8.037E-06 |  |  |  |
| Lack of Fit | 0.0001 | 4 | 0.0000 | 4.95 | 0.0752 | not significant |
| Pure Error | 0.0000 | 4 | 2.700E-06 |  |  |  |
| Cor Total | 0.0639 | 16 |  |  |  |  |

Fit Statistics

| Std. Dev. | 0.0028 |  | R² | 0.9990 |
| --- | --- | --- | --- | --- |
| Mean | 0.2135 |  | Adjusted R² | 0.9980 |
| C.V. % | 1.33 |  | Predicted R² | 0.9912 |
|  |  |  | Adeq Precision | 128.4055 |

Response 3: CO conversion (T500)

ANOVA for Reduced 2FI model

| Source | Sum of Squares | df | Mean Square | F-value | p-value |  |
| --- | --- | --- | --- | --- | --- | --- |
| Model | 392.29 | 5 | 78.46 | 10.01 | 0.0008 | significant |
| A-pH* | 16.30 | 1 | 16.30 | 2.08 | 0.1773 |  |
| B-Ratio | 166.38 | 1 | 166.38 | 21.22 | 0.0008 |  |
| C-T* | 16.92 | 1 | 16.92 | 2.16 | 0.1698 |  |
| AB | 82.01 | 1 | 82.01 | 10.46 | 0.0080 |  |
| BC | 110.68 | 1 | 110.68 | 14.12 | 0.0032 |  |
| Residual | 86.25 | 11 | 7.84 |  |  |  |
| Lack of Fit | 39.64 | 7 | 5.66 | 0.4860 | 0.8097 | not significant |
| Pure Error | 46.61 | 4 | 11.65 |  |  |  |
| Cor Total | 478.54 | 16 |  |  |  |  |

*To ensure the hierarchy of the model, A-pH and C-T factors were retained in the reduced model even though they were not statistically significant on their own.

Fit Statistics

| Std. Dev. | 2.80 |  | R² | 0.8198 |
| --- | --- | --- | --- | --- |
| Mean | 88.92 |  | Adjusted R² | 0.7378 |
| C.V. % | 3.15 |  | Predicted R² | 0.5968 |
|  |  |  | Adeq Precision | 11.8069 |

Fig. S1. The perturbation plot of CO oxidation (T500) % by F127-templated CeO2

Table S1. Detailed fitting parameters used for O 1s XPS deconvolution

Table S2. T10, T50, and T90 temperatures of various CeO2 for CO oxidation