Supplementary Material

Table 7: Particle size measurements to figure 2a and 3

| Carbon Black | Particle Size | 15 min | 30 min | 1 h | 2 h | 4 h | 8 h |
| --- | --- | --- | --- | --- | --- | --- | --- |
| CB1 | 6540 | 0.0 | 0.0 | 0.0 | 0.0 | 0.0 | 0.0 |
|  | 5500 | 0.0 | 0.0 | 0.0 | 0.0 | 0.0 | 0.0 |
|  | 4620 | 0.0 | 0.0 | 0.0 | 0.0 | 0.0 | 0.0 |
|  | 3890 | 0.0 | 0.0 | 0.0 | 0.0 | 0.0 | 0.0 |
|  | 3270 | 0.0 | 0.0 | 0.0 | 0.0 | 0.0 | 0.0 |
|  | 2750 | 0.0 | 0.0 | 0.0 | 0.0 | 0.0 | 0.0 |
|  | 2312 | 0.0 | 0.0 | 0.0 | 0.0 | 0.0 | 0.0 |
|  | 1944 | 0.0 | 0.0 | 0.0 | 0.0 | 0.0 | 0.0 |
|  | 1635 | 0.0 | 0.0 | 0.0 | 0.0 | 0.0 | 0.0 |
|  | 1375 | 0.0 | 0.0 | 0.0 | 0.0 | 0.0 | 0.0 |
|  | 1156 | 0.0 | 0.0 | 0.0 | 0.0 | 0.0 | 0.0 |
|  | 972 | 0.0 | 0.0 | 0.0 | 0.0 | 0.0 | 0.0 |
|  | 818 | 0.1 | 0.0 | 0.1 | 0.0 | 0.1 | 0.0 |
|  | 687 | 1.0 | 0.0 | 1.1 | 0.0 | 0.7 | 0.0 |
|  | 578 | 3.5 | 1.1 | 3.5 | 1.1 | 1.2 | 0.5 |
|  | 486 | 8.4 | 5.2 | 8.3 | 3.9 | 2.6 | 1.1 |
|  | 409 | 15.2 | 11.9 | 13.2 | 8.9 | 6.5 | 3.1 |
|  | 344 | 19.8 | 18.7 | 16.6 | 15.2 | 12.9 | 8.0 |
|  | 289 | 18.5 | 20.6 | 17.1 | 19.3 | 19.7 | 15.8 |
|  | 243 | 13.8 | 16.9 | 14.4 | 18.9 | 21.0 | 19.5 |
|  | 204.4 | 8.9 | 11.2 | 10.4 | 14.9 | 15.5 | 17.2 |
|  | 171.9 | 5.2 | 6.5 | 6.8 | 9.5 | 8.9 | 12.7 |
|  | 144.5 | 2.9 | 3.6 | 4.2 | 4.9 | 4.7 | 8.3 |
|  | 121.5 | 1.6 | 2.2 | 2.4 | 2.2 | 2.7 | 5.3 |
|  | 102.2 | 1.0 | 1.3 | 1.4 | 1.1 | 1.8 | 3.6 |
|  | 85.9 | 0.1 | 0.7 | 0.5 | 0.1 | 1.3 | 2.6 |
|  | 72.3 | 0.0 | 0.1 | 0.1 | 0.0 | 0.5 | 1.8 |
|  | 60.8 | 0.0 | 0.0 | 0.0 | 0.0 | 0.0 | 0.5 |
|  | 51.1 | 0.0 | 0.0 | 0.0 | 0.0 | 0.0 | 0.0 |
|  | 43 | 0.0 | 0.0 | 0.0 | 0.0 | 0.0 | 0.0 |
|  | 36.1 | 0.0 | 0.0 | 0.0 | 0.0 | 0.0 | 0.0 |
|  | 30.4 | 0.0 | 0.0 | 0.0 | 0.0 | 0.0 | 0.0 |
|  | 25.55 | 0.0 | 0.0 | 0.0 | 0.0 | 0.0 | 0.0 |
|  | 21.48 | 0.0 | 0.0 | 0.0 | 0.0 | 0.0 | 0.0 |
|  | 18.06 | 0.0 | 0.0 | 0.0 | 0.0 | 0.0 | 0.0 |
|  | 15.19 | 0.0 | 0.0 | 0.0 | 0.0 | 0.0 | 0.0 |
|  | 12.77 | 0.0 | 0.0 | 0.0 | 0.0 | 0.0 | 0.0 |
|  | 10.74 | 0.0 | 0.0 | 0.0 | 0.0 | 0.0 | 0.0 |
|  | 9.03 | 0.0 | 0.0 | 0.0 | 0.0 | 0.0 | 0.0 |
|  | 7.6 | 0.0 | 0.0 | 0.0 | 0.0 | 0.0 | 0.0 |
|  | 6.39 | 0.0 | 0.0 | 0.0 | 0.0 | 0.0 | 0.0 |
|  | 5.37 | 0.0 | 0.0 | 0.0 | 0.0 | 0.0 | 0.0 |
|  | 4.52 | 0.0 | 0.0 | 0.0 | 0.0 | 0.0 | 0.0 |
|  | 3.8 | 0.0 | 0.0 | 0.0 | 0.0 | 0.0 | 0.0 |
|  | 3.19 | 0.0 | 0.0 | 0.0 | 0.0 | 0.0 | 0.0 |
|  | 2.69 | 0.0 | 0.0 | 0.0 | 0.0 | 0.0 | 0.0 |
|  | 2.26 | 0.0 | 0.0 | 0.0 | 0.0 | 0.0 | 0.0 |
|  | 1.9 | 0.0 | 0.0 | 0.0 | 0.0 | 0.0 | 0.0 |
|  | 1.6 | 0.0 | 0.0 | 0.0 | 0.0 | 0.0 | 0.0 |
|  | 1.34 | 0.0 | 0.0 | 0.0 | 0.0 | 0.0 | 0.0 |
|  | 1.13 | 0.0 | 0.0 | 0.0 | 0.0 | 0.0 | 0.0 |
|  | 0.95 | 0.0 | 0.0 | 0.0 | 0.0 | 0.0 | 0.0 |
|  | D10 | 167.9 | 154.5 | 150.9 | 150.4 | 140.5 | 108.1 |
|  | D20 | 205.2 | 189.4 | 187.1 | 177.2 | 172.4 | 139.1 |
|  | D30 | 233.8 | 215.1 | 216.1 | 198.9 | 194.1 | 162.0 |
|  | D40 | 259.2 | 237.6 | 242.6 | 219.3 | 212.9 | 181.8 |
|  | D50 | 283.9 | 259.3 | 268.9 | 239.8 | 231.0 | 200.6 |
|  | D60 | 309.0 | 281.9 | 297.2 | 261.7 | 250.4 | 219.4 |
|  | D70 | 338.0 | 307.0 | 329.0 | 286.8 | 272.9 | 239.7 |
|  | D80 | 374.0 | 338.0 | 370.0 | 318.0 | 302.0 | 264.4 |
|  | D90 | 429.0 | 383.0 | 431.0 | 367.0 | 352.0 | 302.0 |
|  | D100 | 480.0 | 422.0 | 482.0 | 410.0 | 402.0 | 340.0 |
| Carbon Black | Particle Size | 15 min | 30 min | 1 h | 2 h | 4 h | 8 h |
| CB2 | 6540 | 0.0 | 0.0 | 0.0 | 0.0 | 0.0 | 0.0 |
|  | 5500 | 0.0 | 0.0 | 0.0 | 0.0 | 0.0 | 0.0 |
|  | 4620 | 0.0 | 0.0 | 0.0 | 0.0 | 0.0 | 0.0 |
|  | 3890 | 0.0 | 0.0 | 0.0 | 0.0 | 0.0 | 0.0 |
|  | 3270 | 0.0 | 0.0 | 0.0 | 0.0 | 0.0 | 0.0 |
|  | 2750 | 0.0 | 0.0 | 0.0 | 0.0 | 0.0 | 0.0 |
|  | 2312 | 0.0 | 0.0 | 0.0 | 0.0 | 0.0 | 0.0 |
|  | 1944 | 0.0 | 0.0 | 0.0 | 0.0 | 0.0 | 0.0 |
|  | 1635 | 0.0 | 0.0 | 0.0 | 0.0 | 0.0 | 0.0 |
|  | 1375 | 0.0 | 0.0 | 0.0 | 0.0 | 0.0 | 0.0 |
|  | 1156 | 0.0 | 0.0 | 0.0 | 0.0 | 0.0 | 0.0 |
|  | 972 | 0.0 | 0.0 | 0.0 | 0.0 | 0.0 | 0.0 |
|  | 818 | 0.0 | 0.0 | 0.0 | 0.0 | 0.0 | 0.0 |
|  | 687 | 0.0 | 0.0 | 0.0 | 0.0 | 0.0 | 0.0 |
|  | 578 | 0.0 | 0.0 | 0.0 | 0.0 | 0.0 | 0.0 |
|  | 486 | 0.0 | 0.2 | 0.0 | 0.0 | 0.0 | 0.0 |
|  | 409 | 0.0 | 1.1 | 0.3 | 0.5 | 0.5 | 0.1 |
|  | 344 | 1.0 | 2.6 | 1.4 | 2.0 | 1.6 | 0.6 |
|  | 289 | 3.8 | 5.0 | 3.5 | 4.6 | 3.5 | 1.9 |
|  | 243 | 10.1 | 9.1 | 8.0 | 8.5 | 6.8 | 4.5 |
|  | 204.4 | 19.1 | 14.5 | 15.6 | 13.4 | 11.1 | 9.2 |
|  | 171.9 | 23.1 | 18.5 | 21.3 | 16.6 | 14.8 | 14.7 |
|  | 144.5 | 18.5 | 18.2 | 19.3 | 16.1 | 16.6 | 17.9 |
|  | 121.5 | 11.5 | 13.8 | 13.1 | 13.1 | 15.7 | 17.1 |
|  | 102.2 | 6.5 | 8.6 | 7.8 | 9.8 | 12.3 | 13.5 |
|  | 85.9 | 3.7 | 4.9 | 4.7 | 7.0 | 8.4 | 9.4 |
|  | 72.3 | 2.1 | 2.8 | 3.2 | 5.0 | 5.4 | 6.1 |
|  | 60.8 | 0.5 | 0.7 | 1.6 | 3.2 | 3.0 | 3.9 |
|  | 51.1 | 0.1 | 0.1 | 0.2 | 0.5 | 0.4 | 1.1 |
|  | 43 | 0.0 | 0.0 | 0.0 | 0.0 | 0.0 | 0.0 |
|  | 36.1 | 0.0 | 0.0 | 0.0 | 0.0 | 0.0 | 0.0 |
|  | 30.4 | 0.0 | 0.0 | 0.0 | 0.0 | 0.0 | 0.0 |
|  | 25.55 | 0.0 | 0.0 | 0.0 | 0.0 | 0.0 | 0.0 |
|  | 21.48 | 0.0 | 0.0 | 0.0 | 0.0 | 0.0 | 0.0 |
|  | 18.06 | 0.0 | 0.0 | 0.0 | 0.0 | 0.0 | 0.0 |
|  | 15.19 | 0.0 | 0.0 | 0.0 | 0.0 | 0.0 | 0.0 |
|  | 12.77 | 0.0 | 0.0 | 0.0 | 0.0 | 0.0 | 0.0 |
|  | 10.74 | 0.0 | 0.0 | 0.0 | 0.0 | 0.0 | 0.0 |
|  | 9.03 | 0.0 | 0.0 | 0.0 | 0.0 | 0.0 | 0.0 |
|  | 7.6 | 0.0 | 0.0 | 0.0 | 0.0 | 0.0 | 0.0 |
|  | 6.39 | 0.0 | 0.0 | 0.0 | 0.0 | 0.0 | 0.0 |
|  | 5.37 | 0.0 | 0.0 | 0.0 | 0.0 | 0.0 | 0.0 |
|  | 4.52 | 0.0 | 0.0 | 0.0 | 0.0 | 0.0 | 0.0 |
|  | 3.8 | 0.0 | 0.0 | 0.0 | 0.0 | 0.0 | 0.0 |
|  | 3.19 | 0.0 | 0.0 | 0.0 | 0.0 | 0.0 | 0.0 |
|  | 2.69 | 0.0 | 0.0 | 0.0 | 0.0 | 0.0 | 0.0 |
|  | 2.26 | 0.0 | 0.0 | 0.0 | 0.0 | 0.0 | 0.0 |
|  | 1.9 | 0.0 | 0.0 | 0.0 | 0.0 | 0.0 | 0.0 |
|  | 1.6 | 0.0 | 0.0 | 0.0 | 0.0 | 0.0 | 0.0 |
|  | 1.34 | 0.0 | 0.0 | 0.0 | 0.0 | 0.0 | 0.0 |
|  | 1.13 | 0.0 | 0.0 | 0.0 | 0.0 | 0.0 | 0.0 |
|  | 0.95 | 0.0 | 0.0 | 0.0 | 0.0 | 0.0 | 0.0 |
|  | D10 | 95.9 | 89.2 | 86.5 | 75.1 | 74.5 | 70.5 |
|  | D20 | 115.0 | 106.7 | 106.3 | 93.5 | 89.9 | 85.3 |
|  | D30 | 129.1 | 120.4 | 120.6 | 109.2 | 102.9 | 97.6 |
|  | D40 | 141.2 | 133.0 | 132.8 | 123.7 | 115.1 | 108.9 |
|  | D50 | 152.7 | 145.8 | 144.5 | 137.9 | 127.8 | 120.3 |
|  | D60 | 164.4 | 159.8 | 156.6 | 152.8 | 141.9 | 132.3 |
|  | D70 | 177.6 | 176.4 | 170.1 | 169.8 | 158.5 | 146.1 |
|  | D80 | 193.9 | 198.7 | 187.6 | 191.6 | 180.2 | 163.7 |
|  | D90 | 219.2 | 236.6 | 215.9 | 226.3 | 214.7 | 191.7 |
|  | D100 | 242.3 | 275.4 | 244.7 | 258.8 | 248.3 | 218.8 |
| Carbon Black | Particle Size | 15 min | 30 min | 1 h | 2 h | 4 h | 8 h |
| CB3 | 6540 | 0.0 | 0.0 | 0.0 | 0.0 | 0.0 | 0.0 |
|  | 5500 | 0.0 | 0.0 | 0.0 | 0.0 | 0.0 | 0.3 |
|  | 4620 | 0.0 | 0.0 | 0.0 | 0.0 | 0.0 | 0.6 |
|  | 3890 | 0.0 | 0.0 | 0.0 | 0.0 | 0.0 | 0.3 |
|  | 3270 | 0.0 | 0.0 | 0.0 | 0.0 | 0.0 | 0.0 |
|  | 2750 | 0.0 | 0.0 | 0.0 | 0.0 | 0.0 | 0.0 |
|  | 2312 | 0.0 | 0.0 | 0.0 | 0.0 | 0.0 | 0.0 |
|  | 1944 | 0.0 | 0.0 | 0.0 | 0.0 | 0.0 | 0.0 |
|  | 1635 | 0.0 | 0.0 | 0.0 | 0.0 | 0.0 | 0.0 |
|  | 1375 | 0.0 | 0.0 | 0.0 | 0.0 | 0.0 | 0.0 |
|  | 1156 | 0.0 | 0.0 | 0.0 | 0.0 | 0.0 | 0.0 |
|  | 972 | 0.0 | 0.0 | 0.0 | 0.0 | 0.0 | 0.0 |
|  | 818 | 0.0 | 0.0 | 0.0 | 0.0 | 0.0 | 0.0 |
|  | 687 | 0.0 | 0.0 | 0.0 | 0.0 | 0.0 | 0.0 |
|  | 578 | 0.1 | 0.1 | 0.0 | 0.0 | 0.0 | 0.0 |
|  | 486 | 0.8 | 0.6 | 0.1 | 0.1 | 0.1 | 0.0 |
|  | 409 | 2.1 | 1.6 | 0.7 | 0.3 | 0.2 | 0.0 |
|  | 344 | 3.5 | 2.2 | 1.5 | 1.2 | 0.5 | 0.0 |
|  | 289 | 5.2 | 3.0 | 2.5 | 2.0 | 0.8 | 0.1 |
|  | 243 | 7.0 | 4.3 | 3.5 | 3.0 | 1.2 | 0.1 |
|  | 204.4 | 8.9 | 6.6 | 4.9 | 3.8 | 1.7 | 0.2 |
|  | 171.9 | 10.6 | 9.7 | 6.7 | 4.3 | 2.3 | 0.3 |
|  | 144.5 | 11.8 | 12.4 | 9.0 | 5.0 | 3.0 | 0.5 |
|  | 121.5 | 11.9 | 13.1 | 11.2 | 6.2 | 4.0 | 0.8 |
|  | 102.2 | 10.7 | 11.7 | 12.5 | 8.0 | 5.2 | 1.4 |
|  | 85.9 | 9.0 | 9.5 | 12.3 | 10.2 | 6.4 | 2.3 |
|  | 72.3 | 7.2 | 7.6 | 10.7 | 11.8 | 7.5 | 3.8 |
|  | 60.8 | 5.8 | 6.4 | 8.7 | 12.1 | 8.4 | 6.0 |
|  | 51.1 | 4.4 | 5.9 | 7.1 | 11.2 | 9.4 | 8.9 |
|  | 43 | 1.0 | 4.1 | 5.5 | 9.8 | 10.5 | 12.1 |
|  | 36.1 | 0.0 | 1.3 | 2.9 | 7.9 | 11.7 | 14.5 |
|  | 30.4 | 0.0 | 0.0 | 0.3 | 2.8 | 12.5 | 15.2 |
|  | 25.55 | 0.0 | 0.0 | 0.0 | 0.4 | 12.1 | 14.3 |
|  | 21.48 | 0.0 | 0.0 | 0.0 | 0.0 | 2.6 | 12.6 |
|  | 18.06 | 0.0 | 0.0 | 0.0 | 0.0 | 0.0 | 5.8 |
|  | 15.19 | 0.0 | 0.0 | 0.0 | 0.0 | 0.0 | 0.1 |
|  | 12.77 | 0.0 | 0.0 | 0.0 | 0.0 | 0.0 | 0.0 |
|  | 10.74 | 0.0 | 0.0 | 0.0 | 0.0 | 0.0 | 0.0 |
|  | 9.03 | 0.0 | 0.0 | 0.0 | 0.0 | 0.0 | 0.0 |
|  | 7.6 | 0.0 | 0.0 | 0.0 | 0.0 | 0.0 | 0.0 |
|  | 6.39 | 0.0 | 0.0 | 0.0 | 0.0 | 0.0 | 0.0 |
|  | 5.37 | 0.0 | 0.0 | 0.0 | 0.0 | 0.0 | 0.0 |
|  | 4.52 | 0.0 | 0.0 | 0.0 | 0.0 | 0.0 | 0.0 |
|  | 3.8 | 0.0 | 0.0 | 0.0 | 0.0 | 0.0 | 0.0 |
|  | 3.19 | 0.0 | 0.0 | 0.0 | 0.0 | 0.0 | 0.0 |
|  | 2.69 | 0.0 | 0.0 | 0.0 | 0.0 | 0.0 | 0.0 |
|  | 2.26 | 0.0 | 0.0 | 0.0 | 0.0 | 0.0 | 0.0 |
|  | 1.9 | 0.0 | 0.0 | 0.0 | 0.0 | 0.0 | 0.0 |
|  | 1.6 | 0.0 | 0.0 | 0.0 | 0.0 | 0.0 | 0.0 |
|  | 1.34 | 0.0 | 0.0 | 0.0 | 0.0 | 0.0 | 0.0 |
|  | 1.13 | 0.0 | 0.0 | 0.0 | 0.0 | 0.0 | 0.0 |
|  | 0.95 | 0.0 | 0.0 | 0.0 | 0.0 | 0.0 | 0.0 |
|  | D10 | 58.8 | 49.3 | 44.6 | 35.4 | 24.1 | 19.3 |
|  | D20 | 74.7 | 64.2 | 55.8 | 42.4 | 27.4 | 21.9 |
|  | D30 | 89.8 | 79.0 | 66.8 | 49.6 | 31.6 | 24.7 |
|  | D40 | 105.1 | 93.1 | 77.5 | 57.4 | 36.7 | 27.7 |
|  | D50 | 121.6 | 107.1 | 88.9 | 66.2 | 43.4 | 31.1 |
|  | D60 | 140.8 | 122.2 | 102.2 | 77.3 | 52.3 | 35.0 |
|  | D70 | 165.1 | 140.4 | 119.3 | 93.1 | 64.5 | 40.0 |
|  | D80 | 199.4 | 166.3 | 144.2 | 120.5 | 82.8 | 47.4 |
|  | D90 | 256.4 | 217.4 | 191.2 | 174.6 | 119.3 | 62.1 |
|  | D100 | 310.0 | 279.0 | 240.2 | 222.3 | 163.0 | 81.8 |
| Carbon Black | Particle Size | 15 min | 30 min | 1 h | 2 h | 4 h | 8 h |
| CB4 | 6540 | 0.0 | 0.0 | 0.0 | 0.0 | 0.0 | 0.0 |
|  | 5500 | 0.0 | 0.0 | 0.0 | 0.0 | 0.0 | 0.0 |
|  | 4620 | 0.0 | 0.0 | 0.0 | 0.0 | 0.0 | 0.0 |
|  | 3890 | 0.0 | 0.0 | 0.0 | 0.0 | 0.0 | 0.0 |
|  | 3270 | 0.0 | 0.0 | 0.0 | 0.0 | 0.0 | 0.0 |
|  | 2750 | 0.0 | 0.0 | 0.0 | 0.0 | 0.0 | 0.0 |
|  | 2312 | 0.0 | 0.0 | 0.0 | 0.0 | 0.0 | 0.0 |
|  | 1944 | 0.0 | 0.0 | 0.0 | 0.0 | 0.0 | 0.0 |
|  | 1635 | 0.0 | 0.0 | 0.0 | 0.0 | 0.0 | 0.0 |
|  | 1375 | 0.0 | 0.0 | 0.0 | 0.0 | 0.0 | 0.1 |
|  | 1156 | 0.0 | 0.0 | 0.0 | 0.0 | 0.0 | 0.2 |
|  | 972 | 0.0 | 0.0 | 0.0 | 0.0 | 0.0 | 0.0 |
|  | 818 | 0.0 | 0.0 | 0.0 | 0.0 | 0.0 | 0.0 |
|  | 687 | 0.0 | 0.0 | 0.0 | 0.0 | 0.0 | 0.0 |
|  | 578 | 0.0 | 0.0 | 0.0 | 0.0 | 0.0 | 0.0 |
|  | 486 | 0.0 | 0.0 | 0.0 | 0.1 | 0.1 | 0.0 |
|  | 409 | 0.0 | 0.2 | 0.0 | 0.3 | 0.3 | 0.0 |
|  | 344 | 0.2 | 0.3 | 0.5 | 0.5 | 0.4 | 0.2 |
|  | 289 | 0.7 | 0.8 | 1.0 | 1.0 | 0.7 | 0.4 |
|  | 243 | 1.7 | 1.6 | 1.7 | 1.5 | 1.0 | 0.7 |
|  | 204.4 | 3.4 | 3.5 | 2.8 | 2.3 | 1.5 | 1.0 |
|  | 171.9 | 6.2 | 6.3 | 4.4 | 3.4 | 2.3 | 1.5 |
|  | 144.5 | 9.7 | 9.0 | 6.8 | 5.2 | 3.4 | 2.0 |
|  | 121.5 | 12.9 | 10.7 | 10.0 | 7.5 | 4.9 | 2.7 |
|  | 102.2 | 14.7 | 11.8 | 12.8 | 9.8 | 7.3 | 3.8 |
|  | 85.9 | 14.2 | 12.4 | 14.2 | 11.4 | 10.1 | 5.6 |
|  | 72.3 | 11.9 | 12.2 | 13.5 | 12.0 | 12.6 | 8.3 |
|  | 60.8 | 9.1 | 11.0 | 11.5 | 11.9 | 13.9 | 11.4 |
|  | 51.1 | 6.9 | 9.3 | 9.3 | 11.1 | 13.3 | 13.8 |
|  | 43 | 5.5 | 7.4 | 7.6 | 10.1 | 11.5 | 14.4 |
|  | 36.1 | 2.7 | 3.5 | 4.0 | 8.6 | 9.6 | 13.0 |
|  | 30.4 | 0.3 | 0.1 | 0.1 | 3.2 | 6.4 | 11.1 |
|  | 25.55 | 0.0 | 0.0 | 0.0 | 0.1 | 0.7 | 8.1 |
|  | 21.48 | 0.0 | 0.0 | 0.0 | 0.0 | 0.0 | 1.7 |
|  | 18.06 | 0.0 | 0.0 | 0.0 | 0.0 | 0.0 | 0.0 |
|  | 15.19 | 0.0 | 0.0 | 0.0 | 0.0 | 0.0 | 0.0 |
|  | 12.77 | 0.0 | 0.0 | 0.0 | 0.0 | 0.0 | 0.0 |
|  | 10.74 | 0.0 | 0.0 | 0.0 | 0.0 | 0.0 | 0.0 |
|  | 9.03 | 0.0 | 0.0 | 0.0 | 0.0 | 0.0 | 0.0 |
|  | 7.6 | 0.0 | 0.0 | 0.0 | 0.0 | 0.0 | 0.0 |
|  | 6.39 | 0.0 | 0.0 | 0.0 | 0.0 | 0.0 | 0.0 |
|  | 5.37 | 0.0 | 0.0 | 0.0 | 0.0 | 0.0 | 0.0 |
|  | 4.52 | 0.0 | 0.0 | 0.0 | 0.0 | 0.0 | 0.0 |
|  | 3.8 | 0.0 | 0.0 | 0.0 | 0.0 | 0.0 | 0.0 |
|  | 3.19 | 0.0 | 0.0 | 0.0 | 0.0 | 0.0 | 0.0 |
|  | 2.69 | 0.0 | 0.0 | 0.0 | 0.0 | 0.0 | 0.0 |
|  | 2.26 | 0.0 | 0.0 | 0.0 | 0.0 | 0.0 | 0.0 |
|  | 1.9 | 0.0 | 0.0 | 0.0 | 0.0 | 0.0 | 0.0 |
|  | 1.6 | 0.0 | 0.0 | 0.0 | 0.0 | 0.0 | 0.0 |
|  | 1.34 | 0.0 | 0.0 | 0.0 | 0.0 | 0.0 | 0.0 |
|  | 1.13 | 0.0 | 0.0 | 0.0 | 0.0 | 0.0 | 0.0 |
|  | 0.95 | 0.0 | 0.0 | 0.0 | 0.0 | 0.0 | 0.0 |
|  | D10 | 53.3 | 42.1 | 41.5 | 34.9 | 32.1 | 25.7 |
|  | D20 | 66.7 | 50.8 | 50.2 | 41.5 | 38.0 | 30.0 |
|  | D30 | 78.7 | 59.6 | 58.7 | 48.6 | 44.0 | 34.4 |
|  | D40 | 89.9 | 68.8 | 67.1 | 56.5 | 50.1 | 38.9 |
|  | D50 | 101.5 | 79.1 | 75.9 | 65.3 | 56.8 | 43.9 |
|  | D60 | 114.1 | 91.2 | 85.7 | 75.5 | 64.6 | 49.7 |
|  | D70 | 129.1 | 106.0 | 97.9 | 88.2 | 74.6 | 57.4 |
|  | D80 | 148.9 | 125.1 | 114.9 | 106.0 | 89.5 | 69.2 |
|  | D90 | 181.2 | 154.1 | 145.7 | 139.8 | 120.3 | 96.2 |
|  | D100 | 212.7 | 181.4 | 179.8 | 180.1 | 159.2 | 132.8 |
| Carbon Black | Particle Size | 15 min | 30 min | 1 h | 2 h | 4 h | 8 h |
| CB1 | 6540 | 0.0 | 0.0 | 0.0 | 0.0 | 0.0 | 0.0 |
|  | 5500 | 0.0 | 0.0 | 0.0 | 0.0 | 0.0 | 0.0 |
|  | 4620 | 0.0 | 0.0 | 0.0 | 0.0 | 0.0 | 0.0 |
|  | 3890 | 0.0 | 0.0 | 0.0 | 0.0 | 0.0 | 0.0 |
|  | 3270 | 0.0 | 0.0 | 0.0 | 0.0 | 0.0 | 0.0 |
|  | 2750 | 0.0 | 0.0 | 0.0 | 0.0 | 0.0 | 0.0 |
|  | 2312 | 0.0 | 0.0 | 0.0 | 0.0 | 0.0 | 0.0 |
|  | 1944 | 0.0 | 0.0 | 0.0 | 0.0 | 0.0 | 0.0 |
|  | 1635 | 0.0 | 0.0 | 0.0 | 0.0 | 0.0 | 0.0 |
|  | 1375 | 0.0 | 0.0 | 0.0 | 0.0 | 0.0 | 0.0 |
|  | 1156 | 0.0 | 0.0 | 0.0 | 0.0 | 0.0 | 0.0 |
|  | 972 | 0.0 | 0.0 | 0.0 | 0.0 | 0.0 | 0.0 |
|  | 818 | 0.0 | 0.0 | 0.0 | 0.0 | 0.0 | 0.0 |
|  | 687 | 0.0 | 0.0 | 0.0 | 0.0 | 0.0 | 0.0 |
|  | 578 | 0.0 | 0.0 | 0.0 | 0.0 | 0.2 | 0.0 |
|  | 486 | 0.0 | 0.0 | 0.1 | 0.0 | 0.3 | 0.2 |
|  | 409 | 0.2 | 0.1 | 0.4 | 0.1 | 0.4 | 0.4 |
|  | 344 | 0.5 | 0.3 | 0.5 | 0.4 | 0.4 | 0.6 |
|  | 289 | 0.7 | 0.7 | 0.7 | 0.5 | 0.4 | 0.7 |
|  | 243 | 1.0 | 1.1 | 0.9 | 0.8 | 0.5 | 0.7 |
|  | 204.4 | 1.5 | 1.8 | 1.3 | 1.1 | 0.7 | 0.7 |
|  | 171.9 | 2.4 | 3.0 | 2.1 | 1.6 | 1.2 | 0.8 |
|  | 144.5 | 4.0 | 4.5 | 3.4 | 2.4 | 2.0 | 1.2 |
|  | 121.5 | 6.3 | 6.1 | 5.3 | 3.7 | 3.2 | 1.9 |
|  | 102.2 | 9.4 | 7.8 | 7.8 | 5.7 | 5.2 | 3.4 |
|  | 85.9 | 12.4 | 9.7 | 10.5 | 8.6 | 7.8 | 5.7 |
|  | 72.3 | 14.3 | 11.8 | 12.3 | 11.6 | 10.5 | 8.8 |
|  | 60.8 | 14.4 | 13.4 | 12.8 | 13.7 | 12.5 | 11.7 |
|  | 51.1 | 12.8 | 13.4 | 12.2 | 13.9 | 13.4 | 13.8 |
|  | 43 | 10.3 | 11.8 | 11.1 | 12.7 | 13.2 | 14.5 |
|  | 36.1 | 7.8 | 9.6 | 10.0 | 11.0 | 12.1 | 13.8 |
|  | 30.4 | 2.1 | 4.7 | 7.5 | 9.3 | 10.7 | 11.9 |
|  | 25.55 | 0.1 | 0.2 | 1.3 | 3.0 | 5.3 | 9.0 |
|  | 21.48 | 0.0 | 0.0 | 0.0 | 0.0 | 0.1 | 0.3 |
|  | 18.06 | 0.0 | 0.0 | 0.0 | 0.0 | 0.0 | 0.0 |
|  | 15.19 | 0.0 | 0.0 | 0.0 | 0.0 | 0.0 | 0.0 |
|  | 12.77 | 0.0 | 0.0 | 0.0 | 0.0 | 0.0 | 0.0 |
|  | 10.74 | 0.0 | 0.0 | 0.0 | 0.0 | 0.0 | 0.0 |
|  | 9.03 | 0.0 | 0.0 | 0.0 | 0.0 | 0.0 | 0.0 |
|  | 7.6 | 0.0 | 0.0 | 0.0 | 0.0 | 0.0 | 0.0 |
|  | 6.39 | 0.0 | 0.0 | 0.0 | 0.0 | 0.0 | 0.0 |
|  | 5.37 | 0.0 | 0.0 | 0.0 | 0.0 | 0.0 | 0.0 |
|  | 4.52 | 0.0 | 0.0 | 0.0 | 0.0 | 0.0 | 0.0 |
|  | 3.8 | 0.0 | 0.0 | 0.0 | 0.0 | 0.0 | 0.0 |
|  | 3.19 | 0.0 | 0.0 | 0.0 | 0.0 | 0.0 | 0.0 |
|  | 2.69 | 0.0 | 0.0 | 0.0 | 0.0 | 0.0 | 0.0 |
|  | 2.26 | 0.0 | 0.0 | 0.0 | 0.0 | 0.0 | 0.0 |
|  | 1.9 | 0.0 | 0.0 | 0.0 | 0.0 | 0.0 | 0.0 |
|  | 1.6 | 0.0 | 0.0 | 0.0 | 0.0 | 0.0 | 0.0 |
|  | 1.34 | 0.0 | 0.0 | 0.0 | 0.0 | 0.0 | 0.0 |
|  | 1.13 | 0.0 | 0.0 | 0.0 | 0.0 | 0.0 | 0.0 |
|  | 0.95 | 0.0 | 0.0 | 0.0 | 0.0 | 0.0 | 0.0 |
|  | D10 | 36.1 | 33.5 | 31.1 | 29.3 | 27.7 | 25.9 |
|  | D20 | 42.8 | 39.3 | 36.9 | 34.4 | 32.2 | 29.9 |
|  | D30 | 49.1 | 45.2 | 43.2 | 39.7 | 37.0 | 34.0 |
|  | D40 | 55.6 | 51.3 | 49.8 | 45.2 | 42.2 | 38.4 |
|  | D50 | 62.7 | 58.3 | 57.0 | 51.2 | 48.0 | 43.3 |
|  | D60 | 70.8 | 67.0 | 65.4 | 58.0 | 54.8 | 49.0 |
|  | D70 | 80.9 | 78.7 | 75.7 | 66.6 | 63.4 | 56.2 |
|  | D80 | 95.3 | 96.4 | 90.3 | 79.0 | 75.6 | 66.7 |
|  | D90 | 122.7 | 127.8 | 118.8 | 104.3 | 99.1 | 88.0 |
|  | D100 | 157.1 | 160.5 | 155.6 | 138.0 | 131.2 | 125.8 |

Table 8: spectral data to figure 2a and 3

| Carbon Black | Wavelength [nm] | 15 min | 30 min | 1 h | 2 h | 4 h | 8 h |
| --- | --- | --- | --- | --- | --- | --- | --- |
| CB1 | 400 | 0.537 | 0.562 | 0.570 | 0.579 | 0.615 | 0.615 |
|  | 410 | 0.526 | 0.553 | 0.559 | 0.567 | 0.605 | 0.603 |
|  | 420 | 0.522 | 0.548 | 0.556 | 0.564 | 0.602 | 0.600 |
|  | 430 | 0.543 | 0.567 | 0.578 | 0.586 | 0.623 | 0.624 |
|  | 440 | 0.543 | 0.569 | 0.580 | 0.587 | 0.625 | 0.625 |
|  | 450 | 0.544 | 0.572 | 0.580 | 0.586 | 0.624 | 0.623 |
|  | 460 | 0.544 | 0.576 | 0.581 | 0.587 | 0.628 | 0.624 |
|  | 470 | 0.549 | 0.582 | 0.586 | 0.591 | 0.636 | 0.625 |
|  | 480 | 0.550 | 0.579 | 0.587 | 0.592 | 0.632 | 0.627 |
|  | 490 | 0.560 | 0.590 | 0.599 | 0.603 | 0.643 | 0.638 |
|  | 500 | 0.569 | 0.602 | 0.608 | 0.612 | 0.654 | 0.647 |
|  | 510 | 0.565 | 0.602 | 0.605 | 0.609 | 0.653 | 0.637 |
|  | 520 | 0.570 | 0.608 | 0.606 | 0.609 | 0.658 | 0.640 |
|  | 530 | 0.581 | 0.622 | 0.621 | 0.624 | 0.671 | 0.655 |
|  | 540 | 0.584 | 0.626 | 0.624 | 0.627 | 0.674 | 0.656 |
|  | 550 | 0.591 | 0.634 | 0.629 | 0.631 | 0.680 | 0.657 |
|  | 560 | 0.599 | 0.642 | 0.639 | 0.641 | 0.687 | 0.667 |
|  | 570 | 0.591 | 0.634 | 0.630 | 0.632 | 0.678 | 0.656 |
|  | 580 | 0.611 | 0.657 | 0.652 | 0.653 | 0.702 | 0.677 |
|  | 590 | 0.605 | 0.653 | 0.647 | 0.647 | 0.696 | 0.669 |
|  | 600 | 0.614 | 0.664 | 0.656 | 0.655 | 0.704 | 0.676 |
|  | 610 | 0.626 | 0.677 | 0.668 | 0.667 | 0.715 | 0.685 |
|  | 620 | 0.633 | 0.682 | 0.673 | 0.672 | 0.719 | 0.688 |
|  | 630 | 0.632 | 0.681 | 0.672 | 0.670 | 0.714 | 0.684 |
|  | 640 | 0.645 | 0.692 | 0.684 | 0.682 | 0.724 | 0.694 |
|  | 650 | 0.644 | 0.688 | 0.681 | 0.679 | 0.717 | 0.688 |
|  | 660 | 0.652 | 0.697 | 0.689 | 0.686 | 0.722 | 0.694 |
|  | 670 | 0.664 | 0.708 | 0.701 | 0.698 | 0.731 | 0.703 |
|  | 680 | 0.666 | 0.710 | 0.703 | 0.699 | 0.730 | 0.702 |
|  | 690 | 0.663 | 0.705 | 0.699 | 0.695 | 0.724 | 0.696 |
|  | 700 | 0.679 | 0.720 | 0.716 | 0.711 | 0.737 | 0.710 |
| Carbon Black | Wavelength [nm] | 15 min | 30 min | 1 h | 2 h | 4 h | 8 h |
| CB2 | 400 | 0.426 | 0.418 | 0.418 | 0.411 | 0.397 | 0.385 |
|  | 410 | 0.414 | 0.406 | 0.407 | 0.399 | 0.385 | 0.372 |
|  | 420 | 0.404 | 0.397 | 0.396 | 0.388 | 0.374 | 0.361 |
|  | 430 | 0.414 | 0.406 | 0.406 | 0.397 | 0.381 | 0.368 |
|  | 440 | 0.409 | 0.400 | 0.399 | 0.391 | 0.375 | 0.362 |
|  | 450 | 0.404 | 0.395 | 0.394 | 0.385 | 0.370 | 0.356 |
|  | 460 | 0.399 | 0.390 | 0.389 | 0.380 | 0.365 | 0.351 |
|  | 470 | 0.394 | 0.385 | 0.384 | 0.374 | 0.359 | 0.345 |
|  | 480 | 0.386 | 0.377 | 0.375 | 0.366 | 0.351 | 0.335 |
|  | 490 | 0.386 | 0.376 | 0.375 | 0.365 | 0.350 | 0.334 |
|  | 500 | 0.385 | 0.375 | 0.373 | 0.364 | 0.348 | 0.332 |
|  | 510 | 0.375 | 0.365 | 0.364 | 0.354 | 0.339 | 0.323 |
|  | 520 | 0.369 | 0.359 | 0.357 | 0.347 | 0.333 | 0.316 |
|  | 530 | 0.370 | 0.360 | 0.358 | 0.348 | 0.333 | 0.316 |
|  | 540 | 0.365 | 0.355 | 0.353 | 0.343 | 0.328 | 0.311 |
|  | 550 | 0.359 | 0.349 | 0.347 | 0.337 | 0.322 | 0.305 |
|  | 560 | 0.355 | 0.345 | 0.343 | 0.333 | 0.318 | 0.301 |
|  | 570 | 0.342 | 0.332 | 0.330 | 0.320 | 0.305 | 0.289 |
|  | 580 | 0.345 | 0.335 | 0.332 | 0.323 | 0.307 | 0.291 |
|  | 590 | 0.335 | 0.325 | 0.322 | 0.313 | 0.298 | 0.282 |
|  | 600 | 0.332 | 0.322 | 0.319 | 0.310 | 0.295 | 0.278 |
|  | 610 | 0.330 | 0.320 | 0.318 | 0.308 | 0.294 | 0.276 |
|  | 620 | 0.326 | 0.316 | 0.313 | 0.303 | 0.289 | 0.271 |
|  | 630 | 0.317 | 0.307 | 0.304 | 0.295 | 0.281 | 0.264 |
|  | 640 | 0.316 | 0.307 | 0.304 | 0.294 | 0.280 | 0.263 |
|  | 650 | 0.309 | 0.300 | 0.297 | 0.287 | 0.274 | 0.257 |
|  | 660 | 0.306 | 0.296 | 0.293 | 0.284 | 0.270 | 0.253 |
|  | 670 | 0.304 | 0.295 | 0.291 | 0.282 | 0.268 | 0.251 |
|  | 680 | 0.298 | 0.288 | 0.285 | 0.276 | 0.262 | 0.245 |
|  | 690 | 0.289 | 0.280 | 0.277 | 0.268 | 0.255 | 0.238 |
|  | 700 | 0.288 | 0.279 | 0.276 | 0.267 | 0.253 | 0.237 |
| Carbon Black | Wavelength [nm] | 15 min | 30 min | 1 h | 2 h | 4 h | 8 h |
| CB3 | 400 | 0.152 | 0.143 | 0.128 | 0.112 | 0.087 | 0.053 |
|  | 410 | 0.147 | 0.137 | 0.123 | 0.108 | 0.083 | 0.051 |
|  | 420 | 0.139 | 0.130 | 0.116 | 0.101 | 0.077 | 0.047 |
|  | 430 | 0.141 | 0.131 | 0.117 | 0.101 | 0.077 | 0.046 |
|  | 440 | 0.138 | 0.128 | 0.113 | 0.098 | 0.074 | 0.044 |
|  | 450 | 0.135 | 0.124 | 0.110 | 0.095 | 0.072 | 0.043 |
|  | 460 | 0.133 | 0.122 | 0.108 | 0.093 | 0.070 | 0.041 |
|  | 470 | 0.130 | 0.119 | 0.105 | 0.090 | 0.067 | 0.040 |
|  | 480 | 0.125 | 0.114 | 0.100 | 0.086 | 0.064 | 0.038 |
|  | 490 | 0.124 | 0.113 | 0.099 | 0.084 | 0.063 | 0.037 |
|  | 500 | 0.123 | 0.112 | 0.098 | 0.083 | 0.062 | 0.036 |
|  | 510 | 0.119 | 0.108 | 0.094 | 0.080 | 0.059 | 0.034 |
|  | 520 | 0.116 | 0.105 | 0.091 | 0.077 | 0.057 | 0.033 |
|  | 530 | 0.116 | 0.105 | 0.091 | 0.077 | 0.057 | 0.033 |
|  | 540 | 0.114 | 0.103 | 0.089 | 0.075 | 0.055 | 0.032 |
|  | 550 | 0.112 | 0.101 | 0.087 | 0.073 | 0.053 | 0.031 |
|  | 560 | 0.110 | 0.098 | 0.085 | 0.071 | 0.052 | 0.030 |
|  | 570 | 0.105 | 0.094 | 0.081 | 0.068 | 0.049 | 0.028 |
|  | 580 | 0.106 | 0.095 | 0.081 | 0.068 | 0.049 | 0.028 |
|  | 590 | 0.103 | 0.091 | 0.078 | 0.065 | 0.047 | 0.027 |
|  | 600 | 0.102 | 0.090 | 0.077 | 0.064 | 0.046 | 0.026 |
|  | 610 | 0.101 | 0.089 | 0.076 | 0.063 | 0.045 | 0.026 |
|  | 620 | 0.099 | 0.088 | 0.074 | 0.062 | 0.044 | 0.026 |
|  | 630 | 0.096 | 0.085 | 0.072 | 0.060 | 0.043 | 0.025 |
|  | 640 | 0.096 | 0.085 | 0.071 | 0.059 | 0.042 | 0.024 |
|  | 650 | 0.094 | 0.083 | 0.070 | 0.058 | 0.041 | 0.024 |
|  | 660 | 0.093 | 0.081 | 0.068 | 0.056 | 0.040 | 0.023 |
|  | 670 | 0.092 | 0.081 | 0.068 | 0.056 | 0.040 | 0.023 |
|  | 680 | 0.090 | 0.079 | 0.066 | 0.054 | 0.038 | 0.022 |
|  | 690 | 0.087 | 0.076 | 0.064 | 0.052 | 0.036 | 0.021 |
|  | 700 | 0.087 | 0.076 | 0.063 | 0.052 | 0.036 | 0.021 |
| Carbon Black | Wavelength [nm] | 15 min | 30 min | 1 h | 2 h | 4 h | 8 h |
| CB4 | 400 | 0.165 | 0.150 | 0.146 | 0.134 | 0.116 | 0.103 |
|  | 410 | 0.158 | 0.143 | 0.140 | 0.128 | 0.110 | 0.098 |
|  | 420 | 0.150 | 0.134 | 0.131 | 0.120 | 0.103 | 0.091 |
|  | 430 | 0.150 | 0.134 | 0.131 | 0.120 | 0.102 | 0.091 |
|  | 440 | 0.145 | 0.129 | 0.126 | 0.115 | 0.098 | 0.087 |
|  | 450 | 0.140 | 0.125 | 0.122 | 0.111 | 0.095 | 0.084 |
|  | 460 | 0.137 | 0.121 | 0.119 | 0.108 | 0.092 | 0.081 |
|  | 470 | 0.133 | 0.117 | 0.115 | 0.105 | 0.089 | 0.078 |
|  | 480 | 0.127 | 0.112 | 0.110 | 0.100 | 0.085 | 0.074 |
|  | 490 | 0.125 | 0.110 | 0.108 | 0.098 | 0.083 | 0.073 |
|  | 500 | 0.123 | 0.108 | 0.106 | 0.096 | 0.081 | 0.071 |
|  | 510 | 0.118 | 0.103 | 0.101 | 0.092 | 0.077 | 0.068 |
|  | 520 | 0.115 | 0.100 | 0.098 | 0.089 | 0.075 | 0.065 |
|  | 530 | 0.114 | 0.099 | 0.097 | 0.088 | 0.074 | 0.065 |
|  | 540 | 0.111 | 0.097 | 0.095 | 0.086 | 0.072 | 0.063 |
|  | 550 | 0.108 | 0.093 | 0.092 | 0.083 | 0.070 | 0.061 |
|  | 560 | 0.105 | 0.091 | 0.090 | 0.081 | 0.068 | 0.059 |
|  | 570 | 0.100 | 0.087 | 0.085 | 0.077 | 0.064 | 0.056 |
|  | 580 | 0.100 | 0.087 | 0.085 | 0.077 | 0.065 | 0.056 |
|  | 590 | 0.096 | 0.083 | 0.082 | 0.074 | 0.062 | 0.054 |
|  | 600 | 0.095 | 0.081 | 0.080 | 0.072 | 0.061 | 0.052 |
|  | 610 | 0.093 | 0.080 | 0.079 | 0.071 | 0.059 | 0.052 |
|  | 620 | 0.091 | 0.078 | 0.077 | 0.070 | 0.058 | 0.051 |
|  | 630 | 0.088 | 0.075 | 0.074 | 0.067 | 0.056 | 0.049 |
|  | 640 | 0.087 | 0.074 | 0.074 | 0.067 | 0.055 | 0.048 |
|  | 650 | 0.085 | 0.072 | 0.071 | 0.065 | 0.053 | 0.047 |
|  | 660 | 0.083 | 0.070 | 0.070 | 0.063 | 0.052 | 0.046 |
|  | 670 | 0.082 | 0.070 | 0.069 | 0.063 | 0.052 | 0.045 |
|  | 680 | 0.080 | 0.067 | 0.067 | 0.061 | 0.050 | 0.043 |
|  | 690 | 0.077 | 0.065 | 0.065 | 0.058 | 0.048 | 0.042 |
|  | 700 | 0.077 | 0.064 | 0.064 | 0.058 | 0.048 | 0.042 |
| Carbon Black | Wavelength [nm] | 15 min | 30 min | 1 h | 2 h | 4 h | 8 h |
| CB5 | 400 | 0.111 | 0.108 | 0.108 | 0.105 | 0.093 | 0.091 |
|  | 410 | 0.106 | 0.102 | 0.103 | 0.100 | 0.088 | 0.086 |
|  | 420 | 0.099 | 0.096 | 0.096 | 0.093 | 0.082 | 0.080 |
|  | 430 | 0.099 | 0.095 | 0.096 | 0.093 | 0.081 | 0.079 |
|  | 440 | 0.095 | 0.092 | 0.093 | 0.089 | 0.078 | 0.076 |
|  | 450 | 0.092 | 0.089 | 0.089 | 0.086 | 0.075 | 0.073 |
|  | 460 | 0.089 | 0.086 | 0.087 | 0.083 | 0.073 | 0.071 |
|  | 470 | 0.086 | 0.083 | 0.083 | 0.080 | 0.070 | 0.068 |
|  | 480 | 0.082 | 0.079 | 0.079 | 0.077 | 0.067 | 0.065 |
|  | 490 | 0.080 | 0.077 | 0.078 | 0.075 | 0.065 | 0.063 |
|  | 500 | 0.078 | 0.076 | 0.076 | 0.073 | 0.064 | 0.062 |
|  | 510 | 0.075 | 0.072 | 0.073 | 0.070 | 0.060 | 0.059 |
|  | 520 | 0.072 | 0.071 | 0.070 | 0.068 | 0.059 | 0.057 |
|  | 530 | 0.072 | 0.070 | 0.070 | 0.067 | 0.058 | 0.057 |
|  | 540 | 0.070 | 0.068 | 0.068 | 0.065 | 0.056 | 0.055 |
|  | 550 | 0.067 | 0.065 | 0.066 | 0.063 | 0.054 | 0.053 |
|  | 560 | 0.066 | 0.064 | 0.064 | 0.061 | 0.053 | 0.052 |
|  | 570 | 0.062 | 0.060 | 0.061 | 0.059 | 0.050 | 0.049 |
|  | 580 | 0.062 | 0.061 | 0.061 | 0.058 | 0.050 | 0.049 |
|  | 590 | 0.060 | 0.058 | 0.058 | 0.056 | 0.048 | 0.047 |
|  | 600 | 0.059 | 0.057 | 0.057 | 0.055 | 0.047 | 0.046 |
|  | 610 | 0.058 | 0.056 | 0.056 | 0.054 | 0.046 | 0.046 |
|  | 620 | 0.056 | 0.054 | 0.055 | 0.053 | 0.045 | 0.045 |
|  | 630 | 0.054 | 0.052 | 0.053 | 0.051 | 0.043 | 0.043 |
|  | 640 | 0.054 | 0.052 | 0.052 | 0.051 | 0.043 | 0.043 |
|  | 650 | 0.052 | 0.050 | 0.051 | 0.049 | 0.041 | 0.042 |
|  | 660 | 0.051 | 0.049 | 0.050 | 0.048 | 0.041 | 0.041 |
|  | 670 | 0.051 | 0.049 | 0.049 | 0.048 | 0.040 | 0.041 |
|  | 680 | 0.049 | 0.047 | 0.048 | 0.046 | 0.038 | 0.039 |
|  | 690 | 0.047 | 0.045 | 0.046 | 0.045 | 0.038 | 0.038 |
|  | 700 | 0.047 | 0.045 | 0.046 | 0.044 | 0.037 | 0.038 |

Table 9: Particle size measurements to figure 2b

| Carbon Black | Dispersing additive concentration [%] | Particle Size | 30 min | 4 h | 24 h |
| --- | --- | --- | --- | --- | --- |
| CB1 | 70 | 6540 | 0.0 | 0.0 | 0.0 |
|  |  | 5500 | 0.0 | 0.0 | 0.0 |
|  |  | 4620 | 0.0 | 0.0 | 0.0 |
|  |  | 3890 | 0.0 | 0.0 | 0.0 |
|  |  | 3270 | 0.0 | 0.0 | 0.0 |
|  |  | 2750 | 0.0 | 0.0 | 0.0 |
|  |  | 2312 | 0.0 | 0.0 | 0.0 |
|  |  | 1944 | 0.0 | 0.0 | 0.0 |
|  |  | 1635 | 0.0 | 0.0 | 0.0 |
|  |  | 1375 | 0.0 | 0.0 | 0.0 |
|  |  | 1156 | 0.0 | 0.0 | 0.0 |
|  |  | 972 | 0.0 | 0.0 | 0.0 |
|  |  | 818 | 0.0 | 0.1 | 0.0 |
|  |  | 687 | 0.0 | 0.7 | 0.0 |
|  |  | 578 | 1.1 | 1.2 | 0.0 |
|  |  | 486 | 5.2 | 2.6 | 0.5 |
|  |  | 409 | 11.9 | 6.5 | 2.5 |
|  |  | 344 | 18.7 | 12.9 | 5.7 |
|  |  | 289 | 20.6 | 19.7 | 9.7 |
|  |  | 243 | 16.9 | 21.0 | 13.4 |
|  |  | 204.4 | 11.2 | 15.5 | 14.9 |
|  |  | 171.9 | 6.5 | 8.9 | 13.8 |
|  |  | 144.5 | 3.6 | 4.7 | 11.6 |
|  |  | 121.5 | 2.2 | 2.7 | 9.3 |
|  |  | 102.2 | 1.3 | 1.8 | 7.2 |
|  |  | 85.9 | 0.7 | 1.3 | 5.3 |
|  |  | 72.3 | 0.1 | 0.5 | 3.8 |
|  |  | 60.8 | 0.0 | 0.0 | 1.9 |
|  |  | 51.1 | 0.0 | 0.0 | 0.3 |
|  |  | 43 | 0.0 | 0.0 | 0.0 |
|  |  | 36.1 | 0.0 | 0.0 | 0.0 |
|  |  | 30.4 | 0.0 | 0.0 | 0.0 |
|  |  | 25.55 | 0.0 | 0.0 | 0.0 |
|  |  | 21.48 | 0.0 | 0.0 | 0.0 |
|  |  | 18.06 | 0.0 | 0.0 | 0.0 |
|  |  | 15.19 | 0.0 | 0.0 | 0.0 |
|  |  | 12.77 | 0.0 | 0.0 | 0.0 |
|  |  | 10.74 | 0.0 | 0.0 | 0.0 |
|  |  | 9.03 | 0.0 | 0.0 | 0.0 |
|  |  | 7.6 | 0.0 | 0.0 | 0.0 |
|  |  | 6.39 | 0.0 | 0.0 | 0.0 |
|  |  | 5.37 | 0.0 | 0.0 | 0.0 |
|  |  | 4.52 | 0.0 | 0.0 | 0.0 |
|  |  | 3.8 | 0.0 | 0.0 | 0.0 |
|  |  | 3.19 | 0.0 | 0.0 | 0.0 |
|  |  | 2.69 | 0.0 | 0.0 | 0.0 |
|  |  | 2.26 | 0.0 | 0.0 | 0.0 |
|  |  | 1.9 | 0.0 | 0.0 | 0.0 |
|  |  | 1.6 | 0.0 | 0.0 | 0.0 |
|  |  | 1.34 | 0.0 | 0.0 | 0.0 |
|  |  | 1.13 | 0.0 | 0.0 | 0.0 |
|  |  | 0.95 | 0.0 | 0.0 | 0.0 |
|  |  | D10 | 154.5 | 140.5 | 82.6 |
|  |  | D20 | 189.4 | 172.4 | 105.3 |
|  |  | D30 | 215.1 | 194.1 | 125.9 |
|  |  | D40 | 237.6 | 212.9 | 145.7 |
|  |  | D50 | 259.3 | 231.0 | 165.4 |
|  |  | D60 | 281.9 | 250.4 | 185.9 |
|  |  | D70 | 307.0 | 272.9 | 209.0 |
|  |  | D80 | 338.0 | 302.0 | 237.7 |
|  |  | D90 | 383.0 | 352.0 | 281.4 |
|  |  | D100 | 422.0 | 402.0 | 319.0 |
| Carbon Black | Dispersing additive concentration [%] | Particle Size | 30 min | 4 h | 24 h |
| CB1 | 100 | 6540 | 0.0 | 0.0 | 0.0 |
|  |  | 5500 | 0.0 | 0.0 | 0.0 |
|  |  | 4620 | 0.0 | 0.0 | 0.0 |
|  |  | 3890 | 0.0 | 0.0 | 0.0 |
|  |  | 3270 | 0.0 | 0.0 | 0.0 |
|  |  | 2750 | 0.0 | 0.0 | 0.0 |
|  |  | 2312 | 0.0 | 0.0 | 0.0 |
|  |  | 1944 | 0.0 | 0.0 | 0.0 |
|  |  | 1635 | 0.0 | 0.0 | 0.0 |
|  |  | 1375 | 0.0 | 0.0 | 0.0 |
|  |  | 1156 | 0.1 | 0.0 | 0.0 |
|  |  | 972 | 0.8 | 0.0 | 0.0 |
|  |  | 818 | 0.8 | 0.0 | 0.0 |
|  |  | 687 | 0.9 | 0.0 | 0.0 |
|  |  | 578 | 2.1 | 0.2 | 0.0 |
|  |  | 486 | 4.4 | 3.0 | 0.2 |
|  |  | 409 | 9.2 | 8.2 | 1.7 |
|  |  | 344 | 15.5 | 15.2 | 4.8 |
|  |  | 289 | 19.5 | 20.0 | 10.0 |
|  |  | 243 | 18.4 | 18.9 | 16.2 |
|  |  | 204.4 | 13.2 | 13.9 | 19.3 |
|  |  | 171.9 | 7.4 | 8.9 | 17.4 |
|  |  | 144.5 | 3.6 | 5.5 | 12.7 |
|  |  | 121.5 | 1.9 | 3.3 | 8.2 |
|  |  | 102.2 | 1.2 | 2.0 | 4.9 |
|  |  | 85.9 | 0.6 | 0.8 | 3.0 |
|  |  | 72.3 | 0.4 | 0.1 | 1.7 |
|  |  | 60.8 | 0.1 | 0.0 | 0.1 |
|  |  | 51.1 | 0.0 | 0.0 | 0.0 |
|  |  | 43 | 0.0 | 0.0 | 0.0 |
|  |  | 36.1 | 0.0 | 0.0 | 0.0 |
|  |  | 30.4 | 0.0 | 0.0 | 0.0 |
|  |  | 25.55 | 0.0 | 0.0 | 0.0 |
|  |  | 21.48 | 0.0 | 0.0 | 0.0 |
|  |  | 18.06 | 0.0 | 0.0 | 0.0 |
|  |  | 15.19 | 0.0 | 0.0 | 0.0 |
|  |  | 12.77 | 0.0 | 0.0 | 0.0 |
|  |  | 10.74 | 0.0 | 0.0 | 0.0 |
|  |  | 9.03 | 0.0 | 0.0 | 0.0 |
|  |  | 7.6 | 0.0 | 0.0 | 0.0 |
|  |  | 6.39 | 0.0 | 0.0 | 0.0 |
|  |  | 5.37 | 0.0 | 0.0 | 0.0 |
|  |  | 4.52 | 0.0 | 0.0 | 0.0 |
|  |  | 3.8 | 0.0 | 0.0 | 0.0 |
|  |  | 3.19 | 0.0 | 0.0 | 0.0 |
|  |  | 2.69 | 0.0 | 0.0 | 0.0 |
|  |  | 2.26 | 0.0 | 0.0 | 0.0 |
|  |  | 1.9 | 0.0 | 0.0 | 0.0 |
|  |  | 1.6 | 0.0 | 0.0 | 0.0 |
|  |  | 1.34 | 0.0 | 0.0 | 0.0 |
|  |  | 1.13 | 0.0 | 0.0 | 0.0 |
|  |  | 0.95 | 0.0 | 0.0 | 0.0 |
|  |  | D10 | 153.9 | 138.2 | 103.0 |
|  |  | D20 | 184.7 | 170.3 | 125.8 |
|  |  | D30 | 207.8 | 194.7 | 143.6 |
|  |  | D40 | 228.8 | 215.9 | 159.5 |
|  |  | D50 | 249.9 | 236.1 | 175.1 |
|  |  | D60 | 272.8 | 257.1 | 191.4 |
|  |  | D70 | 299.9 | 280.3 | 209.9 |
|  |  | D80 | 336.0 | 309.0 | 233.0 |
|  |  | D90 | 399.0 | 352.0 | 269.2 |
|  |  | D100 | 476.0 | 388.0 | 302.0 |
| Carbon Black | Dispersing additive concentration [%] | Particle Size | 30 min | 4 h | 24 h |
| CB1 | 130 | 6540 | 0.0 | 0.0 | 0.0 |
|  |  | 5500 | 0.0 | 0.0 | 0.0 |
|  |  | 4620 | 0.0 | 0.0 | 0.0 |
|  |  | 3890 | 0.0 | 0.0 | 0.0 |
|  |  | 3270 | 0.0 | 0.0 | 0.0 |
|  |  | 2750 | 0.0 | 0.0 | 0.0 |
|  |  | 2312 | 0.0 | 0.0 | 0.0 |
|  |  | 1944 | 0.0 | 0.0 | 0.0 |
|  |  | 1635 | 0.0 | 0.0 | 0.0 |
|  |  | 1375 | 0.0 | 0.0 | 0.0 |
|  |  | 1156 | 0.0 | 0.0 | 0.0 |
|  |  | 972 | 0.0 | 0.0 | 0.0 |
|  |  | 818 | 0.0 | 0.0 | 0.0 |
|  |  | 687 | 0.7 | 0.3 | 0.0 |
|  |  | 578 | 2.2 | 1.1 | 0.0 |
|  |  | 486 | 5.4 | 3.6 | 0.2 |
|  |  | 409 | 9.6 | 8.8 | 2.2 |
|  |  | 344 | 14.4 | 16.3 | 6.0 |
|  |  | 289 | 17.6 | 21.5 | 12.3 |
|  |  | 243 | 17.9 | 19.5 | 19.4 |
|  |  | 204.4 | 14.9 | 13.3 | 21.2 |
|  |  | 171.9 | 9.7 | 7.7 | 15.9 |
|  |  | 144.5 | 4.8 | 4.1 | 9.6 |
|  |  | 121.5 | 2.0 | 2.1 | 5.6 |
|  |  | 102.2 | 0.7 | 1.3 | 3.5 |
|  |  | 85.9 | 0.0 | 0.5 | 2.1 |
|  |  | 72.3 | 0.0 | 0.0 | 1.5 |
|  |  | 60.8 | 0.0 | 0.0 | 0.4 |
|  |  | 51.1 | 0.0 | 0.0 | 0.0 |
|  |  | 43 | 0.0 | 0.0 | 0.0 |
|  |  | 36.1 | 0.0 | 0.0 | 0.0 |
|  |  | 30.4 | 0.0 | 0.0 | 0.0 |
|  |  | 25.55 | 0.0 | 0.0 | 0.0 |
|  |  | 21.48 | 0.0 | 0.0 | 0.0 |
|  |  | 18.06 | 0.0 | 0.0 | 0.0 |
|  |  | 15.19 | 0.0 | 0.0 | 0.0 |
|  |  | 12.77 | 0.0 | 0.0 | 0.0 |
|  |  | 10.74 | 0.0 | 0.0 | 0.0 |
|  |  | 9.03 | 0.0 | 0.0 | 0.0 |
|  |  | 7.6 | 0.0 | 0.0 | 0.0 |
|  |  | 6.39 | 0.0 | 0.0 | 0.0 |
|  |  | 5.37 | 0.0 | 0.0 | 0.0 |
|  |  | 4.52 | 0.0 | 0.0 | 0.0 |
|  |  | 3.8 | 0.0 | 0.0 | 0.0 |
|  |  | 3.19 | 0.0 | 0.0 | 0.0 |
|  |  | 2.69 | 0.0 | 0.0 | 0.0 |
|  |  | 2.26 | 0.0 | 0.0 | 0.0 |
|  |  | 1.9 | 0.0 | 0.0 | 0.0 |
|  |  | 1.6 | 0.0 | 0.0 | 0.0 |
|  |  | 1.34 | 0.0 | 0.0 | 0.0 |
|  |  | 1.13 | 0.0 | 0.0 | 0.0 |
|  |  | 0.95 | 0.0 | 0.0 | 0.0 |
|  |  | D10 | 152.6 | 153.0 | 111.6 |
|  |  | D20 | 178.4 | 183.6 | 138.7 |
|  |  | D30 | 200.0 | 206.5 | 157.8 |
|  |  | D40 | 221.1 | 226.6 | 173.9 |
|  |  | D50 | 243.1 | 246.1 | 188.9 |
|  |  | D60 | 267.7 | 266.4 | 204.7 |
|  |  | D70 | 296.8 | 289.3 | 222.6 |
|  |  | D80 | 335.0 | 319.0 | 245.1 |
|  |  | D90 | 394.0 | 365.0 | 281.1 |
|  |  | D100 | 449.0 | 409.0 | 314.0 |
| Carbon Black | Dispersing additive concentration [%] | Particle Size | 30 min | 4 h | 24 h |
| CB4 | 70 | 6540 | 0.0 | 0.0 | 0.0 |
|  |  | 5500 | 0.0 | 0.0 | 0.0 |
|  |  | 4620 | 0.0 | 0.0 | 0.0 |
|  |  | 3890 | 0.0 | 0.0 | 0.0 |
|  |  | 3270 | 0.0 | 0.0 | 0.0 |
|  |  | 2750 | 0.0 | 0.0 | 0.0 |
|  |  | 2312 | 0.0 | 0.0 | 0.0 |
|  |  | 1944 | 0.0 | 0.0 | 0.0 |
|  |  | 1635 | 0.0 | 0.0 | 0.0 |
|  |  | 1375 | 0.0 | 0.0 | 0.0 |
|  |  | 1156 | 0.0 | 0.0 | 0.0 |
|  |  | 972 | 0.0 | 0.0 | 0.0 |
|  |  | 818 | 0.0 | 0.0 | 0.0 |
|  |  | 687 | 0.0 | 0.0 | 0.0 |
|  |  | 578 | 0.0 | 0.0 | 0.3 |
|  |  | 486 | 0.0 | 0.1 | 0.4 |
|  |  | 409 | 0.2 | 0.3 | 0.6 |
|  |  | 344 | 0.3 | 0.4 | 0.6 |
|  |  | 289 | 0.8 | 0.7 | 0.7 |
|  |  | 243 | 1.6 | 1.0 | 0.8 |
|  |  | 204.4 | 3.5 | 1.5 | 0.9 |
|  |  | 171.9 | 6.3 | 2.3 | 1.3 |
|  |  | 144.5 | 9.0 | 3.4 | 1.8 |
|  |  | 121.5 | 10.7 | 4.9 | 2.7 |
|  |  | 102.2 | 11.8 | 7.3 | 3.9 |
|  |  | 85.9 | 12.4 | 10.1 | 5.6 |
|  |  | 72.3 | 12.2 | 12.6 | 7.8 |
|  |  | 60.8 | 11.0 | 13.9 | 10.3 |
|  |  | 51.1 | 9.3 | 13.3 | 12.2 |
|  |  | 43 | 7.4 | 11.5 | 13.0 |
|  |  | 36.1 | 3.5 | 9.6 | 12.8 |
|  |  | 30.4 | 0.1 | 6.4 | 12.1 |
|  |  | 25.55 | 0.0 | 0.7 | 10.0 |
|  |  | 21.48 | 0.0 | 0.0 | 2.3 |
|  |  | 18.06 | 0.0 | 0.0 | 0.1 |
|  |  | 15.19 | 0.0 | 0.0 | 0.0 |
|  |  | 12.77 | 0.0 | 0.0 | 0.0 |
|  |  | 10.74 | 0.0 | 0.0 | 0.0 |
|  |  | 9.03 | 0.0 | 0.0 | 0.0 |
|  |  | 7.6 | 0.0 | 0.0 | 0.0 |
|  |  | 6.39 | 0.0 | 0.0 | 0.0 |
|  |  | 5.37 | 0.0 | 0.0 | 0.0 |
|  |  | 4.52 | 0.0 | 0.0 | 0.0 |
|  |  | 3.8 | 0.0 | 0.0 | 0.0 |
|  |  | 3.19 | 0.0 | 0.0 | 0.0 |
|  |  | 2.69 | 0.0 | 0.0 | 0.0 |
|  |  | 2.26 | 0.0 | 0.0 | 0.0 |
|  |  | 1.9 | 0.0 | 0.0 | 0.0 |
|  |  | 1.6 | 0.0 | 0.0 | 0.0 |
|  |  | 1.34 | 0.0 | 0.0 | 0.0 |
|  |  | 1.13 | 0.0 | 0.0 | 0.0 |
|  |  | 0.95 | 0.0 | 0.0 | 0.0 |
|  |  | D10 | 42.1 | 32.1 | 24.7 |
|  |  | D20 | 50.8 | 38.0 | 28.5 |
|  |  | D30 | 59.6 | 44.0 | 32.7 |
|  |  | D40 | 68.8 | 50.1 | 37.4 |
|  |  | D50 | 79.1 | 56.8 | 42.8 |
|  |  | D60 | 91.2 | 64.6 | 49.2 |
|  |  | D70 | 106.0 | 74.6 | 57.8 |
|  |  | D80 | 125.1 | 89.5 | 71.2 |
|  |  | D90 | 154.1 | 120.3 | 101.9 |
|  |  | D100 | 181.4 | 159.2 | 153.9 |
| Carbon Black | Dispersing additive concentration [%] | Particle Size | 30 min | 4 h | 24 h |
| CB4 | 100 | 6540 | 0.0 | 0.0 | 0.0 |
|  |  | 5500 | 0.0 | 0.0 | 0.0 |
|  |  | 4620 | 0.0 | 0.0 | 0.0 |
|  |  | 3890 | 0.0 | 0.0 | 0.0 |
|  |  | 3270 | 0.0 | 0.0 | 0.0 |
|  |  | 2750 | 0.0 | 0.0 | 0.0 |
|  |  | 2312 | 0.0 | 0.0 | 0.0 |
|  |  | 1944 | 0.0 | 0.0 | 0.0 |
|  |  | 1635 | 0.0 | 0.0 | 0.0 |
|  |  | 1375 | 0.0 | 0.0 | 0.0 |
|  |  | 1156 | 0.0 | 0.0 | 0.0 |
|  |  | 972 | 0.0 | 0.0 | 0.0 |
|  |  | 818 | 0.0 | 0.0 | 0.0 |
|  |  | 687 | 0.0 | 0.0 | 0.0 |
|  |  | 578 | 0.0 | 0.0 | 0.0 |
|  |  | 486 | 0.0 | 0.0 | 0.2 |
|  |  | 409 | 0.1 | 0.0 | 0.3 |
|  |  | 344 | 0.2 | 0.2 | 0.4 |
|  |  | 289 | 0.7 | 0.4 | 0.5 |
|  |  | 243 | 1.2 | 0.5 | 0.6 |
|  |  | 204.4 | 2.0 | 0.8 | 0.7 |
|  |  | 171.9 | 3.3 | 1.2 | 0.9 |
|  |  | 144.5 | 5.8 | 2.1 | 1.3 |
|  |  | 121.5 | 9.6 | 3.6 | 2.1 |
|  |  | 102.2 | 13.7 | 6.0 | 3.5 |
|  |  | 85.9 | 16.1 | 9.3 | 5.7 |
|  |  | 72.3 | 15.6 | 12.5 | 8.8 |
|  |  | 60.8 | 12.9 | 14.8 | 12.4 |
|  |  | 51.1 | 9.7 | 15.1 | 15.0 |
|  |  | 43 | 7.2 | 13.4 | 15.5 |
|  |  | 36.1 | 2.1 | 10.9 | 13.7 |
|  |  | 30.4 | 0.0 | 7.6 | 11.1 |
|  |  | 25.55 | 0.0 | 1.7 | 6.9 |
|  |  | 21.48 | 0.0 | 0.0 | 0.4 |
|  |  | 18.06 | 0.0 | 0.0 | 0.0 |
|  |  | 15.19 | 0.0 | 0.0 | 0.0 |
|  |  | 12.77 | 0.0 | 0.0 | 0.0 |
|  |  | 10.74 | 0.0 | 0.0 | 0.0 |
|  |  | 9.03 | 0.0 | 0.0 | 0.0 |
|  |  | 7.6 | 0.0 | 0.0 | 0.0 |
|  |  | 6.39 | 0.0 | 0.0 | 0.0 |
|  |  | 5.37 | 0.0 | 0.0 | 0.0 |
|  |  | 4.52 | 0.0 | 0.0 | 0.0 |
|  |  | 3.8 | 0.0 | 0.0 | 0.0 |
|  |  | 3.19 | 0.0 | 0.0 | 0.0 |
|  |  | 2.69 | 0.0 | 0.0 | 0.0 |
|  |  | 2.26 | 0.0 | 0.0 | 0.0 |
|  |  | 1.9 | 0.0 | 0.0 | 0.0 |
|  |  | 1.6 | 0.0 | 0.0 | 0.0 |
|  |  | 1.34 | 0.0 | 0.0 | 0.0 |
|  |  | 1.13 | 0.0 | 0.0 | 0.0 |
|  |  | 0.95 | 0.0 | 0.0 | 0.0 |
|  |  | D10 | 43.7 | 30.7 | 26.8 |
|  |  | D20 | 52.0 | 36.0 | 31.0 |
|  |  | D30 | 59.5 | 41.1 | 35.2 |
|  |  | D40 | 66.7 | 46.3 | 39.5 |
|  |  | D50 | 74.3 | 51.9 | 44.1 |
|  |  | D60 | 82.6 | 58.3 | 49.4 |
|  |  | D70 | 92.8 | 66.2 | 56.3 |
|  |  | D80 | 106.7 | 77.4 | 66.5 |
|  |  | D90 | 132.3 | 97.7 | 87.8 |
|  |  | D100 | 162.2 | 122.4 | 120.9 |
| Carbon Black | Dispersing additive concentration [%] | Particle Size | 30 min | 4 h | 24 h |
| CB4 | 130 | 6540 | 0.0 | 0.0 | 0.0 |
|  |  | 5500 | 0.0 | 0.0 | 0.0 |
|  |  | 4620 | 0.0 | 0.0 | 0.0 |
|  |  | 3890 | 0.0 | 0.0 | 0.0 |
|  |  | 3270 | 0.0 | 0.0 | 0.0 |
|  |  | 2750 | 0.0 | 0.0 | 0.0 |
|  |  | 2312 | 0.0 | 0.0 | 0.0 |
|  |  | 1944 | 0.0 | 0.0 | 0.0 |
|  |  | 1635 | 0.0 | 0.0 | 0.0 |
|  |  | 1375 | 0.0 | 0.0 | 0.0 |
|  |  | 1156 | 0.0 | 0.0 | 0.0 |
|  |  | 972 | 0.0 | 0.0 | 0.0 |
|  |  | 818 | 0.0 | 0.0 | 0.0 |
|  |  | 687 | 0.0 | 0.0 | 0.2 |
|  |  | 578 | 0.0 | 0.0 | 0.2 |
|  |  | 486 | 0.0 | 0.1 | 0.4 |
|  |  | 409 | 0.0 | 0.3 | 0.5 |
|  |  | 344 | 0.1 | 0.4 | 0.5 |
|  |  | 289 | 0.4 | 0.6 | 0.5 |
|  |  | 243 | 0.9 | 0.7 | 0.6 |
|  |  | 204.4 | 1.6 | 1.0 | 0.8 |
|  |  | 171.9 | 3.0 | 1.5 | 1.3 |
|  |  | 144.5 | 5.3 | 2.5 | 2.0 |
|  |  | 121.5 | 8.9 | 4.5 | 3.0 |
|  |  | 102.2 | 13.3 | 7.8 | 4.6 |
|  |  | 85.9 | 16.8 | 11.8 | 6.9 |
|  |  | 72.3 | 17.2 | 15.1 | 9.9 |
|  |  | 60.8 | 14.3 | 15.9 | 13.0 |
|  |  | 51.1 | 10.2 | 14.0 | 15.0 |
|  |  | 43 | 6.8 | 11.1 | 14.7 |
|  |  | 36.1 | 1.3 | 8.6 | 12.4 |
|  |  | 30.4 | 0.0 | 4.1 | 10.0 |
|  |  | 25.55 | 0.0 | 0.1 | 3.7 |
|  |  | 21.48 | 0.0 | 0.0 | 0.0 |
|  |  | 18.06 | 0.0 | 0.0 | 0.0 |
|  |  | 15.19 | 0.0 | 0.0 | 0.0 |
|  |  | 12.77 | 0.0 | 0.0 | 0.0 |
|  |  | 10.74 | 0.0 | 0.0 | 0.0 |
|  |  | 9.03 | 0.0 | 0.0 | 0.0 |
|  |  | 7.6 | 0.0 | 0.0 | 0.0 |
|  |  | 6.39 | 0.0 | 0.0 | 0.0 |
|  |  | 5.37 | 0.0 | 0.0 | 0.0 |
|  |  | 4.52 | 0.0 | 0.0 | 0.0 |
|  |  | 3.8 | 0.0 | 0.0 | 0.0 |
|  |  | 3.19 | 0.0 | 0.0 | 0.0 |
|  |  | 2.69 | 0.0 | 0.0 | 0.0 |
|  |  | 2.26 | 0.0 | 0.0 | 0.0 |
|  |  | 1.9 | 0.0 | 0.0 | 0.0 |
|  |  | 1.6 | 0.0 | 0.0 | 0.0 |
|  |  | 1.34 | 0.0 | 0.0 | 0.0 |
|  |  | 1.13 | 0.0 | 0.0 | 0.0 |
|  |  | 0.95 | 0.0 | 0.0 | 0.0 |
|  |  | D10 | 44.6 | 34.4 | 28.8 |
|  |  | D20 | 52.3 | 40.6 | 33.3 |
|  |  | D30 | 59.1 | 46.6 | 37.9 |
|  |  | D40 | 65.7 | 52.4 | 42.6 |
|  |  | D50 | 72.5 | 58.4 | 47.8 |
|  |  | D60 | 80.1 | 65.1 | 54.0 |
|  |  | D70 | 89.4 | 73.4 | 62.1 |
|  |  | D80 | 102.4 | 84.9 | 74.5 |
|  |  | D90 | 125.7 | 107.2 | 101.5 |
|  |  | D100 | 151.4 | 138.3 | 142.6 |
| Carbon Black | Dispersing additive concentration [%] | Particle Size | 30 min | 4 h | 24 h |
| CB5 | 70 | 6540 | 0.0 | 0.0 | 0.0 |
|  |  | 5500 | 0.0 | 0.0 | 0.0 |
|  |  | 4620 | 0.0 | 0.0 | 0.0 |
|  |  | 3890 | 0.0 | 0.0 | 0.0 |
|  |  | 3270 | 0.0 | 0.0 | 0.0 |
|  |  | 2750 | 0.0 | 0.0 | 0.0 |
|  |  | 2312 | 0.0 | 0.0 | 0.0 |
|  |  | 1944 | 0.0 | 0.0 | 0.0 |
|  |  | 1635 | 0.0 | 0.0 | 0.0 |
|  |  | 1375 | 0.0 | 0.0 | 0.0 |
|  |  | 1156 | 0.0 | 0.0 | 0.0 |
|  |  | 972 | 0.0 | 0.0 | 0.0 |
|  |  | 818 | 0.0 | 0.0 | 0.0 |
|  |  | 687 | 0.0 | 0.0 | 0.1 |
|  |  | 578 | 0.0 | 0.2 | 0.2 |
|  |  | 486 | 0.0 | 0.3 | 0.2 |
|  |  | 409 | 0.1 | 0.4 | 0.3 |
|  |  | 344 | 0.3 | 0.4 | 0.3 |
|  |  | 289 | 0.7 | 0.4 | 0.4 |
|  |  | 243 | 1.1 | 0.5 | 0.5 |
|  |  | 204.4 | 1.8 | 0.7 | 0.6 |
|  |  | 171.9 | 3.0 | 1.2 | 0.9 |
|  |  | 144.5 | 4.5 | 2.0 | 1.4 |
|  |  | 121.5 | 6.1 | 3.2 | 2.2 |
|  |  | 102.2 | 7.8 | 5.2 | 3.5 |
|  |  | 85.9 | 9.7 | 7.8 | 5.3 |
|  |  | 72.3 | 11.8 | 10.5 | 8.0 |
|  |  | 60.8 | 13.4 | 12.5 | 11.4 |
|  |  | 51.1 | 13.4 | 13.4 | 14.3 |
|  |  | 43 | 11.8 | 13.2 | 15.4 |
|  |  | 36.1 | 9.6 | 12.1 | 14.4 |
|  |  | 30.4 | 4.7 | 10.7 | 12.0 |
|  |  | 25.55 | 0.2 | 5.3 | 8.1 |
|  |  | 21.48 | 0.0 | 0.1 | 0.6 |
|  |  | 18.06 | 0.0 | 0.0 | 0.0 |
|  |  | 15.19 | 0.0 | 0.0 | 0.0 |
|  |  | 12.77 | 0.0 | 0.0 | 0.0 |
|  |  | 10.74 | 0.0 | 0.0 | 0.0 |
|  |  | 9.03 | 0.0 | 0.0 | 0.0 |
|  |  | 7.6 | 0.0 | 0.0 | 0.0 |
|  |  | 6.39 | 0.0 | 0.0 | 0.0 |
|  |  | 5.37 | 0.0 | 0.0 | 0.0 |
|  |  | 4.52 | 0.0 | 0.0 | 0.0 |
|  |  | 3.8 | 0.0 | 0.0 | 0.0 |
|  |  | 3.19 | 0.0 | 0.0 | 0.0 |
|  |  | 2.69 | 0.0 | 0.0 | 0.0 |
|  |  | 2.26 | 0.0 | 0.0 | 0.0 |
|  |  | 1.9 | 0.0 | 0.0 | 0.0 |
|  |  | 1.6 | 0.0 | 0.0 | 0.0 |
|  |  | 1.34 | 0.0 | 0.0 | 0.0 |
|  |  | 1.13 | 0.0 | 0.0 | 0.0 |
|  |  | 0.95 | 0.0 | 0.0 | 0.0 |
|  |  | D10 | 33.5 | 27.7 | 26.1 |
|  |  | D20 | 39.3 | 32.2 | 30.1 |
|  |  | D30 | 45.2 | 37.0 | 34.1 |
|  |  | D40 | 51.3 | 42.2 | 38.2 |
|  |  | D50 | 58.3 | 48.0 | 42.8 |
|  |  | D60 | 67.0 | 54.8 | 48.1 |
|  |  | D70 | 78.7 | 63.4 | 55.0 |
|  |  | D80 | 96.4 | 75.6 | 65.6 |
|  |  | D90 | 127.8 | 99.1 | 87.8 |
|  |  | D100 | 160.5 | 131.2 | 119.7 |
| Carbon Black | Dispersing additive concentration [%] | Particle Size | 30 min | 4 h | 24 h |
| CB5 | 100 | 6540 | 0.0 | 0.0 | 0.0 |
|  |  | 5500 | 0.0 | 0.0 | 0.0 |
|  |  | 4620 | 0.0 | 0.0 | 0.0 |
|  |  | 3890 | 0.0 | 0.0 | 0.0 |
|  |  | 3270 | 0.0 | 0.0 | 0.0 |
|  |  | 2750 | 0.0 | 0.0 | 0.0 |
|  |  | 2312 | 0.0 | 0.0 | 0.0 |
|  |  | 1944 | 0.0 | 0.0 | 0.0 |
|  |  | 1635 | 0.0 | 0.0 | 0.0 |
|  |  | 1375 | 0.0 | 0.0 | 0.0 |
|  |  | 1156 | 0.0 | 0.0 | 0.0 |
|  |  | 972 | 0.0 | 0.0 | 0.0 |
|  |  | 818 | 0.0 | 0.0 | 0.0 |
|  |  | 687 | 0.0 | 0.0 | 0.0 |
|  |  | 578 | 0.0 | 0.0 | 0.0 |
|  |  | 486 | 0.1 | 0.3 | 0.1 |
|  |  | 409 | 0.2 | 0.6 | 0.2 |
|  |  | 344 | 0.3 | 0.8 | 0.4 |
|  |  | 289 | 0.5 | 0.9 | 0.5 |
|  |  | 243 | 0.7 | 0.9 | 0.7 |
|  |  | 204.4 | 1.2 | 1.1 | 0.8 |
|  |  | 171.9 | 2.0 | 1.4 | 1.0 |
|  |  | 144.5 | 3.4 | 2.1 | 1.3 |
|  |  | 121.5 | 5.6 | 3.2 | 1.9 |
|  |  | 102.2 | 8.7 | 5.0 | 3.0 |
|  |  | 85.9 | 12.1 | 8.1 | 5.3 |
|  |  | 72.3 | 14.6 | 12.1 | 8.8 |
|  |  | 60.8 | 15.2 | 15.3 | 12.8 |
|  |  | 51.1 | 13.7 | 15.7 | 15.6 |
|  |  | 43 | 11.1 | 13.6 | 15.8 |
|  |  | 36.1 | 8.3 | 10.7 | 13.8 |
|  |  | 30.4 | 2.5 | 7.1 | 11.1 |
|  |  | 25.55 | 0.0 | 1.3 | 6.7 |
|  |  | 21.48 | 0.0 | 0.0 | 0.2 |
|  |  | 18.06 | 0.0 | 0.0 | 0.0 |
|  |  | 15.19 | 0.0 | 0.0 | 0.0 |
|  |  | 12.77 | 0.0 | 0.0 | 0.0 |
|  |  | 10.74 | 0.0 | 0.0 | 0.0 |
|  |  | 9.03 | 0.0 | 0.0 | 0.0 |
|  |  | 7.6 | 0.0 | 0.0 | 0.0 |
|  |  | 6.39 | 0.0 | 0.0 | 0.0 |
|  |  | 5.37 | 0.0 | 0.0 | 0.0 |
|  |  | 4.52 | 0.0 | 0.0 | 0.0 |
|  |  | 3.8 | 0.0 | 0.0 | 0.0 |
|  |  | 3.19 | 0.0 | 0.0 | 0.0 |
|  |  | 2.69 | 0.0 | 0.0 | 0.0 |
|  |  | 2.26 | 0.0 | 0.0 | 0.0 |
|  |  | 1.9 | 0.0 | 0.0 | 0.0 |
|  |  | 1.6 | 0.0 | 0.0 | 0.0 |
|  |  | 1.34 | 0.0 | 0.0 | 0.0 |
|  |  | 1.13 | 0.0 | 0.0 | 0.0 |
|  |  | 0.95 | 0.0 | 0.0 | 0.0 |
|  |  | D10 | 35.6 | 31.3 | 27.0 |
|  |  | D20 | 41.8 | 36.6 | 31.2 |
|  |  | D30 | 47.8 | 41.6 | 35.4 |
|  |  | D40 | 53.8 | 46.7 | 39.6 |
|  |  | D50 | 60.3 | 52.0 | 44.2 |
|  |  | D60 | 67.7 | 58.1 | 49.2 |
|  |  | D70 | 76.9 | 66.1 | 55.7 |
|  |  | D80 | 89.7 | 78.4 | 65.3 |
|  |  | D90 | 114.1 | 107.6 | 86.0 |
|  |  | D100 | 143.5 | 159.6 | 123.3 |
| Carbon Black | Dispersing additive concentration [%] | Particle Size | 30 min | 4 h | 24 h |
| CB5 | 130 | 6540 | 0.0 | 0.0 | 29.4 |
|  |  | 5500 | 0.0 | 0.0 | 33.9 |
|  |  | 4620 | 0.0 | 0.0 | 38.3 |
|  |  | 3890 | 0.0 | 0.0 | 42.8 |
|  |  | 3270 | 0.0 | 0.0 | 47.5 |
|  |  | 2750 | 0.0 | 0.0 | 52.9 |
|  |  | 2312 | 0.0 | 0.0 | 59.7 |
|  |  | 1944 | 0.0 | 0.0 | 69.6 |
|  |  | 1635 | 0.0 | 0.0 | 90.9 |
|  |  | 1375 | 0.0 | 0.0 | 130.7 |
|  |  | 1156 | 0.0 | 0.0 | 29.4 |
|  |  | 972 | 0.0 | 0.0 | 33.9 |
|  |  | 818 | 0.0 | 0.0 | 38.3 |
|  |  | 687 | 0.0 | 0.0 | 42.8 |
|  |  | 578 | 0.0 | 0.2 | 47.5 |
|  |  | 486 | 0.0 | 0.2 | 52.9 |
|  |  | 409 | 0.0 | 0.3 | 59.7 |
|  |  | 344 | 0.3 | 0.3 | 69.6 |
|  |  | 289 | 0.4 | 0.5 | 90.9 |
|  |  | 243 | 0.6 | 0.6 | 130.7 |
|  |  | 204.4 | 0.9 | 0.8 | 29.4 |
|  |  | 171.9 | 1.6 | 1.3 | 33.9 |
|  |  | 144.5 | 2.9 | 2.1 | 38.3 |
|  |  | 121.5 | 5.3 | 3.5 | 42.8 |
|  |  | 102.2 | 8.9 | 5.9 | 47.5 |
|  |  | 85.9 | 12.8 | 9.1 | 52.9 |
|  |  | 72.3 | 15.2 | 12.3 | 59.7 |
|  |  | 60.8 | 15.1 | 14.4 | 69.6 |
|  |  | 51.1 | 13.2 | 14.6 | 90.9 |
|  |  | 43 | 10.7 | 13.2 | 130.7 |
|  |  | 36.1 | 8.4 | 11.0 | 29.4 |
|  |  | 30.4 | 3.6 | 8.3 | 33.9 |
|  |  | 25.55 | 0.3 | 1.5 | 38.3 |
|  |  | 21.48 | 0.0 | 0.0 | 42.8 |
|  |  | 18.06 | 0.0 | 0.0 | 47.5 |
|  |  | 15.19 | 0.0 | 0.0 | 52.9 |
|  |  | 12.77 | 0.0 | 0.0 | 59.7 |
|  |  | 10.74 | 0.0 | 0.0 | 69.6 |
|  |  | 9.03 | 0.0 | 0.0 | 90.9 |
|  |  | 7.6 | 0.0 | 0.0 | 130.7 |
|  |  | 6.39 | 0.0 | 0.0 | 29.4 |
|  |  | 5.37 | 0.0 | 0.0 | 33.9 |
|  |  | 4.52 | 0.0 | 0.0 | 38.3 |
|  |  | 3.8 | 0.0 | 0.0 | 42.8 |
|  |  | 3.19 | 0.0 | 0.0 | 47.5 |
|  |  | 2.69 | 0.0 | 0.0 | 52.9 |
|  |  | 2.26 | 0.0 | 0.0 | 59.7 |
|  |  | 1.9 | 0.0 | 0.0 | 69.6 |
|  |  | 1.6 | 0.0 | 0.0 | 90.9 |
|  |  | 1.34 | 0.0 | 0.0 | 130.7 |
|  |  | 1.13 | 0.0 | 0.0 | 29.4 |
|  |  | 0.95 | 0.0 | 0.0 | 33.9 |
|  |  | D10 | 34.7 | 30.5 | 29.4 |
|  |  | D20 | 41.1 | 35.7 | 33.9 |
|  |  | D30 | 47.3 | 40.8 | 38.3 |
|  |  | D40 | 53.5 | 46.3 | 42.8 |
|  |  | D50 | 60.0 | 52.0 | 47.5 |
|  |  | D60 | 67.1 | 58.6 | 52.9 |
|  |  | D70 | 75.6 | 66.8 | 59.7 |
|  |  | D80 | 87.1 | 78.4 | 69.6 |
|  |  | D90 | 107.9 | 101.2 | 90.9 |
|  |  | D100 | 132.9 | 132.9 | 130.7 |

Table 10: spectral data to figure 2b

| Carbon Black | Dispersing additive concentration [%] | Wavelength [nm] | 30 min | 4 h | 24 h |
| --- | --- | --- | --- | --- | --- |
| CB1 | 70 | 400 | 0.562 | 0.615 | 0.531 |
|  |  | 410 | 0.553 | 0.605 | 0.519 |
|  |  | 420 | 0.548 | 0.602 | 0.511 |
|  |  | 430 | 0.567 | 0.623 | 0.525 |
|  |  | 440 | 0.569 | 0.625 | 0.522 |
|  |  | 450 | 0.572 | 0.624 | 0.519 |
|  |  | 460 | 0.576 | 0.628 | 0.518 |
|  |  | 470 | 0.582 | 0.636 | 0.517 |
|  |  | 480 | 0.579 | 0.632 | 0.509 |
|  |  | 490 | 0.590 | 0.643 | 0.513 |
|  |  | 500 | 0.602 | 0.654 | 0.517 |
|  |  | 510 | 0.602 | 0.653 | 0.511 |
|  |  | 520 | 0.608 | 0.658 | 0.510 |
|  |  | 530 | 0.622 | 0.671 | 0.516 |
|  |  | 540 | 0.626 | 0.674 | 0.514 |
|  |  | 550 | 0.634 | 0.680 | 0.511 |
|  |  | 560 | 0.642 | 0.687 | 0.511 |
|  |  | 570 | 0.634 | 0.678 | 0.498 |
|  |  | 580 | 0.657 | 0.702 | 0.508 |
|  |  | 590 | 0.653 | 0.696 | 0.496 |
|  |  | 600 | 0.664 | 0.704 | 0.497 |
|  |  | 610 | 0.677 | 0.715 | 0.501 |
|  |  | 620 | 0.682 | 0.719 | 0.499 |
|  |  | 630 | 0.681 | 0.714 | 0.492 |
|  |  | 640 | 0.692 | 0.724 | 0.495 |
|  |  | 650 | 0.688 | 0.717 | 0.487 |
|  |  | 660 | 0.697 | 0.722 | 0.486 |
|  |  | 670 | 0.708 | 0.731 | 0.488 |
|  |  | 680 | 0.710 | 0.730 | 0.482 |
|  |  | 690 | 0.705 | 0.724 | 0.473 |
|  |  | 700 | 0.720 | 0.737 | 0.477 |
| Carbon Black | Dispersing additive concentration [%] | Wavelength [nm] | 30 min | 4 h | 24 h |
| CB1 | 100 | 400 | 0.562 | 0.611 | 0.601 |
|  |  | 410 | 0.553 | 0.602 | 0.589 |
|  |  | 420 | 0.549 | 0.599 | 0.582 |
|  |  | 430 | 0.568 | 0.620 | 0.600 |
|  |  | 440 | 0.570 | 0.622 | 0.599 |
|  |  | 450 | 0.572 | 0.622 | 0.596 |
|  |  | 460 | 0.576 | 0.626 | 0.595 |
|  |  | 470 | 0.582 | 0.633 | 0.598 |
|  |  | 480 | 0.579 | 0.630 | 0.590 |
|  |  | 490 | 0.590 | 0.641 | 0.596 |
|  |  | 500 | 0.602 | 0.652 | 0.602 |
|  |  | 510 | 0.602 | 0.652 | 0.597 |
|  |  | 520 | 0.607 | 0.656 | 0.597 |
|  |  | 530 | 0.621 | 0.670 | 0.606 |
|  |  | 540 | 0.625 | 0.672 | 0.605 |
|  |  | 550 | 0.632 | 0.679 | 0.604 |
|  |  | 560 | 0.640 | 0.685 | 0.605 |
|  |  | 570 | 0.632 | 0.677 | 0.591 |
|  |  | 580 | 0.655 | 0.700 | 0.604 |
|  |  | 590 | 0.651 | 0.694 | 0.592 |
|  |  | 600 | 0.661 | 0.702 | 0.594 |
|  |  | 610 | 0.674 | 0.713 | 0.600 |
|  |  | 620 | 0.679 | 0.716 | 0.600 |
|  |  | 630 | 0.677 | 0.712 | 0.592 |
|  |  | 640 | 0.689 | 0.721 | 0.597 |
|  |  | 650 | 0.685 | 0.714 | 0.588 |
|  |  | 660 | 0.693 | 0.719 | 0.589 |
|  |  | 670 | 0.705 | 0.728 | 0.592 |
|  |  | 680 | 0.706 | 0.727 | 0.587 |
|  |  | 690 | 0.701 | 0.720 | 0.577 |
|  |  | 700 | 0.717 | 0.733 | 0.584 |
| Carbon Black | Dispersing additive concentration [%] | Wavelength [nm] | 30 min | 4 h | 24 h |
| CB1 | 130 | 400 | 0.557 | 0.606 | 0.630 |
|  |  | 410 | 0.547 | 0.596 | 0.620 |
|  |  | 420 | 0.543 | 0.593 | 0.614 |
|  |  | 430 | 0.562 | 0.614 | 0.635 |
|  |  | 440 | 0.564 | 0.617 | 0.634 |
|  |  | 450 | 0.566 | 0.617 | 0.631 |
|  |  | 460 | 0.570 | 0.620 | 0.632 |
|  |  | 470 | 0.576 | 0.628 | 0.637 |
|  |  | 480 | 0.573 | 0.624 | 0.629 |
|  |  | 490 | 0.584 | 0.635 | 0.637 |
|  |  | 500 | 0.595 | 0.647 | 0.645 |
|  |  | 510 | 0.596 | 0.646 | 0.641 |
|  |  | 520 | 0.601 | 0.651 | 0.642 |
|  |  | 530 | 0.615 | 0.664 | 0.651 |
|  |  | 540 | 0.619 | 0.666 | 0.650 |
|  |  | 550 | 0.626 | 0.673 | 0.653 |
|  |  | 560 | 0.634 | 0.679 | 0.655 |
|  |  | 570 | 0.626 | 0.670 | 0.641 |
|  |  | 580 | 0.648 | 0.694 | 0.659 |
|  |  | 590 | 0.644 | 0.688 | 0.649 |
|  |  | 600 | 0.655 | 0.697 | 0.653 |
|  |  | 610 | 0.667 | 0.707 | 0.659 |
|  |  | 620 | 0.673 | 0.711 | 0.658 |
|  |  | 630 | 0.671 | 0.707 | 0.649 |
|  |  | 640 | 0.683 | 0.717 | 0.656 |
|  |  | 650 | 0.679 | 0.710 | 0.647 |
|  |  | 660 | 0.688 | 0.715 | 0.649 |
|  |  | 670 | 0.699 | 0.725 | 0.655 |
|  |  | 680 | 0.701 | 0.724 | 0.649 |
|  |  | 690 | 0.697 | 0.718 | 0.640 |
|  |  | 700 | 0.712 | 0.731 | 0.648 |
| Carbon Black | Dispersing additive concentration [%] | Wavelength [nm] | 30 min | 4 h | 24 h |
| CB4 | 70 | 400 | 0.150 | 0.116 | 0.094 |
|  |  | 410 | 0.143 | 0.110 | 0.089 |
|  |  | 420 | 0.134 | 0.103 | 0.083 |
|  |  | 430 | 0.134 | 0.102 | 0.082 |
|  |  | 440 | 0.129 | 0.098 | 0.080 |
|  |  | 450 | 0.125 | 0.095 | 0.077 |
|  |  | 460 | 0.121 | 0.092 | 0.074 |
|  |  | 470 | 0.117 | 0.089 | 0.072 |
|  |  | 480 | 0.112 | 0.085 | 0.068 |
|  |  | 490 | 0.110 | 0.083 | 0.067 |
|  |  | 500 | 0.108 | 0.081 | 0.065 |
|  |  | 510 | 0.103 | 0.077 | 0.062 |
|  |  | 520 | 0.100 | 0.075 | 0.061 |
|  |  | 530 | 0.099 | 0.074 | 0.060 |
|  |  | 540 | 0.097 | 0.072 | 0.058 |
|  |  | 550 | 0.093 | 0.070 | 0.056 |
|  |  | 560 | 0.091 | 0.068 | 0.054 |
|  |  | 570 | 0.087 | 0.064 | 0.052 |
|  |  | 580 | 0.087 | 0.065 | 0.052 |
|  |  | 590 | 0.083 | 0.062 | 0.049 |
|  |  | 600 | 0.081 | 0.061 | 0.048 |
|  |  | 610 | 0.080 | 0.059 | 0.047 |
|  |  | 620 | 0.078 | 0.058 | 0.046 |
|  |  | 630 | 0.075 | 0.056 | 0.045 |
|  |  | 640 | 0.074 | 0.055 | 0.044 |
|  |  | 650 | 0.072 | 0.053 | 0.042 |
|  |  | 660 | 0.070 | 0.052 | 0.042 |
|  |  | 670 | 0.070 | 0.052 | 0.041 |
|  |  | 680 | 0.067 | 0.050 | 0.040 |
|  |  | 690 | 0.065 | 0.048 | 0.038 |
|  |  | 700 | 0.064 | 0.048 | 0.038 |
| Carbon Black | Dispersing additive concentration [%] | Wavelength [nm] | 30 min | 4 h | 24 h |
| CB4 | 100 | 400 | 0.131 | 0.103 | 0.088 |
|  |  | 410 | 0.124 | 0.097 | 0.083 |
|  |  | 420 | 0.116 | 0.091 | 0.077 |
|  |  | 430 | 0.115 | 0.089 | 0.076 |
|  |  | 440 | 0.111 | 0.086 | 0.073 |
|  |  | 450 | 0.107 | 0.084 | 0.071 |
|  |  | 460 | 0.104 | 0.081 | 0.069 |
|  |  | 470 | 0.100 | 0.078 | 0.066 |
|  |  | 480 | 0.095 | 0.074 | 0.063 |
|  |  | 490 | 0.093 | 0.072 | 0.061 |
|  |  | 500 | 0.091 | 0.071 | 0.060 |
|  |  | 510 | 0.087 | 0.068 | 0.057 |
|  |  | 520 | 0.085 | 0.066 | 0.056 |
|  |  | 530 | 0.084 | 0.065 | 0.055 |
|  |  | 540 | 0.081 | 0.063 | 0.053 |
|  |  | 550 | 0.078 | 0.061 | 0.051 |
|  |  | 560 | 0.076 | 0.059 | 0.050 |
|  |  | 570 | 0.073 | 0.056 | 0.047 |
|  |  | 580 | 0.072 | 0.056 | 0.047 |
|  |  | 590 | 0.069 | 0.054 | 0.045 |
|  |  | 600 | 0.068 | 0.053 | 0.044 |
|  |  | 610 | 0.066 | 0.052 | 0.043 |
|  |  | 620 | 0.065 | 0.051 | 0.042 |
|  |  | 630 | 0.063 | 0.049 | 0.041 |
|  |  | 640 | 0.062 | 0.048 | 0.040 |
|  |  | 650 | 0.060 | 0.047 | 0.039 |
|  |  | 660 | 0.058 | 0.046 | 0.038 |
|  |  | 670 | 0.058 | 0.045 | 0.038 |
|  |  | 680 | 0.056 | 0.043 | 0.036 |
|  |  | 690 | 0.054 | 0.042 | 0.035 |
|  |  | 700 | 0.053 | 0.042 | 0.035 |
| Carbon Black | Dispersing additive concentration [%] | Wavelength [nm] | 30 min | 4 h | 24 h |
| CB4 | 130 | 400 | 0.127 | 0.101 | 0.094 |
|  |  | 410 | 0.120 | 0.095 | 0.089 |
|  |  | 420 | 0.113 | 0.089 | 0.083 |
|  |  | 430 | 0.112 | 0.088 | 0.082 |
|  |  | 440 | 0.107 | 0.085 | 0.079 |
|  |  | 450 | 0.104 | 0.082 | 0.077 |
|  |  | 460 | 0.101 | 0.079 | 0.074 |
|  |  | 470 | 0.097 | 0.076 | 0.072 |
|  |  | 480 | 0.093 | 0.073 | 0.068 |
|  |  | 490 | 0.090 | 0.071 | 0.067 |
|  |  | 500 | 0.088 | 0.069 | 0.065 |
|  |  | 510 | 0.084 | 0.066 | 0.062 |
|  |  | 520 | 0.082 | 0.064 | 0.061 |
|  |  | 530 | 0.081 | 0.064 | 0.060 |
|  |  | 540 | 0.078 | 0.062 | 0.058 |
|  |  | 550 | 0.076 | 0.060 | 0.056 |
|  |  | 560 | 0.074 | 0.058 | 0.055 |
|  |  | 570 | 0.070 | 0.055 | 0.052 |
|  |  | 580 | 0.070 | 0.055 | 0.052 |
|  |  | 590 | 0.067 | 0.053 | 0.050 |
|  |  | 600 | 0.066 | 0.052 | 0.049 |
|  |  | 610 | 0.064 | 0.051 | 0.048 |
|  |  | 620 | 0.063 | 0.050 | 0.047 |
|  |  | 630 | 0.061 | 0.048 | 0.045 |
|  |  | 640 | 0.060 | 0.047 | 0.045 |
|  |  | 650 | 0.058 | 0.046 | 0.043 |
|  |  | 660 | 0.057 | 0.045 | 0.043 |
|  |  | 670 | 0.056 | 0.045 | 0.042 |
|  |  | 680 | 0.054 | 0.043 | 0.041 |
|  |  | 690 | 0.053 | 0.041 | 0.040 |
|  |  | 700 | 0.053 | 0.041 | 0.039 |
| Carbon Black | Dispersing additive concentration [%] | Wavelength [nm] | 30 min | 4 h | 24 h |
| CB5 | 70 | 400 | 0.108 | 0.093 | 0.083 |
|  |  | 410 | 0.102 | 0.088 | 0.078 |
|  |  | 420 | 0.096 | 0.082 | 0.072 |
|  |  | 430 | 0.095 | 0.081 | 0.071 |
|  |  | 440 | 0.092 | 0.078 | 0.069 |
|  |  | 450 | 0.089 | 0.075 | 0.066 |
|  |  | 460 | 0.086 | 0.073 | 0.064 |
|  |  | 470 | 0.083 | 0.070 | 0.062 |
|  |  | 480 | 0.079 | 0.067 | 0.059 |
|  |  | 490 | 0.077 | 0.065 | 0.057 |
|  |  | 500 | 0.076 | 0.064 | 0.056 |
|  |  | 510 | 0.072 | 0.060 | 0.053 |
|  |  | 520 | 0.071 | 0.059 | 0.052 |
|  |  | 530 | 0.070 | 0.058 | 0.051 |
|  |  | 540 | 0.068 | 0.056 | 0.049 |
|  |  | 550 | 0.065 | 0.054 | 0.048 |
|  |  | 560 | 0.064 | 0.053 | 0.046 |
|  |  | 570 | 0.060 | 0.050 | 0.044 |
|  |  | 580 | 0.061 | 0.050 | 0.044 |
|  |  | 590 | 0.058 | 0.048 | 0.042 |
|  |  | 600 | 0.057 | 0.047 | 0.041 |
|  |  | 610 | 0.056 | 0.046 | 0.040 |
|  |  | 620 | 0.054 | 0.045 | 0.039 |
|  |  | 630 | 0.052 | 0.043 | 0.038 |
|  |  | 640 | 0.052 | 0.043 | 0.037 |
|  |  | 650 | 0.050 | 0.041 | 0.036 |
|  |  | 660 | 0.049 | 0.041 | 0.035 |
|  |  | 670 | 0.049 | 0.040 | 0.035 |
|  |  | 680 | 0.047 | 0.038 | 0.034 |
|  |  | 690 | 0.045 | 0.038 | 0.033 |
|  |  | 700 | 0.045 | 0.037 | 0.032 |
| Carbon Black | Dispersing additive concentration [%] | Wavelength [nm] | 30 min | 4 h | 24 h |
| CB5 | 100 | 400 | 0.104 | 0.091 | 0.081 |
|  |  | 410 | 0.098 | 0.086 | 0.077 |
|  |  | 420 | 0.092 | 0.080 | 0.071 |
|  |  | 430 | 0.091 | 0.079 | 0.070 |
|  |  | 440 | 0.088 | 0.076 | 0.067 |
|  |  | 450 | 0.084 | 0.073 | 0.065 |
|  |  | 460 | 0.082 | 0.071 | 0.063 |
|  |  | 470 | 0.079 | 0.068 | 0.060 |
|  |  | 480 | 0.075 | 0.065 | 0.058 |
|  |  | 490 | 0.073 | 0.064 | 0.056 |
|  |  | 500 | 0.072 | 0.062 | 0.055 |
|  |  | 510 | 0.068 | 0.059 | 0.052 |
|  |  | 520 | 0.066 | 0.058 | 0.051 |
|  |  | 530 | 0.065 | 0.057 | 0.050 |
|  |  | 540 | 0.063 | 0.055 | 0.049 |
|  |  | 550 | 0.061 | 0.053 | 0.047 |
|  |  | 560 | 0.059 | 0.052 | 0.046 |
|  |  | 570 | 0.056 | 0.049 | 0.043 |
|  |  | 580 | 0.056 | 0.049 | 0.043 |
|  |  | 590 | 0.054 | 0.047 | 0.041 |
|  |  | 600 | 0.053 | 0.046 | 0.041 |
|  |  | 610 | 0.052 | 0.045 | 0.040 |
|  |  | 620 | 0.050 | 0.044 | 0.039 |
|  |  | 630 | 0.049 | 0.043 | 0.038 |
|  |  | 640 | 0.048 | 0.042 | 0.037 |
|  |  | 650 | 0.046 | 0.041 | 0.036 |
|  |  | 660 | 0.045 | 0.040 | 0.035 |
|  |  | 670 | 0.045 | 0.040 | 0.035 |
|  |  | 680 | 0.043 | 0.038 | 0.034 |
|  |  | 690 | 0.042 | 0.038 | 0.033 |
|  |  | 700 | 0.042 | 0.037 | 0.033 |
| Carbon Black | Dispersing additive concentration [%] | Wavelength [nm] | 30 min | 4 h | 24 h |
| CB5 | 130 | 400 | 0.100 | 0.091 | 0.085 |
|  |  | 410 | 0.094 | 0.086 | 0.080 |
|  |  | 420 | 0.088 | 0.080 | 0.074 |
|  |  | 430 | 0.087 | 0.079 | 0.073 |
|  |  | 440 | 0.084 | 0.076 | 0.071 |
|  |  | 450 | 0.081 | 0.073 | 0.068 |
|  |  | 460 | 0.078 | 0.071 | 0.066 |
|  |  | 470 | 0.075 | 0.068 | 0.064 |
|  |  | 480 | 0.072 | 0.065 | 0.061 |
|  |  | 490 | 0.070 | 0.064 | 0.059 |
|  |  | 500 | 0.068 | 0.062 | 0.058 |
|  |  | 510 | 0.065 | 0.059 | 0.056 |
|  |  | 520 | 0.063 | 0.058 | 0.054 |
|  |  | 530 | 0.062 | 0.057 | 0.053 |
|  |  | 540 | 0.060 | 0.055 | 0.052 |
|  |  | 550 | 0.058 | 0.053 | 0.050 |
|  |  | 560 | 0.057 | 0.052 | 0.049 |
|  |  | 570 | 0.054 | 0.049 | 0.047 |
|  |  | 580 | 0.054 | 0.049 | 0.047 |
|  |  | 590 | 0.051 | 0.047 | 0.045 |
|  |  | 600 | 0.050 | 0.046 | 0.044 |
|  |  | 610 | 0.049 | 0.045 | 0.043 |
|  |  | 620 | 0.048 | 0.044 | 0.042 |
|  |  | 630 | 0.046 | 0.043 | 0.041 |
|  |  | 640 | 0.045 | 0.042 | 0.040 |
|  |  | 650 | 0.044 | 0.041 | 0.040 |
|  |  | 660 | 0.044 | 0.040 | 0.039 |
|  |  | 670 | 0.043 | 0.040 | 0.039 |
|  |  | 680 | 0.042 | 0.038 | 0.037 |
|  |  | 690 | 0.040 | 0.038 | 0.037 |
|  |  | 700 | 0.040 | 0.037 | 0.036 |

Table 11: measured color strength and absorption coefficient. calculated scattering coefficient to figure 5

| Carbon Black | Dispersion- time | Color strength [%] | Absorption coefficient [-] | Scattering coefficient [-] |
| --- | --- | --- | --- | --- |
| CB1 | 15 min | 121.26767 | 0.47772503 | 0.00393943 |
|  | 30 min | 113.893753 | 0.45169097 | 0.0039659 |
|  | 1 h | 113.847519 | 0.44427812 | 0.0039024 |
|  | 2 h | 113.381714 | 0.43615991 | 0.00384683 |
|  | 4 h | 106.271561 | 0.39814281 | 0.00374647 |
|  | 8 h | 108.927483 | 0.39955813 | 0.00366811 |
| CB2 | 15 min | 204.387604 | 0.71155459 | 0.0034814 |
|  | 30 min | 210.174072 | 0.72052559 | 0.00342823 |
|  | 1 h | 211.592667 | 0.7241219 | 0.00342224 |
|  | 2 h | 217.702744 | 0.73280367 | 0.00336607 |
|  | 4 h | 227.87 | 0.74660346 | 0.00327645 |
|  | 8 h | 240.546173 | 0.76302405 | 0.00317205 |
| CB3 | 15 min | 652.478088 | 0.9130946 | 0.00139943 |
|  | 30 min | 726.803528 | 0.92426064 | 0.00127168 |
|  | 1 h | 846.232605 | 0.93724222 | 0.00110755 |
|  | 2 h | 1008.15729 | 0.94826758 | 0.00094059 |
|  | 4 h | 1384.80 | 0.96380951 | 0.00069599 |
|  | 8 h | 2390.39014 | 0.97916307 | 0.00040962 |
| CB4 | 15 min | 681.262695 | 0.92315982 | 0.00135507 |
|  | 30 min | 788.3573 | 0.93571098 | 0.00118691 |
|  | 1 h | 799.561035 | 0.9358881 | 0.0011705 |
|  | 2 h | 882.719543 | 0.9420758 | 0.00106724 |
|  | 4 h | 1054.16309 | 0.95246437 | 0.00090353 |
|  | 8 h | 1206.56824 | 0.95824899 | 0.00079419 |
| CB5 | 15 min | 1084.41663 | 0.95312554 | 0.00087893 |
|  | 30 min | 1125.6731 | 0.95529502 | 0.00084864 |
|  | 1 h | 1114.70642 | 0.95414035 | 0.00085596 |
|  | 2 h | 1154.56531 | 0.95553673 | 0.00082762 |
|  | 4 h | 1352.35779 | 0.9628788 | 0.000712 |
|  | 8 h | 1363.26794 | 0.96232728 | 0.0007059 |

Table 12: undertone values for figure 6

| Carbon Black | Dispersiontime | Undertone dm [-] |
| --- | --- | --- |
| CB1 | 15 min | -4.1 |
|  | 30 min | -4.9 |
|  | 1 h | -4.1 |
|  | 2 h | -3.7 |
|  | 4 h | -3.9 |
|  | 8 h | -2.7 |
| CB2 | 15 min | 5.9 |
|  | 30 min | 6.2 |
|  | 1 h | 6.4 |
|  | 2 h | 6.6 |
|  | 4 h | 6.8 |
|  | 8 h | 7.4 |
| CB3 | 15 min | 8.7 |
|  | 30 min | 9.9 |
|  | 1 h | 11.0 |
|  | 2 h | 12.0 |
|  | 4 h | 13.3 |
|  | 8 h | 14.5 |
| CB4 | 15 min | 12.0 |
|  | 30 min | 13.0 |
|  | 1 h | 12.8 |
|  | 2 h | 13.1 |
|  | 4 h | 13.6 |
|  | 8 h | 14.1 |
| CB5 | 15 min | 13.6 |
|  | 30 min | 13.6 |
|  | 1 h | 13.6 |
|  | 2 h | 13.5 |
|  | 4 h | 14.3 |
|  | 8 h | 13.9 |

Text 1: Deviation of the equation (9)

The calculations of the reflection spectra are based on the scattering of a plane wave by spherical particles. Those particles can be dielectric and absorbing depending on their size. The calculations were developed by Gustav Mie. Furthermore, Mie’s theory also considers the angular distribution of the scattered radiation. The scattering angle used is represented below as θ. The partial waves are functions of the scattering angle, which are calculated via the relative refraction index m and the variable x. The relative refraction index is the quotient of the refraction index of the scattering particle n (here: Carbon black) and the surrounding medium n0 (here: clear coat), see equation 9-1:

| m≡nn0 | (9-1) |
| --- | --- |

The variable x, also called Mie-parameter, is the ratio of the particle circumference π∙dP, where dP is the diameter of the particle, and the incident wavelength λ, see equation 9-2:

| x≡π∙dPλ | (9-2) |
| --- | --- |

an and bn are functions of m and x corresponding to the electric (an) and magnetic (bn) partial waves (equation 9-3 and 9-4). The polar coordinates of the particles are φ and ϑ and the spherical functions are Pn for the electric and Bn for the magnetic with respect to the polar coordinates. f is the field parameter.

| aϑ,n=+ i ∙bφ,n =- i∙λπ∙e-πidPλdP∙1∞fn∙(n+1)∙∂Pn∂ϑ+pnn∙(n+1)∙1sinϑ∙∂Bn∂φ | (9-3) |
| --- | --- |
| aφ,n=- i ∙bϑ,n =- i∙λπ∙e-πidPλdP∙1∞fn∙(n+1)∙1sinϑ∙∂Pn∂φ-pnn∙(n+1)∙∂Bn∂ϑ | (9-4) |

In colloidal systems with very fine particles, only the first electrical oscillations make a significant contribution, while in coarser colloidal systems, the second electrical oscillation and the first magnetic oscillation also make a significant contribution.

S1 and S2 are the intensities of the scattered radiation (equation 9-5 and 9-6). Their vectors are oscillating vertically and horizontally to the plane of incidence and observation. The relationship of the spherical shape of the particles is established via Pn and Bn according to cosθ.

| S1=n=1∞2∙n+1n∙n+1∙anPncosθS+bnBncosθS | (9-5) |
| --- | --- |
| S2=n=1∞2∙n+1n∙n+1∙bnPnncosθS+anBncosθS | (9-6) |

The resulting scattering (equation 9) of particles by irradiation with primary radiation of the intensity I0 at a distance A from the spheric particle therefore results in:

| Iλ, dP, θ=I0∙λ28∙π2∙A2∙S12θ+S22θ | (9) |
| --- | --- |

[9-1] Mie, G. 1908. Beitrag zur Optik trüber Medien. Annalen der Physik, 25

[9-2] Kortüm, G. 1969. Reflexionsspektroskopie: Grundlagen, Methodik, Anwendungen. 1st ed., Springer, Berlin Heidelberg

Text 2: Long-term Stability

Material and methods: To investigate the long-term stability of the coating’s dispersion two variants of CB5 were used. One variant had a medium high level of aftertreatment and the other a high level of aftertreatment. This was done due to the before investigated positive effect of the aftertreatment on the dispersibility. The dispersions contain the mill base named in table 2 and were dispersed on the BA S 20 from Skandex-Dispers for 1 hour. The manufactured dispersions were mixed with the clear coat and coated immediately after production and four weeks after production. During these four weeks the dispersions were stored at 40 °C. This was done to simulate a longer storage time. Afterwards the undertone was measured and is shown in figure 9.

Figure 10: Effect of a four weeks long storage time on the undertone dM of two carbon blacks with a medium high and a high level of aftertreatment, dM is a dimensionless parameter, [-] means that there are no units

The undertone of both samples, shown in figure 9, can be seen as equivalent, directly after the production of the dispersion, due to the deviation in measurement accuracy. This means that the levels of aftertreatment used had no different effect on the undertone. This also implies that the size of the carbon black aggregates in the dispersion is similar. When considering the undertone measured in the samples that were stored for four weeks after production and then applicated, the undertone is higher for both samples. The higher undertone implies that the aggregates did not reagglomerate over time. The higher undertone also suggests that the wetting process and the resulting distribution of the aggregates in the dispersion is a time-dependent process and is not finished after one hour.

These findings prove that a longer storage time of the dispersion does not lead to inferior optical properties and in this case even leads to better results.