# Supplementary Information

n-Nonane hydroisomerization over hierarchical SAPO-11 based catalysts with sodium dodecylbenzene sulfonate as a dispersant

Chenglong Wen·Jundong Xu1·Xueman Wang1·Yu Fan1

1 State Key Laboratory of Heavy Oil Processing, China University of Petroleum, Beijing 102249, People’s Republic of China

- Yu Fan

fanyu@cup.edu.cn

1. Experimental

The total pore volume of the sample was determined from the liquid N2 amount adsorbed at a relative pressure (P/P0) of 0.99. The micropore volume was calcualted by the t-plot method (Scherdel et al. 2010). The mesopore volume was calculated by subtracting the micropore volume from the total pore volume.

The amounts of acid centers on these samples were calculated by the following formula (Emeis et al. 1993):

| CL;B=AS/mɛ | (1) |
| --- | --- |

where CL;B, S, A and m refer to the amount of L or B acid centers (μmol g-1), the area of the sample (cm2), the integral of the spectrum for L or B acid centers (cm-1) and the mass of the sample (g), respectively.

Pt dispersions of these catalysts were calculated using the following equation (Veldurthi et al. 2012):

| DPt=V×22414×SF×MW×100% | (2) |
| --- | --- |

where DPt is the Pt dispersion; V is the volume of the adsorbed H2 (mL); M is the Pt mole mass (g mol-1); SF is the stoichiometry factor, and W is the weight of the supported Pt on the SAPO-11 sample (g).

2. Results and discussion

The relative crystallinities of these samples were calculated by dividing the areas of six major XRD characteristic peaks at 2θ=8.0~24.0° on these SAPO-11 samples by the total areas of those peaks on the S-C sample, and the results were displayed in Table S1.

Table S1 Relative crystallinity of S-C and S-Sx (x=1, 2, 3, 4 and 5)

| Samples | Relative crystallinity, % |
| --- | --- |
| S-C | 100 |
| S-S1 | 98.4 |
| S-S2 | 97.6 |
| S-S3 | 97.1 |
| S-S4 | 32.5 |
| S-S5 | 0 |

29Si solid-state nuclear magnetic resonance (29Si NMR) of S-C and S-S3 were conducted on an Avance III spectrometer to measure the coordinated environment of Si atoms in the SAPO-11 samples. The 29Si NMR spectra of S-C and S-S3 are shown in Fig. S1. The Brønsted (B) acid sites of the silicoaluminophosphate molecular sieves are produced by Si substitution in the AlPO4 framework. There are two main mechanisms (SM2 and SM3) of Si substitution for SAPO-11 (Jahn et al. 1990). In the SM2 mechanism, one P atom in the AlPO4 framework is replaced by one Si atom, and SAPO domains (Si(4Al)) are formed. In the SM3 mechanism, two adjacent P and Al atoms are replaced by two Si atoms, and aluminosilicate (SA) domains are formed. The 29Si MAS NMR spectra of S-C and S-S3 have a broad peak from -70 ~ -120 ppm, which can be deconvoluted six peaks, and the results are displayed in Table S2. The peaks centered at ca. -86 (peak 1), -97 (peak 3), -102 (peak 4), -107 (peak 5) and -110 (peak 6) ppm represent the different Si coordination structures in the SA domains, with structures of Si (4Al), Si (3Al), Si (2Al), Si (1Al) and Si (4Si), respectively; the peak centered at -91 ppm (peak 2) represents the structure of Si (4Al) in the SAPO domains (Mériaudeau et al. 1998). According to the data in Table S1, S-C and S-S3 show almost the same amounts of Si (nAl) (n=1~4) and Si (4Si) structures, indicating that the Si coordination structure of the synthesized SAPO-11 molecular sieve is hardly affected by the addition of SDBS, which is in accordance with the obtained Py-IR results.

Fig. S1 29Si MAS NMR spectra of S-C and S-S3.

Table S2. Deconvolution analysis results of 29Si MAS-NMR spectra of S-C and S-S3

| Sample |  | SAPO domain |  | SA domain |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  | Si (4Al), % -91 ppm |  | Si (4Al), % -86 ppm | Si (3Al, Si), % -97 ppm | Si (2Al, 2Si), % -102 ppm | Si (1Al, 3Si), % -107 ppm |  | Si(4Si), % -110 ppm |
| S-C | 10.61 |  | 15.46 | 23.84 | 16.39 | 16.01 |  | 17.69 |
| S-S3 | 10.40 |  | 15.52 | 23.71 | 16.47 | 16.10 |  | 17.80 |

References

Emeis CA. Determination of integrated molar extinction coefficients for infrared absorption bands of pyridine adsorbed on solid acid catalysts. J Catal. 1993;141:347-54. https://doi.org/10.1006/jcat.1993.1145.

Jahn E, Müller D, Becker K. Characterization of the local environment of Si atoms incorporated into AlPO4-11 by means of 27Al, 31P and 29Si MAS N.M.R. spectroscopy. Zeolites 1990;10:151-156. https://doi.org/10.1016/0144-2449(90)90038-S.

Mériaudeau P, Tuan VA, Lefebvre F, Nghiem VT, Naccache C. Isomorphous substitution of silicon in the AlPO4 framework with AEL structure: n-octane hydroconversion. Micropor. Mesopor. Mater., 1998;22:435-449. https://doi.org/10.1016/S1387-1811(98)00095-X.

Scherdel C, Reichenauer G, Wiener M. Relationship between pore volumes and surface areas derived from the evaluation N2-sorption data by DR-, BET- and t-plot. Micropor. Mesopor. Mat. 2010;132:572-575. https://doi.org/10.1016/j.micromeso.2010.03.034.

Veldurthi S, Sshin CH, Joo OS, Jung KD. Promotional effects of Cu on Pt/Al2O3 and Pd/Al2O3 catalysts during n-butane dehydrogenation. Catal. Today, 2012;185:88-93. https://doi.org/10.1016/j.cattod.2011.11.021.