Electronic supplementary material for

pH-Responsive and Buffering Macromolecule Aqueous Absorbent and Mathematic Model-Based Feasibility Evaluation for SO2 Capture

Wei Feng1, Wenhao Gu1, Lühong Zhang1, Xiaowei Tantai1, Bin Jiang1, Huawei Yang1,2, Hongjie Zhang1

1  School of Chemical Engineering and Technology, Tianjin University, Tianjin 300350, China

2  School of Chemistry and Materials Science, Ludong University, Yantai 264025, China

Lühong Zhang, zhanglvh@tju.edu.cn and Huawei Yang, huaweiyang@tju.edu.cn

Contents

Figure S1  1HNMR spectrum of PVIM……………………………………..…page 2

Figure S2  Average size of the PVIM micelles in different pH values.…….…page 2

Figure S3  pH variation in the absorption process of the 5 cycles. ……..…..  page 3

Figure S4  pH variation in the desorption process of the 5 cycles. ………...…page 3

Table S1  Relative critical parameters……………………………………….…page 4

Table S2  Solubilities of SO2 in the absorbent at temperature and equilibrium pressure..………………………………………………………….…………..page 4

Mathematic Model of Titration Process……………………………….…   page 5

Mathematic Model of SO2 Absorption Equilibrium…………………………page 7

Fig. S1 1HNMR spectrum of PVIM

Fig. S2 Average size of the PVIM micelles in different pH values.

Fig. S3 pH variation in the absorption process of the 5 cycles.

Fig. S4 pH variation in the desorption process of the 5 cycles.

Table S1 Relative critical parameters

| ij | Tcij/K | Pcij/MPa | Vcij/m3·kmol-1 | Zcij | ωij |
| --- | --- | --- | --- | --- | --- |
| 11 | 126.10 | 3.394 | 0.0901 | 0.292 | 0.040 |
| 22 | 430.75 | 7.884 | 0.1220 | 0.269 | 0.245 |

1 and 2 are represents N2 and SO2, respectively.

Table S2 Solubilities of SO2 in the absorbent at temperature and equilibrium pressure.

| T = 298.2K |  | T = 313.2K |  | T = 328.2K |  |
| --- | --- | --- | --- | --- | --- |
| p/ kPa | a | p/kPa | a | p/ kPa | a |
| 0 | 0 | 0 | 0 | 0 | 0 |
| 0.1 | 0.21552 | 0.2 | 0.07633 | 0.2 | 0.05346 |
| 0.299 | 0.43081 | 0.4 | 0.15254 | 0.4 | 0.12658 |
| 0.599 | 0.63392 | 0.598 | 0.20539 | 0.803 | 0.19452 |
| 0.8 | 0.85427 | 1.202 | 0.42015 | 1.604 | 0.39405 |
| 1.002 | 1.06827 | 2.112 | 0.64029 | 2.31 | 0.59704 |
| 1.204 | 1.27492 | 2.213 | 0.85595 | 2.811 | 0.79961 |
| 1.408 | 1.50033 | 2.82 | 1.0613 | 3.316 | 0.99922 |
| 1.714 | 1.71964 | 3.523 | 1.28472 | 3.623 | 1.2048 |
| 2.412 | 1.93955 | 3.923 | 1.47608 | 4.324 | 1.4063 |
| 9.367 | 2.12572 | 5.428 | 1.75723 | 5.928 | 1.60162 |
| 20.456 | 2.28352 | 14.996 | 2.00605 | 9.053 | 1.77985 |
| 32.279 | 2.44126 | 29.732 | 2.16838 | 18.918 | 1.938 |
| 44.309 | 2.59603 | 46.901 | 2.31814 | 35.961 | 2.06836 |
| 56.651 | 2.75638 | 64.095 | 2.46616 | 52.402 | 2.19397 |
| 69.021 | 2.92451 | 80.993 | 2.61097 | 71.692 | 2.30968 |
| 81.168 | 3.08798 | 97.698 | 2.76728 | 99.191 | 2.46838 |
| 92.836 | 3.24893 |  |  |  |  |
| 104.802 | 3.41321 |  |  |  |  |

aSolubilities of SO2 on the basis of molSO2 / kg absorbent.

Mathematic Model of the Titration Process

The detailed mathematic model of the titration experiment was as follow:

Firstly, following assumptions were made:

(1) Hydrochloric acid was fully ionized since the pKavalue of hydrochloric acid is -8.00 .

(2) The repeated unit VIM instead of PVIM was used to calculate to concentration of the absorbent, and the PVIMwere assumed to be the same molecular weight.

(3) Ionic activity coefficient was estimated by the Debye-Huckelequation.

|  | (1) |
| --- | --- |
|  | (2) |

where is the ionic strength,  and  are the molality and the charge of spicesrespectively, is the activity coefficient of spices andis the parameter.

(4)Volume change on mixing are zero.

|  | (3) |
| --- | --- |

Chemical equilibrium model is as follows:

|  | (4) |
| --- | --- |
|  | (5) |

where is the activity of component, is the ionic product constant of water and  is the reaction equilibrium constant.

|  | (6) |
| --- | --- |
|  | (7) |

whereand is the reaction equilibrium constant of VIM at (25°C) and  respectively, and  is the molar protonated reaction enthalpy.

Mass balance model is as follows:

|  | (8) |
| --- | --- |
|  | (9) |
|  | (10) |
|  | (11) |

where is the amount of VIM added in water, is the volume of the solution formed by VIM and water before titration and is the volume of added HCl solution during titration.

Mathematic Model of SO2 Absorption Equilibrium

Firstly, following assumptions were made:

(1) Hydrochloric acid was fully ionized since the pKa value of hydrochloric acid is -8.00 .

(2) The repeated unit VIM instead of PVIM was used to calculate to concentration of the absorbent, and the PVIM were assumed to be the same molecular weight.

(3) Ionic activity coefficient was estimated by the Debye-Huckel equation .

|  | (1) |
| --- | --- |
|  | (2) |

where  is the ionic strength, and  are the molality and the charge of spicesrespectively, is the activity coefficient of spices andis the parameter.

(4)Volume change on mixing are zero.

|  | (3) |
| --- | --- |

Chemical equilibrium model is as follows:

|  | (12) |
| --- | --- |
|  | (13) |
|  | (14) |
|  | (5) |

where  is the activity of component, is the Henry's constant of SO2, and  and  are the first and secondary dissociation constant of H2SO3 respectively.

|  | (7) |
| --- | --- |

where  and  is the reaction equilibrium constant of VIM at (25°C) and  respectively, and  is the molar protonated reaction enthalpy.

Mass balance model is as follows:

|  | (15) |
| --- | --- |
|  | (16) |
|  | (17) |

where  is the amount of SO2 captured by the absorbent,  is the amount of VIM added in water and  is the volume of the solution formed by VIM and water.