Supplementary Materials

Fluorine Doped Hard Carbon as the Advanced Performance Anode Material of Sodium Ion Batteries

Lingchen Kong1 ·Yu Li1 ·Wei Feng1

1School of Materials Science and Engineering, Tianjin University, Tianjin 300072, China

Correspondence to Wei Feng, E-mail address: weifeng@tju.edu.cn

Fig. S1 Experimental process and digital photographs of pristine HC and synthesized F–HC

Fig. S2 SEM images of a HC, b F–HC50, c F–HC100, and d F–HC150

Fig. S3 XPS survey spectra of F–HC

Fig. S4 Elemental mapping image of C and F components of F–HC

Fig. S5 Typical discharge/charge profiles of F–HC100 at different current densities

Fig. S6 Nyquist plots of HC and F–HC after 100 cycles at 50 mA/g

Fig. S7 SEM images of a HC, b F–HC50, c F–HC100, and d F–HC150 after 100 cycles at 50 mA/g

Table S1 Structural parameters of HC and F–HC

| Sample | d-spacing (Å) | ID/IG | Surface area (m2/g) | Pore volume (cm3/g) |
| --- | --- | --- | --- | --- |
| HC | 3.86 | 1.01 | 2.60 | 0.006 |
| F–HC50 | 4.02 | 1.02 | 3.31 | 0.010 |
| F–HC100 | 4.12 | 104 | 4.44 | 0.011 |
| F–HC150 | 4.05 | 1.07 | 4.56 | 0007 |

Table S2 C1s and F1s peak assignments and proportions obtained from the XPS spectra of F–HC

| Sample | C1s assignments (eV) |  |  |  |  | F1s assignments (eV) |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  | sp2 C (at.%) | sp3 C (at.%) | C–O (at.%) | Semi-ionic C–F bond (at.%) | Covalent C–F bond (at.%) | Absorbed F atom (at.%) | Semi-ionic F atom (at.%) | Covalent F atom (at.%) |
| F–HC50 | 284.7 | 285.3 | 286.1 | 286.6 | 289.2 | 686.5 | 687.4 | 688.6 |
|  | 24.6 | 25.0 | 14.1 | 22.8 | 13.5 | 36.4 | 33.3 | 30.3 |
| F–HC100 | 286.4 | 285.5 | 286.0 | 286.8 | 289.3 | 686.7 | 687.8 | 688.9 |
|  | 26.8 | 16.8 | 17.3 | 19.4 | 19.7 | 31.1 | 38.9 | 30.0 |
| F–HC150 | 284.8 | 285.4 | 285.9 | 286.7 | 298.5 | 686.8 | 687.7 | 689.0 |
|  | 30.8 | 15.9 | 13.8 | 12.8 | 26.7 | 28.8 | 35.1 | 36.1 |

Table S3 Comparison of the energy density of F–HC products in this study and previously reported cathode of sodium-ion battery

| Reference | Published year | Cathode type | Reversible capacity | Initial coulombic efficiency | Retained capacity |
| --- | --- | --- | --- | --- | --- |
| [21] | 2020 | Lignin-derived N-doped carbon | 320.5 mAh/g | 99.32% | 130.8 mAh/g (after 1144 cycles) |
| [23] | 2015 | F-doped carbon derived from lotus petioles | 230 mAh/g | 52.3% | 228 mAh/g (after 200 cycles) |
| [25] | 2019 | N, F co-doped porous carbon | 329.93 mAh/g | ~99% | 312.6 mAh/g (after 300 cycles) |
| [26] | 2017 | N, F co-doped graphene | 220 mAh/g | 95% | 203 mAh/g (after 100 cycles) |
| [27] | 2021 | N-enriched carbon nanofibers | 199 mAh/g | / | 150 mAh/g (after 2000 cycles) |
| [53] | 2019 | Na3V2(PO4)3@C@ CNT porous network | 100 mAh/g | 99% | 83 mAh/g (after 4500 cycles) |
| [54] | 2020 | Microspherical Sb@C composite | 721.6 mAh/g | 63.5% | 280 mAh/g (after 500 cycles) |
| [55] | 2021 | Porous polyaniline-PEDOT | 81.9 mAh/g | ~92% | 80.91 mAh/g (after 200 cycles) |
| This work |  | F–HC100 | 358 mAh/g | 78.13% | 343 mAh/g (after 100 cycles) |