# Research Article

# Li2TiO3 Dopant and Phosphate Coating Improve the Electrochemical Performance of LiCoO2 at 3.0–4.6 V

Baozhao Shi1∙ Jiangli Feng1 ∙ Jing Liu1 ∙Yanan Zhou1 ∙Jinli Zhang1, 2 ∙ Wei Li1, 2

1School of Chemical Engineering and Technology, Tianjin University, Tianjin 300350, China

2Haihe Laboratory of Sustainable Chemical Transformations, Tianjin 300192, China

Correspondence to Wei Li, Email: liwei@tju.edu.cn

Received: 5 July 2022 / Revised: 11 July 2022 / Accepted: 25 July 2022 / Published online:

Contents

- Fig. S1 Rietveld refinements for the a LCO-P and b LCO-Ti

- Fig. S2 SEM images of a LCO, b LCO-Ti/P, c LCO-P and d LCO-Ti

- Fig. S3 EDS elemental mapping of Co, O, P and Ti for LCO-Ti/P

- Fig. S4 XPS spectra of four kinds of samples

- Fig. S5 FT-IR spectra of LCO and LCO-Ti/P

- Fig. S6 Discharge mean voltage fading in the cycling process for all the samples at 1 C and room temperature

- Fig. S7 The full spectra of in-situ XRD characterization for a LCO and b LCO-Ti/P during the first charge-discharge process

- Fig. S8 EIS spectra of a LCO-P and b LCO-Ti based on the 1st, 5th, 10th, 50th and 100th cycles

- Fig. S9 Linear fit of the cell voltage as a function of the τ1/2. b Single titration step of GITT curve for LCO-Ti/P. c DLi+ calculated from GITT during 100th cycle of the discharging process of all samples

- Fig. S10 The interface structure models of matched crystal planes between Li2TiO3 and LiCoO2: a Li2TiO3(002) and LiCoO2(104), b Li2TiO3(202) and LiCoO2(003)

- Table S1 Comparison of electrochemical performance with the results in the literature

- Table S2 Relative percentages and binding energies of O Species in O 1s XPS spectra

- Table S3 Relativepercentages and binding energy of Co3+/Co2+ in Co 2p XPS spectra

- Table S4 EIS fitting results of LCO-Ti and LCO-P

Fig. S1 Rietveld refinements for the a LCO-Pand b LCO-Ti

Fig. S2 SEM images of a LCO, b LCO-Ti/P, c LCO-P and d LCO-Ti

Fig. S3 EDS elemental mapping of Co, O, P and Ti for LCO-Ti/P

Fig. S4 XPS spectra of four kinds of samples

Fig. S5 FT-IR spectra of LCO and LCO-Ti/P

Fig. S6 Discharge mean voltage fading in the cycling process for all the samples at 1C and room temperature

Fig. S7 The full spectra of in-situ XRD characterization for a LCO and b LCO-Ti/P during the first charge-discharge process

Fig. S8 EIS spectra of a LCO-Pand b LCO-Ti based on the 1st, 5th, 10th, 50th and 100th cycles

Fig. S9 a Linear fit of the cell voltage as a function of the τ1/2. b Single titration step of GITT curve for LCO-Ti/P. c DLi+ calculated from GITT during 100th cycle of the discharging process of all samples

Fig. S10 The models of interface structure of different crystal planes between Li2TiO3 and LiCoO2: a Li2TiO3(002) and LiCoO2(104), b Li2TiO3(202) and LiCoO2(003)

Table S1 Comparison of electrochemical performance with the results in the literature

| Modified cathodes | Voltage range(V); Temperature | Current density (mA/g) | Initial capacity (mAh/g) (current rate) | Capacity after n-cycles (mAh/g) | Capacity retention | Ref. |
| --- | --- | --- | --- | --- | --- | --- |
| Li3PO4 and AlPO4 -coated with Al and P -doped LiCoO2 | 3.0-4.6 RT | 1 C = 274 | 214.1 (0.1 C) | 180.4 (200th, 0.5 C) | 88.6% | [1] |
| BaTiO3 and TiO2-coated with Mg and Ti -doped LiCoO2 | 3.0-4.6 RT | 1 C = 200 | 208.8 (0.5 C) | 150.7 (300th, 1 C) | 75.0% | [2] |
| Li1.5Al0.5Ti1.5(PO4)3 -coated LiCoO2 | 3.0-4.6 RT | 1 C = 274 | 214.6 (0.2 C) | 180.3 (100th, 0.5 C) | 88.3% | [3] |
|  | 3.0-4.6 45℃ |  |  | 160.9 (100th, 0.5 C) | 72.9% |  |
| ZnO -coated and Al -doped LiCoO2 | 3.0-4.6 RT | 1 C = 185 | 183.9 (1 C) | 120.8 (500th, 1 C) | 65.7% | [4] |
| Mg -doped LiCoO2 | 3.0-4.6 RT | 1 C = 270 mA/g | 204 (0.2 C) | 158 (100th, 1C) | 84% | [5] |
| Spinel LiNi0.5Mn1.5O4 -coated LiCoO2 | 3.0-4.6 RT | 1 C = 220 | 219 (0.5 C) | 156.8 (55th, 0.5 C) | 71.6% | [6] |
| Ti and Mg and Al -doped LiCoO2 | 3.0-4.6 RT | 1 C = 274 | 202.3 (0.5 C) | 174 (100th, 0.5 C) | 86% | [7] |
| Ti and Mg and Al -doped LiCoO2 | 3.0-4.6 RT | 1 C = 140 | 224.9 (0.1 C) | 169.9 (200th, 0.5 C) | 78% | [8] |
| F-doped Al2O3 -coated LiCoO2 | 3.0-4.6 RT | 27.4 | 208.6 (27.4mA/g) | 185.3 (100th, 27.4mA/g) | 89.1% | [9] |
| LiAlO2 -coated LiCoO2 | 3.0-4.6 RT | 20 | 198.7 (20mA/g) | 172.2 (50th, 20 mA/g) | 86.7% | [10] |
| Dual-element Ti and P modified LiCoO2 | 3.0-4.6 RT | 1 C = 200 | 211.6 (0.1 C) 193.8 (1 C) | 166.1 (100th, 1 C) 130.4 (300th, 1 C) | 85.7% 67.3% | This work |

Table S2 Relative percentages and binding energies of O species in O 1s XPS spectra

| Sample | Relative content (%) |  |  |  | Binding energy (eV) |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  | Co–O | Ti–O or P–O | C=O | C–O | Co–O | Ti–O or P–O | C=O | C–O |
| LCO-P | 44.07 | 39.68 | 8.16 | 8.09 | 529.08 | 530.80 | 532.00 | 533.18 |
| LCO-Ti | 9.05 | 8.39 | 40.63 | 41.93 | 529.52 | 531.40 | 532.00 | 533.17 |
| LCO-Ti/P | 39.19 | 37.31 | 13.62 | 9.88 | 529.51 | 531.04 | 532.00 | 533.17 |

Table S3 Relative percentages and binding energy of Co3+/Co2+ in Co 2p 3/2 XPS spectra

| Sample | Relative content(%) |  | Binding energy(eV) |  |
| --- | --- | --- | --- | --- |
|  | Co3+ | Co2+ | Co3+ | Co2+ |
| LCO | 73.63 | 26.37 | 779.66 | 781.17 |
| LCO-P | 73.99 | 26.01 | 779.52 | 781.06 |
| LCO-Ti | 73.47 | 26.53 | 779.87 | 781.40 |
| LCO-Ti/P | 82.50 | 17.50 | 779.95 | 781.59 |

Table S4 EIS fitting results of LCO-Ti and LCO-P

| Samples | Cycle number | Rs (Ω) | Rf (Ω) | Rct (Ω) | Samples | Cycle number | Rs (Ω) | Rf (Ω) | Rct (Ω) |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| LCO-Ti | 1st | 1.48 | 12.27 | 25.53 | LCO-P | 1st | 2.83 | 80.71 | 347.90 |
|  | 5th | 1.11 | 16.18 | 128.20 |  | 5th | 4.28 | 13.41 | 100.60 |
|  | 10th | 1.59 | 18.98 | 193.10 |  | 10th | 4.82 | 13.68 | 156.80 |
|  | 50th | 1.30 | 15.78 | 701.30 |  | 50th | 2.47 | 19.40 | 539.70 |
|  | 100th | 1.96 | 26.75 | 1048.00 |  | 100th | 1.17 | 18.63 | 952.60 |

The Analysis Details of Galvanostatic Intermittent Titration Technique (GITT)

The GITT experiments were performed with coin-type cells at charge/discharge at 0.1 C for 0.5 h with 2 h relaxation time between each pulse (voltage range of 3.0–4.6 V). The diffusion co-efficient of Li+ can be calculated according to the following formula:

DLi+ = 4πτmBVMMBS2ΔESΔEt2       τ ≪ L2DLi+

Where τ is the time of the constant current pulse; S represents the contact area between the cathode active material and the electrolyte; ΔEt is the voltage change before and after the constant current pulse, and ΔEs is the steady-state voltage change. VM, MB and mB are the molar volume, molar mass and mass of the electrode material, respectively. The value of VM is obtained from the Rietveld refinement results of GSAS. L is the diffusion length.

References

1.	Wang X, Wu Q, Li SY et al (2021) Lithium-Aluminum-Phosphate coating enables stable 4.6 V cycling performance of LiCoO2 at room temperature and beyond. Energy Storage Materials 37:67–76

2.	Hu B, Geng FS, Shen M et al (2021) A multifunctional manipulation to stabilize oxygen redox and phase transition in 4.6 V high-voltage LiCoO2 with sXAS and EPR studies. J Power Sources 516: 230661

3.	Wang Y, Zhang QH, Xue ZC et al (2020) An in situ formed surface coating layer enabling LiCoO2 with stable 4.6 V high‐voltage cycle performances. Adv Energy Mater 10(28):2001413

4.	Cheng T, Ma ZT, Qian RC et al (2021) Achieving stable cycling of LiCoO2 at 4.6 V by multilayer surface modification. Adv Funct Mater 31(2):2001974

5.	Huang YY, Zhu YC, Fu HY et al (2021) Mg-Pillared LiCoO2 : towards stable cycling at 4.6 V. Angew Chem Int Ed Engl 60(9):4682–4688

6.	Pang PP, Wang Z, Deng YM et al (2020) Delayed phase transition and improved cycling/thermal stability by spinel LiNi0.5Mn1.5O4 modification for LiCoO2 cathode at high voltages. ACS Appl Mater Interfaces 12(24):27339–27349

7.	Zhang JN, Li QH, Ouyang CY et al (2019) Trace doping of multiple elements enables stable battery cycling of LiCoO2 at 4.6 V. Nat Energy 4(7):594–603

8.	Wang LL, Ma J, Wang C et al (2019) A novel bifunctional self-stabilized strategy enabling 4.6 V LiCoO2 with excellent long-term cyclability and high-rate capability. Adv Sci 6(12):1900355

9.	Qian JW, Liu L, Yang JX et al (2018) Electrochemical surface passivation of LiCoO2 particles at ultrahigh voltage and its applications in lithium-based batteries. Nat Commun 9(1):4918

10.	Xie J, Zhao J, Liu YY et al (2017) Engineering the surface of LiCoO2 electrodes using atomic layer deposition for stable high-voltage lithium ion batteries. Nano Res 10(11):3754–3764