Supporting Information

Ultrafast Carbonized Wood of Electrode-Scaled Aligned-Porous Structure for High-Performance Lithium Batteries

Shaojie Chen1 · Lu Nie1 · Hongsheng Shi1 · Xiangchen Hu1 · Zeyu Wang1 · Xinshui Zhang1 · Yuyao Zhang1 · Qilin Hu1 · Tianyi Gao1 · Yi Yu1,2 · Wei Liu1,2,3

1School of Physical Science and Technology, ShanghaiTech University, Shanghai 201210, China

2Shanghai Key Laboratory of High-resolution Electron Microscopy, ShanghaiTech University, Shanghai 201210, China

3Key Laboratory of Advanced Energy Materials Chemistry (Ministry of Education), Nankai University, Tianjin 300071, China

Received: 19 April 2023/ Revised: 7 June 2023/ Accepted: 13 July 2023/ Published online:

Corresponding to Wei Liu, E-mail: liuwei1@shanghaitech.edu.cn

Fig. S1 XRD of CW-ZnO

Fig. S2 SEM image of the CW anode after cycling

Fig. S3 Cycling performance of S@CW cathode at 0.1 C

Table S1 Carbon, hydrogen, oxygen and nitrogen contents of carbonized wood samples

| Sample | Carbon/% | Hydrogen/% | Nitrogen/% | Oxygen/% | H/C | O/C |
| --- | --- | --- | --- | --- | --- | --- |
| Pyrolysis | 94.01 | 0.82 | 0.71 | 4.46 | 0.009 | 0.047 |
| MAUCT | 96.15 | 0.88 | 1.21 | 1.76 | 0.009 | 0.018 |