Supporting Information

Pd0–Ov–Ce3+ Interfacial Sites with Charge Redistribution for Enhanced Hydrogenation of Methyl Oleate to Methyl Stearate

Zhaohui Meng1 · Ying Liao2· Ling Liu1· Yaqian Li2·Hao Yan2· Xiang Feng2· Xiaobo Chen2· Yibin Liu2· Chaohe Yang2

1SINOPEC Dalian Research Institute of Petroleum and Petrochemicals Co., Ltd.

2State Key Laboratory of Heavy Oil Processing, China University of Petroleum, Qingdao 266580, China

Correspondence to Hao Yan, Email:haoyan@upc.edu.cn; Yibin Liu, Email:liuyibin@upc.edu.cn

- Catalytic Performance of the Pd/CeO2-x Catalysts

Table S1 Catalytic performance of Cis-C18:1 hydrogenation over Pd/CeO2-x catalysts

| Catalysts | Cis-C18:1 conversion (%) | Selectivity (%) |  |  |  | Pd dispersion (FE)a |
| --- | --- | --- | --- | --- | --- | --- |
|  |  | MS | Trans-C18:1 |  |  |  |
| Pd/CeO2-300 | 89.1 | 86.9 |  | 12.6 | 0.52 |  |  |
| Pd/CeO2-500 | 99.8 | 93.2 |  | 5.4 | 0.56 |  |  |
| Pd/CeO2-700 | 80.6 | 85.4 |  | 14.0 | 0.52 |  |  |
| Pd/CeO2-900 | 74.7 | 81.7 |  | 18.0 | 0.50 |  |  |

Reaction condition: [25 mL Cis-C18:1 in n-hexane solution (0.14 mol/L), 0.03 g Pd/CeO2-x catalyst, 0.3 MPa H2, 1 h, 30 °C]. aThe formula for the Pd dispersion (FE) is calculated as: drel(VS)= 3.32FE1.23, in which drel(VS)= dVSdat, dvs refers to the particle size of the metal measured by TEM, while dat represents the atomic diameter of the metal (Langmuir 1997, 13, 5613–5620)

2. Physical Property of Pd/CeO2-x Catalysts

Fig. S1 a N2 absorption-desorption isotherms and b pore size distribution of Pd/CeO2-x catalysts

Fig. S2 TEM images of a Pd/CeO2-500 and b Pd/CeO2-700

Fig. S3. TEM images of a-1 Pd/CeO2-300, and a-2 Pd/CeO2-900 with particle-size distribution. EDX mapping of b-1 Pd/CeO2-300, b-2 Pd/CeO2-900, b-3 Pd/CeO2-500, and b-2 Pd/CeO2-700

Table S2 Composition, structure and structural data of Pd/CeO2-x samples

| Catalysts | Pd (wt%)a | SBET (m2/g)b | Vp (cm3/g)b | Dp (nm)b | dCeO2 (nm)c |
| --- | --- | --- | --- | --- | --- |
| Pd/CeO2-300 | 0.98 | 33.15 | 0.33 | 28.13 | 23.60 |
| Pd/CeO2-500 | 1.01 | 23.12 | 0.29 | 33.29 | 23.80 |
| Pd/CeO2-700 | 0.97 | 18.17 | 0.27 | 33.33 | 26.50 |
| Pd/CeO2-900 | 1.00 | 5.49 | 0.32 | 67.06 | 89.50 |

aPd loading of catalyst samples, determined by ICP-AES. bSBET and Vp represented the BET surface area, pore volume, respectively, which were measured by N2 adsorption-desorption. cAverage diameter of CeO2 crystal particles, calculated by the Debye-Scherrer equation based on XRD patterns.

3. Chemical States of Catalyst Surface Elements

Table S3 Raman data of the Pd/CeO2-x catalysts

| Catalysts | F2g peaka (℃) | OV defects peaka (℃) | I(584)/I(467)b |
| --- | --- | --- | --- |
| Pd/CeO2-300 | 467 | 586 | 0.14 |
| Pd/CeO2-500 | 468 | 583 | 0.27 |
| Pd/CeO2-700 | 466 | 584 | 0.08 |
| Pd/CeO2-900 | 464 | 580 | 0.07 |

a The temperature of the corresponding peak.

b Determined from relative peak area of Raman results.

Table S4 O 1s data of the Pd/CeO2-x catalysts

| Catalysts | OⅠ |  | OⅡ |  | OⅢ |  |
| --- | --- | --- | --- | --- | --- | --- |
|  | B.E. (eV)a | Content (%)b | B.E. (eV) | Content (%) | B.E. (eV) | Content (%) |
| Pd/CeO2-300 | 529.2 | 67.8 | 531.1 | 23.2 | 532.6 | 9.0 |
| Pd/CeO2-500 | 529.2 | 64.7 | 531.2 | 28.0 | 532.5 | 7.3 |
| Pd/CeO2-700 | 529.2 | 65.7 | 531.1 | 25.4 | 532.7 | 8.9 |
| Pd/CeO2-900 | 529.2 | 50.8 | 531.4 | 22.4 | 533.3 | 26.8 |

a Binding energy for O 1s.

b Determined from relative peak area of fitted XPS results.

Table S5 Ce 3d data of the Pd/CeO2-x catalysts

| Catalysts | Ce3+ |  |  |  | Ce4+ |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- |
|  | B.E. (eV)a |  | Content (%)b |  | B.E. (eV) |  | Content (%) |
| Pd/CeO2-300 | 903.0, 900.0 | 30.9 |  | 916.4, 906.9, 900.8 |  | 69.1 |  |
| Pd/CeO2-500 | 902.8, 900.1 | 33.0 |  | 916.4, 906.9, 900.8 |  | 67.0 |  |
| Pd/CeO2-700 | 902.9, 900.0 | 29.6 |  | 916.2, 906.6, 900.6 |  | 70.4 |  |
| Pd/CeO2-900 | 902.7, 900.0 | 28.6 |  | 916.3, 907.1, 900.6 |  | 71.1 |  |

a Binding energy for Ce 3d3/2.

b Determined from relative peak area of fitted XPS results.

Table S6 Pd 3d data of the Pd/CeO2-x catalysts

| Catalysts | Pd0 |  | Pd2+ |  |  |
| --- | --- | --- | --- | --- | --- |
|  | B.E. (eV)a | Content (%)b | B.E. (eV) |  | Content (%) |
| Pd/CeO2-300 | 335.7 | 41.8 | 337.7 | 58.2 |  |
| Pd/CeO2-500 | 335.4 | 64.0 | 337.3 | 36.0 |  |
| Pd/CeO2-700 | 335.6 | 60.3 | 337.6 | 39.7 |  |
| Pd/CeO2-900 | 335.8 | 56.6 | 337.7 | 43.4 |  |

a Binding energy for Pd 3d5/2.

b Determined from relative peak area of fitted XPS results.

4. Structure-Dependent Kinetics over Pd/CeO2-x Catalysts

Table S7 Catalytic performance of Cis-C18:1 hydrogenation over Pd/CeO2-x catalysts

| Reaction time (h) | Cis-C18:1 conversion (%) | Selectivity (%) |  |  | Carbon balance (%) |
| --- | --- | --- | --- | --- | --- |
|  |  | MS | Trans-C18:1MS |  |  |
| 0.5 | 75.6 | 80.2 |  | 18.9 | 99.1 |
| 1.0 | 99.8 | 93.2 |  | 5.4 | 98.6 |
| 1.5 | 99.6 | 96.3 |  | 2.4 | 98.7 |
| 2.0 | 100.0 | 99.8 |  | 0.0 | 99.8 |

Reaction condition: [25 mL Cis-C18:1 in n-hexane solution (0.14 mol/L), 0.03 g Pd/CeO2-x catalyst, 0.3 MPa H2, 30 °C].

Table S8 Catalytic performance of Cis-C18:1 hydrogenation over Pd/CeO2-x catalysts

| Reaction temperature (°C) | Cis-C18:1 Conversion (%) | Selectivity (%) |  |  |  | Carbon balance (%) |
| --- | --- | --- | --- | --- | --- | --- |
|  |  | Trans-C18:1 |  | MS |  |  |
| 30 | 75.6 | 80.2 | 18.9 |  | 99.1 |  |
| 40 | 86.4 | 85.9 | 13.3 |  | 99.2 |  |
| 50 | 91.3 | 86.2 | 12.6 |  | 98.8 |  |
| 60 | 94.7 | 86.3 | 11.1 |  | 97.4 |  |

Reaction condition: [25 mL Cis-C18:1 in n-hexane solution (0.14 mol/L), 0.03 g Pd/CeO2-x catalyst, 0.3 MPa H2, 0.5h].